Supporting information

Engineered Biohydrogel Orchestrates Soil Hydro-Saline-Porous Microenvironments for Saline-Alkali Land Revitalization

Fig. S1 Fabrication process of KGM–SA/B–Zn double-network hydrogel

Table S1

| Sample | SA solution (0.01 g mL⁻¹) | KGM solution (0.01 g mL⁻¹) | SA:KGM (v/v) |  |  | Borax solution |  | Zn²⁺ treatment |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA20KGM40 | 20 mL | 40 mL |  | 1:2 |  | Borax solution added at 1:30 (v/v,) |  | 0.01 mol·L-1 Zn(CH3COO)2, 30 min |
| SA20KGM60 | 20 mL | 60 mL |  | 1:3 | Same |  | Same |  |
| SA20KGM80 | 20 mL | 80 mL |  | 1:4 | Same |  | Same |  |

C

B

A

Fig. S2 TEM images of (A) KGM-SA (B) KGM-SA-B (C) KGM-SA-B-Zn.

Fig. S3 Load-unload cyclic curves of SA20KGM60 in the cyclic experiment.

Fig. S4 Droplet photos and quantitative contact angle data of SA20KGM60.

Fig. S5 Time-dependent volume ratio and swelling ratio of SA20KGM60 soaked in different salt solutions over 20 hours.

Table S2 Physicochemical properties of saline-alkali soil before and after treatment with SA20KGM60.

| Sample | organic carbon(%) | total salt content(g/kg) | Basicity(%) |
| --- | --- | --- | --- |
| Soil | 0.70 | 12.0 | 54.4 |
| Soil with SA20GKM60 | 0.99 | 8.2 | 34.5 |