1 Materials and Methods

1.1 Materials

All materials were purchased from Sinopharm Group Chemical reagent Co., Ltd. (Shanghai, China). Millipore water was used for all experiments.

1.2 Determination of the carboxyl content in the sample

Following the method of Ruan et al. [1] and making some modifications, the carboxyl content in each SPI sample (1 mg‧mL-1) was determined by the conductivity titration method.

1.3 Determination of samples by frozen scanning electron microscopy

The O/W emulsions of different treated proteins were prepared according to the method in manuscript 2.4.2.3, and the surface morphology of the samples was observed and images were taken using a cryo-scanning electron microscope (Gemini 30, ZEISS, Germany).

References

[1] Ruan C Q, Strømme M, Mihranyan A , et al. Favored surface-limited oxidation of cellulose with Oxone® in water. RSC Advances, 2017, 7(64): 40600–40607.

Table S1 Design and results of response surface experiment.

| Test number | Factors and codes |  |  | Real factors and levels |  |  | DD (%) | DH (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | C | T/℃ | pH | E/S (U/g) |  |  |
| 1 | -1 | -1 | 0 | 50 | 6 | 21.5 | 45.07 ± 2.59 | 1.58 ± 0.57 |
| 2 | 1 | -1 | 0 | 60 | 6 | 21.5 | 45.40 ± 2.13 | 1.00 ± 0.07 |
| 3 | -1 | 1 | 0 | 50 | 8 | 21.5 | 46.38 ± 1.34 | 1.84 ± 0.29 |
| 4 | 1 | 1 | 0 | 60 | 8 | 21.5 | 42.77 ± 1.69 | 1.72 ± 0.18 |
| 5 | -1 | 0 | -1 | 50 | 7 | 13 | 43.31 ± 1.02 | 1.16 ± 0.10 |
| 6 | 1 | 0 | -1 | 60 | 7 | 13 | 42.91 ± 2.04 | 0.94 ± 0.08 |
| 7 | -1 | 0 | 1 | 50 | 7 | 30 | 46.38 ± 1.02 | 1.13 ± 0.14 |
| 8 | 1 | 0 | 1 | 60 | 7 | 30 | 43.42 ± 0.21 | 0.72 ± 0.06 |
| 9 | 0 | -1 | -1 | 55 | 6 | 13 | 45.66 ± 0.90 | 1.08 ± 0.17 |
| 10 | 0 | 1 | -1 | 55 | 8 | 13 | 44.69 ± 2.61 | 1.60 ± 0.15 |
| 11 | 0 | -1 | 1 | 55 | 6 | 30 | 46.26 ± 4.44 | 1.06 ± 0.14 |
| 12 | 0 | 1 | 1 | 55 | 8 | 30 | 46.54 ± 0.98 | 1.39 ± 0.15 |
| 13 | 0 | 0 | 0 | 55 | 7 | 21.5 | 47.11 ± 1.01 | 0.92 ± 0.04 |
| 14 | 0 | 0 | 0 | 55 | 7 | 21.5 | 47.42 ± 4.46 | 0.87 ± 0.04 |
| 15 | 0 | 0 | 0 | 55 | 7 | 21.5 | 46.92 ± 1.08 | 0.93 ± 0.07 |
| 16 | 0 | 0 | 0 | 55 | 7 | 21.5 | 46.88 ± 0.66 | 0.89 ± 0.16 |
| 17 | 0 | 0 | 0 | 55 | 7 | 21.5 | 47.28 ± 1.29 | 0.91 ± 0.03 |

Table S2 Analysis of variance for the degree of deamidation model.

| Sources of error | Sum of squares | Degree of freedom | Mean square | F value | P value |
| --- | --- | --- | --- | --- | --- |
| Model | 40.26 | 9 | 4.47 | 73.98 | < 0.0001*** |
| A-T | 5.51 | 1 | 5.51 | 91.14 | < 0.0001*** |
| B-pH | 0.5050 | 1 | 0.5050 | 8.35 | 0.0233* |
| C-E/S | 4.55 | 1 | 4.55 | 75.16 | < 0.0001*** |
| AB | 3.88 | 1 | 3.88 | 64.18 | < 0.0001*** |
| AC | 1.64 | 1 | 1.64 | 27.09 | 0.0012** |
| BC | 0.3906 | 1 | 0.3906 | 6.46 | 0.0386* |
| A² | 16.84 | 1 | 16.84 | 278.44 | < 0.0001*** |
| B² | 0.1987 | 1 | 0.1987 | 3.29 | 0.1128 |
| C² | 5.26 | 1 | 5.26 | 86.91 | < 0.0001*** |
| Residual | 0.4233 | 7 | 0.0605 |  |  |
| Lack of fit | 0.2100 | 3 | 0.0700 | 1.31 | 0.3864 |
| Pure error | 0.2133 | 4 | 0.0533 |  |  |
| Total | 40.69 | 16 |  |  |  |

Note: In the table, * indicates that the factor has a significant effect on the model (P < 0.05); ** indicates that the factor has a highly significant effect on the model (P < 0.01); *** indicates that the factor has an extremely significant effect on the model (P < 0.001).

Table S3 Analysis of variance for the degree of hydrolysis model.

| Sources of error | Sum of squares | Degree of freedom | Mean square | F value | P value |
| --- | --- | --- | --- | --- | --- |
| Model | 1.81 | 9 | 0.2010 | 276.10 | < 0.0001*** |
| A-T | 0.2211 | 1 | 0.2211 | 303.79 | < 0.0001*** |
| B-pH | 0.4186 | 1 | 0.4186 | 575.13 | < 0.0001*** |
| C-E/S | 0.0288 | 1 | 0.0288 | 39.57 | 0.0004*** |
| AB | 0.0529 | 1 | 0.0529 | 72.68 | < 0.0001*** |
| AC | 0.0090 | 1 | 0.0090 | 12.40 | 0.0097** |
| BC | 0.0090 | 1 | 0.0090 | 12.40 | 0.0097** |
| A² | 0.1188 | 1 | 0.1188 | 163.27 | < 0.0001*** |
| B² | 0.9026 | 1 | 0.9026 | 1240.09 | < 0.0001*** |
| C² | 0.0301 | 1 | 0.0301 | 41.31 | 0.0004*** |
| Residual | 0.0051 | 7 | 0.0007 |  |  |
| Lack of fit | 0.0028 | 3 | 0.0009 | 1.59 | 0.3235 |
| Pure error | 0.0023 | 4 | 0.0006 |  |  |
| Total | 1.81 | 16 |  |  |  |

Note: In the table, * indicates that the factor has a significant effect on the model (P < 0.05); ** indicates that the factor has a highly significant effect on the model (P < 0.01); *** indicates that the factor has an extremely significant effect on the model (P < 0.001).

Fig. S1 Degrees of deamidation and hydrolysis of SPI at different processing times.

Fig. S2 The carboxyl content of different SPI samples.

Fig. S3 Cryo-SEM images of different samples.