Electronic Supplementary Material

Support effect of MoOxCy catalyst in the reverse water gas shift reaction

Qiuying Jia1, Dazhuang Li1, Xiaoqiao Zhang2, Xinlan Na1, Shugang Sun1, Mei-Yan Wang1, Yong Wang ()1, Shengping Wang1,3, Xinbin Ma ()1,4

1 Key Laboratory for Green Chemical Technology of Ministry of Education, School of Chemical Engineering and Technology, Tianjin University, Tianjin 300072, China

2 Research Institute of Petroleum Processing Co., Ltd, SINOPEC, Beijing 100083, China

3 State Key Laboratory of High-efficiency Utilization of Coal and Green Chemical Engineering, School of Chemistry and Chemical Engineering, Ningxia University, Yinchuan 750021, China

4 School of Chemical Engineering, Xinjiang University, Urumqi 830017, China

E-mails: yong.wang@tju.edu.cn (Wang Y); xbma@tju.edu.cn (Ma X)

Figure S1. XRD patterns of spent a) WO3, b) MoO3, c) V2O5, d) Cr2O3, e) ZrO2, f) TiO2, g) Nb2O5 catalysts.

Figure S2. XRD patterns of reduced a) WO3, b) MoO3, c) V2O5, d) Cr2O3, e) ZrO2, f) TiO2, g) Nb2O5 catalysts.

Figure S3. XPS spectra for a) survey spectrum and (b) V 2p spectrum of spent V2O5 catalyst, (c) survey spectrum and (d) Cr 2p spectrum of spent Cr2O3 catalyst, (e) survey spectrum and (f) Zr 3d spectrum of spent ZrO2 catalyst, (g) survey spectrum and (h) Ti 2p spectrum of spent TiO2 catalyst, (i) survey spectrum and (j) Nb 3d spectrum of spent Nb2O5 catalyst.

Figure S4. a) CO2 conversion over 8.4 wt% W/SiO2 and Mo/SiO2 catalysts as a function of TOS, b) Forward rate of CO formation (rf, molCO/molmetal/h) over unsupported MoO3 and WO3, and supported Mo/SiO2 and W/SiO2 catalysts. (Reaction conditions: mcat = 60 mg, H2/CO2/N2=3/1/1, WHSV = 100,000 mL/gcat/h, 550 °C, 1×105 Pa)

Figure S5. Long-term stability test of 8.4 Mo/SiO2. (Reaction conditions: mcat = 60 mg, H2/CO2/N2=3/1/1, WHSV = 100,000 mL/gcat/h, 550 °C, 1×105 Pa)

Figure S6. a) CO2 conversion over Mo/SiO2 catalysts with different Mo loadings as a function of TOS (Reaction conditions: mcat = 60 mg, H2/CO2/N2=3/1/1, WHSV = 100,000 mL/gcat/h, 550 °C, 1×105 Pa), b) XRD patterns of calcined Mo/SiO2 catalysts with different Mo loadings.

Figure S7. CO2 conversion of different supported Mo catalysts as a function of TOS. (Reaction conditions: mcat = 60 mg, H2/CO2/N2=3/1/1, WHSV = 100,000 mL/gcat/h, 550 °C, 1×105 Pa)

Figure S8. TEM and the corresponding EDX elemental mapping images of calcined a) Mo/SiO2, b) Mo/ZrO2, c) Mo/TiO2, d) Mo/γ-Al2O3, e) Mo/CeO2, f) Mo/MgO catalysts.

Figure S9. N2 adsorption-desorption isotherms of different supported Mo catalysts.

Figure S10. Correlation between rf and specific surface area of different catalysts.

Figure S11. XRD patterns of calcined and reduced a) Mo/SiO2, b) Mo/ZrO2, c) Mo/TiO2, d) Mo/γ-Al2O3, e) Mo/CeO2, f) Mo/MgO catalysts and the bare supports. (Mo/support-C represents catalyst calcined in air at 500 °C, Mo/support-H represents catalyst reduced in H2 at 500 °C)

Figure S12. XRD patterns of spent a) Mo/SiO2, b) Mo/ZrO2, c) Mo/TiO2, d) Mo/γ-Al2O3, e) Mo/CeO2, f) Mo/MgO catalysts and the bare supports.

Figure S13. XPS survey spectra and high-resolution spectra of support elements of spent supported Mo catalysts transferred under inert atmosphere protection.

Figure S14. Correlation of RWGS activity with the surface atomic percentages of a) Mo4+, b) Mo5+ and c) Mo6+ derived from Mo 3d XPS spectra transferred under inert atmosphere protection.

Figure S15. XPS survey spectra and high-resolution spectra of support elements of spent supported Mo catalysts.

Figure S16. XPS spectra for a) Mo 3d and b) C 1s of different supported Mo catalysts after reaction shown in Figure S6, c) the correlation between RWGS activity and Mo2C surface content calculated from the Mo 3d XPS spectra.

Figure 17. Correlation of RWGS activity with the surface atomic percentages of a) Mo4+, b) Mo5+ and c) Mo6+ derived from Mo 3d XPS spectra.

Figure S18. Arrhenius plots of various supported Mo catalysts with different loadings.

Figure S19. Reaction order with respect to a) CO2 (Reaction conditions: 550 °C, 0.4×105 Pa H2, 0.05~0.3×105 Pa CO2, N2 used as balance gas in the tests to maintain the total pressure of 1×105 Pa) and b) H2 (Reaction conditions: 550 °C, 0.4×105 Pa CO2, 0.05~0.5×105 Pa H2, N2 used as balance gas in the tests to maintain the total pressure of 1×105 Pa), c) Ea of MoO3 catalysts. (Reaction conditions: H2/CO2/N2=1/3/1, 100 mL/min in total, 470~550 °C, 1×105 Pa)

Figure S20. Raman spectra for the calcined catalysts with different Mo loadings of a) Mo/SiO2, b) Mo/ZrO2, c) Mo/TiO2, d) Mo/γ-Al2O3, e) Mo/CeO2, f) Mo/MgO.

Figure S21. Raman spectra of a) 21 Mo/SiO2, b) 21 Mo/ZrO2, c) 21 Mo/TiO2, d) 21 Mo/γ-Al2O3, e) 21 Mo/CeO2, f) 21 Mo/MgO catalyst after CO-TPSR tests shown in Figure 7.

Figure S22. H2-TPR profiles of calcined Mo/SiO2, Mo/ZrO2, Mo/TiO2, Mo/γ-Al2O3 and MoO3 catalysts.

Figure S23. TG-DSC curves of uncalcined a) Mo/SiO2, b) Mo/ZrO2, c) Mo/TiO2, d) Mo/γ-Al2O3, e) Mo/CeO2, f) Mo/MgO samples.

Figure S24. a) CO2 conversion (Reaction conditions: mcat = 60 mg, H2/CO2/N2=3/1/1, WHSV = 100,000 mL/gcat/h, 550 °C, 1×105 Pa), b) XRD patterns, c) apparent activation energy of 8.4 Mo/SiO2-500 °C and 8.4 Mo/SiO2-300 °C catalysts (Reaction conditions: H2/CO2/N2=1/3/1, 100 mL/min in total, 470~550 °C, 1×105 Pa, 0.04g 8.4 Mo/SiO2-500 °C, 0.02g 8.4 Mo/SiO2-300 °C).

Figure S25. a) CO2 conversion (Reaction conditions: mcat = 60 mg, H2/CO2/N2=3/1/1, WHSV = 100,000 mL/gcat/h, 550 °C, 1×105 Pa), b) XRD patterns, c) apparent activation energy of 8.4 Mo/ZrO2-500 °C and 8.4 Mo/ZrO2-300 °C catalysts (Reaction conditions: H2/CO2/N2=1/3/1, 100 mL/min in total, 470~550 °C, 1×105 Pa, 0.04g 8.4 Mo/ZrO2-500 °C, 0.02g 8.4 Mo/ZrO2-300 °C).

Figure S26. a) CO2 conversion (Reaction conditions: mcat = 60 mg, H2/CO2/N2=3/1/1, WHSV = 100,000 mL/gcat/h, 550 °C, 1×105 Pa), b) XRD patterns, c) apparent activation energy of 8.4 Mo/TiO2-500 °C and 8.4 Mo/TiO2-300 °C catalysts (Reaction conditions: H2/CO2/N2=1/3/1, 100 mL/min in total, 470~550 °C, 1×105 Pa, 0.06g 8.4 Mo/TiO2-500 °C, 0.02g 8.4 Mo/TiO2-300 °C).

Figure S27. a) CO2 conversion (Reaction conditions: mcat = 60 mg, H2/CO2/N2=3/1/1, WHSV = 100,000 mL/gcat/h, 550 °C, 1×105 Pa), b) XRD patterns, c) apparent activation energy of 8.4 Mo/γ-Al2O3-500 °C and 21 Mo/γ-Al2O3-300 °C catalysts (Reaction conditions: H2/CO2/N2=1/3/1, 100 mL/min in total, 470~550 °C, 1×105 Pa, 0.01g 21 Mo/γ-Al2O3-500 °C, 0.01g 21 Mo/γ-Al2O3-300 °C).

Figure S28. a) CO2 conversion (Reaction conditions: mcat = 60 mg, H2/CO2/N2=3/1/1, WHSV = 100,000 mL/gcat/h, 550 °C, 1×105 Pa), b) XRD patterns, c) apparent activation energy of 21 Mo/MgO-500 °C and 21 Mo/MgO-300 °C catalysts (Reaction conditions: H2/CO2/N2=1/3/1, 100 mL/min in total, 470~550 °C, 1×105 Pa, 0.02g 21 Mo/MgO-500 °C, 0.02g 21 Mo/MgO-300 °C).

Table S1. Chemical equations for the carbonization of early transition metal oxides shown in Figure 1b in the main text.

| Equation | ∆Hθ (kJ/mol)a | ∆Gθ (kJ/mol)a |
| --- | --- | --- |
| MoO3+4COg=1/2Mo2C+7/2CO2g | -223.1 | -137.2 |
| WO3+4COg=1/2W2C+7/2CO2g | -108.4 | -27.5 |
| V2O3+5COg=V2C+4CO2g | 69.4 | 238.0 |
| Cr2O3+17/3COg=2/3Cr3C2+13/3CO2g | -5.7 | 185.6 |
| ZrO2+4COg=ZrC+3CO2g | 163.0 | 305.8 |
| TiO2+4COg=TiC+3CO2g | 18.4 | 170.4 |
| Nb2O5+7COg=Nb2C+6CO2g | 111.2 | 275.5 |
| a 550 °C, 1×105 Pa |  |  |

Table S2. Comparison of catalytic performance with reported literatures.

| Catalysts | H2: CO2 | Temperature (°C) | WHSV (mL/gcat/h) | P (MPa) | X(CO2) (%) | S(CO) (%) | CO formation rate (μmolco/gcat/s) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 25.2 Mo/SiO2 | 3:1 | 550 | 100000 | 0.1 | 46.5 | 100 | 107.5 | this work |
| 8.4 Mo/SiO2 | 3:1 | 550 | 100000 | 0.1 | 31.8 | 100 | 78 |  |
| 8.4 Mo/SiO2 | 3:1 | 600 | 100000 | 0.1 | 38.4 | 100 | 126.6 |  |
| MoCx@Al2O3 | 4:1 | 400 | 24000 | 0.1 | 35 | 98.3 | 20.8 | [1] |
| MoCx/SiO2 | 3:1 | 400 | / | 0.1 | 27.5 | 98.5 | 12.8 | [2] |
| MoCx/Al2O3 | 3:1 | 400 | / | 0.1 | 23.5 | 94.5 | 11.3 | [2] |
| MoCx/TiO2 | 3:1 | 400 | / | 0.1 | 8 | 97 | 3.8 | [2] |
| MoOx | 1:1 | 400 | 30000 | 0.1 | 13.7 | 97.8 | 25 | [3] |
| Cu/MoOx | 4:1 | 400 | 60000 | 0.1 | 35.9 | 99 | 24.2 | [4] |
| MoO3/Ti3AlC2 | 4:1 | 560 | 30000 | 0.1 | 18 | 89 | 10.9 | [5] |
| MoO3/TiO2 | 4:1 | 560 | 30000 | 0.1 | 18 | 84 | 10.3 | [5] |
| MoO3/Al2O3 | 4:1 | 560 | 30000 | 0.1 | 18 | 85 | 10.4 | [5] |
| MoOx/Mo2N | 3:1 | 600 | 200000 | 0.1 | 50.8 | 100 | 290 | [6] |
| MoO3 | 3:1 | 600 | 200000 | 0.1 | 5.9 | 100 | 34 | [6] |
| Co/Mo2C | 2:1 | 300 | 36000 | 0.1 | 9.5 | 98.1 | 12.7 | [7] |
| MoO2 | 3:1 | 500 | 10000 | 0.1 | 28 | 100 | 1 | [8] |
| Ru-Mo-Ox | 3:1 | 500 | 10000 | 0.1 | 49 | 99 | 2 | [8] |
| Cu/β-Mo2C | 2:1 | 600 | 300000 | 0.1 | 29 | 100 | 473 | [9] |
| α-Mo2C | 3:1 | 600 | 100000 | 0.1 | 58 | 100 | 131.5 | [10] |
| Ni1Mo/SiO2 | 4:1 | 400 | 100000 | 0.1 | 23.6 | 93.8 | 22.4 | [11] |
| Ir-MoO3 | 3:1 | 600 | 100000 | 0.1 | 51 | 100 | 138.9 | [12] |
| Mo2N | 3:1 | 550 | 24000 | 0.1 | 55.9 | 99.9 | 19.9 | [13] |
| 0.5Pt-MoO3/Mo2N | 3:1 | 300 | 300000 | 0.1 | ~20 | 100 | 172 | [14] |

| Catalysts | CO2 Conversion (%) | CO selectivity (%) | SBET (m2/g) |
| --- | --- | --- | --- |
| Mo/SiO2 | 31.3 | 100 | 46.5 |
| Mo/ZrO2 | 27.6 | 100 | 7.5 |
| Mo/TiO2 | 22.0 | 100 | 47.9 |
| Mo/γ-Al2O3 | 17.4 | 100 | 135.5 |
| Mo/CeO2 | 9.4 | 100 | 20 |
| Mo/MgO | 7.9 | 100 | 9.6 |
| SiO2 | 0.5 | 100 | 64.8 |
| ZrO2 | 3.3 | 100 | 7.1 |
| TiO2 | 2.2 | 100 | 53.4 |
| γ-Al2O3 | 2.2 | 100 | 148.6 |
| CeO2 | 6.5 | 100 | 39.8 |
| MgO | 0.8 | 100 | 7.0 |

Table S3. CO2 conversion, CO selectivity and BET surface area (SBET) of the different supported Mo catalysts and bare supports.

Table S4. The binding energy position of Mo species with different valence states on the catalyst surface corresponding to Figure 4a.

| Catalysts | Binding Energy (eV) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Mo6+ | Mo5+ | Mo4+ | Mo2+ |
| Mo/SiO2-spent | 232.9 | 231.1 | 229.5 | 228.5 |
| Mo/ZrO2-spent | 232.8 | 231.2 | 229.6 | 228.6 |
| Mo/TiO2-spent | 232.8 | 231.2 | 229.4 | 228.4 |
| Mo/γ-Al2O3-spent | 232.6 | 231.2 | 229.6 | 228.5 |
| Mo/CeO2-spent | 232.8 | 231.3 | 229.6 | 228.6 |
| Mo/MgO-spent | 232.8 | 231.3 | 229.6 | 228.6 |

Table S5. The content of Mo species with different valence states on the catalyst surface shown in Figure 4a.

| Catalysts | atomic percentage on the surface (%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Mo6+ | Mo5+ | Mo4+ | Mo2+ |
| Mo/SiO2-spent | 20.3 | 21.3 | 26.4 | 32.0 |
| Mo/ZrO2-spent | 33.0 | 7.5 | 29.0 | 30.5 |
| Mo/TiO2-spent | 20.7 | 8.8 | 45.8 | 24.7 |
| Mo/γ-Al2O3-spent | 44.4 | 15.5 | 26.4 | 13.7 |
| Mo/CeO2-spent | 41.3 | 36.7 | 14.5 | 7.5 |
| Mo/MgO-spent | 37.0 | 34.1 | 22.8 | 6.1 |

| Catalysts | CO2 Conversion (%) | Onset Temperature (°C) | Integral area |
| --- | --- | --- | --- |
| 21 Mo/SiO2 | 41.5 | 226 | 2.924e-9 |
| 21 Mo/ZrO2 | 41.4 | 240 | 2.066e-9 |
| 21 Mo/TiO2 | 36.2 | 260 | 2.591e-9 |
| 21 Mo/γ-Al2O3 | 36.5 | 248 | 4.5653e-9 |
| 21 Mo/CeO2 | 5.2 | 305 | 1.451e-9 |
| 21 Mo/MgO | 19.3 | 314 | 1.113e-9 |
| 21 Mo/CeO2-300 °C | 29 | 273 | 1.738e-9 |

Table S6. Onset temperature and integral area of CO-TPSR profiles for the 21 wt% Mo catalysts on different supports.

Reference

[1] Cao S, Ma Y, Chu W, Zhang B, Peng B, Liu Y. Self-Assembling of a Mo–Al Composite toward Efficient Catalysts for RWGS Reaction: Overcoming the Trade-off between Ultrasmall Size and High Loading [J]. ACS Catalysis, 2025, 15(17): 15559-15569.

[2] Pajares A, Liu X, Busacker J R, Ramírez de la Piscina P, Homs N. Supported Nanostructured MoxC Materials for the Catalytic Reduction of CO2 through the Reverse Water Gas Shift Reaction [J]. Nanomaterials, 2022, 12(18): 3165.

[3] Jin F, Yang X, Yang J, Lei Y, Xu W, Jiang W, Ma Z, Liang G, Ben H, Li X. Unraveling the influence of oxygen vacancies in MoOx catalysts on CO2 hydrogenation [J]. Chemical Engineering Journal, 2024, 495: 153333.

[4] Gao Y, Xiong K, Zhu B. Design of Cu/MoOx for CO2 Reduction via Reverse Water Gas Shift Reaction [J]. Catalysts, 2023, 13(4): 684.

[5] Ronda-Lloret M, Yang L, Hammerton M, S. V, Tromp M, Sofer Z, Sepúlveda-Escribano A, V. E, Jose J, Rothenberg G. Molybdenum Oxide Supported on Ti3AlC2 is an Active Reverse Water–Gas Shift Catalyst [J]. ACS Sustainable Chemistry & Engineering, 2021, 9: 4957-4966.

[6] Liu H X, Wang W W, Fu X P, Liu J C, Jia C J. Direct cleavage of C=O double bond in CO2 by the subnano MoOx surface on Mo2N [J]. Nature Communications, 2024, 15(1): 9126.

[7] Porosoff M D, Yang X, Boscoboinik J A, Chen J G. Molybdenum Carbide as Alternative Catalysts to Precious Metals for Highly Selective Reduction of CO2 to CO [J]. Angewandte Chemie International Edition, 2014, 53(26): 6705-6709.

[8] Xin H, Lin L, Li R, Li D, Song T, Mu R, Fu Q, Bao X. Overturning CO2 Hydrogenation Selectivity with High Activity via Reaction-Induced Strong Metal–Support Interactions [J]. Journal of the American Chemical Society, 2022, 144(11): 4874-4882.

[9] Zhang X, Zhu X, Lin L, Yao S, Zhang M, Liu X, Wang X, Li Y-W, Shi C, Ma D. Highly Dispersed Copper over β-Mo2C as an Efficient and Stable Catalyst for the Reverse Water Gas Shift (RWGS) Reaction [J]. ACS Catalysis, 2017, 7(1): 912-918.

[10] Ahmadi Khoshooei M, Wang X, Vitale G, Formalik F, Kirlikovali K O, Snurr R Q, Pereira-Almao P, Farha O K. An active, stable cubic molybdenum carbide catalyst for the high-temperature reverse water-gas shift reaction [J]. Science, 2024, 384(6695): 540-546.

[11] Zhang R, Wei A, Zhu M, Wu X, Wang H, Zhu X, Ge Q. Tuning reverse water gas shift and methanation reactions during CO2 reduction on Ni catalysts via surface modification by MoOx [J]. Journal of CO2 Utilization, 2021, 52: 101678.

[12] Sun X, Yu J, Zada H, Han Y, Zhang L, Chen H, Yin W, Sun J. Reaction-induced unsaturated Mo oxycarbides afford highly active CO2 conversion catalysts [J]. Nature Chemistry, 2024, 16: 2044-2053.

[13] Tian J, Fang L, Ouyang N, Xia L, Wang Z, Cai H, Feng Q, Jiang X, Zhao J, Tan M, Zhang L, Wang Y, Li X, Zhu Y. Breaking activity-selectivity-stability trade-offs in reverse water-gas shift reaction via high-energy micro-faceted Mo2N nanocrystals [J]. Nature Communications, 2026, 17(1): 2240.

[14] Liu H X, Li J Y, Qin X, Ma C, Wang W W, Xu K, Yan H, Xiao D, Jia C J, Fu Q, Ma D. Ptn–Ov synergistic sites on MoOx/γ-Mo2N heterostructure for low-temperature reverse water–gas shift reaction [J]. Nature Communications, 2022, 13(1): 5800.