Supplementary material

Oxygen vacancy enhanced oxidative dehydrogenation of propane with carbon dioxide over PtSn/Ce1-xLaxO2-δ

Guo-Qing Yang, Huan-Yu Du, Han-Qing Ge, Zhong-Wen Liu*

Key Laboratory of Syngas Conversion of Shaanxi Province, School of Chemistry & Chemical Engineering, Shaanxi Normal University, Xi’an 710119, China

*Corresponding author: zwliu@snnu.edu.cn

Table of Contents

Figure S1. Carbon balance of CO2-ODP for PtSn/Ce1-xLaxO2-δ under the conditions of T = 500 °C, Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 20 mL∙min-1, and catalyst mass = 0.5 g.	4

Figure S2. N2 adsorption-desorption isotherms (a) and pore size distributions (b) of PtSn/Ce1-xLaxO2-δ.	5

Figure S3. Images of EDS elemental mapping for PtSn/Ce0.9La0.1O2-δ.	6

Figure S4. Relationship between I580/I460 and La content in Ce1-xLaxO2-δ.	7

Figure S5. CeO2 (111) reflection of CeO2 and PtSn/Ce1-xLaxO2-δ.	8

Figure S6. O 1s XPS of PtSn/Ce1-xLaxO2-δ.	9

Figure S7. Sn 3d5/2 XPS of PtSn/Ce1-xLaxO2-δ.	10

Figure S8. Time-on-stream C3H8 conversion over Ce0.9La0.1O2-δ for CO2-ODP under the conditions of T = 500 °C, Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 20 mL∙min-1, and catalyst mass = 0.5 g.	11

Figure S9. Time-on-stream C3H8 conversion, C3H6 selectivity (a) and CO2 conversion (b) over PtSn/CeO2 and PtSn/Ce0.9La0.1O2-δ for CO2-ODP under the conditions of T = 500 °C, Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 20 mL∙min-1, and catalyst mass = 0.5 g.	12

Figure S10. Time-on-stream C3H8 conversion (a), CO2 conversion (b), C3H6 selectivity (c), and C3H6 yield (d) of PtSn/Ce0.9La0.1O2-δ for CO2-ODP at different temperatures under the conditions of Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 20 mL∙min-1, and catalyst mass = 0.5 g.	13

Figure S11. Correlations of Pt dispersion (a) and Pt0/(Pt0 + Pt2+) (b) with the C3H6 selectivity over PtSn/Ce1-xLaxO2-δ for CO2-ODP.	14

Figure S12. In situ Raman spectra of PtSn/CeO2 under 10 vol% H2/Ar from 25 to 500 °C in the range of 300 to 600 cm-1.	15

Figure S13. Raman shift of the Pt–O vibration in Pt–O–Ce bonds versus CO selectivity for PtSn/Ce1-xLaxO2-δ.	16

Figure S14. Regeneration performance of PtSn/CeO2 for CO2-ODP under the reaction conditions of T = 500 °C, Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 25 mL∙min-1, and catalyst mass = 0.25 g, and the regeneration conditions of T = 500 °C, air flow = 25 mL∙min-1, t = 1 h.	17

Figure S15. O2-TPO profiles of PtSn/CeO2 and PtSn/Ce0.9La0.1O2-δ after 21.83 h of reaction, with simultaneous monitoring of MS signals for O2, CO, and CO2 (reaction conditions are given in Figure 4a).	18

Figure S16. Comparison of propene yield as a function of reaction time between PtSn/Ce0.9La0.1O2-δ and PtSn/Ce0.7La0.3O2-δ under the conditions of T = 500 °C, Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 20 mL∙min-1, and catalyst mass = 0.5 g.	19

Table S1 Summarizing the composition of PtSn/CeO2 and PtSn/Ce0.9La0.1O2-δ derived from EDS elemental mapping results.	20

Table S2 Reaction conditions of CO2-ODP reported in this work and references over Pt-based catalysts.	21

Table S3 Catalytic performance of CO2-ODP reported in this work and references over Pt-based catalysts.	22

Table S4 Comparison of catalytic stability and activity for CO2-ODP reported in this work and references over Pt-based catalysts.	23

Figure S1. Carbon balance of CO2-ODP for PtSn/Ce1-xLaxO2-δ under the conditions of T = 500 °C, Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 20 mL∙min-1, and catalyst mass = 0.5 g.

Figure S2. N2 adsorption-desorption isotherms (a) and pore size distributions (b) of PtSn/Ce1-xLaxO2-δ.

Figure S3. Images of EDS elemental mapping for PtSn/Ce0.9La0.1O2-δ.

Figure S4. Relationship between I580/I460 and La content in Ce1-xLaxO2-δ.

Figure S5. CeO2 (111) reflection of CeO2 and PtSn/Ce1-xLaxO2-δ.

Figure S6. O 1s XPS of PtSn/Ce1-xLaxO2-δ.

Figure S7. Sn 3d5/2 XPS of PtSn/Ce1-xLaxO2-δ.

Figure S8. Time-on-stream C3H8 conversion over Ce0.9La0.1O2-δ for CO2-ODP under the conditions of T = 500 °C, Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 20 mL∙min-1, and catalyst mass = 0.5 g.

Figure S9. Time-on-stream C3H8 conversion, C3H6 selectivity (a) and CO2 conversion (b) over PtSn/CeO2 and PtSn/Ce0.9La0.1O2-δ for CO2-ODP under the conditions of T = 500 °C, Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 20 mL∙min-1, and catalyst mass = 0.5 g.

Figure S10. Time-on-stream C3H8 conversion (a), CO2 conversion (b), C3H6 selectivity (c), and C3H6 yield (d) of PtSn/Ce0.9La0.1O2-δ for CO2-ODP at different temperatures under the conditions of Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 20 mL∙min-1, and catalyst mass = 0.5 g.

Figure S11. Correlations of Pt dispersion (a) and Pt0/(Pt0 + Pt2+) (b) with the C3H6 selectivity over PtSn/Ce1-xLaxO2-δ for CO2-ODP.

Figure S12. In situ Raman spectra of PtSn/CeO2 under 10 vol% H2/Ar from 25 to 500 °C in the range of 300 to 600 cm-1.

Figure S13. Raman shift of the Pt–O vibration in Pt–O–Ce bonds versus CO selectivity over PtSn/Ce1-xLaxO2-δ for CO2-ODP.

Figure S14. Regeneration performance of PtSn/CeO2 for CO2-ODP under the reaction conditions of T = 500 °C, Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 25 mL∙min-1, and catalyst mass = 0.25 g, and the regeneration conditions of T = 500 °C, air flow = 25 mL∙min-1, t = 1 h.

Figure S15. O2-TPO profiles of PtSn/CeO2 and PtSn/Ce0.9La0.1O2-δ after 21.83 h of reaction, with simultaneous monitoring of MS signals for O2, CO, and CO2 (reaction conditions are given in 4a).

Figure S16. Comparison of propene yield as a function of reaction time between PtSn/Ce0.9La0.1O2-δ and PtSn/Ce0.7La0.3O2-δ under the conditions of T = 500 °C, Ar/C3H8/CO2 molar ratio = 1/2/2, total flow rate = 20 mL∙min-1, and catalyst mass = 0.5 g.

Table S1 Summarizing the composition of PtSn/CeO2 and PtSn/Ce0.9La0.1O2-δ derived from EDS elemental mapping results.

| Sample | Ce (at%) | La (at%) | Pt (at%) | Sn (at%) | La/(Ce+La) molar ratio | Pt/Sn molar ratio | Pt (wt%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PtSn/CeO2 | 22.08 | -- | 0.23 | 0.22 | -- | 1.05 | 1.2 |
| PtSn/Ce0.9La0.1O2-δ | 20.82 | 2.34 | 0.20 | 0.22 | 0.10 | 0.91 | 1.1 |

Table S2 Reaction conditions of CO2-ODP reported in this work and references over Pt-based catalysts.

| No. | Catalyst* | Pt content (wt%) | Catalyst mass (g) | Temp. (ºC) | GHSV(C3H8) (mL∙g-1cat∙h-1) | Feed composition (molar ratio) | C3H8 flow rate (mL∙min-1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | PtSn/Ce0.9La0.1O2-δ | 1 | 0.5 | 500 | 960 | C3H8:CO2:Ar = 8:8:4 | 8 | This work |
| 2 | 1Pt5Sn/Ce0.5Zr0.5O2 | 1 | 0.5 | 500 | 960 | C3H8:CO2:N2 = 4:20:1 | 8 | [1] |
| 3 | 1Pt5Sn/CeO2 | 1 | 0.5 | 500 | 960 | C3H8:CO2:N2 = 4:20:1 | 8 | [2] |
| 4 | PtMn/SiO2 | 0.5 | 0.3 | 550 | 2000 | C3H8:CO2:N2 = 10:10:5 | 10 | [3] |
| 5 | PtSnMg0.5/Ce-DMSN | 0.5 | 0.1 | 550 | 4800 | C3H8:CO2:He:Ar = 8:8:8:1 | 8 | [4] |
| 6 | PtSn/SH-CeO2 | 1 | 0.25 | 550 | 960 | C3H8:CO2:He:Ar = 4:4:16:1 | 4 | [5] |
| 7 | PtSnCe/SiO2 | 0.5 | 0.25 | 550 | 1920 | C3H8:CO2:He:Ar = 4:4:16:1 | 8 | [6] |
| 8 | RhPt@Zn-MFI | 0.5 | 0.5 | 600 | 720 | C3H8:CO2:He:N2 = 6:6:16.5:1.5 | 6 | [7] |
| 9 | PtCoIn/CeO2 | 3 | 0.1 | 600 | 3000 | C3H8:CO2:He = 1:1:2 | 5 | [8] |
| 10 | PtCoNiSnInGa/CeO2 | 1 | 0.1 | 600 | 3000 | C3H8:CO2:He = 1:1:2 | 5 | [9] |
| 11 | PtSn1.5/SiO2 | 2 | 0.2 | 550 | 1500 | C3H8:CO2 = 1:1 | 5 | [10] |
| 12 | PtZn/silicalite-1 | 1 | 0.5 | 600 | 1200 | C3H8:CO2 = 1:1 | 10 | [11] |
| 13 | PtSn/Mg-SBA-15 | 0.3 | 0.2 | 550 | 750 | C3H8:CO2:N2 = 1:2:5 | 2.5 | [12] |
| 14 | PtCo-Sibeta | 1 | 0.1 | 550 | 2400 | C3H8:CO2:N2 = 1:1:3 | 4 | [13] |
| 15 | PtFe/S-1 | 0.5 | 0.15 | 550 | 2000 | C3H8:CO2:N2 = 1:1:6 | 5 | [14] |
| 16 | PtZn/Co@S-1 | 0.2 | 0.1 | 550 | 3300 | C3H8:CO2:He = 1:1:4 | 5.5 | [15] |
| 17 | Pt/Sn-CeO2 | 0.1 | 1 | 550 | 144 | C3H8:CO2:N2 =2.4:4.8:10 | 2.4 | [16] |
| 18 | Si/PtSn/Al2O3 | 3 | 0.2 | 550 | 1500 | C3H8:CO2:He = 1:1:2 | 5 | [17] |
| 19 | PtSn/CeOx-Al2O3 | 0.15 | 0.15 | 500 | 2000 | C3H8:CO2:N2 =5:3:27 | 5 | [18] |
| 20 | PtGa/CeO2 | 1 | 0.3 | 600 | 1600 | C3H8:CO2:Ar = 1:1:3 | 8 | [19] |

*: The catalysts included here are only the best performing ones from the references considered.

Table S3 Catalytic performance of CO2-ODP reported in this work and references over Pt-based catalysts.

| No. | Catalyst* | Initial TOS (h) | Final TOS (h) | Initial C3H8 conv. (%) | Final C3H8 conv. (%) | Initial C3H6 selec. (%) | Final C3H6 selec. (%) | Initial C3H6 yield (%) | Final C3H6 yield (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | PtSn/Ce0.9La0.1O2-δ | 0.17 | 21.83 | 33 | 22 | 70 | 90 | 23.1 | 19.8 |
| 2 | 1Pt5Sn/Ce0.5Zr0.5O2 | 0.08 | 1.33 | 35 | 24 | 86 | 88 | 30.1 | 21.1 |
| 3 | 1Pt5Sn/CeO2 | 0.08 | 1.33 | 20 | 14 | 80 | 86 | 16.0 | 12.0 |
| 4 | PtMn/SiO2 | 0.08 | 1.83 | 32 | 27 | 97 | 98 | 31.0 | 26.5 |
| 5 | PtSnMg0.5/Ce-DMSN | 0.08 | 50.00 | 48.2 | 22.4 | 92 | 93 | 44.5 | 20.9 |
| 6 | PtSn/SH-CeO2 | 0.08 | 3.33 | 51 | -- | 77 | -- | 39.3 | 19.3 |
| 7 | PtSnCe/SiO2 | 0.08 | 2.08 | 53 | 39 | 89 | 93 | 47.2 | 36.3 |
| 8 | RhPt@Zn-MFI | 0.08 | 10.42 | 48 | 23 | 61 | 80 | 29.3 | 18.4 |
| 9 | PtCoIn/CeO2 | 0.08 | 50.00 | 61 | 35 | 82 | 94 | 50.0 | 32.9 |
| 10 | PtCoNiSnInGa/CeO2 | 8.00 | 50.00 | 30 | 20 | 94 | 90 | 28.2 | 18.0 |
| 11 | PtSn1.5/SiO2 | 0.04 | 20.00 | 50 | 38 | 90 | 97 | 45.0 | 37.0 |
| 12 | PtZn/silicalite-1 | 0.25 | 3.00 | 47 | 30 | 80 | 80 | 37.6 | 24.0 |
| 13 | PtSn/Mg-SBA-15 | 0.17 | 3.00 | 43 | 34 | 89 | 92 | 38.3 | 31.3 |
| 14 | PtCo-Sibeta | 1.00 | 5.00 | 51.8 | 36 | 92 | 90 | 47.7 | 32.4 |
| 15 | PtFe/S-1 | 0.25 | 3.33 | 25 | 20 | 93 | 96 | 23.3 | 19.2 |
| 16 | PtZn/Co@S-1 | 0.00 | 60.00 | 60 | 40 | 80 | 95 | 48.0 | 38.0 |
| 17 | Pt/Sn-CeO2 | 0.33 | 4.67 | 28 | 15 | 41 | 64 | 11.5 | 9.6 |
| 18 | Si/PtSn/Al2O3 | 0.25 | 7.75 | 48 | 37 | 88 | 88 | 42.2 | 32.6 |
| 19 | PtSn/CeOx-Al2O3 | 0.25 | 3.00 | 32 | 25 | 98 | 98 | 31.4 | 24.5 |
| 20 | PtGa/CeO2 | 0.33 | 1.33 | 38 | 25 | 58 | 64 | 22.0 | 16.0 |

*: The reaction conditions and cited references are given in Table S2.

Table S4 Comparison of catalytic stability and activity for CO2-ODP reported in this work and references over Pt-based catalysts.

| No. | Catalyst* | kd (h-1) | τ** (h) | Y(C3H6_eq)_PDH*** (%) | Y(C3H6_exp)/Y(C3H6_eq)_PDH**** (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | PtSn/Ce0.9La0.1O2-δ | 0.009 | 110.4 | 26 | 90.4 |
| 2 | 1Pt5Sn/Ce0.5Zr0.5O2 | 0.380 | 2.6 | 37 | 82.4 |
| 3 | 1Pt5Sn/CeO2 | 0.264 | 3.8 | 37 | 43.8 |
| 4 | PtMn/SiO2 | 0.128 | 7.8 | 43 | 72.9 |
| 5 | PtSnMg0.5/Ce-DMSN | 0.022 | 44.9 | 46 | 97.1 |
| 6 | PtSn/SH-CeO2 | 0.306 | 3.3 | 57 | 69.4 |
| 7 | PtSnCe/SiO2 | 0.225 | 4.4 | 57 | 83.4 |
| 8 | RhPt@Zn-MFI | 0.059 | 17.0 | 72 | 40.8 |
| 9 | PtCoIn/CeO2 | 0.014 | 70.0 | 69 | 72.9 |
| 10 | PtCoNiSnInGa/CeO2 | 0.014 | 72.2 | 69 | 41.1 |
| 11 | PtSn1.5/SiO2 | 0.017 | 60.2 | 40 | 113.8 |
| 12 | PtZn/silicalite-1 | 0.235 | 4.3 | 59 | 64.2 |
| 13 | PtSn/Mg-SBA-15 | 0.109 | 9.2 | 61 | 63.2 |
| 14 | PtCo-Sibeta | 0.160 | 6.2 | 53 | 89.9 |
| 15 | PtFe/S-1 | 0.079 | 12.7 | 61 | 38.4 |
| 16 | PtZn/Co@S-1 | 0.007 | 146.5 | 56 | 85.8 |
| 17 | Pt/Sn-CeO2 | 0.046 | 21.7 | 59 | 19.5 |
| 18 | Si/PtSn/Al2O3 | 0.055 | 18.1 | 50 | 85.3 |
| 19 | PtSn/CeOx-Al2O3 | 0.124 | 8.0 | 38 | 82.2 |
| 20 | PtGa/CeO2 | 0.393 | 2.5 | 72 | 30.6 |

*: The reaction conditions and cited references are given in Table S2.

**: The inverse of the kd calculated from the propene yield and reaction time

***: Equilibrium propene yield of PDH calculated according to the reaction conditions given in Table S2.

****: The ratio of the initial propene yield of CO2-ODP (Table S3) to the equilibrium propene yield in PDH.

Reference

(1) Ren, X, Yang, G-Q, Liu, Z-W. Oxidative dehydrogenation of propane to propene with carbon dioxide catalyzed by PtSn/Ce1-xZrxO2. SCIENTIA SINICA Chimica, 2024, 54(10): 1943-1954.

(2) Yang, G-Q, Ren, X, Kondratenko, V A, Zhang, H-B, Kondratenko, E V, Liu, Z-W. Promotional nature of Sn on Pt/CeO2 for the oxidative dehydrogenation of propane with carbon dioxide. Nano Research, 2023, 16: 6237-6250.

(3) Zhang, H-B, Yang, G-Q, Li, J, Liu, Z-W. Comparative study on transition metal promoted Pt/SiO2 for oxidative dehydrogenation of propane with carbon dioxide. Journal of CO2 Utilization, 2025, 97: 103116.

(4) Peng, C, Li, J, Ge, H-Q, Yan, M, Liu, Z-W. MgO-modified PtSn/Ce-DMSN as an efficient catalyst for oxidative dehydrogenation of propane with carbon dioxide. Chemical Engineering Journal, 2026, 542: 178176.

(5) Peng, C, Yang, G, Ge, H, Liu, Z. Morphology engineered PtSn/CeO2 catalysts for oxidative dehydrogenation of propane with carbon dioxide. Journal of Rare Earths, 2025, 10.1021/acscatal.6c00338.

(6) Wang, L, Yang, G-Q, Ren, X, Liu, Z-W. CeO2-promoted PtSn/SiO2 as a high-performance catalyst for the oxidative dehydrogenation of propane with carbon dioxide. Nanomaterials, 2022, 12(3): 417.

(7) Yuan, E-H, Niu, Y, Huang, X, Li, M, Bao, J, Song, Y-H, Zhang, B, Liu, Z-T, Willinger, M-G, Liu, Z-W. Finned Zn-MFI zeolite encapsulated noble metal nanoparticle catalysts for the oxidative dehydrogenation of propane with carbon dioxide. Journal of Energy Chemistry, 2023, 80: 479-491.

(8) Xing, F, Nakaya, Y, Yasumura, S, Shimizu, K-i, Furukawa, S. Ternary platinum–cobalt–indium nanoalloy on ceria as a highly efficient catalyst for the oxidative dehydrogenation of propane using CO2. Nature Catalysis, 2022, 5(1): 55-65.

(9) Xing, F, Ma, J, Shimizu, K-i, Furukawa, S. High-entropy intermetallics on ceria as efficient catalysts for the oxidative dehydrogenation of propane using CO2. Nature Communications, 2022, 13(1): 5065.

(10) Zhai, P, Xie, Z, Huang, E, Aireddy, D R, Yu, H, Cullen, D A, Liu, P, Chen, J G, Ding, K. CO2-mediated oxidative dehydrogenation of propane enabled by Pt-based bimetallic catalysts. Chem, 2023, 9(11): 3268-3285.

(11) Rodaum, C, Chaipornchalerm, P, Nunthakitgoson, W, Thivasasith, A, Maihom, T, Atithep, T, Kidkhunthod, P, Uthayopas, C, Nutanong, S, Thongratkaew, S, Faungnawakij, K, Wattanakit, C. Highly efficient propane dehydrogenation promoted by reverse water–gas shift reaction on Pt-Zn alloy surfaces. Fuel, 2022, 325: 124833.

(12) Castillón-Barraza, F F, Sólis-Garcia, A, Gómez, S A, Valente, J S, Lara-Moreno, L, Galindo-Ortega, Y I, Zepeda, T A. Propane CO2-oxidative dehydrogenation catalyzed by Pt-Sn supported on magnesium-chemically grafted SBA-15. Molecular Catalysis, 2024, 565: 114384.

(13) Wang, H, Zhang, X, Su, Z, Chen, T. Dealuminated Beta stabilized bimetallic PtCo nanoparticles for oxidative dehydrogenation of propane with CO2. Fuel, 2024, 358: 130248.

(14) Bian, K, Zhang, G, Zhu, J, Wang, X, Wang, M, Lou, F, Liu, Y, Song, C, Guo, X. Promoting propane dehydrogenation with CO2 over the PtFe bimetallic catalyst by eliminating the non-selective Fe(0) phase. ACS Catalysis, 2022, 12(11): 6559-6569.

(15) Li, W, Wang, T, Cao, X, Li, Y, Miao, G, Sun, N, Li, J, Han, W, Wei, W, Chen, X. Bifunctional catalysts with separated and tunable sites on zeolites for relay catalysis of the oxidative dehydrogenation of propane using CO2. Advanced Functional Materials, 2025, 35(4): 2414231.

(16) Wang, Y, Wang, J, Zhang, Y, Guo, Q, An, J, Liang, Y, Wang, Y, Cao, P, Heggen, M, Dunin-Borkowski, R E, Zhu, X, Li, X, Wang, F. Revealing the catalytic role of Sn dopant in CO2-oxidative dehydrogenation of propane over Pt/Sn-CeO2 catalyst. ChemCatChem, 2022, 14(23): e202200982.

(17) Kim, J, Kim, D H. Enhanced stability of silica-coated PtSn/Al2O3 catalyst for oxidative dehydrogenation of propane with CO2. Fuel, 2025, 384: 134003.

(18) Tian, K, Chen, S, Sun, G, Sun, J, Wang, X, Cai, J, Wang, Z, Fu, D, Zhao, Z-J, Pei, C, Gong, J. Unraveling the hydrogen spillover in tandem propane dehydrogenation and reverse water gas shift reaction. Nature Communications, 2025, 16(1): 10186.

(19) Wang, J, Wang, F, Li, L, Zhao, W, Wang, S, Ma, Z, Kong, Y, Shuang, Y, Xia, W, Jian, J, Guo, P, Wang, H. Synergistic effect of scattered rare metals on Pt/CeO2 for propane oxidative dehydrogenation with CO2. RSC Advances, 2025, 15(4): 2319-2328.