Electronic Supplementary Material

# High CO2 conversion via plasma assisted reverse water-gas shift reaction over Ag/ZnO catalyst

Chunhong Pan1,2, Biao Wang (*)1,2, Jinman Mao1,2, Mengjia Li1,2, Huimin Wang1,2, Wenyi Chen1,2, Feng Gao3, Guoping Hu (*)1,2, Xiaolei Fan (*)4,5,6, Feng Huang1,2

1 School of Rare Earths, University of Science and Technology of China, Hefei 230026, China

2 Key Laboratory of Rare Earths, Ganjiang Innovation Academy, Chinese Academy of Sciences, Ganzhou 341000, China

3 School of Materials, Sun Yat-sen University, Shenzhen 518107, China

4 Department of Chemical Engineering, School of Engineering, The University of Manchester, Manchester M139PL, UK

5 Ningbo China Beacons of Excellence Research and Innovation Institute, University of Nottingham Ningbo China, Ningbo 315048, China

6 Institute of Wenzhou, Zhejiang University, Wenzhou 325006, China

E-mails: biaowang@gia.cas.cn (Wang B); gphu@gia.cas.cn (Hu G); xiaolei.fan@manchester.ac.uk (Fang X)

# 1. Supplementary figures

Fig. S1  Schematic of the DBD plasma collaborating with catalysts reaction.

Fig. S2  Q-U Lissajous figures of the discharges. The peak to-peak applied voltage was 28 kV for Plasma Only, Plasma + ZnO and Plasma + Ag/ZnO, respectively (H2/CO2 = 3:1, total flow rate = 20 mL · min−1, discharge power = 25.31±0.2 W).

Fig. S3  SEM images of (a) fresh, (b) reduced and (c) used Ag/ZnO.

Fig. S4  (a) N2 adsorption isotherms of and the calcined, reduced, and used Ag/ZnO catalyst; (b) corresponding pore size distributions.

Fig. S5  Schematic of plasma assisted RWGS reaction over the Ag/ZnO catalyst.

Fig. S6  XRD patterns of (a) Ag/ZnO catalysts supported by different Ag contents and (b) Reduced and Spent Ag/ZnO catalyst.

Fig. S7  (a) CO2 conversion of the Ag/ZnO catalysts with different Ag loading amounts under NTP conditions; (b) Catalytic performance of Ag-based catalysts supported on different materials;  Catalytic performance at different flow rates(c) and (d) different applied voltages.

Fig. S8  The stability tests of different plasma-assisted RWGS systems (H2/CO2 = 3:1, total flow = 20 mL·min−1, applied peak voltage of 28 kV ± 0.2 kV, frequency of 7.5 kHz, discharge power of 25.31 ± 0.2 W).

Fig. S9  Ag 3d XPS spectra of the reduced and used Ag/ZnO catalyst.

Fig. S10  Comparing of energy efficiency of CO production with plasma catalytic RWGS reactions that previous reported (1, 2, 3, 4, 5, 6, 7, 8).

# 2. Supplementary table

Table S1  Porous properties of the calcined, reduced and used Ag/ZnO catalyst.

| Catalyst | BET surface area (m2/g) | Pore volume (cm3/g) | Pore diameter (nm) |
| --- | --- | --- | --- |
| Calcined | 17 | 0.12 | 36 |
| Reduced | 14 | 0.10 | 40 |
| used | 13 | 0.09 | 33 |

*Determined at P/P0 = 0.99

# 3. Reference

1.	Chen S, Liu T, Niu J, Huang J, Peng X, Zhou H, et al. Plasma-catalytic CO2 methanation over Ni supported on MCM-41 catalysts: Effect of metal dispersion and process optimization. Carbon Capture Science & Technology. 2024;11:100194.

2.	Xu S, Sarayute CS, Shao Y, Xu S, Wang YC, Haigh S, et al. Mechanistic study of non-thermal plasma assisted CO2 hydrogenation over Ru supported on MgAl layered double hydroxide. Applied Catalysis B: Environmental. 2020;268:118752.

3.	Kim Y, Kim KJ, Song Y, Lee YL, Roh HS, Na K. Highly CO-selective Ni–MgO–CexZr1–xO2 catalyst for efficient low-temperature reverse water–gas shift reaction. Journal of Industrial and Engineering Chemistry. 2023;118:341-50.

4.	Tang CW, Chuang SSC. The effect of reduction of pretreated NiO–ZnO catalysts on the water–gas shift reaction for hydrogen production as studied by in situ DRIFTS/MS. International Journal of Hydrogen Energy. 2014;39(2):788-797.

5.	Pastor-Pérez L, Shah M, Le Saché E, Ramirez Reina T. Improving Fe/Al2O3 Catalysts for the Reverse Water-Gas Shift Reaction: On the Effect of Cs as Activity/Selectivity Promoter. Catalysts. 2018;8(12):608.

6.	Zeng YX, Wang L, Wu CF, Wang JQ, Shen BX, Tu X. Low temperature reforming of biogas over K-, Mg- and Ce-promoted Ni/Al2O3 catalysts for the production of hydrogen rich syngas: Understanding the plasma-catalytic synergy. Applied Catalysis B: Environment and Energy. 2018;224:469-78.

7.	Sun Y, Wu J, Wang Y, Li J, Wang N, Harding J, et al. Plasma-Catalytic CO2 Hydrogenation over a Pd/ZnO Catalyst: In Situ Probing of Gas-Phase and Surface Reactions. JACS Au. 2022;2:1800 - 10.

8.	Liu M, Yi Y, Wang L, Guo H, Bogaerts A. Hydrogenation of Carbon Dioxide to Value-Added Chemicals by Heterogeneous Catalysis and Plasma Catalysis. Catalysts. 2019;9(3):275.