Electronic Supplementary Material

# Tailoring ammonia adsorption in UiO-67 via defect and metal site engineering

Guilian Wang1*, Ka Tsun Wong2*, Yihan Lu1, Yuhui Huang1, S. C. Edman Tsang2, Pu Zhao (*)1

1 State Key Laboratory of Bioinspired Interfacial Materials Science, Innovation Center for Chemical Science, College of Chemistry, Chemical Engineering and Materials Science, Soochow University, Suzhou 215123, China

2 Department of Chemistry, University of Oxford, Oxford OX1 3QR, UK

E-mail: puzhao@suda.edu.cn

Fig. S1 Appearance of a typical 1H NMR spectrum of Acet samples with peaks assigned to their corresponding protons.

Fig. S2 Appearance of a typical 1H NMR spectrum of Dif samples with peaks assigned to their corresponding protons.

Fig. S3 Appearance of a typical 19F NMR spectrum of Trif samples with peaks assigned to their corresponding F atoms.

Fig. S4 Appearance of a typical 1H NMR spectrum of UiO-67-bpydc samples before Cu loading, with peaks assigned to their corresponding protons.

Fig. S5 TGA curves of 20py and 20py-Cu. The weight percentage is referenced to the final mass at 800 °C.

Fig. S6 Percentage change in final adsorption capacity for individual UiO-67-bpydc samples before and after Cu loading. Note that the value for 10py is calculated from an extrapolated isotherm.

Fig. S7 Three consecutive NH3 adsorption-desorption cycles at 298 K for Trif20.

Fig. S8 Three consecutive NH3 adsorption-desorption cycles at 298 K for 5py-Cu.

Fig. S9 PXRD patterns of Trif20 before and after three NH3 adsorption-desorption cycles.

Fig. S10 PXRD patterns of 5py-Cu before and after three NH3 adsorption-desorption cycles.

Fig. S11 PXRD patterns of 5py-Cu before and after immersion in deionized water for 24 hours.

Table S1 Volume of modulator added in the synthesis of each defect-engineered UiO-67 sample. The number in the sample label refers to the molar equivalents of modulator relative to ZrCl4.

| Sample | Acid | Volume of acid/mL |
| --- | --- | --- |
| Acet8 | Acetic acid | 0.254 |
| Acet30 |  | 0.952 |
| Acet60 |  | 1.90 |
| Acet90 |  | 2.85 |
| Dif5 | Difluoroacetic acid (DFA) | 0.175 |
| Dif20 |  | 0.700 |
| Dif30 |  | 1.05 |
| Trif5 | Trifluoroacetic acid (TFA) | 0.212 |
| Trif10 |  | 0.424 |
| Trif20 |  | 0.848 |

Table S2 Mass of the two linkers added in the synthesis of each UiO-67-bpydc sample. The number in the sample labels denote the percentage of H2bpydc. For each sample mixture, the total molar quantity of linkers is 1.11 mmol.

| Sample | H2bpdc/mg | H2bpydc/mg |
| --- | --- | --- |
| 5py | 256 | 14 |
| 10py | 242 | 27 |
| 15py | 229 | 40 |
| 20py | 215 | 54 |

Table S3 The defect content, number of missing linkers per Zr6 formula unit, and actual chemical formulae of defect-engineered UiO-67 samples calculated from NMR data.

| Sample | Mod/Linker | Defect Content (%) | No. of missing linkers per Zr6 formula unit | Formula Zr6O4(OH)4(bpdc)6-x(mod)2x |
| --- | --- | --- | --- | --- |
| Acet8 | 0.115 | 5.4 | 0.33 | Zr6O4(OH)4(bpdc)5.67(acet)0.66 |
| Acet30 | 0.206 | 9.3 | 0.56 | Zr6O4(OH)4(bpdc)5.44(acet)1.12 |
| Acet60 | 0.263 | 11.6 | 0.70 | Zr6O4(OH)4(bpdc)5.30(acet)1.40 |
| Acet90 | 0.276 | 12.1 | 0.73 | Zr6O4(OH)4(bpdc)5.27(acet)1.46 |
| Dif5 | 0.385 | 16.1 | 0.97 | Zr6O4(OH)4(bpdc)5.03(DFA)1.94 |
| Dif20 | 1.689 | 45.8 | 2.75 | Zr6O4(OH)4(bpdc)3.25(DFA)5.50 |
| Dif30 | 1.780 | 47.1 | 2.83 | Zr6O4(OH)4(bpdc)3.17(DFA)5.66 |
| Trif5 | 0.546 | 21.4 | 1.29 | Zr6O4(OH)4(bpdc)4.71(TFA)3.58 |
| Trif10 | 1.231 | 38.1 | 2.29 | Zr6O4(OH)4(bpdc)3.71(TFA)4.58 |
| Trif20 | 2.011 | 50.1 | 3.01 | Zr6O4(OH)4(bpdc)2.99(TFA)6.02 |

Table S4 pKa values of the linker and modulators[1].

| Species | pKa |
| --- | --- |
| H2bpdc linker | 3.77 ± 0.10* |
| Acetic acid | 4.76 |
| Difluoroacetic acid | 1.24 |
| Trifluoroacetic acid | 0.23 |

*The value for H2bpdc is that for pKa1 and is a predicted value.

Table S5 The defect content, number of missing linkers per Zr6 formula unit, and actual chemical formulae of defect-engineered UiO-67 samples calculated from TGA data.

| Sample | Mod/Linker | Defect Content (%) | No. of missing linkers per Zr6 formula unit | Formula Zr6O4(OH)4(bpdc)6-x(mod)2x |
| --- | --- | --- | --- | --- |
| Acet8 | 64.8 | 5.7 | 0.34 | Zr6O4(OH)4(bpdc)5.66(acet)0.68 |
| Acet90 | 62.9 | 12.9 | 0.77 | Zr6O4(OH)4(bpdc)5.23(acet)1.54 |
| Dif5 | 62.0 | 16.4 | 0.98 | Zr6O4(OH)4(bpdc)5.02(DFA)1.96 |
| Dif30 | 50.4 | 47.8 | 2.87 | Zr6O4(OH)4(bpdc)3.13(DFA)5.74 |
| Trif5 | 60.6 | 21.1 | 1.26 | Zr6O4(OH)4(bpdc)4.74(TFA)3.52 |
| Trif20 | 48.7 | 51.3 | 3.08 | Zr6O4(OH)4(bpdc)2.92(TFA)6.16 |

Table S6 Comparison of defect contents calculated from NMR and TGA data respectively.

| Sample | Defect Content (%) |  |
| --- | --- | --- |
|  | NMR | TGA |
| Acet8 | 5.4 | 5.7 |
| Acet90 | 12.1 | 12.9 |
| Dif5 | 16.1 | 16.4 |
| Dif30 | 47.1 | 47.8 |
| Trif5 | 21.4 | 21.1 |
| Trif20 | 50.1 | 51.3 |

Table S7 %bpydc of 5py, 10py, 15py and 20py.

| Sample | bpydc/bpdc | %bpydc |
| --- | --- | --- |
| 5py | 0.0673 | 6.3 |
| 10py | 0.1457 | 12.7 |
| 15py | 0.2175 | 17.9 |
| 20py | 0.2956 | 22.8 |

Table S8 The data of percentage change in final adsorption capacity for individual samples before and after Cu loading.

| Sample | % change in final adsorption |
| --- | --- |
| 5py | +50.6 |
| 10py | +31.3 |
| 15py | -1.5 |
| 20py | -11.5 |

References

- Forgan, R.S., Modulated self-assembly of metal-organic frameworks. Chemical Science, 2020. 11(18): p. 4546-4562.