Supporting Information

Modulating the Secondary Coordination Sphere of the Cu Site for Boosting Acetylene Hydrochlorination

Dingqiang Feng1, Linfeng Li1, Yunsheng Dai2, Wei Li1, Jinli Zhang1, Bao Wang()1, Jiangjiexing Wu()3

1School of Chemical Engineering and Technology, Tianjin University, Tianjin 300072, China

2Yunnan Precious Metals Lab Co., Ltd., Kunming 650106, China

3School of Marine Science and Technology, Tianjin University, Tianjin 300072, China

Corresponding authors: Dr. Bao Wang, E-mail: wangbao2020@tju.edu.cn

Dr. Jiangjiexing Wu, E-mail: wjjx1987@tju.edu.cn

Fig. S1 (a, b) C2H2 conversion and VCM selectivity of Cu catalysts. (c, d) C2H2 conversion and VCM selectivity of Cu-MMTB/AC with various MMTB additions. (T = 180°C, V(HCl)/V(C2H2) = 1.2 and GHSV(C2H2) = 180 h−1)

Fig. S2 The long-life test performance of Cu-MMTB/AC for acetylene hydrochlorination. (T = 180°C, V(HCl)/V(C2H2) = 1.2 and GHSV(C2H2) = 50 h−1)

Fig. S3 XPS Cu 2p spectra of fresh Cu-ligand catalysts. (a)Cu-MMTB. (b) Cu-EMTB. (c) Cu-TMTB. (d) Cu-BMTB. (e) Cu-EETB. (f) Cu-EPTB.

Fig. S4 XPS Cu LMM spectra of fresh Cu-ligand catalysts. (a)Cu-MMTB. (b) Cu-EMTB. (c) Cu-TMTB. (d) Cu-BMTB. (e) Cu-EETB. (f) Cu-EPTB.

Fig. S5 C2H2 adsorption schematic structure of the catalysts. (a) Cu-MMTB. (b) Cu-EMTB. (c) Cu-TMTB. (d) Cu-BMTB. (e) Cu-EETB. (f) Cu-EPTB.

Fig. S6 EXAFS fitting of the first-shell for Cu foil.

Fig. S7 EXAFS fitting of the first-shell for Cu/AC.

Fig. S8 Coordination structure schematic between copper chloride and MMTB.

Fig. S9 Energy barrier diagram of the catalysts catalyzed acetylene hydrochlorination reaction based on the Langmuir-Hinshelwood mechanism.

Fig. S10 HAADF-STEM image of Cu-MMTB/AC.

Fig. S11 The particle size distribution of the catalysts. (a) Cu/AC. (b) Cu/AC-used. (c) Cu-MMTB/AC. (d) Cu-MMTB/AC-used.

Fig. S12 EDS image of samples. (a) Cu/AC. (b) Cu-MMTB/AC-used.

Fig. S13 TG-DTG curve of Cu/AC and Cu/AC-used.

Table S1. The catalytic performance of Cu catalysts published in the last five years

| Catalysts | Reaction Conditions | Initial maximum C2H2 conversion | During the time period |
| --- | --- | --- | --- |
| Cu-MOMTPPC/SAC [1] | T = 180°C, V(HCl)/V(C2H2) = 1.2, GHSV(C2H2) = 180 h−1 | 92.2% | 48 h |
| Cu/PC800 [2] | T = 150°C, V(HCl)/V(C2H2) = 1.2, GHSV(C2H2) = 90 h−1 | 83.1% | 10 h |
| Cu-TPPO/AC [3] | T = 180°C, V(HCl)/V(C2H2) = 1.2, GHSV(C2H2) = 180 h−1 | 88.0% | 12 h |
| Cu/O-FLP [4] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 360 h−1 | 59.4% | 9 h |
| Cu-iPr2PCl/AC [5] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 180 h−1 | 93.7% | 24 h |
| Cu-MPPO/AC [6] | T = 180°C, V(HCl)/V(C2H2) = 1.2, GHSV(C2H2) = 180 h−1 | 96.1% | 24 h |
| Cu/NP-AC [7] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 180 h−1 | 92.4% | 12 h |
| Cu-NHP-AC/N [8] | T = 150°C, V(HCl)/V(C2H2) = 1.08, GHSV(C2H2) = 90 h−1 | 88.4% | 40 h |
| Cu-Urea/USY [9] | T = 160°C, V(HCl)/V(C2H2) = 1.25, GHSV(C2H2) = 120 h−1 | 73.6% | 8 h |
| Cu/O-FLP [10] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 180 h−1 | 61.4% | 9 h |
| Cu-MMTB/ACThis work | T = 180°C, V(HCl)/V(C2H2) = 1.2, GHSV(C2H2) = 180 h−1 | 88.5% | 24 h |

Table S2. The long-life performance of Cu catalysts published in the last five years

| Catalysts | Long-Life Reaction Conditions | Final C2H2 Conversion | Longevity |
| --- | --- | --- | --- |
| Cu-MOMTPPC/SAC [1] | T = 180°C, V(HCl)/V(C2H2) = 1.20, GHSV(C2H2) = 36 h−1 | 98.7% | 360 h |
| Cu/PC800 [2] | T = 150°C, V(HCl)/V(C2H2) = 1.20, GHSV(C2H2) = 90 h−1 | 83.1% | 10 h |
| Cu-TPPO/AC [3] | T = 180°C, V(HCl)/V(C2H2) = 1.20, GHSV(C2H2) = 50−1 | 94.0% | 327 h |
| Cu/O-FLP [4] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 360 h−1 | 59.4% | 9 h |
| Cu-iPr2PCl/AC [5] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 40 h−1 | 95.0% | 400 h |
| Cu-MPPO/AC [6] | T = 180°C, V(HCl)/V(C2H2) = 1.20, GHSV(C2H2) = 50 h−1 | 90.0% | 600 h |
| Cu/NP-AC [7] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 180 h−1 | 92.4% | 12 h |
| Cu-NHP-AC/N [8] | T = 150°C, V(HCl)/V(C2H2) = 1.08, GHSV(C2H2) = 90 h−1 | 88.4% | 40 h |
| Cu-Urea/USY [9] | T = 160°C, V(HCl)/V(C2H2) = 1.25, GHSV(C2H2) = 120 h−1 | 73.6% | 8 h |
| Cu/O-FLP [10] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 180 h−1 | 61.4% | 9 h |
| Cu-MMTB/ACThis work | T = 180°C, V(HCl)/V(C2H2) = 1.20, GHSV(C2H2) = 50 h−1 | 97.5% | 308 h |

Table S3. The catalytic performance of Au, Ru and Hg catalysts published

| Catalysts | Reaction Conditions | C2H2 conversion | During the time period |
| --- | --- | --- | --- |
| [AuCl2(phen)]Cl/AC [11] | T = 180°C, V(HCl)/V(C2H2) = 1.20, GHSV(C2H2) = 280 h−1 | 96.0% | 40 h |
| Au NCS/AC [12] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 160 h−1 | 88.0% | 8 h |
| Au/MCN [13] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 220 h−1 | 93.1% | 7 h |
| AuPPh3Cl/AC [14] | T = 170°C, V(HCl)/V(C2H2) = 1.10, GHSV(C2H2) = 360 h−1 | 96.3% | 48 h |
| [Prmim]AuCl4/AC [15] | T = 180°C, V(HCl)/V(C2H2) = 1.20, GHSV(C2H2) = 370 h−1 | 77.1% | 50 h |
| Ru/AC [16] | T = 170°C, V(HCl)/V(C2H2) = 1.10, GHSV(C2H2) = 180 h−1 | 78.8% | 48 h |
| Ru(NH4)2Cl6/AC [16] | T = 170°C, V(HCl)/V(C2H2) = 1.10, GHSV(C2H2) = 180 h−1 | 90.5% | 48 h |
| Ru/AC-N2 [17] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 180 h−1 | 84.4 % | 24 h |
| Ru-L1/AC [18] | T = 180°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 180 h−1 | 96.5% | 24 h |
| Hg-Cs/AC [19] | T = 170°C, V(HCl)/V(C2H2) = 1.20, GHSV(C2H2) = 180 h−1 | 51.2% | 24 h |
| HgCl2-4KCl/AC[20] | T = 220°C, V(HCl)/V(C2H2) = 1.20, GHSV(C2H2) = 180 h−1 | 70.0% | 50 h |
| Se–HgCl2/AC [21] | T = 170°C, V(HCl)/V(C2H2) = 1.15, GHSV(C2H2) = 200 h−1 | 83.0% | 12 h |
| Cu-MMTB/ACThis work | T = 180°C, V(HCl)/V(C2H2) = 1.20, GHSV(C2H2) = 180 h−1 | 88.5% | 24 h |

Table S4. EXAFS fitting parameters at the Cu K-edge for various samples

| Sample | Path | Distance (Å) | C.N. | σ2 (Å2) | ΔE0 (eV) | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Cu foil | Cu−Cu | 2.55 | 12 | 0.009 | 4.9 | 0.002 |
| Cu/AC | Cu−Cl | 2.20 | 4.7 | 0.015 | −9.9 | 0.017 |
| Cu-MMTB/AC | Cu−Cl | 2.21 | 4.3 | 0.016 | −9.0 | 0.012 |

Note: aCN, coordination number; bR, the distance to the neighboring atom; cσ2, the mean square relative displacement (MSRD); dΔE0, inner potential correction. R factor indicates the goodness of the fit. S02 was fixed to 0.933, according to the experimental EXAFS fit of Cu foil by fixing CN as the known crystallographic value. A reasonable range of EXAFS fitting parameters: 0.700 < S02 < 1.000; CN > 0; σ 2 > 0 Å2; |ΔE0| < 10 eV, R factor < 0.020.

Table S5. Mulliken charges of copper chloride and MMTB pre- and after-coordination.

| Atom |  | Pre-Coordination | After-Coordination |
| --- | --- | --- | --- |
| Copper Chloride | 1#Cu | 0.442 | 0.389 |
|  | 2#Cu | 0.433 | 0.386 |
|  | 3#Cu | 0.455 | 0.441 |
|  | 1#Cl | −0.184 | −0.243 |
|  | 2#Cl | −0.222 | −0.235 |
|  | 3#Cl | −0.269 | −0.307 |
|  | 4#Cl | −0.174 | −0.264 |
|  | 5#Cl | −0.208 | −0.191 |
|  | 6#Cl | −0.273 | −0.317 |
|  | Sum Cu | 1.33 | 1.22 |
|  | Sum Cl | −1.33 | −1.56 |
|  | Sum Cu+Cl | 0.00 | −0.341 |
| MMTB | Oxygen | −0.347 | −0.324 |
|  | Sum MMTB | 0.00 | 0.341 |

Table S6. Energy based on the Eley-Rideal mechanism (kcal·mol−1)

| Paths | Cu-MMTB | Cu-EMTB | Cu-EETB |
| --- | --- | --- | --- |
| Cat | 0 | 0 | 0 |
| C2H2* | −8.46 | −10.8 | −11.6 |
| TS1 | 1.63 | 1.26 | 1.18 |
| C2H2Cl* | −13.7 | −12.6 | −13.0 |
| HCl* | −18.4 | −18.1 | −18.4 |
| TS2 | −16.8 | −15.7 | −15.9 |
| VCM* | −47.9 | −45.4 | −52.3 |
| VCM | −39.5 | −39.5 | −39.5 |

Table S7. Energy based on the Langmuir-Hinshelwood mechanism (kcal·mol−1)

| Paths | Cu-MMTB | Cu-EMTB | Cu-EETB |
| --- | --- | --- | --- |
| co-ads | 0 | 0 | 0 |
| TS | 13.2 | 15.9 | 14.3 |
| VCM* | −33.6 | −28.4 | −29.4 |

Table S8. Cu and P content of Cu catalysts in terms of the total mass.

| Sample | Cu (wt.%) | P (wt.%) |
| --- | --- | --- |
| Cu/AC | 10.4 | - |
| Cu/AC-used | 10.3 | - |
| Cu-MMTB/AC | 10.3 | 0.577 |
| Cu-MMTB/AC-used | 10.9 | 0.586 |

Table S9. TG-DTG results for Cu catalysts

| Sample | 150°C (%) | 290°C (%) | Δ (%) | Coke (%) |
| --- | --- | --- | --- | --- |
| Cu/AC | 95.0 | 89.7 | 5.34 | 5.72 |
| Cu/AC-used | 97.4 | 86.7 | 10.8 |  |
| Cu-MMTB/AC | 95.9 | 89.6 | 6.29 | 5.05 |
| Cu-MMTB/AC-used | 97.2 | 86.2 | 11.0 |  |

Reference

1. Wang Y, Nian Y, Zhang J, Li W, Han Y. MOMTPPC improved Cu-based heterogeneous catalyst with high efficiency for acetylene hydrochlorination. Molecular Catalysis, 2019, 479: 110612.

2. Wang T, Jiang Z, Tang Q, Wang B, Wang S, Yu M, Chang R, Yue Y, Zhao J, Li X. Interactions between atomically dispersed copper and phosphorous species are key for the hydrochlorination of acetylene. Communications Chemistry, 2022, 5(1): 2.

3. Wang B, Zhang T, Liu Y, Li W, Zhang H, Zhang J. Phosphine-oxide organic ligand improved Cu-based catalyst for acetylene hydrochlorination. Applied Catalysis A: General, 2022, 630: 118461.

4. Peng J, Dong D, Wang Z, Yang H, Qiao D, Wang Q, Sun W, Liu M, Wang J, Zhu M, Dai B, He F, Huang C. Manipulating micro-electric field and coordination-saturated site configuration boosted activity and safety of frustrated single-atom Cu/O Lewis pair for acetylene hydrochlorination. Nano Research, 2023, 16(7): 9039-9049.

5. Zhang T, Wang B, Nian Y, Liu M, Jia Y, Zhang J, Han Y. Excess copper chloride induces active sites over Cu-ligand catalysts for acetylene hydrochlorination. ACS Catalysis, 2023, 13(12): 8307-8316.

6. Wang B, Zhang T, Li L, Zhang H, Wu J, Zhang J. Data-informed discovery of high-performance Cu-ligand catalysts for acetylene hydrochlorination. Chemical Engineering Journal, 2024, 480: 148323.

7. Li F, Wang X, Zhang P, Wang Q, Zhu M, Dai B. Nitrogen and phosphorus co-doped activated carbon induces high density Cu+ active center for acetylene hydrochlorination. Chinese Journal of Chemical Engineering, 2023, 59: 193-199.

8. Wang X, Zhu R, Dai Y, Xia H, Niu Q. N-Hydroxyethyl-2-Pyrrolidone improved Cu-based catalysts with high performance for acetylene hydrochlorination. Catalysis Letters, 2024, 154(5): 2285-2293.

9. Dang L, Wang L, Yan H, Gong B, Yang C, Wang J, Sun H, Li X, Wu R, Liang C. Urea modified USY zeolite supported Cu-based catalyst for acetylene hydrochlorination. Materials Today Communications, 2024, 40: 110070.

10. Peng J, Yin X, Dong D, Guo Z, Wang Q, Liu M, He F, Dai B, Huang C. Promotion effect of epoxy group neighboring single-atom Cu site on acetylene hydrochlorination. Chinese Chemical Letters, 2024, 35(6): 109508.

11. Huang C, Zhu M, Kang L, Dai B. A novel high-stability Au(III)/Schiff-based catalyst for acetylene hydrochlorination reaction. Catalysis Communications, 2014, 54: 61-65.

12. Qiao X, Liu X, Yang Y, Mao Z, Li T, Gao L, Zhao C, Guan Q, Li W. Carbon-Supported Au Catalyst in Acetylene Hydrochlorination: Enhancing Catalytic Performance by Complexation of Dicarbonyl Ligands. ChemCatChem, 2022, 14(21): e202200785.

13. Dai B, Li X, Zhang J, Yu F, Zhu M. Application of mesoporous carbon nitride as a support for an Au catalyst for acetylene hydrochlorination. Chemical Engineering Science, 2015, 135: 472-478.

14. Dong Y, Li W, Yan Z, Zhang J. Hydrochlorination of acetylene catalyzed by an activated carbon supported chlorotriphenylphosphine gold complex. Catalysis Science & Technology, 2016, 6(22): 7946-7955.

15. Zhao J, Gu S, Xu X, Zhang T, Yu Y, Di X, Ni J, Pan Z, Li X. Supported ionic-liquid-phase-stabilized Au(iii) catalyst for acetylene hydrochlorination. Catalysis Science & Technology, 2016, 6(9): 3263-3270.

16. Gu J, Gao Y, Zhang J, Li W, Dong Y, Han Y. Hydrochlorination of Acetylene Catalyzed by an Activated Carbon-Supported Ammonium Hexachlororuthenate Complex. Catalysts, 2017, 7(1): 17.

17. Man B, Zhang H, Zhang C, Li X, Dai H, Yu F, Zhu M, Dai B, Zhang J. Hydrochlorination of acetylene over the Ru-based catalysts treated by plasma under different atmospheres. Plasma Science and Technology, 2019, 21(8): 085501.

18. Li J, Zhang H, Cai M, Li L, Li Y, Zhao R, Zhang J. Enhanced catalytic performance of activated carbon-supported ru-based catalysts for acetylene hydrochlorination by azole ligands. Applied Catalysis A: General, 2020, 592: 117431.

19. Xu X-L, Zhao J, Lu C-S, Zhang T-T, Di X-X, Gu S-C, Li X-N. Improvement of the stability of Hg/AC catalysts by CsCl for the high-temperature hydrochlorination of acetylene. Chinese Chemical Letters, 2016, 27(6): 822-826.

20. Xu X, He H, Zhao J, Wang B, Gu S, Li X. The ligand coordination approach for improving the stability of low-mercury catalyst in the hydrochlorination of acetylene. Chinese Journal of Chemical Engineering, 2017, 25(9): 1217-1221.

21. Sun S, Xu H, Fan Y, Liu Z, Hong Q, Huang W, Qu Z, Yan N. Construction of a Thermally Stable Low-HgCl2 Catalyst via Chalcogen Bonding and Its Enhanced Activity in Acetylene Hydrochlorination. Industrial & Engineering Chemistry Research, 2022, 61(46): 17057-17064.