Electronic Supplementary Material

Unveiling lightweight and high impact tough polypropylene foams through compatibilized in-situ fibrillation integrated chemical foam injection molding

Jing Jiang ()1,2, Caiyi Jia1,2, Suyu Yang1,2, Zhongxing Li1,2, Lian Yang1,2, Xiaofeng Wang2, Changwei Zhu3, Qian Li2

1 School of Mechanical & Power Engineering, Zhengzhou University, Zhengzhou 450001, China

2 National Center for International Joint Research of Micro-Nano Molding Technology, Zhengzhou University, Zhengzhou 450001, China

3 School of Electronics & Mechanical Engineering Technology, Seneca Polytechnic, Toronto M2J2X5, Canada

E-mail: jiangjing@zzu.edu.cn

EXPERIMENTAL

Fig. S1 DSC heating curve (a) and gas volume (b) of the self-developed endo-exothermic mixed CBA in this work.

During the heating process depicted in Fig. S1(a), the initial endothermic temperature was observed to commence at 165 °C. This indicated the onset of the decomposition of the inorganic foaming agent. Subsequently, a distinct exothermic peak adjacent to the endothermic peak was detected. This exothermic peak is characteristic of the decomposition of the organic foaming agents within the CBA. The maximum exothermic peak occurred at approximately 193 °C and concluded at 215 °C. Fig. S1(b) presents the gas release curve as a function of temperature. Evidently, the maximum gas volume of 267 ml/g was achieved at 212 °C. The findings obtained in this study suggest that the self - developed CBA is efficient and can be applied in the subsequent continuous fiber - integrated molding (CFIM) experiments.

Results and discussion

INF Composite Morphology

Fig.S2 SEM micrograph of neat PP fracture surface

Cellular morphology of CFIM parts

Fig.S3 SEM images of the cellular structures along FD in CFIM parts: (a) PP/PA6(S)/M0.5; (b) PP/PA6(S)/M2; (c) PP/PA6(F)/M0.5; (d) PP/PA6(F)/M2

Video S1. Continuous fabrication process of INF composites.

Fig.S5