Electronic Supplementary Material

Synergetic catalysis between ZnZrOx and silanol nest-enriched silicalite-1 in CO2 hydrogenation coupled with toluene alkylation

Yuhang Guo, Weichao Qin, Ruiwen Cao, Linfeng Zhang, Tingjun Fu (), Zhong Li

State Key Laboratory of Clean and Efficient Coal Utilization, College of Chemistry and Chemical Engineering, Taiyuan University of Technology, Taiyuan 030024, China

E-mail: futingjun@tyut.edu.cn

Fig. S1 Catalytic performance of ZZO:AS-1 at a mass ratio of 6:4. Reaction conditions: 350 °C, 3.0 MPa, GHSV of mixture gas (CO2/H2/N2) = 4800mL g-1 h−1, WHSV of toluene = 0.8 h−1.

Fig. S2 In situ DRIFTS spectra at 350 °C. (a, b) ZnZrOx catalyst under a CO2/H2 stream for 30 min: (a) 3200-1000 cm-1 range and (b) 2500-2100 cm-1 range. (c, d) Spectra after switching to a toluene/N2 stream for 30 min over (c) ZZO&ZSM-5 and (d) ZZO&AS-1. (e, f) Control spectra under a toluene/N2 stream for 30 min over (e) ZZO&ZSM-5 and (f) ZZO&AS-1.

Fig. S3 (a) Photographs after being dissolved in 20% HF and extracted by CH2Cl2: ①ZZO&ZSM-5 catalyst, ②ZZO&AS-1 catalyst. (b) GC-MS chromatograms of the organic species extracted by CH2Cl2. (c) ZZO&Z5 catalysts and (d) ZZO&AS-1 catalysts after in situ experiment.

Fig. S4 TEM images of (a) the parent AS-1 and the AHFS-treated samples for (b) 8 h and (c) 16 h.

Fig. S5 (a-b) Influence of different silicon coating on the catalytic performance of AS-1. The ZZO loading ratio is fixed at 1:2. Reaction conditions: 350 °C, 3.0 Mpa. GHSV of mixture gas (CO2/H2/N2) = 8000 mL g-1 h−1, WHSV of toluene = 1.3 h−1.

Fig. S6 XPS patterns of (a) AS-1 in ZZO&AS-1 20-40 PM catalyst, denoted as fresh-AS-1, (b) AS-1 in ZZO&AS-1 20-40 PM catalyst after stability evaluation, denoted as used-AS-1 (c-d) STEM and EDS elemental mapping of Spent-ZZO&AS-1 PM catalyst.

Fig. S7 (a) Photographs after being dissolved in 20% HF and extracted by CH2Cl2: ①spent-ZZO&AS-1 PM catalyst, ②spent-ZZO&AS-1@25%S-1 PM catalyst, ③spent-ZZO/AS-1@25%S-1 catalyst. (b) GC-MS chromatograms of the organic species extracted by CH2Cl2.
Table S1. Textural properties of ZSM-5 and AS-1 catalysts.

| Sample | Surface area / (m2·g-1) |  |  | Pore volume / (cm3·g-1) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | SBET a | Smic b | Sext c | Vtotal d | Vmic e | Vmesof |
| ZSM-5 | 390 | 378 | 12 | 0.22 | 0.16 | 0.07 |
| AS-1 | 397 | 388 | 9 | 0.21 | 0.19 | 0.02 |

a Surface area, determined by BET model.

b Surface area of micropores, determined by t-plot method.

c Surface area of mesopores, determined by SBET-Smicro.

d Total pore volume, estimated from the adsorbed amount at P/P0=0.99.

e Micropores volume, determined by t-plot method.

f Mesopores volume, determined by Vtotal-Vmicro.

Table S2. Acidic properties of ZSM-5 and AS-1.

| Sample | NH3-TPD (μmmol·g-1) |
| --- | --- |
|  | Total |
| ZSM-5 | 443 |
| AS-1 | 38 |

Table S3. The assignments of peaks in in situ DRIFTS.

| Peaks (cm-1) | Assignment | Species |
| --- | --- | --- |
| 2200-2400 | v(C=O) | CO2 |
| 1376 | vs(OCO) | HCOO* |
| 1589 | vas(OCO) |  |
| 2734 | δ(CH)+ vas(OCO) |  |
| 2878 | v(CH) |  |
| 2975 | v(CH) |  |
| 1175 | v(C-O) | CH3O* |
| 1145 | v(C-O) |  |
| 1400-1500 | v(C-C) | The C-H and C-C vibration of aromatic compounds |
| 3000-3100 | v(C-H) |  |

Table S4. Textural properties of samples with defect-repairing treatment at different times

| Sample | Surface area / (m2·g-1) |  |  | Pore volume / (cm3·g-1) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | SBET a | Smic b | Sext c | Vtotal d | Vmic e | Vmesof |
| AS-1 | 397 | 388 | 9 | 0.21 | 0.19 | 0.02 |
| 4F-AS-1 | 318 | 241 | 77 | 0.21 | 0.12 | 0.09 |
| 8F-AS-1 | 307 | 241 | 66 | 0.21 | 0.13 | 0.08 |
| 16F-AS-1 | 309 | 249 | 60 | 0.21 | 0.13 | 0.08 |

a Surface area, determined by BET model.

b Surface area of micropores, determined by t-plot method.

c Surface area of mesopores, determined by SBET-Smicro.

d Total pore volume, estimated from the adsorbed amount at P/P0=0.99.

e Micropores volume, determined by t-plot method.

f Mesopores volume, determined by Vtotal-Vmicro.

Table S5. Acidic properties of with different time points of defect-repairing treatment.

| Sample | NH3-TPD (μmmol·g-1) |
| --- | --- |
|  | Total |
| AS-1 | 38 |
| 4F-AS-1 | 29 |
| 8F-AS-1 | 22 |
| 16F-AS-1 | 12 |

Table S6. Comparison of Data Related to Two Types of Catalysts

| catalysts | STYPX | rxylene | rMeOH1 | rMeOH2 |
| --- | --- | --- | --- | --- |
|  | mg g-1 cat h-1 | mol g-1 cat h-1 | molMeOH g-1 cat h-1 | molMeOH g-1 cat h-1 |
| ZZO (20-40) & AS-1@25%S-1(80-100) | 34.23 | 3.69×10-3 | 0.002015 | 0.000943 |
| ZZO/AS-1@25%S-1 (1:3) | 42.33 | 4.2×10-3 | 0.004114 | 0.002057 |

Table S7. Summary of catalysts and their performances for CO2 hydrogenation to aromatics

| Catalysts | T (°C) | Press. (MPa) | CO2 Conv. (%) | Toluene Conv. (%) | Selectivity of Xylene (%) | PX Selectivity (PX/X) (%) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ZnZrOx /4SZ5 | 360 | 3 | - | - | Xyl 92.4 | 70.8 | Sci. Adv. 2020; 6 : eaba5433 |
| ZnCeZrOx /MCM-22 | 330 | 3 | 7.7 | 23.6 | Xyl 92.4 | 62~67 | Chin. J. Catal. 73 (2025) 174–185 |
| ZnZrO / HZSM-5 (ZZO/Z5-SG) | 400 | 0.5 | 10.5 | 24.7 | Xyl 86.5 | - | Angew. Chem. Int. Ed. 2023, e202309377 |
| ZnZrOx / C-Z5-SiO₂ | 450 | 0.5 | 5-6 | 19.2 | Xyl 91.1 | 90.1 | Appl. Catal. B: Environ. Energy 359 (2024) 124523 |
| ZZO&4Si/MCM-22 | 280-400 | 3 | 4.2 | 10.3 | Xyl 91.0 | 70.4 | Nat. Commun. (2026) 17:967 |

Table S8. Acidic properties of AS-1 and AS-1@25%S-1.

| Sample | NH3-TPD (μmmol·g-1) |
| --- | --- |
|  | Total |
| AS-1 | 38 |
| AS-1@25%S-1 | 21 |