Electronic Supplementary Material

# Breaking the Ni loading-reducibility-dispersion dependence achieved by solid-state co-grinding

# Yong-Shan Xiao, Min-Li Zhu, Han-Qing Ge, Zhong-Wen Liu ()

Key Laboratory of Syngas Conversion of Shaanxi Province, School of Chemistry & Chemical Engineering, Shaanxi Normal University, Xi’an 710119, China

E-mail: zwliu@snnu.edu.cn

# List of Contents

1. Synthesis parameters and NiO loadings…………………...…...…..…...…...….....……...3

2. XRD pattern and TG-DSC curve of the spent catalysts….….……….………...………...4

## 1. Synthesis parameters and NiO loadings

Table S1 Summary of the added list of calculated amount of Ni(NO3)2·6H2O

| Samples | Ni(NO3)2·6H2O/g | OMA-Pa)/g | NiO designed/(wt-%) | NiO measured/(wt-%) |
| --- | --- | --- | --- | --- |
| 40Ni/OMA | 2.6474 | 1.02 | 40.0 | 41.0 |
| 30Ni/OMA | 1.7019 | 1.02 | 30.0 | 30.0 |
| 25Ni/OMA | 1.3237 | 1.02 | 25.0 | 24.7 |
| 20Ni/OMA | 0.9928 | 1.02 | 20.0 | 20.2 |
| 40Ni-OMA | -- | -- | 40.0 | 40.1 |
| 40Ni/OMA-600 | -- | -- | 40.0 | 40.6 |

a): Based on the weight of Al2O3 in a dish after calcination at 600 °C

## 2. XRD pattern and TG-DSC curve of the spent catalysts

Fig. S1. XRD pattern and TG-DSC curve of the spent 40Ni/OMA catalyst after the long-term durability test under the conditions of 600 °C and 240000 mL·g−1·h−1