Electronic Supplementary Material

Co-doping facilitated plasma-catalytic ammonia synthesis over Mo2N-Co catalysts

Yutong Feng1,2, Bianbian Gao1,2, Guoqiang Cao ()1, Donghai Hu1, Yuting Jiao1, Chunyu Li1, Jiantao Zhao1, Yitian Fang1

1 State Key Laboratory of Coal Conversion, Institute of Coal Chemistry, Chinese Academy of Sciences, Taiyuan 030001, China

2 University of Chinese Academy of Sciences, Beijing 100049, China

E-mail: caoguoqiang@sxicc.ac.cn

Table S1 Crystallographic parameters of the Mo2N-Co catalysts.

|  | PDF#25-1366 | Mo2N | Mo2N-Co0.1 | Mo2N-Co1 | Mo2N-Co2 |
| --- | --- | --- | --- | --- | --- |
| Crystal system | Cubic crystal system |  |  |  |  |
| Space group | Fm-3m |  |  |  |  |
| Cell parameter a / Å | 4.163 | 4.18106 | 4.18319 | 4.18814 | 4.17467 |
| Cell volume / Å3 | 72.15 | 73.09 | 73.2 | 73.46 | 72.76 |
| Density / g·cm-3 | 9.474 | 9.3544 | 9.3401 | 9.3071 | 9.3975 |

Table S2 Specific surface areas of Mo2N-Co catalysts.

| Catalyst | Specific surface area a (m2·g-1) | Pore volume b (cm3·g-1) | Pore size c (nm) |
| --- | --- | --- | --- |
| Mo2N | 1.929 | 0.034 | 7.485 |
| Mo2N-Co0.1 | 1.979 | 0.035 | 7.717 |
| Mo2N-Co1 | 1.586 | 0.033 | 7.278 |
| Mo2N-Co2 | 1.330 | 0.037 | 8.728 |

a Calculated by the BET method.

b Total pore volume calculated using BJH method.

c Mean pore size calculated using BJH method.

Table S3 Mo 3d binding energies (eV) and the percentage of Mo species (%).

| Catalyst | Moδ+ | Mo4+ | Mo6+ |
| --- | --- | --- | --- |
| Mo2N | 228.70 （73.58） | 230.60 （5.91） | 232.55 （20.51） |
| Mo2N-Co0.1 | 229.00 （58.03） | 230.33 （13.44） | 232.71 （28.53） |
| Mo2N-Co1 | 229.04 （60.29） | 230.25 （14.62） | 232.72 （25.09） |
| Mo2N-Co2 | 228.90 （61.10） | 230.18 （14.01） | 232.58 （24.89） |

-The percentage of the Mo species were given within the parentheses.

Fig. S1. EPR spectra of the catalysts.