Supporting Information

Electrodeposited High-Entropy Alloys as Electrocatalysts for Water Electrolysis: A Review on Composition and Synthesis Parameters for Hydrogen Production

Daniela Arango*, Antonio G. De Crisci*, Rafal Gieleciak, Mathieu L’Abbe, Jinwen Chen

Natural Resources Canada, CanmetENERGY, One Oil Patch Drive, Devon, AB, T9G 1A8, Canada

*daniela.arangovasquez@nrcan-rncan.gc.ca, antonio.decrisci@nrcan-rncan.gc.ca

© His Majesty the King in Right of Canada, as represented by the Minister of Natural Resources, 2025

Table Of Contents

Figure S1 Schematic representation of current input profiles used in ED a) DC b) PC c) CV	3

Table S1. Compilation of alkaline hydrogen evolution reaction (HER) performance metrics for various electrocatalysts reported in the literature, listing overpotential at 10 mA cm⁻² and Tafel slope values measured in 0.1 M KOH.	3

Table S2. Summary of literature on electrodeposited nanostructured HEAs for water electrolysis	8

Supporting Information References	13

# Figure S1 Schematic representation of current input profiles used in ED a) DC b) PC c) CV

# Table S1. Compilation of alkaline hydrogen evolution reaction (HER) performance metrics for various electrocatalysts reported in the literature, listing overpotential at 10 mA cm⁻² and Tafel slope values measured in 0.1 M KOH.

| Category | Alloy | Overpotential (mV) | Tafel Slope (mV dec−1) | Ref |
| --- | --- | --- | --- | --- |
| HE | FeCoNiAlTi | 88.2 | 40.1 | 1 |
| HE | FeCoNiWMo | 35 | 31 | 2 |
| HE | NiFeCoCuTi | 134 | 43 | 3 |
| HE | CuAlNiMoFe | 23 | 50 | 4 |
| HE | NiCoFeMoMn | 14 | 29 | 5 |
| HE | FeCoNiCu | 155 | 167.8 | 6 |
| HE | FeCoNiAlTi | 88.2 | 40.1 | 7 |
| HE | FeCoNiAlTi | 88.2 | 40.1 | 1 |
| HE | NiCoFeMnCrP | 220 | 94.5 | 8 |
| HE | NiFeMoCoCr | 172 | 66 | 9 |
| HE | NiCoFeMoMn | 14 | 29 | 5 |
| HE | NiFeCoWMo | 171 | 83 | 10 |
| HE | NiFeCoCrMn | 191 | 84.7 | 11 |
| HE | NiFeCoCrMn | 168 | 180 | 12 |
| HE | NiFeCoCrCu | 102 | 68 | 13 |
| HE | NiFeCoCrCu | 84 | 62 | 14 |
| HE | NiFeCoMnPO | 43 | 33.5 | 15 |
| HE | NiFeCoMnV | 7 | 147.5 | 16 |
| HE | NiFeCoMnSn | 4.3 | 59.7 | 17 |
| HE | NiFeCoCuMo | 7 | 34.7 | 18 |
| HE | NiFeMoCoCr | 172 | 66 | 19 |
| HE | CoNiCuPd | 60 | 116 | 5 |
| HE | CoFeNiMnCr | 345 | 173 | 20 |
| HE | FeCoNiAlTi | 88.2 | 40.1 | 1 |
| LE | CoSx/MoS2LE | 200 | 110 | 21 |
| LE | NiSx/MoS2LE | 180 | 100 | 21 |
| LE | N-Ni3S2 | 155 | 113 | 22 |
| LE | NiMoP | 400 | 163 | 23 |
| LE | NiMnP | 490 | 238 | 23 |
| LE | NiFeP | 690 | 116 | 23 |
| LE | NiCoP | 530 | 116 | 23 |
| LE | Ni2P | 710 | 103 | 23 |
| LE | Ni3P:Mo | 20 | 85 | 24 |
| LE | Ni3P:Fe | 46 | 86 | 24 |
| LE | NiCoP-CoP/NF | 73 | 91.3 | 25 |
| LE | Ni2P@CoP/NF | 61 | 55 | 26 |
| LE | CoP/Ni2P@HPNCP | 106 | 61.89 | 27 |
| LE | CoP@NC/GR | 105 | 125 | 28 |
| LE | Ni-Ni3C/CC | 98 | 88.5 | 29 |
| LE | V-Co4N | 37 | 44 | 30 |
| LE | Co4N | 93 | 117 | 30 |
| LE | Mo2N-CoxN-5 | 29 | 81 | 31 |
| LE | Ni3N/Ni/NF | 12 | 29.3 | 32 |
| LE | NiO NRs-m-Ov | 113 | 100 | 33 |
| LE | Ni/NiO-cp | 72 | 93.8 | 34 |
| LE | NSG@CNT-2 | 350 | 89 | 35 |
| LE | NG - Graphene | 259 | 73.2 | 36 |
| LE | G-EX-ST | 194 | 80 | 37 |
| LE | Ni-Co nanocones | 86.7 | 69.8 | 38 |
| LE | NiMo MT/NF | 119 | 119 | 39 |
| LE | Ni-Mn-P | 113 | 74 | 40 |
| LE | 15Mn-CoP | 100 | 53 | 41 |
| LE | Co@NPC-F4 | 259 | 99 | 42 |
| LE | Co-Ni/NCNFs | 86 | 152.3 | 43 |
| LE | Ni-Cu-3.0 | 128 | 57.2 | 44 |
| LE | Ni-Mn3O4/NF | 91 | 110 | 45 |
| LE | MoNi hollow structure | 38 | 31.4 | 46 |
| LE | MoS2@Ni/CC | 91 | 89 | 45 |
| LE | CoS2 nanotubes / carbon cloth | 193 | 88 | 45 |
| LE | FeS2/CoS2 | 78.2 | 44 | 47 |
| LE | Co3S4/EC-MOF | 84 | 82 | 48 |
| LE | NiSe/NF | 96 | 120 | 49 |
| LE | o-CoSe2/P | 104 | 69 | 48 |
| LE | c-CoSe2 | 200 | 85 | 50 |
| LE | Mo₂C-GNR, | 217 | 64 | 51 |
| LE | MoC-Mo₂C | 120 | 42 | 52 |
| LE | Mo₂C nanooctahedrons | 151 | 59 | 53 |
| LE | MoC@GS | 77 | 50 | 54 |
| LE | HC NiCo/C | 98 | 96 | 55 |
| LE | Ni/NiO | 226 | 135 | 56 |
| LE | Ni1.5Co0.5@N-C NT/NF | 114 | 117 | 57 |
| LE | NiFe2O4/N-graphene | 184 | 102 | 58 |
| LE | Ni/MoC /NC-100 | 161 | 105 | 59 |
| LE | Co(OH)2-MoS2 | 89 | 53 | 60 |
| LE | Cr-Co4N | 21 | 38.1 | 61 |
| LE | Ni3N-V2O3 | 57 | 50 | 62 |
| LE | O–NiCu | 23 | 34.1 | 63 |
| LE | Ni/Y2O3 | 61.1 | 52.8 | 64 |
| LE | 1T-MoS2/Ni(OH)2 | 57 | 30 | 65 |
| LE | Ni(OH)2-NiMoOx | 36 | 38 | 66 |
| LE | Ni(OH)2/NiMoPOx | 51 | 33 | 67 |
| LE | Mo-NiO/Ni | 50 | 86 | 68 |
| LE | LixNiO/Ni | 36 | 50 | 69 |
| LE | Ni5P4@NiCo2O4 | 27 | 27 | 70 |
| LE | Ni0.2Mo0.8N/Ni | 14 | 33 | 71 |
| LE | Cu NDs/Ni3S2 | 128 | 76.2 | 72 |
| LE | CoP-CeO2 | 43 | 45 | 73 |
| LE | Co4N-CeO2/GP | 24 | 61 | 74 |
| LE | NiCo-CeO2/GP | 34 | 49.1 | 75 |
| LE | V-CoP@a-CeO2 | 68 | 48.1 | 76 |
| LE | CoW(OH)x | 73.6 | 149.5 | 77 |
| LE | NiCo | 200 | 118 | 78 |
| LE | NiCr | 100 | 118 | 78 |
| LE | Ni2P | 255 | 100 | 79 |
| LE | NIP | 350 | 132.2 | 61 |
| LE | Ni3Se2 | 203 | 79 | 80 |
| LE | Ni-Co | 107 | 120 | 81 |
| LE | NiCo/NiCoOx | 155 | 35 | 82 |
| LE | Co3O4/Co/NF | 90 | 44 | 83 |
| LE | Ni/NiO | 145 | 43 | 84 |
| LE | Ni(OH)2/MoS2/CC | 80 | 60 | 85 |
| LE | FeNi-N/CFC | 106 | 115 | 57 |
| LE | FeNi3/NiFeO | 99 | 45 | 86 |
| ME | MoCoCu-P | 64.7 | 87.7 | 87 |
| ME | NiCo(CrV) | 87 | 96 | 88 |
| ME | CoFePO | 88 | 38 | 89 |
| ME | NiFe-POx/NFF | 110 | 123 | 90 |
| ME | Fe-CoP/Ti | 78 | 82 | 91 |
| ME | NiCo(CrV) | 119 | 105 | 88 |
| ME | NiCoCr | 205 | 159 | 88 |
| ME | NiCoV | 232 | 169 | 88 |
| ME | Ni(OH)2/NiMoPOx/NF | 51 | 33 | 67 |
| ME | Co–Mn–Sn | 136 | 111 | 92 |
| ME | CoFeNi | 326 | 192 | 20 |
| ME | CoFeNiMn | 335 | 194 | 20 |
| ME | CoFeNiCr | 338 | 167 | 20 |
| ME | MoS2/CoNi2S4 | 78 | 67 | 93 |
| ME | CoNiPt | 25 | 43 | 94 |
| ME | NiCoCr | 110 | 109 | 78 |
| ME | Ni-Co-Fe | 91 | 86 | 95 |
| ME | NiCoP/rGO | 209 | 124.1 | 96 |
| ME | Ni57Co24Fe | 50 | 84 | 97 |
| ME | Co53Ni33Fe | 240 | 100 | 98 |
| ME | Ni-Co-S/CF | 140 | 96 | 99 |
| LE | Fe/CoP/Ti | 78 | 75 | 100 |
| NM | Pt/VG Ar-5 | 150 | 36 | 101 |
| NM CA | Ru-g-C3N4-C-TiO2 | 107 | 83 | 102 |
| NM CA | Ru-S/N-C | 10 | 36 | 103 |
| NM CA | Rh NCs/NHCAs | 7 | 24.5 | 104 |
| NM CA | RFNOH-10 | 13 | 30 | 105 |
| NM CA | 1.08 wt.% Pt/N-Mo2C | 100 | 108.63 | 106 |
| NM CA | Er-WS2-Pt | 195 | 65 | 106 |
| NM CA | Pt@PCM | 139 | 73.6 | 106 |
| NM CA | NiFe LDH-Pt | 101 | 127 | 107 |
| NM CA | NiFe LDH-Pt co-precipitated | 128 | 188 | 107 |
| NM CA | RuO2/Co3O4 | 89 | 91 | 45 |
| NM CA | Pt/C | 40 | 29.5 | 44 |
| NM CA | Pt/C on NF | 40 | 43 | 49 |
| NM CA | FeCoCuPd | 63 | 107 | 5 |
| NM CA | Pt/c | 76 | 42 | 88 |
| NM CA | Pt | 281 | 217 | 20 |
| NM CA | NiPt3@NiS/NF | 12 | 24 | 108 |
| NM CA | Ru/(Fe,Ni)(OH)2 | 13 | 30 | 105 |
| NM CA | RuAu SAAs | 24 | 37 | 25 |
| NM CA | Pt/Ni(HCO3)2 | 27 | 45 | 109 |
| NM CA | Ni5P4-Ru | 54 | 52 | 110 |
| NM CA | Ru2P/WO3@NP | 15 | 18 | 111 |
| NM CA | CoRu/CQDs | 18 | 38.5 | 112 |
| NM CA | Pt/MgO | 39 | 39 | 113 |
| NM CA | Ru@MnO2–x | 18 | 26 | 114 |
| NM CA | Ru/NaCoO2 | 24 | 29 | 115 |
| NM CA | P-Ni2P/Ru NCs | 45 | 54.2 | 116 |
| NM CA | PtRu NCs/BP [81] | 22 | 19 | 117 |
| NM CA | RuPdNi [82] | 20 | 65 | 118 |
| NM CA | Pt/Ni3N NSs/Ni mesh | 50 | 36.5 | 119 |
| NM CA | Pt13Cu73Ni14/CNF-CF | 150 | 54 | 120 |
| NM CA | Pt/C/CC | 38 | 68 | 121 |
| NM HE | PtAuPdRhRu/C | 190 | 62 | 122 |
| NM HE | PdFeCoNiCu/C | 18 | 39 | 123 |
| NM HE | PtNiFeCoCu/C | 11 | 30 | 124 |
| NM HE | Pt18Ni26Fe15Co14Cu27/C | 11 | 30 | 125 |
| NM HE | PtNiFeCoCu26/C | 11 | 30 | 126 |
| NM HE | Pt21Ni27Fe19Co17Cu16/C | 12 | 36 | 126 |
| NM HE | Pt15Ni24Fe13Co13Cu35/C | 15 | 45 | 126 |
| NM HE | FeCoPdIrPt/GO | 42 | 82 | 127 |
| NM HE | AlNiCoRuMo | 25 | 30.3 | 128 |
| NM HE | AlNiCoRuMo | 24.5 | 31.4 | 128 |
| NM HE | Al82Ni6Co3Mn3Y3Au3 | 24 | 43 | 129 |
| NM HE | PdFeCoNiCu | 18 | 39 | 130 |
| NM HE | PdPtCuNiP | 32 | 37.4 | 123 |
| NM HE | PtMoPdRhNi | 9.7 | 25.9 | 131 |

# Table S2. Summary of literature on electrodeposited nanostructured HEAs for water electrolysis

|  | Substrate a) | Bath b) | Current Density c,d) (mA/cm2) |  | pH | Temperature (T) | Time (min) | Stirring (rpm) | Morphology | Thickness (µm) | HER n10 e) | OER n10 e) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| NiFeCoWMn | CP | Aq Cl | PC | 8000c 0.2/0.8 | 9.8 | 53 | 50 | - | Granular | - | 32 f) | 595 f) | 132 |
| NiFeCoWCu | Fe | Aq SO4 | DC | 50, 100 | 0.5-4.5 | 10 | 60 | - | Cauliflower | 0.5 | - | 247.3 | 133 |
| NiFeCoWCu | Ag | Aq SO4 | DC | 50 | 8 | 65 | 30 | 0 | Spherical granules | - | - | - | 134 |
| NiFeCoWMo | Brass | Aq SO4 | DC | 10-100 | 5 | 25 | 13 | - | - | 0.2-0.3 | - | - | 135 |
| NiFeCoWMo | Cu | Aq SO4 | PC | - | 4 | 40 | 25 | 450 | Globular | 40 | - | - | 136 |
| NiFeCoWMo | Cu | Aq SO4 | DC | 75-80 | 5 | 60 | - | 250 | - | 40 | - | - | 137 |
| NiFeCoWMo | Cu | Aq SO4 | DC | 75-80 | 5 | 60 | - | 250 | Granular | 40 | - | - | 138 |
| NiFeCoWMo | Cu | Aq SO4 | DC | 75 | 5,6,7 | 60 |  | 250 | Cauliflower | 38 | 171 | - | 139 |
| NiFeCoWP | Cu | Aq SO4 | DC | 30-100 | 5.5 | 50 | - | 0-100 | Globular | - | - | - | 140 |
| NiFeCoCr | Cu | Aq SO4 | DC | 250 | 2.5 | 24.85 | 30 | - | Globular | 5.2 | - | - | 11 |
| NiFeCoCr | Cu | Aq SO4 | DC | 150 - 350 | 1.5-3.5 | 20-60 | 60 | - | Globular | - | - | - | 141 |
| NiFeCoCr | Cu | Aq SO4 | DC | 25 | 1.5 | 30 | 30 | 200 | Colony | 8.6 | - | 295 | 142 |
| NiFeCoCrMn | Steel | Aq Cl | DC | 400 | 1.5 | 30 | 15 | 850 | Globular | - | - | - | 143 |
| NiFeCoCrMn-MoS2 | CC | Aq NO4 | CV | -1.2 - +0.2V | - | - | 30,90 | - | Globular | - | - | 210 | 144 |
| NiFeCoCrMn | Al | DMF:CH3CN Cl | V | 2.5V | - | 25 | - | - | Globular | 100 | - | - | 14 |
| NiFeCoCrMn | Cu | DMF:CH3CN Cl | PC | −2.0 V, −2.5 V, −3.0 V | - | 40 | 10 | - | Spherical particles | 0.5 - 1.5 | - | 295 | 145 |
| NiFeCoCrMn (oxide) | CF | Emul Cl | DC | -1.5V | - | - | 10 | - | Nanoparticles | NP size 0.002−0.05 | - | 185 | 146 |
| NiFeCoCrMn | Cu Foam | Aq Cl | DC | -1, -1.1, -1.2V | 3.5 | 28 | 10 | - | Ultrafine particles | - | 191 | - | 147 |
| NiCoCrMnFe | Ni Foam | Aq Cl |  | 5 | - | - | 60 | - | Globular |  |  | 317 h) | 148 |
| NiFeCoCrMn | Ni Foam | DM:CH3CN Cl | PC | -5V 0.5/0.5 | - | 45 | 20 | - | Nanoparticles | - | 168 | 231 | 149 |
| NiFeCoCrMnP | Ni Foam | Aq Cl,NO4 | DC | -2V | - | - | 7 | - | Nanosheets | - | 51 g) | 268 g) | 15 |
| NiFeCoCrCu | Steel | Aq Cl | DC | 40 | 1.5 | 30 | 15 | - | Granular | 3–5 | - | - | 150 |
| NiFeCoCrCu | Steel | Aq Cl | DC | 160 | 1.5 | 30 | 15 | 850 | Globular | - | - | - | 143 |
| NiFeCoCrCu | Ni Foam | Emul Cl | CV | +0.1 to -1.2 V | - | - | - | - | Nanoparticles | 1 | 102 | 235 | 151 |
| NiFeCoCrCu | CP | Aq Cl | DC | 1500 | - | 25 | 20s | - | Dendritic | - | 84 | - | 16 |
| NiFeCoCrCuP | SS | Aq Cl | DC | 2.8V | - | - | 3 | - | Dendritic | - | 423 h) | 365 h) | 17 |
| NiFeCoCrAl | Steel | Aq Cl | DC | 200 | 1.5 | 30 | 1 | 850 | Globular | - | - | - | 143 |
| NiFeCoMn | CP | Aq Cl | PC | 8000c 0.2/0.8 | 9.8 | 53 | 50 | - | Granular | - | 193 f) | 608 f) | 132 |
| NiFeCoMn | Ni Foam | Aq NO4 | DC | -1V | - | - | - | - | Nanosheets | - | - | 291 h) | 152 |
| NiFeCoMnCu | Cu foam | Aq SO4 | DC | -16V | - | 2 | 4 | - | Nanoparticles | 19.8 mg/cm2 | 190 h) | 260 h) | 153 |
| NiFeCoMnCu | Steel | Aq Cl | DC | 100 | 1.5 | 30 | 15 | 300 | Granular | - | - | - | 18 |
| NiFeCoMnCu | Cu | Aq. SO4 | DC | 3000 | 2 | - | 7 | - | Leaf/feather-like | - | 200h) | 251 h) | 154 |
| NiFeCoMnPO | Ni Foam | Aq SO4, NO4 | DC | -1.8V | 2 | - | 13 | - | Nanosheets | - | 43 | 252 | 155 |
| NiFeCoMnAl | CP | Emul CL | DC | -2.8 V | - | - | 30 | - | Globular | - | - | 190 | 156 |
| NiFeCoMnAl | Steel | Aq SO4, Cl | DC | 55 | 1.5 | 30 | 20 | 350 | Granular | 10 | - | - | 157 |
| NiFeCoMnV | Ni Foam | Aq SO4, Cl | DC | 50,100,150,200 | 6-7 | 25 | 60 | - | Raspberry-like | - | 7 | - | 158 |
| NiFeCoMnSn | Ni Foam | Aq SO4, Cl | DC | 200 | 5.4 | 10 | 30 | - | Cauliflower | - | 4.3 | - | 159 |
| NiFeCoCuZn | Ti | Aq SO4, Cl | PC | -1.5V | - | 25-55 | - | - | Granular | - | - | - | 160 |
| NiFeCoCuZn | Ti | Aq SO4 | PC | 1.5V | 0.5-4.5 | 22-55 | - | 0-500 | Globular | - | - | - | 161 |
| NiFeCoCuMo | Ni Foam | Aq Cl | PC | 4000c 0.2/0.8 | 9 | 50 | - | 300 | Cauliflower |  | 7 | 194 | 90 |
| NiFeCoMoZn | Ni Foam | Aq SO4 | PC | -2V 0.5/0.5 | - | 25 | 3000c |  | Nanosheets |  |  | 248 | 162 |
| NiFeCoMoCrOOH | CC/BiVO4 | Aq N | DC | -1V (5 cycles) | - | - | 10,15,20 | - | Filiform structures | 0.005 | - | 172 | 163 |
| NiFeCuMoMn | Fe | Aq SO4, Cl | DC | 50 | 5.5 | - | 30 | - | Cauliflower | - | 371 i) | - | 164 |
| FeCoMnCu(Ni) | Fe | Aq SO4 | DC | 10, 50, 100 | 6.5 |  | 60 | - | Cauliflower | - | - | 226 | 165 |
| NiFeCoCrMnMo CrCoFeNiCu | Cu | Aq SO4 | DC | 65 | 7 | 70 | - | 250 | Granular | 33 | - | - | 166 |
| a) CP - Carbon paper; CC - Carbon cloth; CF - Carbon fiber; SS - Stainless Steel; GC – Glassy carbon b) ‘Aq’ stands for aqueous electrolyte, ‘Emul’ (short for emulsion) refers to a mixture of organic and aqueous phases. Cl, SO4, and NO4 denote the salt precursor chlorides, sulfates, and nitrates, respectively. DMF – Dimethylformamide. c) DC - Direct current; PC - Pulse current; CV - Cyclic voltammetry d) When reporting PC, the first value specifies the number of cycles if it ends in "c," or the voltage if it ends in "V." The second value indicates the duration of the "on" and "off" times e) n10 - Overpotential calculated at 10mA f) Results reported for acid electrolyte conditions g) Hydrazine containing alkaline electrolyte h) Overpotential reported at 100mA (n100) i) natural seawater 153 |  |  |  |  |  |  |  |  |  |  |  |  |  |

# Supporting Information References

(1) Jia, Z.; Yang, T.; Sun, L.; Zhao, Y.; Li, W.; Luan, J.; Lyu, F.; Zhang, L. C.; Kruzic, J. J.; Kai, J. J. A novel multinary intermetallic as an active electrocatalyst for hydrogen evolution. Advanced Materials 2020, 32 (21), 2000385.

(2) He, Y.; Zhu, X.; Zhang, C.; Liu, Z.; Cao, B.; Sheng, L.; Yang, Y.; Feng, Q.; Wang, N.; Ou, J. Z. Self-circulating adsorption–desorption structure of non-noble high-entropy alloy electrocatalyst facilitates efficient water splitting. ACS Sustainable Chemistry & Engineering 2023, 11 (13), 5055-5064.

(3) Shi, H.; Sun, X.-Y.; Zeng, S.-P.; Liu, Y.; Han, G.-F.; Wang, T.-H.; Wen, Z.; Fang, Q.-R.; Lang, X.-Y.; Jiang, Q. Nanoporous nonprecious high‐entropy alloys as multisite electrocatalysts for ampere‐level current‐density hydrogen evolution. Small Structures 2023, 4 (9), 2300042.

(4) Yao, R. Q.; Zhou, Y. T.; Shi, H.; Wan, W. B.; Zhang, Q. H.; Gu, L.; Zhu, Y. F.; Wen, Z.; Lang, X. Y.; Jiang, Q. Nanoporous surface high‐entropy alloys as highly efficient multisite electrocatalysts for nonacidic hydrogen evolution reaction. Advanced Functional Materials 2021, 31 (10), 2009613.

(5) Liu, H.; Qin, H.; Kang, J.; Ma, L.; Chen, G.; Huang, Q.; Zhang, Z.; Liu, E.; Lu, H.; Li, J. A freestanding nanoporous NiCoFeMoMn high-entropy alloy as an efficient electrocatalyst for rapid water splitting. Chemical Engineering Journal 2022, 435, 134898.

(6) Lu, Y.; Huang, K.; Cao, X.; Zhang, L.; Wang, T.; Peng, D.; Zhang, B.; Liu, Z.; Wu, J.; Zhang, Y. Atomically dispersed intrinsic hollow sites of M‐M1‐M (M1= Pt, Ir; M= Fe, Co, Ni, Cu, Pt, Ir) on FeCoNiCuPtIr nanocrystals enabling rapid water redox. Advanced Functional Materials 2022, 32 (19), 2110645.

(7) Ma, P.; Zhao, M.; Zhang, L.; Wang, H.; Gu, J.; Sun, Y.; Ji, W.; Fu, Z. Self-supported high-entropy alloy electrocatalyst for highly efficient H2 evolution in acid condition. Journal of Materiomics 2020, 6 (4), 736-742.

(8) Lai, D.; Kang, Q.; Gao, F.; Lu, Q. High-entropy effect of a metal phosphide on enhanced overall water splitting performance. Journal of Materials Chemistry A 2021, 9 (33), 17913-17922.

(9) Zhang, G.; Ming, K.; Kang, J.; Huang, Q.; Zhang, Z.; Zheng, X.; Bi, X. High entropy alloy as a highly active and stable electrocatalyst for hydrogen evolution reaction. Electrochimica Acta 2018, 279, 19-23.

(10) Ding, J.; Inoue, A.; Han, Y.; Kong, F.; Zhu, S.; Wang, Z.; Shalaan, E.; Al-Marzouki, F. High entropy effect on structure and properties of (Fe, Co, Ni, Cr)-B amorphous alloys. Journal of Alloys and Compounds 2017, 696, 345-352.

(11) Xu, Z.; Wang, Y.; Gao, X.; Peng, L.; Qiao, Q.; Xiao, J.; Guo, F.; Wang, R.; Yu, J. Electrochemical Deposition and Corrosion Resistance Characterization of FeCoNiCr High-Entropy Alloy Coatings. Coatings 2023, 13 (7), 1167.

(12) Tian, H.; Yu, Y.; Wang, X.; Chen, F.; Liu, H. Preparation of CrCoFeNiMn High-Entropy Alloy Coatings Using Gas Atomization and Laser Cladding: An Investigation of Microstructure, Mechanical Properties, and Wear Resistance. Coatings 2024, 14 (7), 906.

(13) Cao, W.; Yang, X.; Dai, W.; Wu, B.; Zhang, Y.; Zhao, C.; Sui, Y.; Huang, S. An amorphous FeCoNiMnCr high-entropy alloy supported by 2H-MoS 2 on carbon cloth as a highly efficient and robust electrocatalyst for water oxidation. New Journal of Chemistry 2023, 47 (27), 12670-12677.

(14) Popescu, A.-M. J.; Branzoi, F.; Burada, M.; Moreno, J. C.; Anastasescu, M.; Anasiei, I.; Olaru, M. T.; Constantin, V. CoCrFeMnNi High-Entropy Alloy Thin Films Electrodeposited on Aluminum Support. Coatings 2023, 13 (6), 980.

(15) Li, K.; He, J.; Guan, X.; Tong, Y.; Ye, Y.; Chen, L.; Chen, P. Phosphorus‐Modified Amorphous High‐Entropy CoFeNiCrMn Compound as High‐Performance Electrocatalyst for Hydrazine‐Assisted Water Electrolysis. Small 2023, 19 (42), 2302130.

(16) Wang, Y.; Yang, H.; Zhang, Z.; Meng, X.; Cheng, T.; Qin, G.; Li, S. Far-from-equilibrium electrosynthesis ramifies high-entropy alloy for alkaline hydrogen evolution. Journal of Materials Science & Technology 2023, 166, 234-240.

(17) Zhang, T.; Li, J.; Zhang, B.; Wang, G.; Jiang, K.; Zheng, Z.; Shen, J. High-entropy alloy CuCrFeNiCoP film of Cu-based as high-efficiency electrocatalyst for water splitting. Journal of Alloys and Compounds 2023, 969, 172439.

(18) Aliyu, A.; Srivastava, C. Phase constitution, surface chemistry and corrosion behavior of electrodeposited MnFeCoNiCu high entropy alloy-graphene oxide composite coatings. Surface and Coatings Technology 2022, 429, 127943.

(19) Wang, S.; Xu, B.; Huo, W.; Feng, H.; Zhou, X.; Fang, F.; Xie, Z.; Shang, J. K.; Jiang, J. Efficient FeCoNiCuPd thin-film electrocatalyst for alkaline oxygen and hydrogen evolution reactions. Applied Catalysis B: Environmental 2022, 313, 121472.

(20) Božiček, B. L.; Arah, B.; Kušter, M.; Naglič, I.; Markoli, B.; Ponikvar-Svet, M.; Einfalt, L.; Čeh, M.; Marinho, B. A. Electrocatalytic trends of different Cantor entropy alloys for alkaline and acidic hydrogen-evolution reactions. Materials Today Communications 2024, 41, 110876.

(21) Charnetskaya, E.; Chatti, M.; Kerr, B. V.; Tran-Phu, T.; Nguyen, T. D.; Cherepanov, P. V.; Hoogeveen, D. A.; Johannessen, B.; Tricoli, A.; MacFarlane, D. R. Intrinsic catalytic activity for the alkaline hydrogen evolution of layer-expanded MoS2 functionalized with nanoscale Ni and Co sulfides. ACS Sustainable Chemistry & Engineering 2022, 10 (21), 7117-7133.

(22) Kou, T.; Smart, T.; Yao, B.; Chen, I.; Thota, D.; Ping, Y.; Li, Y. Theoretical and experimental insight into the effect of nitrogen doping on hydrogen evolution activity of Ni3S2 in alkaline medium. Advanced Energy Materials 2018, 8 (19), 1703538.

(23) Man, H.-W.; Tsang, C.-S.; Li, M. M.-J.; Mo, J.; Huang, B.; Lee, L. Y. S.; Leung, Y.-c.; Wong, K.-Y.; Tsang, S. C. E. Transition metal-doped nickel phosphide nanoparticles as electro-and photocatalysts for hydrogen generation reactions. Applied Catalysis B: Environmental 2019, 242, 186-193.

(24) Pawar, S.; Aqueel Ahmed, A. T.; Lee, C. H.; Babar, P. T.; Kim, J.; Lee, S. U.; Kim, H.; Im, H. Experimental and theoretical insights into transition-metal (Mo, Fe) codoping in a bifunctional nickel phosphide microsphere catalyst for enhanced overall water splitting. ACS Applied Energy Materials 2021, 4 (12), 14169-14179.

(25) Chen, C. H.; Wu, D.; Li, Z.; Zhang, R.; Kuai, C. G.; Zhao, X. R.; Dong, C. K.; Qiao, S. Z.; Liu, H.; Du, X. W. Ruthenium‐based single‐atom alloy with high electrocatalytic activity for hydrogen evolution. Advanced Energy Materials 2019, 9 (20), 1803913.

(26) Huang, F.; Wang, J.; Wang, M.; Zhang, C.; Xue, Y.; Liu, J.; Xu, T.; Cai, N.; Chen, W.; Yu, F. Core-shell Ni2P@ CoP nanoarrays supported on NF as a highly efficient electrocatalyst for hydrogen evolution reaction. Colloids and Surfaces A: Physicochemical and Engineering Aspects 2021, 623, 126526.

(27) Zhang, R.; Zhu, R.; Li, Y.; Hui, Z.; Song, Y.; Cheng, Y.; Lu, J. CoP and Ni 2 P implanted in a hollow porous N-doped carbon polyhedron for pH universal hydrogen evolution reaction and alkaline overall water splitting. Nanoscale 2020, 12 (46), 23851-23858.

(28) Guo, M.; Qiu, F.; Yuan, Y.; Yu, T.; Yuan, C.; Lu, Z.-H. Active Site Engineering in CoP@NC/Graphene Heterostructures Enabling Enhanced Hydrogen Evolution. Inorganic Chemistry 2021, 60 (21), 16761-16768.

(29) Wang, P.; Qin, R.; Ji, P.; Pu, Z.; Zhu, J.; Lin, C.; Zhao, Y.; Tang, H.; Li, W.; Mu, S. Synergistic coupling of Ni nanoparticles with Ni3C nanosheets for highly efficient overall water splitting. Small 2020, 16 (37), 2001642.

(30) Chen, Z.; Song, Y.; Cai, J.; Zheng, X.; Han, D.; Wu, Y.; Zang, Y.; Niu, S.; Liu, Y.; Zhu, J. Tailoring the d‐band centers enables Co4N nanosheets to be highly active for hydrogen evolution catalysis. Angewandte Chemie International Edition 2018, 57 (18), 5076-5080.

(31) Guo, H.; Wu, A.; Xie, Y.; Yan, H.; Wang, D.; Wang, L.; Tian, C. 2D porous molybdenum nitride/cobalt nitride heterojunction nanosheets with interfacial electron redistribution for effective electrocatalytic overall water splitting. Journal of Materials Chemistry A 2021, 9 (13), 8620-8629.

(32) Song, F.; Li, W.; Yang, J.; Han, G.; Liao, P.; Sun, Y. Interfacing nickel nitride and nickel boosts both electrocatalytic hydrogen evolution and oxidation reactions. Nature communications 2018, 9 (1), 4531.

(33) Zhang, T.; Wu, M.-Y.; Yan, D.-Y.; Mao, J.; Liu, H.; Hu, W.-B.; Du, X.-W.; Ling, T.; Qiao, S.-Z. Engineering oxygen vacancy on NiO nanorod arrays for alkaline hydrogen evolution. Nano Energy 2018, 43, 103-109.

(34) Yuan, Z.; Yao, X.; Zhang, G.; Fu, N.; Liu, Y.; Ye, F. Regulating the heterostructure of metal/oxide toward the enhanced hydrogen evolution reaction. ACS Applied Energy Materials 2022, 5 (5), 5644-5651.

(35) Huang, B.; Hu, X.; Liu, Y.; Qi, W.; Xie, Z. Biomolecule-derived N/S co-doped CNT-graphene hybrids exhibiting excellent electrochemical activities. Journal of Power Sources 2019, 413, 408-417.

(36) Li, Y.; Luo, Y.; Zhang, Z.; Yu, Q.; Li, C.; Zhang, Q.; Zheng, Z.; Liu, H.; Liu, B.; Dou, S. Implanting Ru nanoclusters into N-doped graphene for efficient alkaline hydrogen evolution. Carbon 2021, 183, 362-367.

(37) Zhao, M.; Zhang, J.; Xiao, H.; Hu, T.; Jia, J.; Wu, H. Facile in situ synthesis of a carbon quantum dot/graphene heterostructure as an efficient metal-free electrocatalyst for overall water splitting. Chemical communications 2019, 55 (11), 1635-1638.

(38) Zhang, X.; Li, Y.; Guo, Y.; Hu, A.; Li, M.; Hang, T.; Ling, H. 3D hierarchical nanostructured Ni–Co alloy electrodes on porous nickel for hydrogen evolution reaction. International Journal of Hydrogen Energy 2019, 44 (57), 29946-29955.

(39) Cao, J.; Li, H.; Pu, J.; Zeng, S.; Liu, L.; Zhang, L.; Luo, F.; Ma, L.; Zhou, K.; Wei, Q. Hierarchical NiMo alloy microtubes on nickel foam as an efficient electrocatalyst for hydrogen evolution reaction. International Journal of Hydrogen Energy 2019, 44 (45), 24712-24718.

(40) Liu, X.; Niu, J.; Rajendran, S.; Lei, Y.; Qin, J.; Zhang, X. Electrodeposition of the manganese-doped nickel-phosphorus catalyst with enhanced hydrogen evolution reaction activity and durability. International Journal of Hydrogen Energy 2022, 47 (100), 41994-42000.

(41) Ge, Y.; Chen, J.; Chu, H.; Dong, P.; Craig, S. R.; Ajayan, P. M.; Ye, M.; Shen, J. Urchin-like CoP with controlled manganese doping toward efficient hydrogen evolution reaction in both acid and alkaline solution. ACS Sustainable Chemistry & Engineering 2018, 6 (11), 15162-15169.

(42) Wang, H.; Ma, N.; Cao, Y.; Yu, H.; Zuo, J.; Fan, W.; Peng, F. Cobalt and cobalt oxide supported on nitrogen-doped porous carbon as electrode materials for hydrogen evolution reaction. International Journal of Hydrogen Energy 2019, 44 (7), 3649-3657.

(43) Guan, J.; Liu, Y.; Fang, Y.; Du, X.; Fu, Y.; Wang, L.; Zhang, M. Co-Ni alloy nanoparticles supported by carbon nanofibers for hydrogen evolution reaction. Journal of Alloys and Compounds 2021, 868, 159172.

(44) Hauch, A.; Ebbesen, S. D.; Jensen, S. H.; Mogensen, M. Highly efficient high temperature electrolysis. Journal of Materials Chemistry 2008, 18 (20), 2331-2340.

(45) Eftekhari, A. Electrocatalysts for hydrogen evolution reaction. International Journal of Hydrogen Energy 2017, 42 (16), 11053-11077.

(46) Koper, M. T. Thermodynamic theory of multi-electron transfer reactions: Implications for electrocatalysis. Journal of Electroanalytical Chemistry 2011, 660 (2), 254-260.

(47) Bhattacharjee, S.; Waghmare, U. V.; Lee, S.-C. An improved d-band model of the catalytic activity of magnetic transition metal surfaces. Scientific reports 2016, 6 (1), 35916.

(48) Conway, B.; Tilak, B. Interfacial processes involving electrocatalytic evolution and oxidation of H2, and the role of chemisorbed H. Electrochimica acta 2002, 47 (22-23), 3571-3594.

(49) Pletcher, D.; Li, X. Prospects for alkaline zero gap water electrolysers for hydrogen production. International Journal of Hydrogen Energy 2011, 36 (23), 15089-15104.

(50) Nakamura, M.; Kobayashi, T.; Hoshi, N. Structural dependence of intermediate species for the hydrogen evolution reaction on single crystal electrodes of Pt. Surface science 2011, 605 (15-16), 1462-1465.

(51) Gao, W.; Shi, Y.; Zhang, Y.; Zuo, L.; Lu, H.; Huang, Y.; Fan, W.; Liu, T. Molybdenum carbide anchored on graphene nanoribbons as highly efficient all-pH hydrogen evolution reaction electrocatalyst. ACS Sustainable Chemistry & Engineering 2016, 4 (12), 6313-6321.

(52) Lin, H.; Shi, Z.; He, S.; Yu, X.; Wang, S.; Gao, Q.; Tang, Y. Heteronanowires of MoC–Mo 2 C as efficient electrocatalysts for hydrogen evolution reaction. Chemical Science 2016, 7 (5), 3399-3405.

(53) Wu, H. B.; Xia, B. Y.; Yu, L.; Yu, X.-Y.; Lou, X. W. Porous molybdenum carbide nano-octahedrons synthesized via confined carburization in metal-organic frameworks for efficient hydrogen production. Nature communications 2015, 6 (1), 6512.

(54) Shi, Z.; Wang, Y.; Lin, H.; Zhang, H.; Shen, M.; Xie, S.; Zhang, Y.; Gao, Q.; Tang, Y. Porous nanoMoC@ graphite shell derived from a MOFs-directed strategy: an efficient electrocatalyst for the hydrogen evolution reaction. Journal of Materials Chemistry A 2016, 4 (16), 6006-6013.

(55) Balasubramanian, R.; Abishek, A.; Gobinath, S.; Jaivignesh, K. Alternative fuel: hydrogen and its thermodynamic behaviour. Journal of Human, Earth, and Future 2022, 3 (2), 195-203.

(56) Lee, J. E.; Jeon, K.-J.; Show, P. L.; Jung, S.-C.; Choi, Y. J.; Rhee, G. H.; Lin, K.-Y. A.; Park, Y.-K. Mini review on H2 production from electrochemical water splitting according to special nanostructured morphology of electrocatalysts. Fuel 2022, 308, 122048.

(57) Yan, F.; Wang, Y.; Li, K.; Zhu, C.; Gao, P.; Li, C.; Zhang, X.; Chen, Y. Highly Stable Three‐Dimensional Porous Nickel‐Iron Nitride Nanosheets for Full Water Splitting at High Current Densities. Chemistry–A European Journal 2017, 23 (42), 10187-10194.

(58) Babar, N.-U.-A.; Joya, Y. F.; Khalil, H.; Hussain, F.; Joya, K. S. Thin-film iron-oxide nanobeads as bifunctional electrocatalyst for high activity overall water splitting. International Journal of Hydrogen Energy 2021, 46 (11), 7885-7902.

(59) Li, C.; Baek, J.-B. Recent advances in noble metal (Pt, Ru, and Ir)-based electrocatalysts for efficient hydrogen evolution reaction. ACS omega 2019, 5 (1), 31-40.

(60) Luo, Y.; Li, X.; Cai, X.; Zou, X.; Kang, F.; Cheng, H.-M.; Liu, B. Two-dimensional MoS2 confined Co (OH) 2 electrocatalysts for hydrogen evolution in alkaline electrolytes. ACS nano 2018, 12 (5), 4565-4573.

(61) Feng, Y.; Yu, X.-Y.; Paik, U. Nickel cobalt phosphides quasi-hollow nanocubes as an efficient electrocatalyst for hydrogen evolution in alkaline solution. Chemical Communications 2016, 52 (8), 1633-1636.

(62) Zhou, P.; Zhai, G.; Lv, X.; Liu, Y.; Wang, Z.; Wang, P.; Zheng, Z.; Cheng, H.; Dai, Y.; Huang, B. Boosting the electrocatalytic HER performance of Ni3N-V2O3 via the interface coupling effect. Applied Catalysis B: Environmental 2021, 283, 119590.

(63) Wang, J.; Xin, S.; Xiao, Y.; Zhang, Z.; Li, Z.; Zhang, W.; Li, C.; Bao, R.; Peng, J.; Yi, J. Manipulating the water dissociation electrocatalytic sites of bimetallic nickel‐based alloys for highly efficient alkaline hydrogen evolution. Angewandte Chemie International Edition 2022, 61 (30), e202202518.

(64) Sun, H.; Yao, B.; Han, Y.; Yang, L.; Zhao, Y.; Wang, S.; Zhong, C.; Chen, J.; Li, C. P.; Du, M. Multi‐Interface Engineering of Self‐Supported Nickel/Yttrium Oxide Electrode Enables Kinetically Accelerated and Ultra‐Stable Alkaline Hydrogen Evolution at Industrial‐Level Current Density. Advanced Energy Materials 2024, 14 (11), 2303563.

(65) Chen, W.; Gu, J.; Du, Y.; Song, F.; Bu, F.; Li, J.; Yuan, Y.; Luo, R.; Liu, Q.; Zhang, D. Achieving rich and active alkaline hydrogen evolution heterostructures via interface engineering on 2D 1T‐MoS2 quantum sheets. Advanced Functional Materials 2020, 30 (25), 2000551.

(66) Dong, Z.; Lin, F.; Yao, Y.; Jiao, L. Crystalline Ni (OH) 2/amorphous NiMoOx mixed‐catalyst with Pt‐like performance for hydrogen production. Advanced Energy Materials 2019, 9 (46), 1902703.

(67) Peng, L.; Liao, M.; Zheng, X.; Nie, Y.; Zhang, L.; Wang, M.; Xiang, R.; Wang, J.; Li, L.; Wei, Z. Accelerated alkaline hydrogen evolution on M (OH) x/M-MoPO x (M= Ni, Co, Fe, Mn) electrocatalysts by coupling water dissociation and hydrogen ad-desorption steps. Chemical science 2020, 11 (9), 2487-2493.

(68) Huang, J.; Han, J.; Wu, T.; Feng, K.; Yao, T.; Wang, X.; Liu, S.; Zhong, J.; Zhang, Z.; Zhang, Y. Boosting hydrogen transfer during volmer reaction at oxides/metal nanocomposites for efficient alkaline hydrogen evolution. ACS Energy Letters 2019, 4 (12), 3002-3010.

(69) Lu, K.; Liu, Y.; Lin, F.; Cordova, I. A.; Gao, S.; Li, B.; Peng, B.; Xu, H.; Kaelin, J.; Coliz, D. Li x NiO/Ni heterostructure with strong basic lattice oxygen enables electrocatalytic hydrogen evolution with Pt-like activity. Journal of the American Chemical Society 2020, 142 (29), 12613-12619.

(70) Zhang, T.; Yang, K.; Wang, C.; Li, S.; Zhang, Q.; Chang, X.; Li, J.; Li, S.; Jia, S.; Wang, J. Electrocatalysts: Nanometric Ni5P4 Clusters Nested on NiCo2O4 for Efficient Hydrogen Production via Alkaline Water Electrolysis (Adv. Energy Mater. 29/2018). Advanced Energy Materials 2018, 8 (29), 1870129.

(71) Zhang, B.; Zhang, L.; Tan, Q.; Wang, J.; Liu, J.; Wan, H.; Miao, L.; Jiang, J. Simultaneous interfacial chemistry and inner Helmholtz plane regulation for superior alkaline hydrogen evolution. Energy & Environmental Science 2020, 13 (9), 3007-3013.

(72) Feng, J.-X.; Wu, J.-Q.; Tong, Y.-X.; Li, G.-R. Efficient hydrogen evolution on Cu nanodots-decorated Ni3S2 nanotubes by optimizing atomic hydrogen adsorption and desorption. Journal of the American Chemical Society 2018, 140 (2), 610-617.

(73) Zhang, R.; Ren, X.; Hao, S.; Ge, R.; Liu, Z.; Asiri, A. M.; Chen, L.; Zhang, Q.; Sun, X. Selective phosphidation: an effective strategy toward CoP/CeO 2 interface engineering for superior alkaline hydrogen evolution electrocatalysis. Journal of Materials Chemistry A 2018, 6 (5), 1985-1990.

(74) Sun, H.; Tian, C.; Fan, G.; Qi, J.; Liu, Z.; Yan, Z.; Cheng, F.; Chen, J.; Li, C. P.; Du, M. Hybrid Nanosheet Arrays: Boosting Activity on Co4N Porous Nanosheet by Coupling CeO2 for Efficient Electrochemical Overall Water Splitting at High Current Densities (Adv. Funct. Mater. 32/2020). Advanced Functional Materials 2020, 30 (32), 2070213.

(75) Sun, H.; Tian, C.; Li, Y.; Wu, J.; Wang, Q.; Yan, Z.; Li, C. P.; Cheng, F.; Du, M. Coupling NiCo alloy and CeO2 to enhance electrocatalytic hydrogen evolution in alkaline solution. Advanced Sustainable Systems 2020, 4 (11), 2000122.

(76) Yang, L.; Liu, R.; Jiao, L. Electronic redistribution: construction and modulation of interface engineering on CoP for enhancing overall water splitting. Advanced Functional Materials 2020, 30 (14), 1909618.

(77) Zhang, L.; Liu, P. F.; Li, Y. H.; Wang, C. W.; Zu, M. Y.; Fu, H. Q.; Yang, X. H.; Yang, H. G. Accelerating neutral hydrogen evolution with tungsten modulated amorphous metal hydroxides. ACS Catalysis 2018, 8 (6), 5200-5205.

(78) Tourneur, J.; Lagrost, C.; Fabre, B. Robust and bifunctional electrodeposited NiCoCr ternary alloy for alkaline water electrolysis. Advanced Energy and Sustainability Research 2024, 5 (2), 2300133.

(79) Feng, L.; Vrubel, H.; Bensimon, M.; Hu, X. Easily-prepared dinickel phosphide (Ni 2 P) nanoparticles as an efficient and robust electrocatalyst for hydrogen evolution. Physical Chemistry Chemical Physics 2014, 16 (13), 5917-5921.

(80) Xu, R.; Wu, R.; Shi, Y.; Zhang, J.; Zhang, B. Ni3Se2 nanoforest/Ni foam as a hydrophilic, metallic, and self-supported bifunctional electrocatalyst for both H2 and O2 generations. Nano Energy 2016, 24, 103-110.

(81) Darband, G. B.; Aliofkhazraei, M.; Rouhaghdam, A. S.; Kiani, M. Three-dimensional Ni-Co alloy hierarchical nanostructure as efficient non-noble-metal electrocatalyst for hydrogen evolution reaction. Applied Surface Science 2019, 465, 846-862.

(82) Yan, X.; Li, K.; Lyu, L.; Song, F.; He, J.; Niu, D.; Liu, L.; Hu, X.; Chen, X. From Water Oxidation to Reduction: Transformation from Ni x Co3–x O4 Nanowires to NiCo/NiCoO x Heterostructures. ACS applied materials & interfaces 2016, 8 (5), 3208-3214.

(83) Yan, X.; Tian, L.; He, M.; Chen, X. Three-dimensional crystalline/amorphous Co/Co3O4 core/shell nanosheets as efficient electrocatalysts for the hydrogen evolution reaction. Nano letters 2015, 15 (9), 6015-6021.

(84) Yan, X.; Tian, L.; Chen, X. Crystalline/amorphous Ni/NiO core/shell nanosheets as highly active electrocatalysts for hydrogen evolution reaction. Journal of Power Sources 2015, 300, 336-343.

(85) Zhang, B.; Liu, J.; Wang, J.; Ruan, Y.; Ji, X.; Xu, K.; Chen, C.; Wan, H.; Miao, L.; Jiang, J. Interface engineering: The Ni (OH) 2/MoS2 heterostructure for highly efficient alkaline hydrogen evolution. Nano Energy 2017, 37, 74-80.

(86) Yan, X.; Tian, L.; Li, K.; Atkins, S.; Zhao, H.; Murowchick, J.; Liu, L.; Chen, X. FeNi3/NiFeOx nanohybrids as highly efficient bifunctional electrocatalysts for overall water splitting. Advanced Materials Interfaces 2016, 3 (22), 1600368.

(87) Wang, X.; Yang, C.; Zhang, Y.; Xiong, D.; Xu, S.; Wang, L.; Jiang, L.; Sorokin, P. B.; Chu, P. K. Medium-entropy alloy MoCoCu-P as an efficient bifunctional catalyst for water splitting. Journal of Alloys and Compounds 2024, 988, 174332.

(88) Ahmad, S.; Egilmez, M.; Abuzaid, W.; Mustafa, F.; Kannan, A. M.; Alnaser, A. S. Efficient medium entropy alloy thin films as bifunctional electrodes for electrocatalytic water splitting. International Journal of Hydrogen Energy 2024, 52, 1428-1439.

(89) Abdin, Z.; Zafaranloo, A.; Rafiee, A.; Mérida, W.; Lipiński, W.; Khalilpour, K. R. Hydrogen as an energy vector. Renewable and sustainable energy reviews 2020, 120, 109620.

(90) Huang, C.-L.; Lin, Y.-G.; Chiang, C.-L.; Peng, C.-K.; Raja, D. S.; Hsieh, C.-T.; Chen, Y.-A.; Chang, S.-Q.; Yeh, Y.-X.; Lu, S.-Y. Atomic scale synergistic interactions lead to breakthrough catalysts for electrocatalytic water splitting. Applied Catalysis B: Environmental 2023, 320, 122016.

(91) Li, D.; Liu, H.; Feng, L. A review on advanced FeNi-based catalysts for water splitting reaction. Energy & Fuels 2020, 34 (11), 13491-13522.

(92) Karumuthil, S. C.; Singh, A. K.; Prasad, B. L. Electrodeposited Co–Mn–Sn multicomponent alloy as an efficient electrocatalyst for hydrogen evolution reaction. International Journal of Hydrogen Energy 2024, 49, 658-667.

(93) Hu, J.; Zhang, C.; Yang, P.; Xiao, J.; Deng, T.; Liu, Z.; Huang, B.; Leung, M. K.; Yang, S. Kinetic‐Oriented Construction of MoS2 Synergistic Interface to Boost pH‐Universal Hydrogen Evolution. Advanced Functional Materials 2020, 30 (6), 1908520.

(94) Pan, Y.; Gao, J.; Lv, E.; Li, T.; Xu, H.; Sun, L.; Nairan, A.; Zhang, Q. Integration of Alloy Segregation and Surface Co O Hybridization in Carbon‐Encapsulated CoNiPt Alloy Catalyst for Superior Alkaline Hydrogen Evolution. Advanced Functional Materials 2023, 33 (41), 2303833.

(95) Darband, G. B.; Aliofkhazraei, M.; Rouhaghdam, A. S. Facile electrodeposition of ternary Ni-Fe-Co alloy nanostructure as a binder free, cost-effective and durable electrocatalyst for high-performance overall water splitting. Journal of colloid and interface science 2019, 547, 407-420.

(96) Li, J.; Yan, M.; Zhou, X.; Huang, Z. Q.; Xia, Z.; Chang, C. R.; Ma, Y.; Qu, Y. Mechanistic insights on ternary Ni2− xCoxP for hydrogen evolution and their hybrids with graphene as highly efficient and robust catalysts for overall water splitting. Advanced Functional Materials 2016, 26 (37), 6785-6796.

(97) Baibars, I. O.; Abd El-Moghny, M. G.; Mogoda, A. S.; El-Deab, M. S. Microporous film of ternary Ni/Co/Fe alloy for superior electrolytic hydrogen production in alkaline medium. Journal of the Electrochemical Society 2021, 168 (5), 054509.

(98) Jafarian, M.; Azizi, O.; Gobal, F.; Mahjani, M. Kinetics and electrocatalytic behavior of nanocrystalline CoNiFe alloy in hydrogen evolution reaction. International Journal of Hydrogen Energy 2007, 32 (12), 1686-1693.

(99) Liu, T.; Sun, X.; Asiri, A. M.; He, Y. One-step electrodeposition of Ni–Co–S nanosheets film as a bifunctional electrocatalyst for efficient water splitting. International Journal of Hydrogen Energy 2016, 41 (18), 7264-7269.

(100) Tang, C.; Zhang, R.; Lu, W.; He, L.; Jiang, X.; Asiri, A. M.; Sun, X. Fe‐doped CoP nanoarray: a monolithic multifunctional catalyst for highly efficient hydrogen generation. Advanced materials 2017, 29 (2), 1602441.

(101) Tsounis, C.; Subhash, B.; Kumar, P. V.; Bedford, N. M.; Zhao, Y.; Shenoy, J.; Ma, Z.; Zhang, D.; Toe, C. Y.; Cheong, S. Pt single atom electrocatalysts at graphene edges for efficient alkaline hydrogen evolution. Advanced Functional Materials 2022, 32 (38), 2203067.

(102) Li, Z.; Yang, Y.; Wang, S.; Gu, L.; Shao, S. High-density ruthenium single atoms anchored on oxygen-vacancy-rich g-C3N4-C-TiO2 heterostructural nanosphere for efficient electrocatalytic hydrogen evolution reaction. ACS Applied Materials & Interfaces 2021, 13 (39), 46608-46619.

(103) Li, C.-F.; Zhao, J.-W.; Xie, L.-J.; Wang, Y.; Tang, H.-B.; Zheng, L.-R.; Li, G.-R. N coupling with S-coordinated Ru nanoclusters for highly efficient hydrogen evolution in alkaline media. Journal of Materials Chemistry A 2021, 9 (21), 12659-12669.

(104) Hu, M.; Chen, Q.; Ding, R.; Wu, J.; Wang, Y.; Zhang, Y.; Fan, G. Spatially localized fabrication of uniform Rh nanoclusters on nanosheet-assembled hierarchical carbon architectures as excellent electrocatalysts for boosting alkaline hydrogen evolution. International Journal of Hydrogen Energy 2020, 45 (15), 8118-8125.

(105) Xiao, X.; Wang, X.; Jiang, X.; Song, S.; Huang, D.; Yu, L.; Zhang, Y.; Chen, S.; Wang, M.; Shen, Y. In situ growth of Ru nanoparticles on (Fe, Ni)(OH) 2 to boost hydrogen evolution activity at high current density in alkaline media. Small Methods 2020, 4 (6), 1900796.

(106) Qiu, Y.; Wen, Z.; Jiang, C.; Wu, X.; Si, R.; Bao, J.; Zhang, Q.; Gu, L.; Tang, J.; Guo, X. Rational design of atomic layers of Pt anchored on Mo2C nanorods for efficient hydrogen evolution over a wide pH range. Small 2019, 15 (14), 1900014.

(107) Anantharaj, S.; Karthick, K.; Venkatesh, M.; Simha, T. V.; Salunke, A. S.; Ma, L.; Liang, H.; Kundu, S. Enhancing electrocatalytic total water splitting at few layer Pt-NiFe layered double hydroxide interfaces. Nano Energy 2017, 39, 30-43.

(108) Panda, C.; Menezes, P. W.; Yao, S.; Schmidt, J.; Walter, C.; Hausmann, J. N.; Driess, M. Boosting electrocatalytic hydrogen evolution activity with a NiPt3@ NiS heteronanostructure evolved from a molecular nickel–platinum precursor. Journal of the American Chemical Society 2019, 141 (34), 13306-13310.

(109) Lao, M.; Rui, K.; Zhao, G.; Cui, P.; Zheng, X.; Dou, S. X.; Sun, W. Platinum/nickel bicarbonate heterostructures towards accelerated hydrogen evolution under alkaline conditions. Angewandte Chemie 2019, 131 (16), 5486-5491.

(110) He, Q.; Tian, D.; Jiang, H.; Cao, D.; Wei, S.; Liu, D.; Song, P.; Lin, Y.; Song, L. Achieving efficient alkaline hydrogen evolution reaction over a Ni5P4 catalyst incorporating single‐atomic Ru sites. Advanced Materials 2020, 32 (11), 1906972.

(111) Jiang, X.; Jang, H.; Liu, S.; Li, Z.; Kim, M. G.; Li, C.; Qin, Q.; Liu, X.; Cho, J. The heterostructure of Ru2P/WO3/NPC synergistically promotes H2O dissociation for improved hydrogen evolution. Angewandte Chemie 2021, 133 (8), 4156-4162.

(112) Li, W.; Zhao, Y.; Liu, Y.; Sun, M.; Waterhouse, G. I.; Huang, B.; Zhang, K.; Zhang, T.; Lu, S. Exploiting Ru‐induced lattice strain in CoRu nanoalloys for robust bifunctional hydrogen production. Angewandte Chemie 2021, 133 (6), 3327-3335.

(113) Tan, H.; Tang, B.; Lu, Y.; Ji, Q.; Lv, L.; Duan, H.; Li, N.; Wang, Y.; Feng, S.; Li, Z. Engineering a local acid-like environment in alkaline medium for efficient hydrogen evolution reaction. Nature Communications 2022, 13 (1), 2024.

(114) Yu, H.; Hu, M.; Chen, C.; Hu, C.; Li, Q.; Hu, F.; Peng, S.; Ma, J. Ambient γ‐Rays‐Mediated Noble‐Metal Deposition on Defect‐Rich Manganese Oxide for Glycerol‐Assisted H2 Evolution at Industrial‐Level Current Density. Angewandte Chemie International Edition 2023, 62 (52), e202314569.

(115) Zhu, Y.; Fan, K.; Hsu, C. S.; Chen, G.; Chen, C.; Liu, T.; Lin, Z.; She, S.; Li, L.; Zhou, H. Supported ruthenium single‐atom and clustered catalysts outperform benchmark Pt for alkaline hydrogen evolution. Advanced Materials 2023, 35 (35), 2301133.

(116) Li, J.; Zhang, C.; Zhang, T.; Shen, Z.; Zhou, Q.; Pu, J.; Ma, H.; Wang, T.; Zhang, H.; Fan, H. Multiple-interface relay catalysis: enhancing alkaline hydrogen evolution through a combination of Volmer promoter and electrical-behavior regulation. Chemical Engineering Journal 2020, 397, 125457.

(117) Li, Y.; Pei, W.; He, J.; Liu, K.; Qi, W.; Gao, X.; Zhou, S.; Xie, H.; Yin, K.; Gao, Y. Hybrids of PtRu nanoclusters and black phosphorus nanosheets for highly efficient alkaline hydrogen evolution reaction. ACS Catalysis 2019, 9 (12), 10870-10875.

(118) Zhang, D.; Zhao, H.; Huang, B.; Li, B.; Li, H.; Han, Y.; Wang, Z.; Wu, X.; Pan, Y.; Sun, Y. Advanced ultrathin RuPdM (M= Ni, Co, Fe) nanosheets electrocatalyst boosts hydrogen evolution. ACS central science 2019, 5 (12), 1991-1997.

(119) Wang, Y.; Chen, L.; Yu, X.; Wang, Y.; Zheng, G. Superb alkaline hydrogen evolution and simultaneous electricity generation by pt‐decorated Ni3N nanosheets. Advanced Energy Materials 2017, 7 (2), 1601390.

(120) Shen, Y.; Lua, A. C.; Xi, J.; Qiu, X. Ternary platinum–copper–nickel nanoparticles anchored to hierarchical carbon supports as free-standing hydrogen evolution electrodes. ACS Applied Materials & Interfaces 2016, 8 (5), 3464-3472.

(121) Xing, Z.; Han, C.; Wang, D.; Li, Q.; Yang, X. Ultrafine Pt nanoparticle-decorated Co (OH) 2 nanosheet arrays with enhanced catalytic activity toward hydrogen evolution. ACS Catalysis 2017, 7 (10), 7131-7135.

(122) Liu, M.; Zhang, Z.; Okejiri, F.; Yang, S.; Zhou, S.; Dai, S. Entropy‐maximized synthesis of multimetallic nanoparticle catalysts via a ultrasonication‐assisted wet chemistry method under ambient conditions. Advanced Materials Interfaces 2019, 6 (7), 1900015.

(123) Zhang, D.; Shi, Y.; Zhao, H.; Qi, W.; Chen, X.; Zhan, T.; Li, S.; Yang, B.; Sun, M.; Lai, J. The facile oil-phase synthesis of a multi-site synergistic high-entropy alloy to promote the alkaline hydrogen evolution reaction. Journal of Materials Chemistry A 2021, 9 (2), 889-893.

(124) Schneider, R.; Klooster, K. v. t.; Picard, K. L.; van der Gucht, J.; Demura, T.; Janson, M.; Sampathkumar, A.; Deinum, E. E.; Ketelaar, T.; Persson, S. Long-term single-cell imaging and simulations of microtubules reveal principles behind wall patterning during proto-xylem development. Nature communications 2021, 12 (1), 669.

(125) Zhao, X.; Xue, Z.; Chen, W.; Wang, Y.; Mu, T. Eutectic synthesis of high‐entropy metal phosphides for electrocatalytic water splitting. ChemSusChem 2020, 13 (8), 2038-2042.

(126) Li, H.; Han, Y.; Zhao, H.; Qi, W.; Zhang, D.; Yu, Y.; Cai, W.; Li, S.; Lai, J.; Huang, B. Fast site-to-site electron transfer of high-entropy alloy nanocatalyst driving redox electrocatalysis. Nature communications 2020, 11 (1), 5437.

(127) Gao, S.; Hao, S.; Huang, Z.; Yuan, Y.; Han, S.; Lei, L.; Zhang, X.; Shahbazian-Yassar, R.; Lu, J. Synthesis of high-entropy alloy nanoparticles on supports by the fast moving bed pyrolysis. Nature communications 2020, 11 (1), 2016.

(128) Jin, Z.; Lyu, J.; Zhao, Y.-L.; Li, H.; Lin, X.; Xie, G.; Liu, X.; Kai, J.-J.; Qiu, H.-J. Rugged high-entropy alloy nanowires with in situ formed surface spinel oxide as highly stable electrocatalyst in Zn–air batteries. ACS Materials Letters 2020, 2 (12), 1698-1706.

(129) Fang, G.; Gao, J.; Lv, J.; Jia, H.; Li, H.; Liu, W.; Xie, G.; Chen, Z.; Huang, Y.; Yuan, Q. Multi-component nanoporous alloy/(oxy) hydroxide for bifunctional oxygen electrocatalysis and rechargeable Zn-air batteries. Applied Catalysis B: Environmental 2020, 268, 118431.

(130) Shen, X.; Ting, C. P.; Xu, G.; Maimone, T. J. Programmable meroterpene synthesis. Nature Communications 2020, 11 (1), 508.

(131) Wei, M.; Sun, Y.; Zhang, J.; Ai, F.; Xi, S.; Wang, J. High-entropy alloy nanocrystal assembled by nanosheets with d–d electron interaction for hydrogen evolution reaction. Energy & Environmental Science 2023, 16 (9), 4009-4019.

(132) Chang, S.-Q.; Cheng, C.-C.; Cheng, P.-Y.; Huang, C.-L.; Lu, S.-Y. Pulse electrodeposited FeCoNiMnW high entropy alloys as efficient and stable bifunctional electrocatalysts for acidic water splitting. Chemical Engineering Journal 2022, 446, 137452.

(133) Bian, H.; Wang, R.; Zhang, K.; Zheng, H.; Wen, M.; Li, Z.; Li, Z.; Wang, G.; Xie, G.; Liu, X. Facile electrodeposition synthesis and super performance of nano-porous Ni-Fe-Cu-Co-W high entropy alloy electrocatalyst. Surface and Coatings Technology 2023, 459, 129407.

(134) Ratajczyk, T.; Donten, M. Comparative Analysis of Metal Electrodeposition Rates towards Formation of High-Entropy WFeCoNiCu Alloy. Materials 2024, 17 (7), 1513.

(135) Freitas, G.; Gomes, W. S.; Souza, J. P. I.; Pinotti, C.; Passamani, E.; Montemor, M.; Della Noce, R. Direct electrodeposition of CoFeNiMoW high entropy alloy thin films from aqueous medium. Materials Chemistry and Physics 2023, 309, 128438.

(136) Dehestani, M.; Sharafi, S.; Khayati, G. R. Electrodeposited FeCoNiWMo high entropy alloy/SiC nanocomposite coatings: Microstructure, mechanical properties and corrosion resistance. Intermetallics 2023, 162, 107988.

(137) Haché, M. J.; Tam, J.; Erb, U.; Zou, Y. Electrodeposited NiFeCo-(Mo, W) high-entropy alloys with nanocrystalline and amorphous structures. Journal of Alloys and Compounds 2023, 952, 170026.

(138) Haché, M. J.; Zou, Y.; Erb, U. Thermal stability of electrodeposited nanostructured high-entropy alloys. Surface and Coatings Technology 2024, 482, 130719.

(139) Carroll, Z. L.; Haché, M. J. R.; Wang, B.; Chen, L.; Wu, S.; Erb, U.; Thorpe, S.; Zou, Y. Electrodeposited NiFeCoMoW High-Entropy Alloys with Nanoscale Amorphous Structure as Effective Hydrogen Evolution Electrocatalysts. ACS Applied Energy Materials 2024, 7 (19), 8412-8422.

(140) Bachvarov, V.; Arnaudova, M.; Rashkov, R. S.; Zielonka, A. Electrochemical deposition of alloys based on Ni-Fe-Co, containing W, P, and their characterization for hydrogen evolution reaction. Bul. Chem. Com 2011, 43 (1).

(141) Fuyu, G.; Jinku, Y.; Jingjing, X.; Qi, Q.; Haibo, Y.; Yanqing, G. Preparation of FeCoNiCr high entropy alloy coatings and optimization of process parameters. RARE METAL MATERIALS AND ENGINEERING 2021, 50 (7), 2337-2342.

(142) Li, Y.; Liu, Y.; Shen, J.; Lan, A.; Jin, X.; Han, L.; Qiao, J. High-entropy amorphous FeCoCrNi thin films with excellent electrocatalytic oxygen evolution reaction performance. Journal of Alloys and Compounds 2024, 1005, 176089.

(143) Aliyu, A.; Rekha, M.; Srivastava, C. Electrodeposition of High Entropy Alloy Coatings: Microstructure and Corrosion Properties. In High Entropy Alloys, CRC Press, 2020; pp 313-328.

(144) Cao, W.; Yang, X.; Dai, W.; Wu, B.; Zhang, Y.; Zhao, C.; Sui, Y.; Huang, S. Amorphous FeCoNiMnCr high-entropy alloy supported by 2H-MoS2 on carbon cloth as a highly efficient and robust electrocatalyst for water oxidation. New Journal of Chemistry 2023.

(145) Xiao, T.; Sun, C.; Wang, R. Electrodeposited CrMnFeCoNi Oxy-carbide film and effect of selective dissolution of Cr on oxygen evolution reaction. Journal of Materials Science & Technology 2024, 200, 176-184.

(146) Percival, S. J.; Lu, P.; Lowry, D. R.; Nenoff, T. M. Electrodeposition of complex high entropy oxides via water droplet formation and conversion to crystalline alloy nanoparticles. Langmuir 2022, 38 (5), 1923-1928.

(147) Ju, L.; Wu, W.; Zhou, Y.; Zhang, Y.; Wang, Q. Electrodeposition of FeNiCoCrMn high-entropy alloys on copper foam for enhanced hydrogen evolution reaction——influence of additives and deposition potential. Materials Letters 2024, 374, 137195.

(148) Wang, K.; Wang, Y.; Chen, Y.; Deng, G.; Zhou, Y.; Xu, C. High-entropy alloy NiCoFeCrMn electrocatalyst for alkaline anion exchange membrane water electrolysis. International Journal of Hydrogen Energy 2025, 109, 1108-1113.

(149) Wen, B.; Zhao, X.; Dong, Q.; Li, B.; Lyu, X. Gradient composition design of FeCoCrMnNi high entropy alloys: An efficient and stable electrocatalyst for water splitting. Journal of Power Sources 2025, 627, 235804.

(150) Aliyu, A.; Rekha, M.; Srivastava, C. Microstructure-electrochemical property correlation in electrodeposited CuFeNiCoCr high-entropy alloy-graphene oxide composite coatings. Philosophical Magazine 2019, 99 (6), 718-735.

(151) Nourmohammadi Khiarak, B.; Shariati, K.; Mojaddami, M.; Zamani, Z.; Zekiy, A. O.; Simchi, A. Efficient Electrocatalytic Overall Water Splitting on a Cu-Based High Entropy Alloy: An Electrochemical Study. Available at SSRN 3889206 2021.

(152) He, L.; Wang, N.; Sun, B.; Zhong, L.; Yao, M.; Hu, W.; Komarneni, S. High-entropy FeCoNiMn (oxy) hydroxide as high-performance electrocatalyst for OER and boosting clean carrier production under quasi-industrial condition. Journal of Cleaner Production 2022, 356, 131680.

(153) Yu, C.; Wang, X.-w.; He, W.-x.; Zheng, Z.-y.; Dang, X.-j.; Zhang, Y.-f. Electrodeposition of FeCoNiCuMn high-entropy alloy nanoparticles as efficient bifunctional electrolytic water catalyst. Surfaces and Interfaces 2024, 46, 104084.

(154) Li, J.; Wang, X.-w.; Niu, J.-q.; Li, S.-q.; Guo, C.-w.; Qiu, Z.-x.; Gao, S. Enhancement of electrocatalytic efficiency by rapid bubble detachment at electrodeposited feather-like FeCoNiCuMn high-entropy alloy porous structure. International Journal of Hydrogen Energy 2025, 113, 385-394.

(155) Zhang, H.-M.; Zuo, L.; Gao, Y.; Guo, J.; Zhu, C.; Xu, J.; Sun, J. Amorphous high-entropy phosphoxides for efficient overall alkaline water/seawater splitting. Journal of Materials Science & Technology 2024, 173, 1-10.

(156) Han, M.; Wang, C.; Zhong, J.; Han, J.; Wang, N.; Seifitokaldani, A.; Yu, Y.; Liu, Y.; Sun, X.; Vomiero, A. Promoted self-construction of β-NiOOH in amorphous high entropy electrocatalysts for the oxygen evolution reaction. Applied Catalysis B: Environmental 2022, 301, 120764.

(157) Mohan, M.; Pandel, U.; Kumar, K. Phase composition, surface chemistry and electrochemical studies of electrodeposited AlMnFeCuNi high entropy alloy composite coatings incorporated with carbon nanotubes. Materials Research Express 2024, 11 (4), 046403.

(158) Liu, Z.; Ma, H.; Kang, N.; Jiang, X.; Chu, M.; Xie, G.; Liu, X.; Liu, X. Nanoscale Raspberry-like Ni–Fe–Co–Mn–V high-entropy alloy electrocatalysts: A pathway to ultrlow overpotential hydrogen evolution. Materials Today Chemistry 2024, 42, 102404.

(159) Ma, H.; Liu, Z.; Chu, M.; Kang, N.; Jiang, X.; Zhang, J.; Xie, G.; Liu, X. Electrochemical self-construction to fabricate NiFeCoMnSn electrocatalysts: Enhanced lattice distortion effect induced by Sn incorporation for superior hydrogen evolution performance. Applied Materials Today 2024, 41, 102525.

(160) Reddy, K. S. K. J.; Chokkakula, L. P.; Dey, S. R. Compositional modulation through galvanic displacement in electrochemically deposited FeCoNiCuZn high entropy alloy thin films. Materials Letters 2023, 350, 134941.

(161) Reddy, K. S. K. J.; Chokkakula, L. P.; Dey, S. R. Strategies to engineer FeCoNiCuZn high entropy alloy composition through aqueous electrochemical deposition. Electrochimica Acta 2023, 453, 142350.

(162) Cheng, Z.; Han, X.; Han, L.; Zhang, J.; Liu, J.; Wu, Z.; Zhong, C. Novel High-Entropy FeCoNiMoZn-Layered Hydroxide as an Efficient Electrocatalyst for the Oxygen Evolution Reaction. Nanomaterials 2024, 14 (10), 889.

(163) Wang, L.; Gao, Z.; Su, K.; Nguyen, N. T.; Gao, R. T.; Chen, J.; Wang, L. Stacked High‐Entropy Hydroxides Promote Charge Transfer Kinetics for Photoelectrochemical Water Splitting. Advanced Functional Materials 2024, 2403948.

(164) Kang, N.; Ma, H.; Chu, M.; Jiang, X.; Liu, Z.; Feng, X.; Ren, X.; Liu, X.; Xie, G. Electrochemical performance of in-situ electrodeposited spinel-structured high entropy oxides/NiFeCuMoMn-high entropy alloy multiphase electrocatalysts for seawater electrolysis. Electrochimica Acta 2024, 506, 144931.

(165) Bian, H.; Wang, C.; Zhao, S.; Han, G.; Xie, G.; Qi, P.; Liu, X.; Zeng, Y.; Zhang, D.; Wang, P. Preparation of highly efficient high-entropy alloy catalysts with electrodeposition and corrosion engineering for OER electrocatalysis. International Journal of Hydrogen Energy 2024, 57, 651-659.

(166) Rao, P.; Singh, S.; Kumar, K.; Pandel, U.; Srivastava, C. Electrochemical Behavior and Surface Chemistry Studies of Electrodeposited MnMoCrCoFeNiCu High Entropy Alloy-Carbon Nanotube Composite Coatings. Journal of Materials Engineering and Performance 2024, 1-16.