Electronic Supplementary Material

Granulation mechanism and CO2 capture performance of alkaline metal salt-promoted MgO sorbents

Jinbo Song1,2, Jieying Jing ()1,2, Jinpeng Zhang1,2, Yufeng Xu1,2, Wen-Ying Li ()1,2

1 State Key Laboratory of Clean and Efficient Coal Utilization, Taiyuan University of Technology, Taiyuan 030024, China
2 College of Chemistry and Chemical Engineering, Taiyuan University of Technology, Taiyuan 030024, China

E-mails: jingjieying@tyut.edu.cn (Jing J); ying@tyut.edu.cn (Li W-Y)

Table S1 Response variables and their coded and actual values for optimization.

| Independent variables | Unit | Symbol coded | Coded levels |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | −1 | 0 | 1 |
| sesbania powder | wt% | SP | 1 | 3 | 5 |
| pseudoboehmite | wt% | PB | 1 | 2 | 3 |
| nitric acid | wt% | NA | 10 | 15 | 20 |
| microcrystalline cellulose | wt% | MC | 1 | 5 | 10 |

Table S2 Box-behnken experimental design and response results

| STD | SP | PB | NA | MC | Initial CO2 capture capacity / mmol/g |
| --- | --- | --- | --- | --- | --- |
| 1 | -1 | 0 | 1 | 0 | 9.76 |
| 2 | 0 | 0 | 0 | 0 | 8.62 |
| 3 | 0 | 1 | 0 | -1 | 8.70 |
| 4 | 0 | 0 | 0 | 0 | 8.90 |
| 5 | -1 | 0 | 0 | 1 | 11.46 |
| 6 | 0 | 0 | 0 | 0 | 9.34 |
| 7 | 0 | 1 | 1 | 0 | 8.47 |
| 8 | 0 | 0 | 0 | 0 | 9.47 |
| 9 | 1 | 0 | 1 | 0 | 8.74 |
| 10 | -1 | 0 | 0 | -1 | 10.98 |
| 11 | 0 | 0 | -1 | 1 | 11.29 |
| 12 | -1 | 0 | -1 | 0 | 10.98 |
| 13 | 0 | 1 | -1 | 0 | 9.01 |
| 14 | 1 | 1 | 0 | 0 | 8.09 |
| 15 | 0 | -1 | -1 | 0 | 10.82 |
| 16 | 0 | -1 | 0 | -1 | 8.65 |
| 17 | 0 | 0 | 1 | 1 | 8.47 |
| 18 | 1 | 0 | -1 | 0 | 10.23 |
| 19 | 1 | 0 | 0 | 1 | 8.99 |
| 20 | 0 | 0 | 0 | 0 | 9.22 |
| 21 | 0 | -1 | 0 | 1 | 10.10 |
| 22 | 0 | 1 | 0 | 1 | 8.18 |
| 23 | 1 | -1 | 0 | 0 | 9.68 |
| 24 | 0 | 0 | -1 | -1 | 10.62 |
| 25 | 0 | 0 | 1 | -1 | 9.82 |
| 26 | -1 | 1 | 0 | 0 | 9.38 |
| 27 | -1 | -1 | 0 | 0 | 10.68 |
| 28 | 0 | -1 | 1 | 0 | 8.06 |
| 29 | 1 | 0 | 0 | -1 | 9.93 |

To ensure the accuracy of the test results, the initial CO2 capture capacity of each sorbent pellet (STD) needs to be averaged after 5 measurements.

Table S3 ANOVA results of the RSM–BBD model of responses.

| Source | Sum of squares | Degree of freedom | Mean square | F value | P-value prob > F |
| --- | --- | --- | --- | --- | --- |
| Model | 26.540 | 14 | 1.896 | 12.574 | <0.0001 |
| SP | 5.147 | 1 | 5.147 | 34.142 | <0.0001 |
| PB | 3.559 | 1 | 3.559 | 23.607 | 0.0003 |
| NA | 8.318 | 1 | 8.318 | 55.169 | <0.0001 |
| MC | 0.003 | 1 | 0.003 | 0.023 | 0.8829 |
| SP×PB | 0.020 | 1 | 0.020 | 0.135 | 0.7185 |
| SP×NA | 0.018 | 1 | 0.018 | 0.118 | 0.7365 |
| SP×MC | 0.580 | 1 | 0.580 | 3.849 | 0.0700 |
| PB×NA | 1.227 | 1 | 1.227 | 8.140 | 0.0128 |
| PB×MC | 0.938 | 1 | 0.938 | 6.219 | 0.0258 |
| NA×MC | 1.058 | 1 | 1.058 | 7.018 | 0.0191 |
| SP2 | 2.991 | 1 | 2.991 | 19.841 | 0.0005 |
| PB2 | 1.348 | 1 | 1.348 | 8.939 | 0.0097 |
| NA2 | 0.792 | 1 | 0.792 | 5.255 | 0.0379 |
| MC2 | 1.418 | 1 | 1.418 | 9.404 | 0.0084 |
| Residual | 2.111 | 14 | 0.151 |  |  |
| Lack of fit | 1.631 | 10 | 0.163 | 1.360 | 0.4116 |
| Pure error | 0.480 | 4 | 0.120 |  |  |
| Cor total | 28.650 | 28 |  |  |  |

Note: P< 0.05 means significant difference; P< 0.01 means highly significant difference. SP×PB, SP×NA, SP×MC, PB×NA, PB×MC, and NA×MC represent the interactions between sesbania powder and pseudoboehmite, sesbania powder and nitric acid, sesbania powder and microcrystalline cellulose, pseudoboehmite and nitric acid, pseudoboehmite and microcrystalline cellulose, and nitric acid and microcrystalline cellulose, respectively. SP2, PB2, NA2, and MC2 represent the secondary terms for sesbania powder, pseudoboehmite, nitric acid, and microcrystalline cellulose, respectively.

Fig. S1 Initial CO2 capture capacity: (a) normal probability plot of the residuals, (b) distribution of the residuals versus the predicted values, and (c) distribution of the predicted values versus the actual values.

Fig. S2 Particle images before and after TGA cycling experiments: (a)-(c) before carbonation, (d)-(f) after carbonation.

Fig. S3 Plot of CO2 capture capacity of samples over time.