Electronic Supplementary Material

# Preparation of TiO2@MCC modified PA6 composite membranes and their water-oil separation performance

Pengcheng Hu (), Aonan Lai, Shufeng Zhou

College of Chemical Engineering, Huaqiao University, Xiamen 361021, China

E-mail: hupc1987@hqu.edu.cn

Contents:

Tab. S1. Relative area of different chemical bonds in PA6 and TiO2@2MCC-PA6.

Fig. S1. IR spectra (left) and XRD patterns (right) of PA6, TiO2-PA6, TiO2@MCC-PA6, and TiO2@2MCC-PA6.

Fig. S2. Oil resistance properties of PA6 (a) and TiO2@MCC-PA6 (b).

Fig. S3. Polarizing microscope images of n-hexane/water (a), petroleum ether/water (b), and vacuum oil/water emulsions (c) without SDS before and after filtration by TiO2@MCC-PA6.

Fig. S4. Effect of times of tape stripping on underwater contact angle and separation efficiency and of TiO2@MCC-PA6 for the separation of n-hexane/SDS/water.

Table 1. Relative area of different chemical bonds in PA6 and TiO2@2MCC-PA6.

|  | Relative area of different chemical bonds, % |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | -C-C- | -C-N- | -C-O-/-C-OH | -C=O- | -O-C=O- |
| PA6 | 44.43 | 26.47 | 11.43 | 17.18 | 0.00 |
| TiO2@MCC-PA6 | 19.23 | 11.57 | 47.48 | 18.47 | 3.26 |

Fig. S1. IR spectra (left) and XRD patterns (right) of PA6, TiO2-PA6, TiO2@MCC-PA6, and TiO2@2MCC-PA6.

Fig. S2. IR spectra (a) and XRD patterns (b) of PVA@MCC under different PVA/MCC mass ratios.

Fig. S3. Polarizing microscope images of n-hexane/water (a), petroleum ether/water (b), and vacuum oil/water emulsions (c) without SDS before and after filtration by TiO2@MCC-PA6.

Fig. S4. Effect of times of tape stripping on underwater contact angle and separation efficiency and of TiO2@MCC-PA6 for the separation of n-hexane/SDS/water.