Supporting Information

Research of Synthesis and Neural Network Training on Double Quantum Dot Colorimetric Fluorescent Probe for Freshness Detection

Caihong Lva,b,#, Yuewei Zhenga,#, Zhihao Guana, Jun Qianb, Houbin Lib,*, Xinghai Liua,*

a Hubei Engineering Technology Research Center of Spectrum and Imaging Instrument, Electronic Information School, Wuhan University, Wuhan 430072, P. R. China

b School of Nursing, Wuhan University, Wuhan 430072, P. R. China

#These authors contributed equally to this work.

*Corresponding author.

Email: liuxh@whu.edu.cn, lhb@whu.edu.cn

The fluorescence quantum yield factors of B quantum dot and G quantum dot are calculated according to the equation as follows:

Yu=Ys×FuFs×AsAu

Table S1 Integral area of fluorescent emission spectrum and UV absorption intensity for Rhoda Mine and quantum dots*.

| Quantum Dot | Ys | Fu | Fs | Au | As |
| --- | --- | --- | --- | --- | --- |
| B | 0.69 | 49927785 | 48662174 | 1.1162 | 0.0714 |
| G | 0.89 | 23266725 | 124144234 | 0.2932 | 0.2874 |

*u stands for the sample to be tested, and s stands for the sample of the Rhoda Mine.

Fig. S1. (a) Fluorescence spectra of B quantum dots with excitation time. (b) Maximum fluorescence intensity of B quantum dots with excitation time. (c) Fluorescence spectra of G quantum dots with excitation time. (d) Maximum fluorescence intensity of G quantum dots with excitation time.

Fig. S2 UV-vis absorption spectra of B and G quantum dots and their mixed quantum dots.