Electronic Supplementary Material

# Local hydrophobicity enhanced hydrogen evolution over NiCo2O4/CdS photocatalyst

Xuan Xiang?, Yuyin Mao?, Minghui Zhang?, Hanxiao Wang?, Xiangdong Xue?, Jian Tian ()?, Jian Liu ()?

1 School of Materials Science and Engineering, Shandong University of Science and Technology, Qingdao 266590, China

2 State Key Laboratory of Photoelectric Conversion and Utilization of Solar Energy, Qingdao New Energy Shandong Laboratory, Qingdao Institute of Bioenergy and Bioprocess Technology, Chinese Academy of Sciences, Qingdao 266101, China

E-mails: jiantian@sdust.edu.cn (Tian J); liujian@qibebt.ac.cn (Liu J)

Figure S1 XRD patterns of the samples.

| Sample | Theoretical doping (NiCo2O4) | Actual doping (NiCo2O4) |
| --- | --- | --- |
| NCS-1 | 7% | 4.0% |
| NCS-2 | 12.5% | 8.6% |
| NCS-3 | 22% | 20.4% |
| NCS-4 | 40% | 35.7% |

Table S1 ICP-OES detection of NiCo2O4 doping results.

| Sample | Theoretical doping (SiO2) | Actual doping (SiO2) |
| --- | --- | --- |
| Hb10NCS-3 | 5% | 4.2% |
| Hb20NCS-3 | 10% | 5.9% |
| Hb40NCS-3 | 18% | 11.9% |
| Hb80NCS-3 | 33% | 32.5% |
| Hl40NCS-3 | 20% | 16.2% |

Table S2 ICP-OES detection of SiO2 doping results.

Figure S2 SEM image of (a) CdS and (b) NiCo2O4.

Figure S3 SEM images of the NCS series.

Figure S4 TEM images of Hydrophobic SiO2.

Figure S5 Water contact angles of different samples.

Figure S6 The dispersion of the samples at 0 hours and 4 hours.

Figure S7 The dispersion of the Hydrophobic SiO2 and Hydrophilic SiO2.

Figure S8 Photocatalytic activities of CdS, NiCo2O4 and different proportions.

Figure S9 Comparison of hydrogen production under different ratios.

Figure S10 XRD diagram before and after hydrogen production of Hb40NCS-3.

Figure S11 Water contact angles diagram before and after hydrogen production of Hb40NCS-3.

Figure S12 XPS survey scan spectra.

Figure S13 XPS spectra of Cd 3d and S 2p.

Figure S14 XPS spectra of Ni 2p and Co 2p.

Figure S15 UV–vis absorption spectra of the samples.

Figure S16 CdS, NCS-3, Hl40NCS-3 and Hb40NCS-3 of TRPL.

Table S3 Secondary fitting attenuation parameters for the average life time of CdS, NCS-3, Hl40NCS-3 and Hb40NCS-3.

| Sample | τ1 (ns) | τ2 (ns) | τ3 (ns) | τave (ns) |
| --- | --- | --- | --- | --- |
| CdS | 0.57 | 4.22 | 31.85 | 23.55 |
| NCS-3 | 0.64 | 3.91 | 18.70 | 13.21 |
| Hl40NCS-3 | 0.53 | 4.09 | 24.12 | 16.24 |
| Hb40NCS-3 | 0.53 | 3.61 | 19.14 | 14.13 |

Figure S17 XPS valence band spectra of NiCo2O4.

Figure S18 Mott-Schottky curve of the CdS.