Electronic Supplementary Material

# Effect of binder addition on combustion characteristics of cotton straw pellets and kinetic analysis

Yiwen Dai1*, Bin Guan1*, Xingxiang Wang1, Jinli Zhang1,2, Bin Dai1, Jiangbing Li ()1, Jichang Liu1

1 School of Chemistry and Chemical Engineering/State Key Laboratory Incubation Base for Green Processing of Chemical Engineering, Shihezi University, Shihezi 832003, China

2 School of Chemical Engineering and Technology, Tianjin University, Tianjin 300350, China

* These authors contributed equally.

E-mail: ljbing@126.com

Fig.S1. Diagram of single column molding device

Fig. S2. Influence of Diameter of raw material on physical quality characteristics of biomass molding particles: (a) Forming density; (b) Compressive strength; (c) Hydrophobicity; (d) Energy density

Fig. S3. Influence of moisture content on physical quality characteristics of biomass forming particles: (a) Forming density; (b) Compressive strength; (c) Hydrophobicity ; (d) Energy density

Fig. S4. Influence of temperature on physical quality characteristics of biomass forming particles :    (a) Forming density; (b) Compressive strength; (c) Hydrophobicity; (d) Energy density

Fig. S5. Influence of molding pressure on physical quality characteristics of biomass forming particles : (a)Forming density; (b) Compressive strength; (c) Hydrophobicity; (d) Energy density

Fig. S6. Influence of molding time on physical quality characteristics of biomass forming particles : (a)Forming density; (b) Compressive strength; (c) Hydrophobicity; (d) Energy density

Tab. S1 Level table of factors

| Level | Factor |  |  |  |
| --- | --- | --- | --- | --- |
|  | A Temperature（℃） | B Moisture（%） | C Diameter（mm） | D Pressure （kN） |
| 1 | 120 | 5 | 0~0.5 | 6.5 |
| 2 | 140 | 10 | 0.5~1 | 7 |
| 3 | 160 | 15 | 1~1.5 | 7.5 |

Tab. S2 Orthogonal experiment design and results of L9（34）

| Number | A | B | C | D | Experimental result |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | ρ （g·cm-3） | Compressive strength（N·mm−1） | Hydrophobicity（%） | Energy density (kJ·cm-3) |
| 1 | 120 | 5 | 6.5 | 0~0.5 | 1.245 | 94.323 | 9.774 | 22.225 |
| 2 | 120 | 10 | 7 | 0.5~1 | 1.119 | 48.779 | 2.252 | 19.970 |
| 3 | 120 | 15 | 7.5 | 1~1.5 | 0.880 | 34.611 | 2.217 | 15.665 |
| 4 | 140 | 5 | 7 | 1~1.5 | 1.174 | 115.553 | 9.219 | 20.954 |
| 5 | 140 | 10 | 7.5 | 0~0.5 | 1.271 | 113.269 | 3.506 | 22.708 |
| 6 | 140 | 15 | 6.5 | 0.5~1 | 0.998 | 80.578 | 3.753 | 17.783 |
| 7 | 160 | 5 | 7.5 | 0.5~1 | 1.189 | 108.785 | 11.292 | 21.229 |
| 8 | 160 | 10 | 6.5 | 1~1.5 | 1.113 | 86.929 | 7.309 | 19.848 |
| 9 | 160 | 15 | 7 | 0~0.5 | 1.173 | 82.117 | 5.572 | 20.936 |

Tab. S3 Orthogonal experimental analysis of L9（34）

| ρ |  |  | A | B | C | D |
| --- | --- | --- | --- | --- | --- | --- |
|  | K1 |  | 3.244 | 3.608 | 3.355 | 3.689 |
|  | K2 |  | 3.443 | 3.503 | 3.466 | 3.307 |
|  | K3 |  | 3.475 | 3.051 | 3.341 | 3.167 |
|  | Optimal decision |  | B1D1A3C2 |  |  |  |
| Compressive strength |  |  | A | B | C | D |
|  | K1 |  | 177.713 | 318.660 | 261.830 | 289.709 |
|  | K2 |  | 309.399 | 248.977 | 246.449 | 238.141 |
|  | K3 |  | 277.831 | 197.306 | 256.665 | 237.093 |
|  | Optimal decision |  | A2B1D1C3 |  |  |  |
| Hydrophobicity |  |  | A | B | C | D |
|  | K1 |  | 14.243 | 30.285 | 20.836 | 18.851 |
|  | K2 |  | 16.477 | 13.067 | 17.043 | 17.297 |
|  | K3 |  | 24.173 | 11.541 | 17.014 | 18.744 |
|  | Optimal decision |  | B1A3C2D1 |  |  |  |
| Energy density |  |  | A | B | C | D |
|  | K1 |  | 57.860 | 64.409 | 59.856 | 65.869 |
|  | K2 |  | 61.445 | 62.526 | 61.860 | 58.982 |
|  | K3 |  | 62.013 | 54.383 | 59.602 | 56.467 |
|  | Optimal decision |  | B1D1A3C2 |  |  |  |
| Optimal decision |  | B1A3D1C2 (0–0.5mm, 5%(wt), 160℃, 7 kN, 60s) |  |  |  |  |

Fig. S7. Effects of CG and PE addition on the physical properties of molded particles:

(a) Forming density; (b) Compressive strength; (c) Hydrophobicity; (d) Energy density

Fig. S8. (CG: PE=1:1) Effects of addition on physical properties of formed particles:

(a) Forming density; (b) Compressive strenghth; (c) Hydrophobicity;(d) Energy density

Fig. S9. Effects of adding different proportions of composite waste binder on the physical properties of formed particles: (a) Forming density; (b) Compressive strenghth; (c) Hydrophobicity;(d) Energy density

Fig. S10. Schematic diagram of ignition and burnout temperature

Fig. S11 The XRD of treated and untreated CS raw materials

Fig. S12. SEM of sample: (a) CS powder; (b) CS pellet; (c) CG powder; (d) PE powder; (e) powder 12.5%CG; (f) powder 12.5%PE; (g) pellet 12.5%PE; (h) pellet 12.5%CG; (i) pellet 5%PE+5%CG;  (j) pellet 12.5%PE+12.5%CG

Fig. S13. Composition distribution of combustion gas phase products of CS pellets, 12.5%CG pellets, 12.5%PE pellets and 12.5%PE+12.5%CG pellets.

Tab. S4. Combustion characteristics of samples with different heating rates

| Sample | β | Ti | Th | (dm/dt)max | (dm/dt)mean | SN | C |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | ℃·min-1 | ℃ | ℃ | %·min-1 | %·min-1 | 10-7 | 10-6 |
| PE | 10 | 230 | 528 | 12.85 | 0.196 | 0.90 | 242.91 |
| CS | 10 | 185 | 465 | 11.83 | 0.61 | 4.53 | 345.65 |
| CG | 10 | 560 | 750 | 1.003 | 0.11 | 0.0047 | 3.20 |
| Powder | 30 | 232 | 470 | 29.52 | 2.52 | 25.19 | 548.45 |
|  | 50 | 240 | 525 | 48.05 | 3.56 | 42.39 | 834.20 |
|  | 70 | 243 | 618 | 53.14 | 4.37 | 51.32 | 899.93 |
|  | 90 | 252 | 643 | 76.57 | 4.94 | 60.33 | 1205.75 |
| Pellet | 30 | 240 | 480 | 32.63 | 2.50 | 24.42 | 566.49 |
|  | 50 | 247 | 571 | 48.67 | 3.54 | 49.69 | 797.75 |
|  | 70 | 251 | 638 | 57.05 | 4.33 | 55.79 | 905.54 |
|  | 90 | 253 | 807 | 60.12 | 4.94 | 62.86 | 939.24 |
| Powder 12.5%PE | 30 | 235 | 455 | 28.23 | 2.51 | 28.22 | 511.54 |
|  | 50 | 243 | 453 | 46.31 | 3.49 | 60.42 | 784.26 |
|  | 70 | 245 | 534 | 51.94 | 4.29 | 69.52 | 865.31 |
|  | 90 | 251 | 588 | 62.09 | 4.8 | 80.45 | 985.54 |
| Pellet 12.5%CG | 30 | 233 | 486 | 28.25 | 2.42 | 25.91 | 520.36 |
|  | 50 | 245 | 529 | 46.54 | 3.39 | 49.69 | 775.34 |
|  | 70 | 250 | 649 | 55.06 | 4.11 | 55.79 | 880.96 |
|  | 90 | 255 | 714 | 62.23 | 4.69 | 62.86 | 957.02 |
| Pellet 12.5% CG+12.5%PE | 30 | 235 | 463 | 26.31 | 2.49 | 25.62 | 476.41 |
|  | 50 | 246 | 551 | 39.93 | 3.54 | 42.39 | 659.83 |
|  | 70 | 250 | 650 | 48.15 | 4.33 | 51.32 | 770.40 |
|  | 90 | 250 | 711 | 56.48 | 4.9 | 62.28 | 903.68 |

Tab. S5. C-R kinetic parameters of fuel at different combustion rates

| Sample | β(℃·min-1) | T(℃) | Ea(kJ·mol-1) | A(min−1) | n | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| Powder | 30 | 246.36~290.31 | 122.7121937 | 6.30894E+11 | 3 | 0.99834 |
|  |  | 342.5~430.05 | 13.3534088 | 1.530115944 | 0.5 | 0.98963 |
|  | 50 | 254.02~299.16 | 131.2638084 | 4.49527E+12 | 3 | 0.99863 |
|  |  | 319.49~518.51 | 4.603371344 | 0.150453138 | 0.5 | 0.98152 |
|  | 70 | 250.92~311.43 | 112.8453009 | 99314952036 | 3 | 0.99775 |
|  |  | 350.55~580.44 | 8.231096034 | 0.86494346 | 1 | 0.93052 |
|  | 90 | 260.07~310.23 | 121.3351906 | 5.2093E+11 | 3 | 0.99941 |
|  |  | 370.47~600.17 | 7.86081525 | 0.947948058 | 1 | 0.91455 |
| Pellet | 30 | 242.1~285.09 | 130.6158473 | 3.80243E+12 | 3 | 0.99845 |
|  |  | 307.4~472.16 | 7.091852725 | 0.232905716 | 0.5 | 0.99054 |
|  | 50 | 254.2~292.32 | 136.6164989 | 1.87485E+13 | 3 | 0.99834 |
|  |  | 326.15~550.16 | 8.759490143 | 0.818833219 | 1 | 0.9478 |
|  | 70 | 250.88~300.85 | 125.5357078 | 1.53052E+12 | 3 | 0.9987 |
|  |  | 340.14~600.73 | 5.736504944 | 0.388640631 | 1 | 0.91591 |
|  | 90 | 250.49~311.93 | 110.4053461 | 44220869072 | 3 | 0.99923 |
|  |  | 354.78~730.96 | 5.714871334 | 3.045563348 | 1 | 0.9191 |
| Pellet 12.5% PE | 30 | 250.55~290.11 | 130.5360431 | 3.49226E+12 | 3 | 0.99793 |
|  |  | 345.31~420.14 | 13.25965216 | 1.471596067 | 0.5 | 0.99134 |
|  | 50 | 254.82~292.03 | 138.0161179 | 1.99693E+13 | 3 | 0.99929 |
|  |  | 325.04~451.4 | 8.43150118 | 0.593583298 | 0.5 | 0.9772 |
|  | 70 | 249.74~300.23 | 119.4215557 | 3.58516E+11 | 3 | 0.99858 |
|  |  | 329.33~477.88 | 6.93717857 | 0.473593853 | 0.5 | 0.99088 |
|  | 90 | 259.34~311.25 | 113.3225976 | 1.00353E+11 | 3 | 0.99505 |
|  |  | 350.01~520.09 | 3.89766647 | 0.186188094 | 0.5 | 0.98422 |
| Pellet 12.5%CG | 30 | 246.45~300.33 | 109.4889186 | 28720734750 | 3 | 0.99037 |
|  |  | 315.81~461.22 | 6.960216498 | 0.219290575 | 0.5 | 0.9948 |
|  | 50 | 246.42~292.44 | 129.8373008 | 4.35288E+12 | 3 | 0.99775 |
|  |  | 319.61~493.68 | 3.800711927 | 0.107347488 | 0.5 | 0.99284 |
|  | 70 | 260.02~301.91 | 128.7575306 | 3.06467E+12 | 3 | 0.99416 |
|  |  | 350.21~578.93 | 7.32919531 | 0.660601437 | 1 | 0.93343 |
|  | 90 | 260.95~311.7 | 119.48804 | 3.57185E+11 | 3 | 0.99622 |
|  |  | 351.7~578.24 | 8.739936197 | 1.63996844 | 1.5 | 0.97064 |
| Pellet 12.5%PE+12.5%CG | 30 | 245.91~290.33 | 113.441276 | 59661164252 | 3 | 0.99782 |
|  |  | 320.91~467.04 | 8.206015024 | 0.316820233 | 0.5 | 0.99332 |
|  | 50 | 254.15~299.22 | 115.5063934 | 1.07529E+11 | 3 | 0.99852 |
|  |  | 339.28~543.59 | 2.27993525 | 0.044763352 | 0.5 | 0.98244 |
|  | 70 | 250.68~310.55 | 103.7379441 | 8.19E+09 | 3 | 0.99847 |
|  |  | 350.66~620.68 | 13.90312824 | 5.255386486 | 1.5 | 0.91953 |
|  | 90 | 250.36~300.07 | 105.7225827 | 15483838309 | 3 | 0.99937 |
|  |  | 361.16~601.07 | 6.922035367 | 0.901598449 | 1.5 | 0.9788 |

.

Fig. S14. Dynamics of FWO and Starink without model: (a) (b) CS powder, (c) (d) CS pellet, (e) (f) 12.5%PE pellet, (g) (h) 12.5%CG pellet, (i) (j) 12.5%PE+12.5%CG pellet

Tab. S6. Dynamic parameters of FWO and Starink combustion without model method

| Sample | α （%） | FWO |  | Starink |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Ea( kJ·mol-1) | R2 | Ea( kJ·mol-1) | R2 |
| Powder | 0.1 | 55.56146622 | 0.92915 | 126.3848937 | 0.92092 |
|  | 0.2 | 60.54757433 | 0.97475 | 138.1251364 | 0.97179 |
|  | 0.3 | 61.44085515 | 0.99768 | 140.1021239 | 0.99742 |
|  | 0.4 | 59.9223647 | 0.99978 | 136.2886345 | 0.99975 |
|  | 0.5 | 60.5277377 | 0.99907 | 137.5960787 | 0.99893 |
|  | 0.6 | 58.67178736 | 0.97531 | 132.796125 | 0.97198 |
|  | 0.7 | 33.50344424 | 0.96039 | 71.30690091 | 0.94945 |
|  | 0.8 | 18.78063053 | 0.9784 | 35.0569663 | 0.96401 |
|  | 0.9 | 13.84873728 | 0.97849 | 22.33406958 | 0.95282 |
| Pellet | 0.1 | 68.82055755 | 0.99686 | 158.3594592 | 0.99652 |
|  | 0.2 | 67.96236624 | 0.97594 | 155.9999465 | 0.97343 |
|  | 0.3 | 58.87963736 | 0.94422 | 133.9196788 | 0.9375 |
|  | 0.4 | 52.72751445 | 0.91644 | 118.9165411 | 0.90529 |
|  | 0.5 | 49.63331551 | 0.9087 | 111.2733269 | 0.89546 |
|  | 0.6 | 34.87074951 | 0.88885 | 79.1490812 | 0.87155 |
|  | 0.7 | 26.84829272 | 0.87718 | 55.05115473 | 0.8364 |
|  | 0.8 | 14.26254055 | 0.91264 | 23.54219641 | 0.82186 |
|  | 0.9 | 10.52780008 | 0.92659 | 13.18543908 | 0.74565 |
| Pellet 12.5% PE | 0.1 | 72.93788428 | 0.86321 | 168.2977416 | 0.85228 |
|  | 0.2 | 87.66709945 | 0.93002 | 203.5836598 | 0.92488 |
|  | 0.3 | 80.74079456 | 0.96481 | 186.7088987 | 0.96184 |
|  | 0.4 | 72.53893873 | 0.99374 | 166.7620911 | 0.99313 |
|  | 0.5 | 67.81149717 | 0.99278 | 155.172274 | 0.99201 |
|  | 0.6 | 55.16117715 | 0.95206 | 124.2969921 | 0.94533 |
|  | 0.7 | 45.92963399 | 0.93406 | 101.3940219 | 0.92205 |
|  | 0.8 | 31.72241473 | 0.97626 | 66.50926649 | 0.96821 |
|  | 0.9 | 24.25396118 | 0.94757 | 47.79999157 | 0.92164 |
| Pellet 12.5% CG | 0.1 | 53.37896219 | 0.9889 | 121.0705438 | 0.98735 |
|  | 0.2 | 60.03593141 | 0.96753 | 136.8880179 | 0.9637 |
|  | 0.3 | 60.23192684 | 0.93645 | 137.2142162 | 0.92916 |
|  | 0.4 | 60.2429911 | 0.91604 | 137.0758014 | 0.90637 |
|  | 0.5 | 58.74291473 | 0.86993 | 133.2782989 | 0.8552 |
|  | 0.6 | 55.72482209 | 0.80004 | 132.5646053 | 0.81637 |
|  | 0.7 | 29.04296743 | 0.80356 | 60.39449634 | 0.80194 |
|  | 0.8 | 18.01190165 | 0.90154 | 32.85541712 | 0.83694 |
|  | 0.9 | 13.74283652 | 0.91573 | 21.45860215 | 0.81292 |
| Pellet 12.5% PE+ 12.5% CG | 0.1 | 71.48411973 | 0.93771 | 164.7856834 | 0.93214 |
|  | 0.2 | 75.93740477 | 0.97986 | 175.2426693 | 0.97803 |
|  | 0.3 | 72.70924928 | 0.98885 | 167.2716 | 0.98778 |
|  | 0.4 | 71.85848683 | 0.9927 | 165.0403136 | 0.99195 |
|  | 0.5 | 66.00652144 | 0.98388 | 150.6766506 | 0.98197 |
|  | 0.6 | 58.88398403 | 0.9379 | 133.0654168 | 0.92953 |
|  | 0.7 | 35.23476361 | 0.97534 | 75.22103304 | 0.96825 |
|  | 0.8 | 17.89659627 | 0.98684 | 32.4102698 | 0.97474 |
|  | 0.9 | 12.72927141 | 0.99054 | 18.79194277 | 0.96848 |