Electronic Supplementary Material

Density functional theory study on the selective oxidation of ethylene glycol to glycolic acid over Ptn (n = 4–55) clusters

Shiping Wu1,2, Yanhong Quan1,2, Jun Ren ()1,2

1 State Key Laboratory of Clean and Efficient Coal Utilization, Taiyuan University of Technology, Taiyuan 030024, China

2 College of Chemistry and Chemical Engineering, Taiyuan University of Technology, Taiyuan 030024, China

E-mail: renjun@tyut.edu.cn

- For reproducibility, CIF files of the optimized geometries were provided and were presented in the terms of the linked files, as follow:

(a)

(b)

(c)

(d)

- The most stable adsorption configurations along with their corresponding energies of reactants, possible intermediates and products on the Ptn (n=4-55) clusters

Fig. S1 Adsorbed configurations of all possible species involved in GA formation on Pt4 clustre surface. Color-coding: C, grey; Pt, blue; O, red; H, white.

Fig. S2 Adsorbed configurations of all possible species involved in GA formation on Pt13 clustre surface. Color-coding: C, grey; Pt, blue; O, red; H, white.

Fig. S3 Adsorbed configurations of all possible species involved in GA formation on Pt38 clustre surface. Color-coding: C, grey; Pt, blue; O, red; H, white.

Fig. S4 Adsorbed configurations of all possible species involved in GA formation on Pt55 clustre surface. Color-coding: C, grey; Pt, blue; O, red; H, white

Table S1 Adsorption energies (Eads, kJ/mol) of species involved in GA formation on Pt4, Pt13, Pt38, Pt55 cluster and Pt(111) surfaces.

| Species | Pt4 |  | Pt13 |  | Pt38 |  | Pt55 |  | Pt(111) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Sites | Eads | Sites | Eads | Sites | Eads | Sites | Eads | Sites | Eads |
| O2* | Top | -157.5 | Top | -258.2 | Top-I | -145.4 | Top-I | -85.4 | Top | -42.0 |
| O* | Top | -499.2 | Top | -403.4 | Top-I | -601.4 | Top-I | -399.7 | Hcp | -338.0 |
| H2O* | Top | -88.8 | Top | -63.4 | - | -33.7 | Top-I | -54.3 | Top | -46.0 |
| OOH* | Top | -216.6 | Bri | -187.9 | Top-I | -123.3 | Bri-II | -181.4 | Top | -109.9 |
| OH* | Top | -296.5 | Top | -344.0 | Bri-I | -300.7 | Bri-II | -298.7 | Top | -213.1 |
| H* | Top | -340.1 | Top | -361.5 | Bri-I | -296.2 | Bri-I | -298.6 | Fcc | -271.5 |
| HOCH2CH2OH | Top | -120.3 | Top | -160.5 | Top-I | -95.7 | Top-I | -108.5 | Top | -64.4 |
| HOCH2CH2O | Top | -317.7 | Top | -364.6 | Bri-I | -262.2 | Top-I, Bri-II | -267.4 | Top | -184.8 |
| HOCH2CHO | Top | -177.8 | Top | -219.8 | Top-I, Top-II | -132.0 | Top-I | -99.1 | Top | -60.3 |
| HOCH2CO | Top | -348.2 | Top | -336.7 | Top-II | -106.8 | Top-I, Top-II | -307.3 | Top | -280.8 |
| HOCH2COOH | Top | -96.4 | - | -65.9 | - | -65.9 | - | -67.2 | - | -30.4 |
| HOCH2 | Top | -282.5 | Top | -324.9 | Top-I | -269.3 | Top-I | -273.1 | Top | -228.1 |
| COOH | Top | -331.3 | Top | -334.1 | Top-II | -277.6 | Top-I | -302.2 | Top | -242.1 |

Fig. S5 Side views of the initial states, transition states, and final states involved in O2 activation (R1-R5) over Pt4 surface

Fig. S6 Side views of the initial states, transition states, and final states involved in O2 activation (R1-R5) over Pt13 surface

Fig. S7 Side views of the initial states, transition states, and final states involved in O2 activation (R1-R5) over Pt38 surface

Fig. S8 Side views of the initial states, transition states, and final states involved in O2 activation (R1-R5) over Pt55 surface

Fig. S9 Side views of the initial states, transition states, and final states involved in selective oxidation of EG to GA (R6-R7-11) over Pt4 surface

Fig. S10 Side views of the initial states, transition states, and final states involved in selective oxidation of EG to GA (R6-R11) over Pt13 surface

Fig. S11 Side views of the initial states, transition states, and final states involved in selective oxidation of EG to GA (R6-R11) over Pt38 surface

Fig. S12 Side views of the initial states, transition states, and final states involved in selective oxidation of EG to GA (R6-R11) over Pt55 surface.

- Pt(111) slab model

Pt(111) surface was constructed using a p(4 × 4) slab containing four layers with 16 atoms per layer, which was companied with the vacuum thickness of 15 Å. The two bottom Pt (111) layers were fixed, while the other layers were fully relaxed. Furthermore, the surfaces of the Pt(111) with their possible adsorption sites are shown in Figure S13.

Fig. S13 (a) Top and (b) side views of the slab model of Pt(111)

The most stable adsorption configurations of the reactants, potential intermediates, and products on the Pt(111) surface are illustrated from Figure S14, with the associated adsorption sites and energies compiled in Table S1.

Fig. S14 Adsorbed configurations of all possible species involved in GA formation on Pt(111) surface. Color-coding: C, grey; Pt, blue; O, red; H, white.

Fig. S15 Side views of the initial states, transition states, and final states involved in O2 activation

(R1-R5) over Pt(111) surface

Table S2 Energy barrier Ea (kJ∙mol-1) and reaction energies ∆H (kJ∙mol-1) of GA formation on Pt(111) surface

| Elementary step | Pt(111) |  |  |
| --- | --- | --- | --- |
|  | TS | Ea | ∆H |
| R1 | TS R1 | 129.9 | -14.9 |
| R2 | TS R2 | 196.8 | -86.0 |
| R3 | TS R3 | 125.3 | -20.6 |
| R4 | TS R4 | 28.0 | -24.8 |
| R5 | TS R5 | 142.9 | -79.5 |
| R6 | TS R6 | 59.5 | 50.5 |
| R7 | TS R7 | 63.1 | 52.9 |
| R8 | TS R8 | 307.2 | 62.0 |
| R9 | TS R9 | 56.3 | -27.3 |
| R10 | TS R10 | 107.3 | -185.2 |
| R11 | TS R11 | 262.9 | -22.9 |

On the Pt(111) surface (Figure S15), the O2 molecule undergoes direct dissociation via the transition state TSR1, resulting in 129.9 kJ·mol-1, and an exothermic energy of 14.9 kJ∙mol-1. Then, the dissociated two O atoms are adsorbed on the Fcc sites. Meanwhile, O2 and H react to produce OOH via the transition state TSR3, resulting in a reaction barrier of 125.3 kJ∙mol-1 and an exothermic energy of 20.6 kJ∙mol-1 on the Pt(111) surface. Subsequently, the formed OOH is adsorbed onto the Top site.

Fig. S16 The potential energy diagram of O2 activation on the Pt(111) surface.

Fig. S17 Side views of the initial states, transition states, and final states involved in selective oxidation of EG to GA (R6-R11) over Pt(111) surface

Obviously, EG dehydrogenation to HOCH2CH2O via a transition state TSR6 and the activation energy of R6 on Pt(111) surface is 59.5 kJ∙mol-1, which are significantly lower than that of R7 (63.1 kJ∙mol-1), which indicates that HOCH2CH2O is more readily produced through the direct dehydrogenation of EG.

Subsequently, when HOCH2CH2O dehydrogenates to generate HOCH2CHO, the optimized co-adsorption configuration of H and HOCH2CHO, in conjunction with the most stable adsorption configuration of HOCH2CH2O, was chosen to investigate the transition state. On the Pt(111) surface, the dehydrogenation of HOCH2CH2O to form HOCH2CHO occurs via the TSR8, with activation barrier and reaction energy of 307.2 and 62.0 kJ∙mol-1, respectively. Then, the dissociated H atom and HOCH2CHO are adsorbed on the Fcc and Top sites, respectively.

To study the dehydrogenation of HOCH2CHO to HOCH2CO, the optimized co-adsorption configuration of H and HOCH2CO, along with the most stable adsorption configurations of HOCH2CHO were selected for transition state search. On the Pt(111) surface, the dehydrogenation of HOCH2CHO occurs through TSR9, where the C-H bond cleavage has an activation barrier of 56.3 kJ∙mol-1 and is exothermic by 27.3 kJ∙mol-1, which is followed by the adsorption of the dissociated H atom and HOCH2CO on the Fcc and Top sites, respectively. It should be noted that the activation barrier for the HOCH2CHO dehydrogenation is lower than its adsorption energy (60.3 kJ∙mol-1), indicating that HOCH2CHO favors dehydrogenation rather than desorption on the Pt(111) surface.

Starting from the HOCH2CO intermediate, the reaction of HOCH2CO with OH to form GA via the transition state TS10 requires activation barrier and reaction energies of 107.3 and -185.2 kJ∙mol-1 on the Pt(111) surface, respectively. In addition, HOCH2 and COOH are formed by the C-C cleavage of GA through TS11 with activation barrier and reaction energies of 262.9 and -229 kJ∙mol-1, respectively, and then they are both adsorbed on the Top sites. Significantly, the activation barrier of C-C cleavage of GA is higher than its desorption energy (30.4 kJ∙mol-1), suggesting that GA is more likely to desorb than to undergo oxidation on the Pt(111) surface.