Electronic Supplementary Material

Oxygen vacancy-mediated lewis acid-base pairs on Ce-doped BiOI enable efficient CO2 conversion

Chengguang Yue1, Wenhao Ji1, Tiantian Xiao1, Weiying Pang1, Shouying Huang1, Ji Qi2, Yue Wang1, Mei-Yan Wang ()1, Xinbin Ma ()1

1 School of Chemical Engineering and Technology, Key Laboratory for Green Chemical Technology of Ministry of Education, Tianjin University, Tianjin 300072, China

2 Institute of Molecular Plus, Tianjin University, Tianjin 300072, China

© Higher Education Press 2026

Received March 5, 2026; accepted February 7, 2026

E-mail: mywang2017@tju.edu.cn; xbma@tju.edu.cn

Adsorption energy calculations: Regarding the CexBi1-xOI and BiOI materials synthesized in this work, XRD results confirm that the predominant crystal facet is associated with the (010) orientation, with a relatively minor presence of the (001) facet (Fig. S1). Prior studies1, 2 have also indicated that for BiOX-catalyzed CO2 cycloaddition systems, the (010) facet is a high active surface as it simultaneously exposes Lewis acid sites (Bi3+) and nucleophilic halide ions (X−), which could facilitate the adsorption and ring-opening of epoxide molecules. Therefore, the (010) facet was selected to model the active surface in this work.

Fig. S1 XRD peak intensity ratios for CexBi1-xOI and BiOI samples.

The Perdew-Burke-Ernzerhof (PBE) exchange-correlation functional within the generalized gradient approximation (GGA) was employed to describe the exchange-correlation energy. The projector-augmented-wave (PAW) method was adopted for the pseudopotentials. The energy cutoff for the plane wave basis expansion was set to 400 eV. The force and energy change for all atomic structures were set as 0.03 eV/Å and 10−5 eV for convergence criterion, respectively. The computational model employed a 2 × 4 supercell. The lattice parameters for the BiOI crystal were: a = 4.00421 Å, b = 4.00421 Å, c = 9.60482 Å, α = β = γ = 90°. 15 Å vacuum layer is set up above the Z-direction to make sure that the calculations are free from the influence of periodic boundaries, and the k-point lattice was set to 3 × 3 × 1. In the BiOI (010) and Ce doped BiOI (010) slab models, the top two atomic layers were relaxed during the BO adsorption. Spin polarization was explicitly taken into account during the adsorption energy calculations.

Fig. S2 (a) N2 adsorption-desorption isotherms and (b) pore size distribution of CexBi1-xOI and BiOI samples.

Tab. S1 Specific surface area and pore volume of CexBi1-xOI and BiOI samples

| Samples | SBETa (m2/g) | VPorea (cm3/g) |
| --- | --- | --- |
| BiOI | 72.8 | 0.31 |
| Ce0.1Bi0.9OI | 77.9 | 0.30 |
| Ce0.15Bi0.85OI | 64.6 | 0.22 |
| Ce0.2Bi0.8OI | 58.8 | 0.22 |

a Specific surface area and pore structure data were obtained by BET and BJH methods, respectively.

Fig. S3 EPR spectra of CexBi1-xOI and BiOI samples.

Fig. S4 Catalytic performance of Ce0.1Bi0.9OI toward the CO2 cycloaddition with different epoxides at 120 °C and 2 MPa CO2 for 12 h.

Table S2 Catalytic performance over reported MOX and Ce0.1Bi0.9OI samples

| Catalyst | Reaction conditions | Solvent | Yield of cyclic carbonates a (%) | Ref. |
| --- | --- | --- | --- | --- |
| BiOBr-(010) | 150 °C, 0.8 MPa CO2 | DMF | 85 (PO) | 1 |
|  |  |  | 72 (BO) |  |
| BiO1-xBr1-y-(010) | 100 °C, 2 MPa CO2 | - | 99 (PO) | 2 |
| FeOCl-VFe–Cl | 150 °C, 0.3 MPa CO2 | DMF | 81 (PO) | 3 |
|  |  |  | 30 (BO) |  |
| Ce0.1Bi0.9OI | 120 °C, 2 MPa CO2 | - | 91 (BO) | This work |
|  |  |  | 99 (PO) |  |

a PO: propylene oxide, BO: butylene oxide.

Fig. S5 GC crude spectra for the PO (top) and BO (middle) reaction systems; 1H NMR spectrum for the epichlorohydrin (bottom) system

Fig. S6 (a) Ce 3d and (b) O 1s XPS spectra of Ce0.1Bi0.9OI-O2

Fig. S7 Cyclic stability of Ce0.1Bi0.9OI in the CO2 cycloaddition with BO at 120 °C and 2 MPa CO2 for 12 h.

Fig. S8 TEM images of (a) fresh and (b) reused Ce0.1Bi0.9OI catalyst

Fig. S9 Results of "hot filtration" experiment on Ce0.1Bi0.9OI in the CO2 cycloaddition with BO at 120 °C and 2 MPa CO2 at 6 h.

Fig. S10 Effect of reaction temperature on catalytic activity of Ce0.1Bi0.9OI and BiOI samples (1 mL BO, 2 MPa CO2, 0.1 g catalysts, 12 h)

Fig. S11 The electron density difference image for BO adsorbed on Ov–Ce3+ sites

Fig. S12 The influence of different reaction parameters on BC yield and selectivity over Ce0.1Bi0.9OI: (a) temperature; (b) CO2 pressure; (c) reaction time; (d) catalyst dosage. (Reaction conditions: 1mL BO, 120 ℃, 2MPa CO2, 0.1 g Ce0.1Bi0.9OI for 12 h, when one parameter is varied, the other experimental conditions held constant.)

Table S3 Atomic ratio of Ce and Bi atom in CexBi1-xOI based on ICP data

| Samples | Atomic ratio (Bi:Ce) |  |
| --- | --- | --- |
|  | Theoretical | Actual |
| Ce0.1Bi0.9OI | 1:0.05 | 1:0.09 |
| Ce0.15Bi0.85OI | 1:0.1 | 1:0.17 |
| Ce0.2Bi0.8OI | 1:0.15 | 1:0.28 |

References

- 1.	S. Shang, W. Shao, X. Luo, M. Zuo, H. Wang, X. Zhang and Y. Xie, Research, 2022, 2022, 9878054.

- 2.	L. Xia, H. Chen, W. Wang, X. Jia, D. Zhang, L. Wang, P. Wu, L. Li and J. Huang, J. Mater. Sci. Technol., 2024, 202, 39-49.

- 3.	W. X. Liu, L. Li, W. Shao, H. Wang, Y. Dong, M. Zuo, J. D. Liu, H. J. Zhang, B. J. Ye, X. D. Zhang and Y. Xie, Chem. Sci., 2023, 14, 1397-1402.