Electronic Supplementary Material

Synthesis of bimetallic crednerite nanosheet as an efficient heterogeneous catalyst in Fenton-like degradation of bisphenol A

Hanxiao Chen, Bin Deng, Heng Lin, Hui Zhang ()

Department of Environmental Science and Engineering, School of Resource and Environmental Sciences, Wuhan University, Wuhan 430079, China

Email: eeng@whu.edu.cn

Table S1. Kinetic rate constants of BPA degradation in the CuMnO2/PMS system at different conditions.

| Catalyst dosage (g/L) | PMS concentration (mM) | pH | kobs (min−1) | R2 |
| --- | --- | --- | --- | --- |
| 0.2 | 0.4 | 8.0 | 0.075 | 0.9956 |
| 0.2 | 0.1 | 8.0 | 0.020 | 0.9866 |
| 0.2 | 0.3 | 8.0 | 0.056 | 0.9931 |
| 0.2 | 0.5 | 8.0 | 0.071 | 0.9786 |
| 0.1 | 0.4 | 8.0 | 0.027 | 0.9797 |
| 0.3 | 0.4 | 8.0 | 0.130 | 0.9330 |
| 0.5 | 0.4 | 8.0 | 0.189 | 0.9784 |
| 0.2 | 0.4 | 4.0 | 0.042 | 0.9993 |
| 0.2 | 0.4 | 6.2 | 0.057 | 0.9976 |
| 0.2 | 0.4 | 10.0 | 0.093 | 0.9811 |

Figure S1. Effect of PMS concentration on the CuMnO2/PMS system. Conditions: [BPA] = 0.1 mM, [CuMnO2] = 0.2 g/L, pH 8.0 with BBS.

Figure S2. Effect of CuMnO2 dosage on the CMNS/PMS system. Conditions: [BPA] = 0.1 mM, [PMS] = 0.4 mM, pH 8.0 with BBS.

Figure S3. Effect of pH on the CuMnO2/PMS system. Conditions: [BPA] = 0.1 mM, [PMS] = 0.4 mM, [CuMnO2] = 0.2 g/L.