Electronic Supplementary Material

DFT insights into oxygen vacancy formation and chemical looping dry reforming of methane on metals-substituted CeO2 (111) surface

Mingyi Chen1,2*, Zeshan Wang1,2*, Yuelun Li1,2, Yuxin Wang1,2,3, Lei Jiang1,2, Huicong Zuo1,2, Linan Huang1,2, Yuhao Wang1,2,3, Dong Tian ()1,2,3, Hua Wang ()1,2,3, Kongzhai Li ()1,2,3

1 Engineering Research Center of Metallurgical Energy Conservation and Emission Reduction, Ministry of Education, Kunming University of Science and Technology, Kunming 650093, China

2 Faculty of Metallurgical and Energy Engineering, Kunming University of Science and Technology, Kunming 650093, China

3 State Key Laboratory of Complex Nonferrous Metal Resources Clean Utilization, Kunming University of Science and Technology, Kunming 650093, China

E-mails: dong.tian@aliyun.com; dong.tian@kust.edu.cn (Tian D); wanghua65@163.com (Wang H); kongzhai.li@foxmail.com; kongzhai.li@aliyun.com (Li K)

* These authors contributed equally to this work.

Table S1. DFT calculated the effective bader charge of different metals and the surrounding oxygen atoms for the substituted CeO2 (111) surfaces.

| Substituted-metal |  | M | O1 | O2 | O3 | O4 | O5 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ge |  | -1.28 | 1.20 | 1.11 | 1.20 | 1.20 | 1.11 |
| Zr |  | -2.30 | 1.16 | 1.21 | 1.26 | 1.26 | 1.21 |
| Ta |  | -2.51 | 1.13 | 1.18 | 1.24 | 1.24 | 1.18 |
| Pr |  | -2.02 | 1.16 | 1.19 | 1.24 | 1.24 | 1.19 |
| Hf | -2.27 |  | 1.15 | 1.21 | 1.26 | 1.26 | 1.21 |
| Re | -2.45 |  | 1.10 | 1.06 | 1.14 | 1.14 | 1.06 |
| V | -1.81 |  | 1.07 | 1.06 | 1.24 | 1.24 | 1.06 |
| W | -2.56 |  | 1.11 | 1.09 | 1.16 | 1.16 | 1.09 |
| Pt | -0.81 |  | 1.11 | 1.05 | 1.07 | 1.07 | 1.05 |
| Nb | -2.63 |  | 1.13 | 1.18 | 1.28 | 1.28 | 1.18 |
| Ir | -1.45 |  | 1.00 | 1.03 | 1.07 | 1.07 | 1.03 |
| Rh | -1.24 |  | 1.12 | 1.08 | 1.11 | 1.11 | 1.08 |
| Ti | -1.94 |  | 1.16 | 1.14 | 1.21 | 1.21 | 1.14 |
| La | -2.09 |  | 1.20 | 1.22 | 1.24 | 1.24 | 1.22 |
| Sb | -1.81 |  | 1.19 | 1.17 | 1.23 | 1.23 | 1.17 |
| Ru | -1.60 |  | 1.11 | 1.11 | 1.15 | 1.15 | 1.11 |
| Y | -2.19 |  | 1.27 | 1.25 | 1.28 | 1.28 | 1.25 |
| Cr | -1.70 |  | 1.11 | 1.10 | 1.10 | 1.10 | 1.10 |
| In | -1.07 |  | 1.18 | 1.15 | 1.19 | 1.19 | 1.15 |
| Pd | -0.82 |  | 1.12 | 1.07 | 1.08 | 1.08 | 1.07 |
| Os | -2.07 |  | 1.01 | 1.01 | 1.11 | 1.11 | 1.01 |
| Co | -1.40 |  | 1.09 | 1.09 | 1.18 | 1.18 | 1.09 |
| Sc | -2.09 |  | 1.24 | 1.22 | 1.27 | 1.27 | 1.22 |
| Ga | -1.61 |  | 1.18 | 1.17 | 1.17 | 1.17 | 1.17 |
| Mo | -2.30 |  | 1.08 | 1.00 | 1.16 | 1.16 | 1.00 |
| Al | -2.41 |  | 1.31 | 1.40 | 1.18 | 1.18 | 1.40 |
| Fe | -1.53 |  | 1.18 | 1.10 | 1.18 | 1.18 | 1.10 |
| Au | -1.00 |  | 1.11 | 1.00 | 1.06 | 1.06 | 1.00 |
| Ni | -1.16 |  | 1.19 | 1.09 | 1.19 | 1.19 | 1.09 |
| Mn | -1.41 |  | 1.20 | 1.14 | 1.23 | 1.23 | 1.14 |
| Sr | -1.56 |  | 1.19 | 1.20 | 1.22 | 1.22 | 1.20 |
| Rb | -0.84 |  | 1.14 | 1.12 | 1.16 | 1.16 | 1.12 |
| Ca | -1.55 |  | 1.14 | 1.15 | 1.17 | 1.17 | 1.15 |
| Cd | -1.23 |  | 1.16 | 1.15 | 1.18 | 1.18 | 1.15 |
| K | -0.83 |  | 1.14 | 1.12 | 1.16 | 1.16 | 1.12 |
| Na | -0.83 |  | 1.12 | 1.10 | 1.16 | 1.16 | 1.10 |
| Mg | -1.66 |  | 1.28 | 1.14 | 1.30 | 1.30 | 1.14 |
| Zn | -1.25 |  | 1.20 | 1.10 | 1.21 | 1.21 | 1.10 |

Table S2. DFT calculated adsorption energies of CH4 on pristine CeO2 (111) and Zn substituted CeO2 (111) during the chemical looping dry reforming of methane to produce syngas process.

| Adsorption site | Pristine CeO2(111) Eads/eV | Zn substituted CeO2 (111) Eads/eV |
| --- | --- | --- |
| Ce-TOP | -0.38 | -0.24 |
| Hollow | -0.64 | -0.18 |
| O-TOP | -0.38 | -0.06 |
| O-O bridge | -0.47 | -0.12 |
| Ce-O bridge | -0.49 | -0.18 |
| O vacancy | -0.29 | -0.37 |
| Zn-TOP | / | -0.31 |

Table S3. DFT calculated adsorption energies of CH3 on pristine CeO2 (111) and Zn substituted CeO2 (111) during the chemical looping dry reforming of methane to produce syngas process.

| Adsorption site | Pristine CeO2(111) Eads/eV | Zn substituted CeO2 (111) Eads/eV |
| --- | --- | --- |
| Ce-TOP | -2.33 | -0.98 |
| Hollow | -2.33 | -1.08 |
| O-TOP | -3.22 | -3.42 |
| O-O bridge | -2.34 | -0.76 |
| Ce-O bridge | -3.10 | -2.87 |
| O vacancy | -2.24 | -1.09 |
| Zn-TOP | / | -1.17 |

Table S4. DFT calculated adsorption energies of CH2 on pristine CeO2 (111) and Zn substituted CeO2 (111) during the chemical looping dry reforming of methane to produce syngas process.

| Adsorption site | Pristine CeO2(111) Eads/eV | Zn substituted CeO2 (111) Eads/eV |
| --- | --- | --- |
| Ce-TOP | -3.13 | -1.34 |
| Hollow | -3.12 | -5.92 |
| O-TOP | -4.46 | -5.04 |
| O-O bridge | -3.15 | -1.60 |
| Ce-O bridge | -4.41 | -3.73 |
| O vacancy | -3.14 | -1.33 |
| Zn-TOP | / | -4.50 |

Table S5. DFT calculated adsorption energies of CH on pristine CeO2 (111) and Zn substituted CeO2 (111) during the chemical looping dry reforming of methane to produce syngas process.

| Adsorption site | Pristine CeO2(111) Eads/eV | Zn substituted CeO2 (111) Eads/eV |
| --- | --- | --- |
| Ce-TOP | -3.35 | -5.43 |
| Hollow | -3.61 | -5.65 |
| O-TOP | -4.64 | -5.72 |
| O-O bridge | -3.62 | -6.32 |
| Ce-O bridge | -5.54 | -5.06 |
| O vacancy | -3.62 | -5.20 |
| Zn-TOP | / | -6.27 |

Table S6. DFT calculated adsorption energies of C on pristine CeO2 (111) and Zn substituted CeO2 (111) during the chemical looping dry reforming of methane to produce syngas process.

| Adsorption site | Pristine CeO2(111) Eads/eV | Zn substituted CeO2 (111) Eads/eV |
| --- | --- | --- |
| Ce-TOP | -3.93 | -7.53 |
| Hollow | -3.93 | -8.48 |
| O-TOP | -7.35 | -8.44 |
| O-O bridge | -7.51 | -9.14 |
| Ce-O bridge | -7.27 | -7.30 |
| O vacancy | -3.97 | -6.81 |
| Zn-TOP | / | -8.24 |

Table S7. DFT calculated adsorption energies of H on pristine CeO2 (111) and Zn substituted CeO2 (111) during the chemical looping dry reforming of methane to produce syngas process.

| Adsorption site | Pristine CeO2(111) Eads/eV | Zn substituted CeO2 (111) Eads/eV |
| --- | --- | --- |
| Ce-TOP | 0.08 | 2.17 |
| Hollow | 0.09 | 1.77 |
| O-TOP | -1.50 | -1.53 |
| O-O bridge | 1.88 | 1.77 |
| Ce-O bridge | -1.41 | -1.16 |
| O vacancy | 0.08 | 1.77 |
| Zn-TOP | / | 1.77 |

Table S8. DFT calculated adsorption energies of CHO on pristine CeO2 (111) and Zn substituted CeO2 (111) during the chemical looping dry reforming of methane to produce syngas process.

| Adsorption site | Pristine CeO2(111) Eads/eV | Zn substituted CeO2 (111) Eads/eV |
| --- | --- | --- |
| Ce-TOP | -1.58 | -0.54 |
| Hollow | -1.59 | -3.85 |
| O-TOP | -3.98 | -4.09 |
| O-O bridge | -0.77 | -0.30 |
| Ce-O bridge | -4.04 | -3.62 |
| O vacancy | -1.57 | 0.64 |
| Zn-TOP | / | -1.11 |

Table S9. DFT calculated adsorption energies of CH2O on pristine CeO2 (111) and Zn substituted CeO2 (111) during the chemical looping dry reforming of methane to produce syngas process.

| Adsorption site | Pristine CeO2(111) Eads/eV | Zn substituted CeO2 (111) Eads/eV |
| --- | --- | --- |
| Ce-TOP | -1.21 | -0.59 |
| Hollow | -1.76 | -0.97 |
| O-TOP | -1.75 | -1.04 |
| O-O bridge | -1.16 | -1.03 |
| Ce-O bridge | -1.76 | -1.31 |
| O vacancy | -1.22 | 0.86 |
| Zn-TOP | / | -1.05 |

Table S10. DFT calculated adsorption energies of CH3O on pristine CeO2 (111) and Zn substituted CeO2 (111) during the chemical looping dry reforming of methane to produce syngas process.

| Adsorption site | Pristine CeO2(111) Eads/eV | Zn substituted CeO2 (111) Eads/eV |
| --- | --- | --- |
| Ce-TOP | -3.92 | -1.64 |
| Hollow | -3.90 | -1.75 |
| O-TOP | -3.93 | -0.05 |
| O-O bridge | -9.90 | -0.13 |
| Ce-O bridge | -3.93 | -1.61 |
| O vacancy | -3.72 | 1.65 |

Fig. S1 DFT calculated the charge-density difference of M-substituted CeO2 (111) (M = Ag, Au, CO, Hf, Cr, In, Mg, Mo, Na, Nb, Ni, Pd)

Fig. S2 DFT calculated the charge-density difference of M-substituted CeO2 (111) (M = Pt, Rh, Fe, Ga, W, Y, Zn, Ge, Ir, K, La, Mn)

Fig. S3 DFT calculated the charge-density difference of M-substituted CeO2 (111) (M = Os, Pr, Rb, Re, Ru, Sb, Sc, Sm, Sr, Ta, Ti, V, Zr, Al, Ca, Cd)