Electronic Supplementary Material

Comprehensive mechanism and microkinetic model-driven rational screening of 4N-modulated single-atom catalysts for selective oxidation of benzene to phenol

Rong Fan1, Jiarong Lu1, Hao Yan ()1, Yibin Liu1, Xin Zhou2, Hui Zhao1, Xiang Feng1, Xiaobo Chen ()1, Chaohe Yang1

1 State Key Laboratory of Heavy Oil Processing, China University of Petroleum, Qingdao 266580, China

2 College of Chemistry and Chemical Engineering, Ocean University of China, Qingdao 266100, China

E-mails: haoyan@upc.edu.cn (Yan H); chenxiaobo@upc.edu.cn (Chen X)

Microkinetic analysis

Microkinetic analysis was carried out under typical benzene oxidation reaction conditions at 298.15K [1]. And the oxidation of benzene over metal single catalysts could be regarded as a gas phase reaction in our work [2]. The TOF could be obtained from the mean-field model calculated by the elementary steps [3]. In addition, the rate-determining step is the C-H bond activation of C6H6 (5) judged by the Gibbs free energy analysis plot, which has been confirmed by other literature and our early work [2, 4, 5]. The detailed elementary steps are as follows:

(1)H2O2(g) + * → H2O2*

(2)H2O2* + * → O* + H2O*

(3)H2O* → H2O(g) + *

(4)C6H6(g) + * → C6H6*

(5)C6H6* + O* → C6H6O* + *     (Rate determining step)

(6)C6H6O* → C6H5OH*

(7)C6H5OH* → C6H5OH(g) + *

Where * represents the active site on the catalytic surface.

Step 5 could be regarded as the rate-determining step and other steps as the quasi-equilibrium step.

r1=k1PH2O2θ* = r-1=k-1θH2O2

r2=k2θH2O2θ* = r-2=k-2θOθH2O

r3=k3θH2O = r-3=k-3PH2Oθ*

r4=k4PC6H6θ* = r-4=k-4θC6H6

r5=k5θC6H6θO

r6=k6θC6H6O = r-6=k-6θC6H5OH

r7=k7θC6H5OH = r-7=k-7PC6H5OHθ*

The coverages are hence:

θH2O2 = K1PH2O2θ*                                                                  with K1=k1/k-1

θO = K2θH2O2θ*/θH2O                                                                with K2=k2/k-2

θH2O = PH2Oθ*/K3                                                                   with K3=k3/k-3

θC6H6 = K4PC6H6θ*                                                                   with K4=k4/k-4

θC6H5OH = PC6H5OHθ*/K7                                                            with K7=k7/k-7

Since the sum of all coverages equals 1:

1=θ* +θH2O2 +θH2O +θC6H6 +θC6H5OH

θ* =1/(K1PH2O2 +PH2O/K3 +K4PC6H6 +PC6H5OHθ*/K7)

The total reaction rate is often controlled by the speed control step. So the turnover frequency can be written as:

TOF=r5= k5θC6H6θO=k5K1K2K3K4PC6H6PH2O2θ*2/PH2O

k5=kBThexp-ΔG5+kBT

Ki=exp-ΔGikBT

Deep oxidation of phenol to benzoquinone is an important side reaction of the oxidation of benzene to phenol, and the deduction process of its microscopic dynamics is as follows:

- H2O2(g) + * → H2O2*

- H2O2* + * → O* + H2O*

- H2O* → H2O(g) + *

- C6H5OH(g) + * → C6H5OH*

- C6H5OH* + O* → OC6H5OH* + *

- OC6H5OH* → HOC6H4OH*

- HOC6H4OH* + * → HOC6H4O* + H*    (Rate determining step)

- HOC6H4O* + H* → OC6H4O* + H2*

- OC6H4O* → OC6H4O(g) + *

- H2* → H2(g) + *

1=θ* +θH2O2 +θH2O +θC6H5OH+θOC6H4O+θH2

Similar to the kinetic equation in the oxidation of benzene to phenol, the TOF of the side reaction can be obtained as follows：

TOF^=r7= k7θC6H6θO=k7K1K2K3K4K5K6PC6H5OHPH2O2θ*2/PH2O

The selectivity is defined by the rate of C6H5OH formation divided by the sum of rates of C6H5OH and OC6H4O formation:

S=TOF/(TOF+TOF^)

Figure S1. (a) Top and side views of the optimized TM1-N4/C structure. (b) Formation energies of TM1-N4/C. (c) Binding energy of TM1-N4/C and cohesive energy of TM atom. (d) Hirshfeld charge of TM and N atoms.

Figure S2. Electron density distribution map of the TM1-N4-C configuration. Blue indicates the loss of electrons, and red indicates the acquisition of electrons.

Figure S3. The pathway of H2O2 oxidizing benzene to phenol on TM1-N4-C configurations.

Figure S4. Gibbs free energy change of H2O2 oxidation benzene to phenol on TM1-N4O1 support (TM=Cr, V, Cu, Zn).

Figure S5. Reactant configuration of H2O2 activation elementary reaction on TM1N4O2 support

Figure S6. Product configuration of H2O2 activation elementary reaction and their electron density distribution on (a) Cu1N4O2 and (b) Zn1N4O2 support.

Figure S7. DOSs projected onto the d orbital of the metal atom and p orbital of inert oxygen and nitrogen on Zn1N4O2 configuration.

Figure S8. Adsorption energy for C6H6 over TM1-N4O2 and adsorption energy for C6H5OH over TM1-N4O1.

Figure S9. The d band positions of metal single atom in TM1N4O1 (TM = Ni, Co, Pt, Mn, Fe, Zn, Cu, V, Cr and Mn) as produced by DFT calculations.

Figure S10. Relative energy change of phenol to hydroquinone over TM1-N4O1 support.

Figure S11. Relative energy change of hydroquinone to benzoquinone over TM1-N4 support (TM=Cr, V, Cu, Zn).

Table S1. Gibbs free energy change of benzene to phenol by H2O2 oxidation on TM1-N4O1 support.

|  | Fe1-N4O1/eV | Co1-N4O1/eV | Mn1-N4O1/eV | N1-N4O1/eV | Pt1-N4O1/eV |
| --- | --- | --- | --- | --- | --- |
| support | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| H2O2* | -0.01 | -0.05 | 0.18 | 0.16 | -0.02 |
| TS1 | 0.06 | 0.43 | 1.01 | 0.70 | 0.01 |
| O*+H2O* | -0.97 | -0.62 | -0.87 | 0.01 | -0.84 |
| O* | -0.83 | -0.36 | -0.77 | 0.34 | -0.72 |
| O*+C6H6* | -0.80 | -0.50 | -0.77 | 0.39 | -0.14 |
| TS2 | 0.06 | 0.19 | 0.25 | 0.96 | 0.54 |
| O*+C6H6O* | -0.71 | -0.78 | -0.35 | -0.24 | -0.36 |
| TS3 | -0.17 | -0.31 | 0.23 | 0.13 | 0.28 |
| O*+C6H6OH* | -2.85 | -2.97 | -2.71 | -2.65 | -2.26 |
| support | -2.14 | -2.77 | 1.46 | -2.66 | -2.72 |

|  | Pd1-N4O1/eV | Cu1-N4O1/eV | Zn1-N4O1/eV | V1-N4O1/eV | Cr1-N4O1/eV |
| --- | --- | --- | --- | --- | --- |
| support | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| H2O2* | -0.96 | 0.25 | 0.47 | -0.01 | -0.01 |
| TS1 | -0.37 | 1.85 | 2.09 | 0.48 | 0.29 |
| O*+H2O* | -1.43 | -0.36 | -0.05 | 0.14 | -0.32 |
| O* | 0.07 | -0.42 | -0.20 | -0.26 | -0.43 |
| O*+C6H6* | 0.72 | -0.49 | -0.21 | 0.04 | -0.25 |
| TS2 | 1.12 | 0.24 | 0.81 | 1.45 | 1.28 |
| O*+C6H6O* | 0.26 | -1.07 | -0.84 | -2.48 | -2.26 |
| TS3 | 0.70 | -0.51 | -0.16 | -0.32 | -0.17 |
| O*+C6H6OH* | -2.01 | -3.24 | -3.13 | -3.96 | -3.03 |
| support | -2.70 | -2.90 | -2.47 | -1.83 | 1.29 |

Table S2. Relative energy change of phenol to hydroquinone on TM1-N4O1 support.

|  | Fe1-N4O1/eV | Co1-N4O1/eV | Mn1-N4O1/eV | N1-N4O1/eV | Pt1-N4O1/eV |
| --- | --- | --- | --- | --- | --- |
| O* | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| O*+C6H5OH* | -0.64 | -0.68 | -4.74 | -0.71 | 0.03 |
| TS1 | 0.31 | 0.10 | -3.23 | -0.07 | 0.85 |
| HOC6H5O* | -0.14 | -1.05 | -3.31 | -1.72 | -2.83 |
| TS3 | 1.35 | -0.24 | -1.49 | -1.32 | -0.66 |
| HOC6H4OH* | -1.33 | -2.62 | -4.10 | -4.11 | -3.56 |

|  | Pd1-N4O1/eV | Cu1-N4O1/eV | Zn1-N4O1/eV | V1-N4O1/eV | Cr1-N4O1/eV |
| --- | --- | --- | --- | --- | --- |
| O* | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| O*+C6H5OH* | -4.63 | -0.80 | -0.50 | -1.01 | -4.85 |
| TS1 | -4.13 | -0.19 | 0.10 | 4.93 | -2.60 |
| HOC6H5O* | -7.95 | -1.86 | -1.74 | 1.87 | -2.42 |
| TS3 | -5.70 | -1.30 | -0.66 | 4.07 | -0.77 |
| HOC6H4OH* | -8.59 | -4.16 | -3.31 | 1.13 | -2.64 |

Table S3. Relative energy change of hydroquinone to benzoquinone on TM1-N4 support.

|  | Fe1-N4/eV | Co1-N4/eV | Mn1-N4/eV | N1-N4/eV | Pt1-N4/eV |
| --- | --- | --- | --- | --- | --- |
| support | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| HOC6H4OH* | 0.56 | 0.32 | -1.30 | -0.18 | 0.18 |
| TS3 | 3.87 | 3.44 | 1.92 | 3.06 | 4.43 |
| HOC6H4O* +H* | 1.47 | 1.71 | -0.30 | 1.95 | 2.20 |
| TS4 | 7.70 | 3.77 | 1.89 | 7.08 | 4.55 |
| OC6H4O* +H2* | 1.74 | 1.90 | -0.32 | 1.67 | 1.93 |

|  | Pd1-N4/eV | Cu1-N4/eV | Zn1-N4/eV | V1-N4/eV | Cr1-N4/eV |
| --- | --- | --- | --- | --- | --- |
| support | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| HOC6H4OH* | -0.62 | -0.67 | -0.88 | -1.03 | 0.76 |
| TS3 | 3.94 | 2.53 | 1.96 | 2.63 | 2.56 |
| HOC6H4O* +H* | 1.79 | 1.39 | 0.65 | 1.88 | 0.75 |
| TS4 | 3.50 | 2.87 | 5.56 | 4.16 | 2.62 |
| OC6H4O* +H2* | 1.01 | 0.96 | 0.69 | -0.86 | 0.44 |

Table S4. Comparison of the performance of benzene oxidation to phenol over Fe/Co/CuN4 catalyst

| Catalyst | Reaction Temperature(℃) | Time (h) | Benzene Conversion(%) | Phenol Selectivity(%) | Reference |
| --- | --- | --- | --- | --- | --- |
| FeN4 SA/CNS | 25 | 24 | 22 | 91 | Nat Commun 9, 3861(2018) |
| NiN4 SA/CN | 25 | 24 | 38 | 90 | J. Am. Chem. Soc. 2017, 139, 10976-10979 |
| CoN4 SA/CNS | 25 | 24 | 58 | 94 | Nat Commun 9, 3861(2018) |
| Cu-N2/HCNS | 25 | 24 | 81.2 | 86.6 | iScience 2019, 22, 97-108 |
| Cu SAC/ S-N | 25 | 48 | 60..2 | 85 | J. Am. Chem. Soc. 2020, 142, 12643-12650 |

1   Zhu Y Q, Sun W M, Luo J, Chen W X, Cao T, Zheng L R, Dong J C, Zhang J, Zhang M L, Han Y H, et al. A cocoon silk chemistry strategy to ultrathin N-doped carbon nanosheet with metal single-site catalysts. Nature Communications, 2018, 9(1): 3861

2   Fan R, Li R Y, Wang X P, Kuang X H, Li J B, Liu Y B, Yan H, Zhou X, Zhao H, Feng X, Chen X B, Yang C H. Theoretical study of the local environment of Co-NxCy structure for selective oxidation of benzene to phenol. Molecular Catalysis, 2024, 553: 113795

3  Li S F, Yan H, Liu Y B, Chen X B, Zhou X, Feng X, Yang C H. Rational screening of transition metal single-atom-doped ZSM-5 zeolite catalyst for naphtha cracking from microkinetic analysis. Chemical Engineering Journal, 2022, 445: 136670

4   Pan Y, Chen Y J, Wu K L, Chen Z, Liu S J, Cao X, Cheong W C, Meng T, Luo J, Zheng L R, C, et al. Regulating the coordination structure of single-atom Fe-NxCy catalytic sites for benzene oxidation. Nature Communications, 2019, 10(1): 4290

5  Bu F L, Chen C Q, Yu Y, Hao W T, Zhao S C, Hu Y F, Qin Y. Boosting Benzene Oxidation with a Spin‐State‐Controlled Nuclearity Effect on Iron Sub‐Nanocatalysts. Angewandte Chemie International Edition, 2022, 62(3).