Electronic Supplementary Material

Fe/Ru synthesized by hydrothermal deposition on hyper-crosslinked polystyrene as promising Fischer-Tropsch catalyst

Mariia E. Markova1, Antonina A. Stepacheva ()1, Alexey V. Bykov1, Yurii V. Larichev2, Valentin Y. Doluda1, Mikhail G. Sulman1, Lioubov Kiwi-Minsker1,3

1 Tver State Technical University, Tver 170026, Russia

2 Boreskov Institute of Catalysis SB RAS, Novosibirsk 630090, Russia

3 Ecole Polytechnique Fédérale de Lausanne, ISIC-EPFL, Lausanne CH-1015, Switzerland

E-mail: a.a.stepacheva@mail.ru

Figure S1. FTIR-spectra of the initial HPS and the polymer treated in catalyst synthesis conditions

| (a) | (b) |
| --- | --- |
| (c) | (d) |
| (e) | (f) |

## Figure S2. Nitrogen adsorption-desorption isotherms and differential curve of pore size distribution for 2%-Fe-HPS (a, b), 1%-Ru-HPS (c, d), and 2%-Fe-1%-Ru-HPS (e, f)

## Figure S3. TSM image, two-dimentiona Fourier spectra and electronogramm for 2%-Fe-HPS

| (a) | (b) |
| --- | --- |
| (c) | (d) |

## Figure S4. The survey spectra of the samples of initial HPS (a), 2%-Fe-HPS (b), 1%-Ru-HPS (c), and 2%-Fe-1%-Ru-HPS (d)

Table S1. Surface composition of the catalyst samples

| Element | Surface concentration, at. % |  |  |  |
| --- | --- | --- | --- | --- |
|  | HPS | 2%-Fe-HPS | 1%Ru-HPS | 2%Fe-1%Ru-HPS |
| C | 79.17 | 92.63 | 91.20 | 90.15 |
| O | 17.68 | 6.80 | 6.94 | 7.32 |
| Cl | 1.35 | - | - | - |
| Si | 0.43 | - | - | - |
| S | 0.32 | - | - | - |
| N | 1.04 | - | - | - |
| Na | - | 0.21 | 0.12 | 0.16 |
| Fe | - | 0.36 | - | 0.72 |
| Ru | - | - | 1.74 | 1.65 |

| (a) | (b) |
| --- | --- |

## Figure S5. High-resolution spectra of O 1s sublevel for 2%-Fe-HPS (a), and 2%-Fe-1%-Ru-HPS (b)

| (a) | (b) |
| --- | --- |

## Figure S6. High-resolution spectra for Fe 2p, C1s, and Ru 3d sublevels for as-synthesized 2%-Fe-HPS (a), and 1%-Ru-HPS (b)

## Figure S7. Possible reaction scheme of the liquid-phase FTS over Ru-Fe-HPS

## Figure S8. Particle-size distribution obtained by SAXS for 2%-Fe-HPS, 2%Fe-1%Ru-HPS, and 10%-Fe-1%-Ru-HPS