Electronic Supplementary Material

Selective C–C coupling via copper atom reconfiguration in CO2 electroreduction

Linlin Zhou1, Yang Zhong2, Kai Sun3, Benqiang Tian1, Haoyang Wu1, Wei Liu1, Tong Wan1, Huijun Xin4, Chen Deng5, Xiaojie Li5, Jinjie Fang5, Geoffrey I.N. Waterhouse3, Yun Kuang ()4, Daojin Zhou ()1, Xiaoming Sun ()1

1State Key Laboratory of Chemical Resource Engineering, Beijing University of Chemical Technology, Beijing 100029, China

2 Weichai Power Co., Ltd., Weifang 261061, China

3 School of Chemical Sciences, the University of Auckland, Auckland 1010, New Zealand

4 Ocean Hydrogen Energy R&D Center, Research Institute of Tsinghua University in Shenzhen, Shenzhen 518057, China

5 PetroChina Shenzhen New Energy Research Institute Co., Ltd.

E-mails: kuangy@tsinghua-sz.edu.cn (Kuang Y); zhoudj@buct.edu.cn (Zhou D); sunxm08@126.com (Sun X)

Supplementary Figures:

Figure S1. Morphological characterisation of Cu-50. (a) HAADF image and (b) EDS-mapping of Cu.

Figure S2. Phase composition and crystal structure of Cu foil and Cu-50. XRD patterns of Cu foil and Cu-50.

Figure S3. Morphological characterisation of Cu-15. SEM image of Cu-15.

Figure S4. Morphological characterisation of Cu-75. SEM image of Cu-75.

Figure S5. Morphological characterisation of 0-Cu-50. SEM image of 0-Cu-50.

Figure S6. Morphological characterisation of 10-Cu-50. (a-c) SEM images of 10-Cu-50.

Figure S7. Chemical structure of Cu foil and Cu-50. S 2p XPS spectra of Cu foil and Cu-50.

Figure S8. CER performance of restructured Cu cathodes. LSV curves of (a) Cu foil, (b) Cu-50, (c) Cu-15, (d) Cu-75 and (e) 10-CV-50 collected at a scanning rate of 5 mV/s in an N2/CO2-saturated 0.1 M KCl aqueous solution.

Figure S9. CER performance of the restructured Cu cathodes. Faradaic efficiencies of all products during CER on (a) Cu foil, (b) Cu-15, (c) Cu-50, (d) Cu-75, (e) 0-Cu-50 and (f) 10-Cu-50 in a CO2-saturated 0.1 M KCl aqueous solution.

Figure S10. CER performance of the restructured Cu cathodes. Faradaic efficiencies towards C2+, C1 and H2 during CER on (a) Cu foil, (b) Cu-15, (c) Cu-50, (d) Cu-75, (e) 0-Cu-50 and (f) 10-Cu-50 in a CO2-saturated 0.1 M KCl aqueous solution.

Figure S11. Cyclic voltammetry curves for ECSA determination. CV data for (a) Cu foil and (b) Cu-50. The measurements were performed at various scan rates (60, 80, 100, 120, 140, 160, 180 and 200 mV s−1) from −0.28 to −0.185 VRHE.