Electronic Supplementary Material

Facile fabrication of CdIn2S4/TiO2 heterojunction for enhanced solar light efficient CO2 reduction

Xiaoyu Ma1*, Longlong Wang1*, Houde She ()1, Yu Zhou1, Lei Wang1, Jingwei Huang1, Qizhao Wang ()1,2

1 College of Chemistry and Chemical Engineering, Northwest Normal University, Lanzhou 730070, China

2 School of Environment Science and Engineering, Chang'an University, Xi'an 710064, China

E-mails: shehoude@126.com (She H); wangqizhao@163.com, qizhaosjtu@gmail.com (Wang Q)

* These authors contributed equally to this work.

Figure S1. Transient photocurrent responses of TiO2, CdIn2S4 and 3% CIS/TiO2 composite at 0.1 V vs. Ag/AgCl.

Figure S2. Nyquist plots of EIS measurements on TiO2, CdIn2S4 and 3% CIS/TiO2 composite.

Figure S3. PL spectra of TiO2 and x% CIS/TiO2 composite.

Figure S4. SPV of TiO2, CdIn2S4 and 3% CIS/TiO2 composite.

Figure S5. Production rates of CO and CH4 over 3% CIS/TiO2 composite under various reaction conditions. 
Supplementary Table S1. Performance comparison of TiO2-based, CdIn2S4-based and other similar photocatalysts for CO2 reduction.

| Photocatalysts | Light source | CO evolution rate (µmol·g−1·h−1) | CH4 evolution rate (µmol·g−1·h−1) | Reference |
| --- | --- | --- | --- | --- |
| CdIn2S4/TiO2 | 300 W Xe lamp | 18.32 | 1.03 | This work |
| TiO2@ZnIn2S4 | 300 W Xe lamp | 9.28 | 4.26 | [1] |
| ZnIn2S4/TiO2 | 300 W Xe lamp | — | 1.13 | [2] |
| Cu/TiO2 | 300 W Xe lamp | 1.65 | — | [3] |
| TiO2/C3N4/Ti3C2 | 350 W Xe lamp | 4.39 | 1.20 | [4] |
| WO3/TiO2/ Cu2ZnSnS4 | Xe lamp (λ >420nm) | 15.37 | 1.69 | [5] |
| WO3 QDs/CdIn2S4 | 300 W Xe lamp (λ >420nm) | 8.20 | 1.60 | [6] |
| Ce/Zr-UiO-66-NH2 /CdIn2S4 | 300 W Xe lamp | 6.01 | 1.23 | [7] |
| In2O3/In2S3 | 300 W Xe lamp | 12.22 | — | [8] |
| CdWO4/CdS | 300 W Xe lamp | 4.16 | 0.35 | [9] |
| CdS/WO3 | 300 W Xe lamp (λ >420nm) | — | 1.02 | [10] |

Supplementary References

1. Wang L B, Cheng B, Zhang L Y, Yu J G. In situ irradiated XPS investigation on S-scheme TiO2@ZnIn2S4 photocatalyst for efficient photocatalytic CO2 reduction. Small, 2021, 17(41): 2103447

2. Yang G, Chen D M, Ding H, Feng J J, Zhang J Z, Zhu Y F, Hamid S, Bahnemann D W. Well-designed 3D ZnIn2S4 nanosheets/TiO2 nanobelts as direct Z-scheme photocatalysts for CO2 photoreduction into renewable hydrocarbon fuel with high efficiency. Applied Catalysis B: Environmental, 2017, 219: 611-618

3. Jiang Z Y, Sun W, Miao W K, Yuan Z M, Yang G H, Kong F G, Yan T J, Chen J C, Huang B B, An C H, Ozin G A. Living atomically dispersed Cu ultrathin TiO2 nanosheet CO2 reduction photocatalyst. Advanced Science, 2019, 6(15): 1900289

4. He F, Zhu B C, Cheng B, Yu J G, Ho W K, Macyk W. 2D/2D/0D TiO2/C3N4/Ti3C2 MXene composite S-scheme photocatalyst with enhanced CO2 reduction activity. Applied Catalysis B: Environmental, 2020, 272: 119006

5. Raza A, Shen H L, Haidry A A, Sun L H, Liu R, Cui S C. Studies of Z-scheme WO3-TiO2/Cu2ZnSnS4 ternary nanocomposite with enhanced CO2 photoreduction under visible light irradiation. Journal of CO2 Utilization, 2020, 37: 260-271

6. Zhang Z Z, Cao Y X, Zhang F H, Li W J, Li Y L, Yu H, Wang M Y, Yu H B. Tungsten oxide quantum dots deposited onto ultrathin CdIn2S4 nanosheets for efficient S-scheme photocatalytic CO2 reduction via cascade charge transfer. Chemical Engineering Journal, 2022, 428: 131218

7. Li S M, Li H, Wang Y A, Liang Q, Zhou M, Guo D F, Li Z Y. Mixed-valence bimetallic Ce/Zr-NH2-UiO-66 modified with CdIn2S4 to form S-scheme heterojunction for boosting photocatalytic CO2 reduction. Separation and Purification Technology, 2024, 333: 125994

8. Yang J M, Zhu X W, Yu Q, He M Q, Zhang W, Mo Z, Yuan J J, She Y B, Xu H, Li H M. Multidimensional In2O3/In2S3 heterojunction with lattice distortion for CO2 photoconversion. Chinese Journal of Catalysis, 2022, 43(5): 1286-1294

9. Li Y Y, Wei Z H, Fan J B, Li Z J, Yao H C. Photocatalytic CO2 reduction activity of Z-scheme CdS/CdWO4 catalysts constructed by surface charge directed selective deposition of CdS. Applied Surface Science, 2019, 483: 442-452

10. Jin J, Yu J G, Guo D P, Cui C, Ho W K. A hierarchical Z-scheme CdS-WO3 photocatalyst with enhanced CO2 reduction activity. Small, 2015, 11(39): 5262-5271