Electronic Supplementary Material

Synergistic La2O3-La(OH)3 interface engineering enables deep and durable dehydrogenation of 12H-N-propylcarbazole over Pd/Al2O3 catalysts

Li Liu1,2, Tian Wu1,2, Yu Zhang1,2, Chenggen Li3, Yuan Dong3, Ming Yang ()3

1  Hubei Key Laboratory of Purification and Application of Plant Anti-cancer Active Ingredients, School of Chemistry and Life Science, Hubei University of Education, Wuhan 430205, China

2  Institute of Materials Research and Engineering (IMRE), Hubei University of Education, Wuhan 430205, China

3  Hubei Hydrogen Energy Technology Innovation Center, Faculty of Materials Science and Chemistry, China University of Geosciences, Wuhan 430074, China

E-mail: yangming8180@gmail.com

1. Supplementary Methods

Catalyst Activation Energy Measurement:

To determine the activation energies for each stage of 12H-NPCZ dehydrogenation, reaction data at various temperatures were fitted using MATLAB software. The equilibrium rate constants k1, k2, and k3 for each stage were calculated by nonlinear least squares fitting. The concentrations of 12H-NPCZ, 8H-NPCZ, 4H-NPCZ, and NPCZ are denoted as A, B, C, and D, respectively.

Ak1Bk2Ck3D

-dAdT=k1A

dBdT=k1A-k2B

dCdT=k2B-k3D

dDdT=k3C

By plotting the natural logarithm of the rate constants k1, k2, and k3 against 1/T, Arrhenius plots for each stage were obtained. The activation energies for each stage were then calculated according to the Arrhenius equation (1):

Lnk=-EaRT+C	(1)

2. Supplementary Figures

Figure S1 (a) Pore size distribution curves of LaxAlO supports; (b) Pore size distribution curves of Pd/LaxAlO catalysts.

Figure S2 TEM images and particle size distributions of (a) Pd/La5AlO, (b) Pd/La15AlO, and (c) Pd/La20AlO catalysts.

Figure S3 Product distribution profiles during dehydrogenation over (a) Pd/Al2O3 (b) Pd/La5AlO, (c) Pd/La15AlO, and (d) Pd/La20AlO catalysts.

Figure S4 XPS spectra of Pd/La10AlO catalysts after cycle: (a) La 3d region; (b) O 1s region; (c) Pd 3d region.

3. Supplementary Tables

Table S1 Textural properties of supports and catalysts.

| Catalysts | BET Surface Area | Pore Volume | Pore Size |
| --- | --- | --- | --- |
|  | m2/g | cm3/g | nm |
| Al2O3 | 240 | 0.52 | 8.8 |
| La5AlO | 241 | 0.82 | 11.8 |
| La10AlO | 224 | 1.07 | 12.2 |
| La15AlO | 232 | 0.71 | 10.6 |
| La20AlO | 211 | 0.69 | 11.2 |
| Pd/Al2O3 | 214 | 0.51 | 7.7 |
| Pd/La5AlO | 209 | 0.67 | 9.3 |
| Pd/La10AlO | 231 | 0.74 | 10.2 |
| Pd/La15AlO | 198 | 0.62 | 8.5 |
| Pd/La20AlO | 207 | 0.58 | 9.8 |