Electronic Supplementary Material

The role of Li2CO3 promoter and steam in increasing C2H4/C2H6 selectivity in chemical looping oxidative coupling of CH4 over Mn-Na2WO4/Support catalysts

Jianshu Li1,2*, Juan Chen1,2*, Anna Zanina2, Vita A. Kondratenko2, Henrik Lund2, Wen Jiang1, Hanyang Zhou1, Yuming Li1, Guiyuan Jiang ()1, Evgenii V. Kondratenko ()2

1 State Key Laboratory of Heavy Oil Processing, China University of Petroleum Beijing, Beijing 102249, China

2 Leibniz Institut für Katalyse e.V.,  18059 Rostock, Germany

E-mails: jianggy@cup.edu.cn (Jiang G); evgenii.kondratenko@catalysis.de (Kondratenko E V)

*These authors contributed equally to this work.

Figure S1. XRD patterns of the Mn-Na2WO4/Support catalysts with (red lines) and without (black lines) Li2CO3. Identified phases: Li2(Si2O5) Monoclinic (PDF-No. 01-072-0102), SiO2 Hexagonal (PDF-No. 01-087-2096), Na2WO4 (PDF-No. 01-084-6510), MnWO4 (PDF-No. 01-080-0133), LiAlSiO4 Hexagonal (PDF-No. 01-070-1574), LiAl(Si2O6) Hexagonal (PDF-No. 01-073-2336), LiAl(Si2O6) Tetragonal (PDF-No. 01-071-2058), Mn7SiO12 (PDF-No. 01-071-1791), Li2WO4 Tetragonal (PDF-No. 01-071-1735), TiO2 (PDF-No. 01-077-0440), Mn2O3 (PDF-No. 01-078-0390), (Li0.84Mn0.16)(Li0.16TiMn0.84)O2 (PDF-No. 01-075-7715), CeO2 (PDF-No. 01-080-8533), Li2MnO3 (PDF-No. 01-078-5048).

Figure S2. The selectivity to CO versus CH4 conversion over (a) SiO2-, (b) AlSiOx-, (c) CeO2-or (d) TiO2-supported MnNa2WO4-based catalysts prepared with and without Li2CO3. Reaction conditions: T = 850 °C , single pulsing of CH4/H2O/Ar =40/55/5, catalyst amount: 50-400 mg.

Figure S3. The selectivity to CO2 versus CH4 conversion over (a) SiO2-, (b) AlSiOx-, (c) CeO2-or (d) TiO2-supported MnNa2WO4-based catalysts prepared with and without Li2CO3. Reaction conditions: T = 850 °C , single pulsing of CH4/H2O/Ar =40/55/5, catalyst amount: 50-400 mg.

Figure S4. The sum of C2-hydrocarbons selectivity and CH4 conversion versus CH4 conversion over (a) SiO2-, (b) AlSiOx-, (c) CeO2-or (d) TiO2-supported MnNa2WO4-based catalysts prepared with and without Li2CO3. Reaction conditions: T = 850 °C, single pulsing of CH4/H2O/Ar =40/55/5, catalyst amount: 50-400 mg.

Figure S5 CH4 conversion over the Mn-Na2WO4/Support catalysts prepared with and without Li2CO3. Reaction conditions: single pulsing of CH4/H2O/Ar = 40/30/30; 300 mg of catalyst; T = 850 °C.

Figure S6. XRD patterns of the M2CO3-Mn-Na2WO4/AlSiOx (M = Li, Na, K) catalysts. Identified phases: LiAl(Si2O6) Hexagonal (PDF-No. 01-073-2336), LiAl(Si2O6) Tetragonal (PDF-No. 01-071-2058), Mn7SiO12 (PDF-No. 01-071-1791), MnWO4 (PDF-No. 01-080-0133),  Li2WO4 Tetragonal (PDF-No. 01-071-1735), NaAlSiO4 (PDF-No. 00-035-0424), KAlSiO4 (PDF-No. 00-066-0070).

Figure S7. CL-OCM performance of Li2CO3-MnNa2WO4/AlSiOx and LiNO3-MnNa2WO4/AlSiOx with the same Li loading. Reaction conditions: T = 850 °C, single pulsing of CH4/H2O/Ar =40/55/5, catalyst amount: 300 mg.

Figure S8. SEM images of (a) Mn-Na2WO4/AlSiOx, (b) 5Li2CO3-Mn-Na2WO4/AlSiOx, (c) 10Li2CO3-Mn-Na2WO4/AlSiOx, and (d) 20Li2CO3-Mn-Na2WO4/AlSiOx,

Figure S9. (a) Methane conversion and (b) selectivity to C2-hydrocarbons over XLi2CO3-Mn-Na2WO4/AlSiOx (X =0,5,10,20 wt%). Reaction conditions: T = 850 °C, single pulsing of CH4/H2O/Ar =40/55/5, catalyst amount: 200 mg.

Figure S10. XRD patterns of the xLi2CO3-Mn-Na2WO4/Siral70 (x =0,5,10,20 wt%) catalysts. Identified phases: MnWO4 (PDF-No. 01-080-0133), LiAl(Si2O6) Hexagonal (PDF-No. 01-073-2336), LiAl(Si2O6) Tetragonal (PDF-No. 01-071-2058), Mn7SiO12 (PDF-No. 01-071-1791), Li2WO4 Tetragonal (PDF-No. 01-071-1735).

Figure S11. A correlation between the selectivity to C2-hydrocarbons and the BET surface area of XLi2CO3-Mn-Na2WO4/AlSiOx (X =0,5,10,20 wt%) catalysts.

Figure S12. (a) Effect of water content on methane conversion over Li2CO3-Mn-Na2WO4/AlSiOx, (b) methane conversion obtained over the Li2CO3-Mn-Na2WO4/AlSiOx catalyst used in the CL-OCM reaction with or without treatment in in H2. Reaction conditions: single pulsing of CH4/H2O/Ar =40/(0-55)/(5-60); 300 mg of catalyst; T = 850°C.

Figure S13. XRD patterns of fresh and spent (after 90 CH4/air cycles) Li2CO3-Mn-Na2WO4/AlSiOx catalyst samples.

Figure S14. (a) CO2 profiles obtained during temperature-programmed oxidation (TPO) of fresh and spent (after 90 CH4/air cycles) Li2CO3-Mn-Na2WO4/AlSiOx catalyst samples and (b) the corresponding amounts of CO2 determined from the TPO tests in (a).

Table S1. A survey of supported OCM catalysts exhibiting C2+-hydrocarbons selectivity above 80% at methane conversion above 10% in the reported literature.

| Catalysts | Contact time / g·s·mL-1 | CH4:O2 | X(CH4) / % | S(C2+-hydrocarbons) / % | S(C2H4) / % | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Li/MgO | 0.23 | 9.6 | 16.3 | 84 |  | [1] |
| Li/MgO | 0.23 | 9.6 | 15.4 | 83 |  | [2] |
| Li/MgO | 0.45 | 10 | 12 | 80 |  | [3] |
| Li/MgO | 0.45 | 10 | 16 | 85 |  |  |
| BaCO3/Al2O3 | 0.05 | 19 | 10.5 | 84 | 27 | [4] |
| Sr-MgO | 0.05 | 19 | 10.3 | 83 | 31 |  |
| Ba-MgO | 0.05 | 19 | 10.3 | 83 | 31 |  |
| Sm-Ba-MgO | 0.05 | 19 | 10.2 | 82 |  |  |
| Ba-Ga2O3 |  | 8 | 11 | 89.9 |  | [5] |
| Na/CaO | 0.6 | 9 | 17 | 80 |  | [6] |
| Na/CaO | 0.2 | 9.9 | 13.7 | 80 | 36 | [7] |
| Li2CaSiO4 | 1.8 | 7 | 17 | 80 |  | [8] |
| SnBaTiO3 | 0.21 | 4 | 20.77 | 84.36 |  | [9] |
| PbOx/Na4P2O7 | 6.43 | 5 | 11 | 80 |  | [10] |
| 10%BaF2/LaOF | 0.24 | 6 | 19.53 | 81.2 | 41.22 | [11] |
| 10%BaF2/LaOF | 0.24 | 9 | 16.54 | 84.55 | 23.48 |  |
| SrCO3/La2O2CO3 | 0.18 | 10.1 | 15.3 | 79.2 | 57.3 | [12] |
| SrO/La2O3/SA-5205 | 0.04 | 15.9 | 12.5 | 80.7 | 31.5 | [13] |
| La2O3/SrO/SA-5205 | 0.04 | 15.9 | 12.5 | 85.9 | 31.4 |  |
| Nd2O3/SrO/SA-5205 | 0.04 | 15.9 | 11.1 | 81.7 | 30.3 |  |
| Na2WO4/SiO2 | 1.2 | 2.5 | 13.4 | 81 | 50 | [14] |
| Mn/Na2WO4/MgO | 0.52 | 7.3 | 20 | 80 |  | [15] |
| Mn/Na2WO4/SiO2 | 1.33 | 4.6 | 33 | 80 | 50 | [16] |
| Mn/Na2WO4/SiO2 | 0.22 | 7.5 | 20 | 80 | 46 | [17] |
| 1% Mn/Na2WO4/SiO2 | 0.22 | 7.3 | 22 | 81 |  | [18] |
| Mn−Na2WO4/SiO2 |  | 4 | 20 | 81 |  | [19] |
| Mn−Na2WO4/SiO2 |  | 2.5 | 24.6 | 80.6 |  | [20] |
| Mn−Na2WO4/SiO2 |  | 3 | 19.8 | 84.3 |  |  |
| Mn−Na2WO4/SiO2 |  | 4 | 15.9 | 86.2 |  |  |
| Mn−Na2WO4/SiO2 | 0.15 | 5 | 22.3 | 82.8 |  | [21] |
| Mn−Na2WO4/SiO2 | 0.15 | 10 | 15 | 85.1 |  |  |
| Mn−Na2WO4/SiO2 | 0.15 | 10 | 12.7 | 86.9 |  |  |
| Mn−Na2WO4/SiO2 |  |  | 18 | 89 |  | [22] |
| Mn−Na2WO4/SiO2 |  |  | 21 | 87 |  |  |
| Mn−Na2WO4/SiO2 |  |  | 19 | 87 |  |  |
| Mn−Na2WO4/SiO2 |  |  | 13.2 | 93.8 |  | [23] |
| Mn−Na2WO4/SiO2 |  |  | 16.6 | 92.5 |  |  |
| Mn−Na2WO4/SiO2 |  |  | 21.2 | 87.6 |  |  |
| Li–W–Mn/SiO2 | 0.07 | 2 | 11 | 82 | 30 | [24] |
| Li–W–Mn/SiO2 | 0.07 | 3.2 | 15 | 85 | 36 |  |
| K–W–Mn/SiO2 | 0.07 | 4.6 | 20 | 88 | 46 |  |
| Li2CO3-Mn−Na2WO4/SiO2 |  |  | 10.8 | 95.4 | 56.2 | This work |
| Li2CO3-Mn−Na2WO4/SiO2 |  |  | 11.4 | 93 | 55.4 | This work |
| Li2CO3-Mn−Na2WO4/Siral70 |  |  | 13.6 | 91.3 | 55.7 | This work |
| Li2CO3-Mn−Na2WO4/Siral70 |  |  | 19 | 89 | 59.5 | This work |

# Reference

1. Korf S J, Roos J A, De Bruijn N A, Van Ommen J G, Ross J R H. Lithium chemistry of lithium doped magnesium oxide catalysts used in the oxidative coupling of methane. Applied Catalysis, 1990, 58(1): 131-146

2. Korf S J, Roos J A, Derksen J W H C, Vreeman J A, Van Ommen J G, Ross J R H. Oxidative coupling of methane over Ba/CaO catalysts: A comparison with Li/MgO. Applied Catalysis, 1990, 59(1): 291-309

3. Hoogendam G C, Seshan K, van Ommen J G, Ross J R H. Oxidative coupling of methane over doped Li/MgO catalysts. Catalysis Today, 1994, 21(2): 333-340

4. Maitra A M. Solid-state basicity as a guide to formulation of improved catalysts for oxidative coupling of methane: I. Performance evaluation. Applied Catalysis A: General, 1994, 114(1): 65-81

5. Wu K, Zanina A, Kondratenko V A, Xu L, Li J, Chen J, Lund H, Bartling S, Li Y, Jiang G, Kondratenko E V. Fundamentals of Unanticipated Efficiency of Gd2O3-based Catalysts in Oxidative Coupling of Methane. Angewandte Chemie International Edition, 2024, 63(14): e202319192

6. Déchamp N, Gamez A, Perrard A, Gallezot P. Kinetics of glucose hydrogenation in a trickle-bed reactor. Catalysis Today, 1995, 24(1): 29-34

7. Machocki A, Jezior R. Oxidative coupling of methane over a sodium-calcium oxide catalyst modified with chloride ions. Chemical Engineering Journal, 2008, 137(3): 643-652

8. Matsumoto T, Saito M, Ishikawa S, Fujii K, Yashima M, Ueda W, Motohashi T. High Catalytic Activity of Crystalline Lithium Calcium Silicate for Oxidative Coupling of Methane Originated from Crystallographic Joint Effects of Multiple Cations. ChemCatChem, 2020, 12(7): 1968-1972

9. Yaghobi N, Ghoreishy M H R. Oxidative coupling of methane in a fixed bed reactor over perovskite catalyst: A simulation study using experimental kinetic model. Journal of Natural Gas Chemistry, 2008, 17(1): 8-16

10. Machocki A, Denis A, Borowiecki T, Barcicki J. Promotion of methane conversion catalysts into higher hydrocarbons. Applied Catalysis, 1991, 72(2): 283-294

11. Chao Z S, Zhou X P, Wan H L, Tsai K R. Methane oxidative coupling on BaF2LaOF catalyst. Applied Catalysis A: General, 1995, 130(2): 127-133

12. Mimoun H, Robine A, Bonnaudet S, Cameron C J. Oxypyrolysis of natural gas. Applied Catalysis, 1990, 58(1): 269-280

13. Choudhary V R, Mulla S A R, Uphade B S. Oxidative coupling of methane over alkaline earth oxides deposited on commercial support precoated with rare earth oxides. Fuel, 1999, 78(4): 427-437

14. Yan Q J, Wang Y, Jin Y S, Chen Y. Methane oxidative coupling over Na2WO4/SiO2. Catalysis Letters, 1992, 13(3): 221-228

15. Wang D J, Rosynek M P, Lunsford J H. Oxidative Coupling of Methane over Oxide-Supported Sodium-Manganese Catalysts. Journal of Catalysis, 1995, 155(2): 390-402

16. Palermo A, Holgado Vazquez J P, Lee A F, Tikhov M S, Lambert R M. Critical influence of the amorphous silica-to-cristobalite phase transition on the performance of Mn/Na2WO4/SiO2 catalysts for the oxidative coupling of methane. Journal of Catalysis, 1998, 177(2): 259-266

17. Malekzadeh A, Khodadadi A, Abedini M, Amini M, Bahramian A, Dalai A K. Correlation of electrical properties and performance of OCM MOx/Na2WO4/SiO2 catalysts. Catalysis Communications, 2001, 2(8): 241-247

18. Malekzadeh A, Abedini M, Khodadadi A A, Amini M, Mishra H K, Dalai A K. Critical Influence of Mn on Low-Temperature Catalytic Activity of Mn/Na2WO4/SiO2 Catalyst for Oxidative Coupling of Methane. Catalysis Letters, 2002, 84(1): 45-51

19. Godini H R, Gili A, Görke O, Simon U, Hou K, Wozny G. Performance Analysis of a Porous Packed Bed Membrane Reactor for Oxidative Coupling of Methane: Structural and Operational Characteristics. Energy & Fuels, 2014, 28(2): 877-890

20. Godini H R, Xiao S, Kim M, Holst N, Jašo S, Görke O, Steinbach J, Wozny G. Experimental and model-based analysis of membrane reactor performance for methane oxidative coupling: Effect of radial heat and mass transfer. Journal of Industrial and Engineering Chemistry, 2014, 20(4): 1993-2002

21. Uzunoglu C, Leba A, Yildirim R. Oxidative coupling of methane over Mn-Na2WO4 catalyst supported by monolithic SiO2. Applied Catalysis A: General, 2017, 547(22-29

22. Fleischer V, Littlewood P, Parishan S, Schomäcker R. Chemical looping as reactor concept for the oxidative coupling of methane over a Na2WO4/Mn/SiO2 catalyst. Chemical Engineering Journal, 2016, 306(646–654

23. Zhao K, Gao Y, Wang X, Lis B M, Liu J, Jin B, Smith J, Huang C, Gao W, Wang X, Wang X, Zheng A, Huang Z, Hu J, Schömacker R, Wachs I E, Li F. Lithium carbonate-promoted mixed rare earth oxides as a generalized strategy for oxidative coupling of methane with exceptional yields. Nature Communications, 2023, 14(1): 7749

24. Dedov A G, Nipan G D, Loktev A S, Tyunyaev A A, Ketsko V A, Parkhomenko K V, Moiseev I I. Oxidative coupling of methane: Influence of the phase composition of silica-based catalysts. Applied Catalysis A: General, 2011, 406(1): 1-12