# Electronic Supplementary Material

Enhanced formic acid production for CO2 photocatalytic reduction over Pd/H-TiO2 catalyst

Huimin Gao1*, Jinpeng Zhang1*, Fangyuan Zhang1, Jieying Jing ()1,2, Wen-Ying Li ()1

1 State Key Laboratory of Clean and Efficient Coal Utilization, Taiyuan University of Technology, Taiyuan 030024, China

2 Shanxi-Zheda Institute of Advanced Materials and Chemical Engineering, Taiyuan 030000, China

E-mails: jingjieying@tyut.edu.cn (Jing J); ying@tyut.edu.cn (Li W-Y)

*These authors contributed equally to this work.

Figure S1. Schematic diagram of experimental device for photocatalytic reduction CO2

Figure S2. Total HCOOH production of different catalysts in 3 h

Figure S3. TEM image of Pd/H-TiO2 catalyst after reaction

Figure S4. The models of TiO2, H-TiO2 and Pd/H-TiO2

Figure S5. The models of Pd/H-TiO2-OV12 and Pd/TiO2

Figure S6. The charge density difference and Bader charge analysis of models with CO2 adsorption Pd-TiO2 with/without OV. Yellow and cyan represent the electron accumulation and loss, respectively (isosurfaces = 0.0002 e/Bohr3). Note: This section studies the charge transfer between CO2 and Pd/H-TiO2.

Figure S7. The charge density difference and Bader charge analysis of models with CO2 adsorption Pd-TiO2 with/without OV. Yellow and cyan represent the electron accumulation and loss, respectively (isosurfaces = 0.0002 e/Bohr3). Note: This section studies the charge transfer between CO2-Pd and H-TiO2.

Figure S8. Thermal infrared image of Pd/H-TiO2 in ultraviolet irradiation process

Figure S9. Performance of photocatalytic CO2 reduction with different carbon sources as raw materials.

Table S1. The physical characteristics of the noble-loaded and unloaded mesoporous TiO2 sanmples.

| Catalyst | Theoretical (wt%) | Actual load (wt%)a | Crystallite size (nm) b | CO2 adsorption / mmol/g |
| --- | --- | --- | --- | --- |
| TiO2 | - | - | 39.8 | 0.09 |
| H-TiO2 | - | - | 38.2 | 0.13 |
| 1 wt%Pd/H-TiO2 | 1.00 | 1.06 | 39.0 | 0.18 |

a The Pd loading amount was measured by ICP-OES;

b Estimated according to the Scherrer’s formula.

Table S2. The selected results for photocatalytic CO2 reduction in recent literature

| Catalyst | Pressure (MPa) | Catalyst amount (mg) | HCOOH production rate (mmol·g-1·h-1) | Selectivity (%) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Pd/H-TiO2 | 2.0 | 40 | 14.14 | 100 | This work |
| Cu@Cu2O | 0.1 | 10 | 0.067 | 100% | [1] |
| Cu2O/TiO2 | 0.1 | 30 | 5.240 | 99.67 | [2] |
| 3% Cu/TiO2 | 0.14 | - | 0.026 | 90.1 | [3] |
| ABU-Co | 0.1 | - | 3.452 | 99% | [4] |
| Cu/TiO2 | 0.1 | 60 | 4.03 | - | [5] |
| Pd/TiO2 | 3.0 | 20 | 0.23 | 58.5% | [6] |

Table S3. The amount of charge transferred between substances in different systems.

|  | Model | CO2(Δq) | Pd(Δq) | TiO2(Δq) |
| --- | --- | --- | --- | --- |
| CO2-TiO2 | CO2-TiO2 | -0.120 | - | +0.120 |
|  | CO2-TiO2-x-v1 | -0.127 | - | +0.127 |
|  | CO2-TiO2-x-v2 | -0.170 | - | +0.170 |
|  | CO2-TiO2-x-v12 | -0.178 | - | +0.178 |
| Pd/H-TiO2 | Pd-TiO2 | - | +0.597 | -0.597 |
|  | Pd-TiO2-x-v1 | - | +0.156 | -0.156 |
|  | Pd-TiO2-x-v2 | - | -0.035 | +0.035 |
|  | Pd-TiO2-x-v12 | - | -0.302 | +0.302 |
| CO2-Pd/H-TiO2 | CO2-Pd-TiO2 | -0.359 | +0.931 | -0.572 |
|  | CO2-Pd-TiO2-x-v1 | -0.461 | +0.521 | -0.06 |
|  | CO2-Pd-TiO2-x-v2 | -0.404 | +0.249 | -0.155 |
|  | CO2-Pd-TiO2-x-v12 | -0.405 | -0.221 | +0.626 |

References

[1] Wang H, Cheng S J, Cai X, et al. Photocatalytic CO2 reduction to HCOOH over core-shell Cu@Cu2O catalysts[J]. Catalysis Communications, 2022, 162: 106372.

[2] Zhu Q H, Deng Z S, Xie H J, et al. Investigation of concerted proton-electron donors for promoting the selective production of HCOOH in CO2 photoreduction[J]. Acs Catalysis, 2023, 13(5): 3254-3262.

[3] Gonell F, Puga A V, Julián-López B, et al. Copper-doped titania photocatalysts for simultaneous reduction of CO2 and production of H2 from aqueous sulfide[J]. Applied Catalysis B-Environmental, 2016, 180: 263-270.

[4] Al-Dolaimy F, Kzar M H, Hussein S A, et al. Incorporating of cobalt into UiO-67 Metal-organic framework for catalysis CO2 transformations: An efficient Bi-functional approach for CO2 Insertion and photocatalytic reduction[J]. Journal of Inorganic and Organometallic Polymers and Materials, 2023.

[5] Peña R, Romero R, Amado-Piña D, et al. Cu/TiO2 photo-catalyzed CO2 chemical reduction in a multiphase capillary reactor[J]. Topics in Catalysis, 2023.

[6] Jin B B, Ye X, Zhong H, et al. Light-Driven hydrogenation of bicarbonate into formate over nano-Pd/TiO2[J]. Acs Sustainable Chemistry & Engineering, 2020, 8(17): 6798-6805.