Electronic Supplementary Material

In situ growth of embedded pt nanoparticles in MIL-68(In)-derived In2O3 for enhanced CO2 hydrogenation to methanol

Yanmei Cai1,2,3, Kok Bing Tan ()1,3, Meihong Lin,1,3, Shuhan Luo1,3, Kaishu Wu1,3, Sajid Ali1,3, Guifen Du4, Lanping Huang5, Jianbang Liu5, Dongren Cai ()1, Guowu Zhan ()1,3

1College of Chemical Engineering, Academy of Advanced Carbon Conversion Technology, Huaqiao University, Xiamen 361021, China

2Department of Chemical and Biomolecular Engineering, National University of Singapore, Singapore 117585, Singapore

3Fujian Provincial Key Laboratory of Biomass Low-Carbon Conversion, Huaqiao University, Xiamen 361021, China

4Instrumental Analysis Center, Huaqiao University, Xiamen 361021, China

5Fujian Eversun Technology Co., Ltd., Putian 351156, China

E-mails: gwzhan@hqu.edu.cn (Zhan G); tankokbing@hqu.edu.cn (Tan K B); 15506@hqu.edu.cn (Cai D)

Figure S1. XRD patterns of Matériaux de l'Institut Lavoisier-68 (In), or MIL-68(In).

Figure S2. Product selectivity, CO2 conversion, and space time yield of methanol (STYMeOH) of (a, c) In2O3 and (b, d) Pt/In2O3 catalysts at different temperatures (260, 270, 280, 290, 300℃) and different pressures (10, 15, 20, 25, 30 bar). Reaction conditions: H2/CO2/He = 72%/24%/4%, and 12000 mL·gcat-1·h-1.

Figure S3. Product selectivity, and CO2 conversion of (a) In2O3 and (b) Pt/In2O3 catalysts at different GHSV (6000, 12000, 18000, 24000, 30000, and 36000 mL·gcat-1· h-1). Reaction conditions: 300℃, 3 MPa, H2/CO2/He = 72%/24%/4%.

Figure S4. (a-b) Influence of different Pt loadings on the catalytic performance of Pt/In2O3 catalyst.

Figure S5. (a, b) Influence of different Pt loadings on the catalytic performance of Pt@In2O3 catalyst.

Notes: The Pt loading was controlled by varying the volume (x = 0, 0.5, 1, 2, and 3 mL) of 19.3 mM H2PtCl6·6H2O aqueous solution added during catalyst preparation. Unless otherwise specified, Pt/In2O3 and Pt@In2O3 refer to catalysts prepared using 1 mL of H2PtCl6·6H2O solution.

Figure S6. (a) XRD patterns, and (b) crystallite size of Pt/In2O3 catalysts.

Figure S7. In-situ DRIFTS spectra of (a) Pt/In2O3-3 mL and (b) Pt@In2O3-3 mL treated by CO flow and N2 flow.

Figure S8. STY of (a) In2O3 and (b) Pt/In2O3 catalysts at different GHSV (6000, 12000, 18000, 24000, 30000, and 36000 mL·gcat-1·h-1).

Figure S9. Arrhenius plots and activation energies of CO synthesis over Pure In2O3 and Pt/In2O3 catalysts.

Table S1. The crystallite size of different catalysts

| Catalysts | Peak position/° | FWHM | Crystallite Size/nm |
| --- | --- | --- | --- |
| Pure In2O3 | 30.360 | 0.522 | 15.59 |
| Pt@In2O3 | 30.440 | 0.517 | 15.75 |
| Pt/In2O3-400 | 30.619 | 0.753 | 10.82 |
| Pt/In2O3-500 | 30.459 | 0.687 | 11.85 |
| Pt/In2O3-600 | 30.359 | 0.471 | 17.28 |
| Pt/In2O3-700 | 30.261 | 0.438 | 18.58 |

Table S2. Textural properties of different catalysts.

| Catalysts | Surface Area (m2·g-1) | Pore diameter (nm) |
| --- | --- | --- |
| MIL-68(In) | 1142.0 | 19.1 |
| Pure In2O3 | 45.2 | 12.4 |
| Ni@In2O3 | 38.2 | 30.8 |
| Ni/In2O3 | 48.3 | 9.6 |