Boosting Visible-Light Photocatalytic Performance of Exfoliated Carbon Nitride Nanosheets via Optimizing Dopant Decoration for Efficient Pollutant Removal

Kingsley Igenepo John, Touma B. Issa, Aleksandar N. Nikoloski, Goen Ho, Dan Li*

College of Science, Technology, Engineering & Mathematics, Murdoch University, Murdoch, WA 6150, Australia.

Figures:

Fig. S1. Enlarged XRD patterns at the (002) plane of g-C3N4, Na(0.4)g-C3N4, Fe(0.4)g-C3N4 and Pr(0.4)g-C3N4.

Fig. S2. Enlarged XRD patterns at the (100) plane of g-C3N4 and Pr(x)g-C3N4.

Fig. S3. SEM images of g-C3N4 (a), Pr(0.1)g-C3N4 (b), Pr(0.2)g-C3N4 (c) and Pr(0.4)g-C3N4 (d).

Fig. S4. XPS survey spectrum of Pr(0.4)g-C3N4.

Fig. S5. Mott-Schottky plots with charge carrier density (ND) of g-C3N4, Na(0.4) g-C3N4, Fe(0.4) g-C3N4, and Pr(0.4) g-C3N4.

Fig. S6. The equivalent circuit used to model the EIS Nyquist plots for g-C3N4, Na(0.4)g-C3N4, Fe(0.4)g-C3N4, and Pr(0.4)g-C3N4. (Rs, Rp, Rct, W, and Q represent the electrolyte resistance, pore resistance, charge transfer resistance, Warburg impedance, and constant phase element, respectively) [1].

Fig. S7. Proposed structures of (a) g-C3N4, (b) Na(0.4)g-C3N4, (c) Fe(0.4)g-C3N4, and (d) Pr(0.4)g-C3N4.

Fig. S8. Schematic diagram for degradation mechanism of (a) Na(0.4)g-C3N4 [2]; heterostructures of (b) Fe(0.4)g-C3N4 [3], and (c) Pr(0.4)g-C3N4 [4].

Fig. S9. Point of zero charge of Na(0.4)g-C3N4, Fe(0.4)g-C3N4, and Pr(0.4)g-C3N4.

Fig. S10. (a – b) Effect of different types of dyes on the photocatalytic degradation and corresponding rate constants of g-C3N4 and Pr(0.4)g-C3N4.

Fig. S11. Photocatalytic degradation of MO (a) and RhB (b) using g-C3N4, Na(0.4)g-C3N4, Fe(0.4)g-C3N4, and Pr(0.4)g-C3N4.

Fig. S12. (a) Electronic structure of Pr(0.4)g-C3N4 and (b) mechanism of the reaction using Pr(0.4)g-C3N4.

Tables:

Table S1. MB removal performance of Pr(0.4)g-C3N4 in comparison to some conventional catalysts and modified g-C3N4 in the literature.

| Photocatalyst | Dosage/Conc. (g L-1/mg L-1) | Light source | Time (min) | Removal (%)/k (min-1) | Ref. |
| --- | --- | --- | --- | --- | --- |
| SnO2 | 0.20/10 | UV lamp (3 x 11W) | 100 | 84.8/0.0185 | [5] |
| ZnO | 1.5/10 | UV lamp (8W) | 20 | 72.3/- | [6] |
| WO3 | 1/10 | UV-Vis | 90 | 94.8/- | [7] |
| TiO2 | 0.3/3.2 | UV lamp | 120 | 92.2/0.0072 | [8] |
| MnO2/g-C3N4/ZnO | 0.13/10 | LED (60 W) | 180 | 94/0.0156 | [9] |
| CdSe/g-C3N4 | -/20 | 300 W Xe lamp (λ > 400 nm) | 120 | 89.4/0.0194 | [10] |
| ZnO/g-C3N4 | 1/5 | two 100 W Xe lamp | 180 | 97/0.022 | [11] |
| Alginate/ZnO/g-C3N4 | 0.3 wt%/4 | 300 W Tungsten lamp | 60 | 78.18/- | [12] |
| CuO/g-C3N4 | 1/5 | 400 W Halogen lamp | 40 | 98/- | [13] |
| Ce-MOF/g-C3N4 | 0.25/10 | UV light | 120 | 96.5/0.027 | [14] |
| CeO2/g-C3N4 | 0.5/10 | 36 W UV lamp (OS72) (λ = 254 nm) | 180 | 94.0/0.030 | [15] |
| CeO2/S-doped-g-C3N44 | 1/10 | 300 W Halogen lamp (λ > 400 nm) | 150 | 91.4/0.015 | [16] |
| Sm2O3/S-g-C3N4 | 0.7/8 | 300 W Halogen lamp (λ > 400 nm) | 150 | 93/0.013 | [17] |
| Nd-ZnO/g-C3N4 | 1/20 | 500 W Xe lamp | 105 | 94.9/0.026 | [18] |
| Ho-g-C3N4 | 0.4/10 | 120 W lamp | 300 | 71.4/0.004 | [19] |
| TiO2/Na-doped g-C3N4 | 2/20 | 300 W Xe lamp (λ > 400 nm) | 90 | 99.6/- | [20] |
| P-doped g-C3N4 | 0.5/- | 500 W Xe lamp (λ > 420 nm) | 120 | -/0.0045 | [21] |
| K-doped g-C3N4 | 0.6/10 | 300 W Xe lamp (λ > 400 nm) | 60 | 99.0/- | [22] |
| CuO/g-C3N4 | 1/50 | 500 W halogen lamp (λ > 400 nm) | 100 | 94.0/0.030 | [23] |
| Pr(0.4)g-C3N4 | 0.4/10 | 300 W Xe lamp (λ > 420 nm) | 40 | 95.6/0.108 | This study |
| Na(0.4)g-C3N4 | 0.4/10 | 300 W Xe lamp (λ > 420 nm) | 40 | 92.6/0.053 | This study |
| Fe(0.4)g-C3N4 | 0.4/10 | 300 W Xe lamp (λ > 420 nm) | 40 | 77.5/0.021 | This study |

Table S2. Characteristics of water matrices in this study.

| Water matrix | pH | Turbidity (NTU) | Conductivity (µS cm-1) | Total Organic Carbon (mg C L-1) | Salinity (PPT) |
| --- | --- | --- | --- | --- | --- |
| Deionized Water (control) | 4.6 | 0.6 | 4.6 | < 0.5 | 0 |
| Spring Water | 5.6 | 0.6 | 211.9 | < 0.5 | 0.1 |
| Tap Water | 8.1 | 1.6 | 247.0 | 0.9 | 0.1 |
| Primary Effluent | 7.2 | 15.3 | 1144.0 | 33 | 0.6 |
| Secondary Effluent | 6.9 | 1.2 | 956.0 | 32 | 0.5 |

References

- Tyagi A, Mishra K, Sharma S K, Shukla V K, Performance studies of an electric double-layer capacitor (EDLC) fabricated using edible oil-derived activated carbon. Journal of Materials Science: Materials in Electronics, 2022, 33: 8920–8934.

- Wu S, Yu Y, Qiao K, Meng J, Jiang N, Wang J. A simple synthesis route of sodium-doped g-C3N4 nanotubes with enhanced photocatalytic performance. Journal of Photochemistry and Photobiology A: Chemistry, 2021, 406: 112999.

- Xu F, Chai B, Liu Y, Liu Y, Fan G, Song G. Superior photo-Fenton activity toward tetracycline degradation by 2D α-Fe2O3 anchored on 2D g-C3N4: S-scheme heterojunction mechanism and accelerated Fe3+/Fe2+ cycle. Colloids and Surfaces A: Physicochemical and Engineering Aspects, 2022, 652: 129854.

- Shende A G, Ghugal S G, Vidyasagar D, Kokane S B, Jagannath, Umare S S, Sasikala R. Solvent free solid-state synthesis of Pr6O11/g-C3N4 visible light active photocatalyst for degradation of AV7 dye. Materials Research Bulletin, 2018, 107: 154–163.

- Pandey A K, Nurhidayah E, Yuwono A H, Septiningrum F, Maulana F A, Dhaneswara D, Sofyan N, Pangesty A I, Noviyanto A, Said Z, Tyagi V V.  Optimizing the photocatalytic performance of SnO2 nanoparticles for methylene blue removal with variation in calcination temperatures. 2024, E3S Web of Conferences 488.

- Saadi H, Atmani E H, Fazouan N. Enhanced photocatalytic degradation of methylene blue dye by ZnO nanoparticles: Synthesis, characterization, and efficiency assessment. 2024, Environmental Progress & Sustainable Energy 44(1).

- Shakun S, Manmeet K, Chhavi P, Sonal S.  Temperature dependent structural, optical, photocatalytic and magnetic properties of WO3 nanoparticles. Journal of Water and Environmental Nanotechnology, 2024, 9(3): 318-326.

- Laghrib S, Gherdaoui C E, Belgherbi O, Benaskeur N, Boudissa M, Kanagaraj A, Aouffa N. Photocatalytic degradation of methylene blue using TiO2 nanoparticles synthesized via the sol–gel method in acidic and neutral media. Reaction Kinetics, Mechanisms and Catalysis, 2025.

- Gindose, T.G., Atisme, T.B., Hailegebreal, T.D. and Zereffa, E.A.  ZnO Modified g‐C3N4–MnO2 composite for photodegradation of methylene blue. ChemistrySelect, 2025, 10: e202403418.

- Zhu Y, Jiang C, Meng T, Yao J, Peng Z, Wang P, Zhang Z, Wang C, Zhang Y, Zhao Y.  Heterojunction engineering of g-C3N4 with superior photogenerated electron transfer for boosting photodegradation of methylene blue. Optical Materials, 2025, 159.

- Pourali S, Amrollahi R, Alamolhoda S, Masoudpanah S M. In situ synthesis of ZnO/g-C3N4 based composites for photodegradation of methylene blue under visible light. Scientific Report, 2025, 15(1), 462.

- Valiyathur M D F, Sakvai M S, Mithra S, Majeed S A, Kottur A B, Hameed A S S, Raza A A. Photocatalytic and toxicity assessment of alginate reinforced ZnO-g-C3N4 photocatalyst for the degradation of methylene blue - A sustainable strategy. International Journal of Biological Macromolecules, 2025, 298, 139935.

- Muthuganesh A, Rafi S M, Jacob I D, Soundranayagam J P, Surender S, Elangovan P, Flora X H.  Efficient methylene blue dye degradation via visible light-activated g-C3N4/CuO nanocomposites. Hybrid Advances, 2025. 9: 100420.

- Durmus Z, Köferstein R, Lindenberg T, Lehmann F, Hinderberger D, Maijenburg A W. Preparation and characterization of Ce-MOF/g-C3N4 composites and evaluation of their photocatalytic performance. Ceramics International, 2023, 49(14): 24428–24441.

- Wei X, Wang X, Pu Y, Liu A, Chen C, Zou W, Zheng Y, Huang J, Zhang Y, Yang Y, Naushad M, Gao B, Dong L. Facile ball-milling synthesis of CeO2/g-C3N4 Z-scheme heterojunction for synergistic adsorption and photodegradation of methylene blue: Characteristics, kinetics, models, and mechanisms. Chemical Engineering Journal, 2021, 420: 127719.

- Jourshabani M, Shariatinia Z, Badiei A. Facile one-pot synthesis of cerium oxide/sulfur-doped graphitic carbon nitride (g-C3N4) as efficient nanophotocatalysts under visible light irradiation. Journal of Colloid and Interface Science, 2017, 507: 59–73.

- Jourshabani M, Shariatinia Z, Badiei A. Synthesis and characterization of novel Sm2O3/S-doped g-C3N4 nanocomposites with enhanced photocatalytic activities under visible light irradiation. Applied Surface Science, 2018, 427: 375–387.

- Tian M, Zhang G, Zhao X, Yan Y, Zhao J, Bai H, Jiang J. Construction of rare-metal neodymium-doped ZnO and g-C3N4 Z-type heterostructures enhance the photocatalytic efficiency of methylene blue removal. Diamond and Related Materials, 2023, 140: 110493.

- Yavuz A, Aydin D, Disli B, Ozturk T, Gul B, Gubbuk I H, Ersoz M. Enhancing visible light photocatalytic activity of holmium doped g-C3N4 and DFT theoretical insights. Environmental Science and Pollution Research, 2024, 31(32): 44828–44847.

- Liu H, Yu D, Sun T, Du H, Jiang W, Muhammad Y, Huang L. Fabrication of surface alkalinized g-C3N4 and TiO2 composite for the synergistic adsorption-photocatalytic degradation of methylene blue. Applied Surface Science, 2019, 473: 855–863.

- Liu S, Zhu H, Yao W, Chen K, Chen D. One step synthesis of P-doped g-C3N4 with the enhanced visible light photocatalytic activity. Applied Surface Science, 2018, 430: 309–315.

- Yuan L, Liu W, Zhang W. Potassium-doped g-C3N4 enables efficient visible-light-driven dye degradation. Environmental Science and Pollution Research, 2023, 58276–58281.

- Vijayakumar T P, Benoy M D, Duraimurugan J, Suresh Kumar G, Shkir M, Maadeswaran P, Senthil Kumar A, Ramesh Kumar K A. Hydrothermal synthesis of CuO/g-C3N4 nanosheets for visible-light driven photodegradation of methylene blue. Diamond and Related Materials, 2022, 121: 108735.