# Supporting Information

# Flowerlike CeO2 used as novel adsorption material for removal of hydrogen fluoride gas from lithium-ion battery during thermal runaway

Haozhe Xu1#*, Shuai Yuan2#*, Chunwen Sun1* and Donghao Cheng 2*

1 Beijing School of Chemical and Environmental Engineering, China University of Mining and Technology, Beijing 100083, China

2 China Academy of Civil Aviation Science and Technology, Beijing 100028, China

#These authors contribute equally to this work.

*Emails: csun@cumtb.edu.cn (C. Sun), chengdh@mail.castc.org.cn (D. Cheng)

Table S1  Comparison of maximum adsorption capacities of different absorbents for fluoride in water.

| Adsorbents | Qmax (mg/g) | specific surface area (m2/g) | Refs |
| --- | --- | --- | --- |
| CeO2-Rods | 71.5 | 160.2 | [1] |
| CeO2-Octs | 28.3 | 111.4 | [1] |
| CeO2-Cubes | 7.0 | 55.8 | [1] |
| CeO2 nanoparticles | 66.4 | 65.8 | [2] |
| Commercially available Al2O3 | 5.7 | 62 | [3] |
| Bone char | 11.9 | 104 | [4] |

- Kang, D.; Yu, X.; Ge, M. Morphology-dependent properties and adsorption performance of CeO2 for fluoride removal. Chemical Engineering Journal, 2017, 330, 36-43.

- Trinh T N, Dang P X, Duong L T, et al. Sol–gel synthesis of CeO2 nanoparticles using a gelatine template for effective adsorptive removal of arsenate and fluoride from water. ChemistrySelect, 2024, 9(45): e202404325.

- Kang D, Tong S, Yu X, et al. Template-free synthesis of 3D hierarchical amorphous aluminum oxide microspheres with broccoli-like structure and their application in fluoride removal. RSC Advances, 2015, 5(25): 19159-19165.

- Medellin-Castillo N A, Leyva-Ramos R, Ocampo-Perez R, et al. Adsorption of fluoride from water solution on bone char. Industrial & Engineering Chemistry Research, 2007, 46(26): 9205-9212.

.

Fig. S1  Schematical illustration of synthesis process of flowerlike CeO2 microspheres.

Fig. S2  (a) Nickel foam; (b) Prepared filters; (c, d, e) The folded filters showing its flexibility.

Fig. S3  (a, b) The test device for absorbtion of HF; and (c) method for the adsorption performance of the HF gas produced by lithium-ion battery during thermal runaway; (d) dimensional labeling of the box; (e, f) designed filter ports and filters.

Fig. S4  XRD patterns of the calcined products.

Fig. S5  Gas collection experiments: (a) gas collection bag; (b) battery starts to expand; (c) beginning of thermal runaway; (d) during thermal runaway; (e) end of thermal runaway; (f) completion of collection.

Fig. S6  Temperature change of the gas during thermal runaway of lithium-ion battery

Fig. S7  (a) SEM image of the flowerlike CeO2 microspheres after one adsorption; (b-e) EDX mapping results; (f) SEM image of the flowerlike CeO2 microspheres after regeneration; (g-j) EDX mapping results.

Table S2  EDX data of the CeO2 microspheres after one adsorption (Fig. S7).

|  | Element | wt% | Atomic% |
| --- | --- | --- | --- |
| After adsorption | O K | 28.47 | 75.76 |
|  | Ce L | 70.24 | 21.34 |
|  | F K | 1.29 | 2.89 |
|  | Totals | 100 |  |

Table S3  EDX data of the CeO2 microspheres after regeneration (Figure S7).

|  | Element | wt% | Atomic% |
| --- | --- | --- | --- |
| After regeneration | O K | 26.33 | 75.79 |
|  | Ce L | 73.67 | 24.21 |
|  | F K | 0 | 0 |
|  | Totals | 100 |  |

Fig. S8  HF gas detection concentration: (a) without nickel foam; (b) with four pieces of nickel foam.

Fig. S9  HF gas detection concentrations (repeated experiment): (a) without CeO2; (b) after first adsorption; (c) after second adsorption; (d) after third adsorption; (e) after fourth adsorption; (f) after fifth adsorption; (g) after sixth adsorption; (h) after seventh adsorption; (i) after eighth adsorption; (j) after ninth adsorption; (k) after tenth adsorption; and (l) Comparison of the highest instantaneous HF concentrations.

Fig. S10  XPS spectra of the flowerlike CeO2 microspheres after ten adsorptions (a) Ce 3d; (b) F 1s. XPS spectra of the flowerlike CeO2 microspheres after regeneration (800 oC 60 min): (c) Ce 3d; (d) F 1s. XPS spectra of the flowerlike CeO2 microspheres after regeneration (800 oC 120 min): (e) Ce 3d; (f) F 1s.

Table S4  XPS results of the flowerlike CeO2 materials after ten adsorptions and regeneration

| CeO2 | Ce3+ | Ce4+ | F atomic |
| --- | --- | --- | --- |
| After ten adsorptions | 24.35% | 75.65% | 9.55% |
| After regeneration (800 oC 60 min) | 19.36% | 80.64% | 0.92% |
| After regeneration (800 oC 120 min) | 17.06% | 82.94% | 0.25% |

Table S5  XPS results of the flowerlike CeO2 materials before and after fluoride adsorption.

| CeO2 | Ce3+ | Ce4+ | Ce-O | F atomic |
| --- | --- | --- | --- | --- |
| Before adsorption | 17.01% | 82.99% | 59.02% | 0% |
| After one adsorption | 20.58% | 79.42% | 52.63% | 3.36% |