| Element | wt % | Atomic % |
| --- | --- | --- |
| Pt | 4.69 | 0.31 |
| Fe | 2.11 | 0.49 |

Table S1 The mass and atomic ratio of Pt and Fe elements in the Pt/Fe-N-C catalyst tested by EDS.

Figure S1 (a-c) TEM images of Pt/Fe-N-C catalyst

Figure S2 XRD curves of Pt/Fe-N-C at 100 ℃, 200 ℃, 300 ℃ and 400 ℃ for secondary heat treatment.

Figure S3 (a) XPS spectra of Pt/Fe-N-C catalyst; XPS diagram of Pt/Fe-N-C catalyst (b) C1s, (c) N1s.

Figure S4 (a) Tafel curves fitted by Pt/C, Pt/Fe-N-C catalysts; (b) ORR current-time stability curve of Pt/Fe-N-C, Pt/C; (c) LSV curves of Pt/Fe-N-C catalyst at different secondary heat treatment temperatures at saturation of 0.1 mol L-1KOH; (d) LSV curves of Pt/Fe-N-C catalyst at different secondary heat treatment times at saturation of 0.1 mol L-1KOH.

Figure S5 (a) Polarization curves at different speeds; (b-c) CV graphs and Cdl curves obtained by Pt/Fe-N-C, Pt/C catalysts at different sweep speeds; (d)CV curve in N2-saturated 0.1 M HClO4 solution.

Figure S6 (a-b) Constant discharge curve.

Figure S7 (a) SEM image of Pt/Fe-N-C catalyst 200 nm after the application of the oxygen reduction reaction; XPS spectra of Pt/Fe-N-C catalyst Pt 4f after the application of the oxygen reduction reaction.