Artificial Intelligence for Plastic Pyrolysis into Fuels and Chemicals: From Reaction Kinetics and Reactor Design towards Intelligent Agent Development

Gaoyang Li1, Jie Huang1, Xi Gao2,3,*, Yin-Ning Zhou4,*, Li-Tao Zhu1,*

1College of Smart Energy, Shanghai Jiao Tong University, Shanghai, 200240, China.

2Department of Chemical Engineering, Guangdong Technion-Israel Institute of Technology, Shantou 515063, China.

3Wolfson Department of Chemical Engineering, Technion-Israel Institute of Technology, Haifa 3200003, Israel.

4Department of Chemical Engineering, Shanghai Jiao Tong University, Shanghai, 200240, China.

*Corresponding Author: xi.gao@gtiit.edu.cn; zhouyn@sjtu.edu.cn; sjtu_zlt@sjtu.edu.cn

Tel.: +86-21-64355111-6586; Fax: +86-21-64355111-6586

Table S1 Summary of polymer-specific pyrolysis pathways, products, and AI-relevant

| Polymer | Structural feature | Dominant degradation pathway and major products | AI-relevant descriptors |
| --- | --- | --- | --- |
| PET | Aromatic polyester containing ester linkages and benzene rings | PET pyrolysis mainly involves β-H transfer scission at ester bonds, C–O bond cleavage, decarboxylation, and decarbonylation of unstable end-groups, producing benzoic acid, CO2, CO, acetaldehyde, and acetophenone derivatives; acidic products such as benzoic acid may cause corrosion concerns. | PET fraction; O content; O/C ratio; ester-bond and aromatic-ring indicators; TGA onset/peak temperature; oxygenate or acid-product labels |
| PE / HDPE / LDPE | Saturated polyolefin with linear or branched –CH2– backbone | PE primarily degrades through random main-chain scission, radical recombination, intramolecular hydrogen transfer, β-scission, and disproportionation, generating alkanes, α-olefins, internal olefins, wax/oil fractions, and negligible solid residue under typical pyrolysis conditions. | PE fraction; HDPE/LDPE type; branching proxy; H/C ratio; volatile matter; melting or melt-flow behavior; temperature, heating rate, and residence time |
| PP | Methyl-branched polyolefin containing tertiary carbon centers | PP undergoes random chain scission followed by β-scission, with tertiary radical formation and intramolecular hydrogen transfer favoring the production of propylene, branched alkenes, branched alkanes, and oligomers; its liquid products are often rich in branched aliphatic hydrocarbons. | PP fraction; methyl-branching or tertiary-carbon proxy; H/C ratio; volatile matter; temperature and residence-time descriptors |
| PS | Polyolefin backbone with pendant phenyl groups | PS degradation is dominated by random main-chain scission, chain-end and mid-chain β-scission, depolymerization, and hydrogen-transfer reactions, producing styrene monomer, aromatic dimers, trimers, and other aromatic-rich liquid products. | PS fraction; aromaticity or phenyl-group indicator; C/H ratio; styrene or aromatic-product labels; temperature and vapor residence time |
| PVC | Chlorinated polymer with –CH2–CHCl– repeating units | PVC pyrolysis generally proceeds through low-temperature dehydrochlorination to form conjugated polyenes, followed by high-temperature fragmentation, cyclization, and aromatization, producing HCl, chlorinated hydrocarbons, chlorobenzenes, benzene, toluene, and chlorinated char. | PVC fraction; Cl content; H/Cl ratio; dechlorination-temperature descriptor; HCl-emission label; chlorinated-product and char/coke risk labels |

The descriptors listed in the last column are intended as potential feature-engineering candidates for AI-assisted plastic pyrolysis studies rather than definitive or universally applicable input variables. Their relevance and importance may vary depending on the prediction target, dataset composition, reactor configuration, catalyst system, operating conditions, data availability, and preprocessing strategy. Therefore, these descriptors should be selected and validated according to the specific modeling task, preferably through domain knowledge, correlation analysis, model-based feature importance, ablation tests, and external validation. The inclusion of a descriptor in this table does not imply a causal relationship with pyrolysis products.