Supplementary Information

Performance-enhanced direct ammonia protonic ceramic fuel cells using CeO2-supported Ni and Ru catalyst layer

Xiaoxiao Li1,2, Jiangping Chen1, Yunyun Huang (✉)1,3, Huihuang Fang1,3, Chongqi Chen1,3, Fulan Zhong1,3, Li Lin1,3, Yu Luo (✉)1,3, Yuqing Wang2, Lilong Jiang1,3

1 National Engineering Research Center for Fertilizer Catalysts, School of Petrochemical Engineering, Fuzhou University, Fuzhou 350002, China

2 School of Mechatronical Engineering, Beijing Institute of Technology, Beijing 100081

3 Qingyuan Innovation Laboratory, Quanzhou 362801, China

Supplementary Fig. S1 EIS curves of PCFC with addition of three catalytic layers using NH3 as fuel at 600 °C.

Figure S1 shows the electrochemical impedance spectra (EIS) of PCFC coated with three different catalysts at 600 °C with NH3 as fuel. As can be seen from Fig. S1 that the PCFC coated with 1Ru/CeO2 catalytic layer has a higher ohmic impedance than the PCFC coated with 10Ni/CeO2 and 1Ru-10Ni/CeO2. This is consistent with the results of the performance in the paper.

Supplementary Table S1 Content parameters of active metals for

three catalysts

| Samples | Ni loading/% | Ru loading/% |
| --- | --- | --- |
| 1Ru/CeO2 | - | 0.77 |
| 10Ni/CeO2 | 8.07 | - |
| 1Ru-10Ni/CeO2 | 7.67 | 0.76 |

In order to obtain the active metal content parameters on the three catalysts, inductively coupled plasma optical emission spectrometry (ICP-OES) tests were performed with the results tabulated in Table S1. The actual active metal loading content is about 80% of the intended quantity.

Supplementary Fig. S2 Catalytic activity and stability of 1Ru-10Ni/CeO2 catalyst for NH3 decomposition at 600 ℃.

Figure S2 shows that the 1Ru-10Ni/CeO2 catalyst exhibits a good stability in the ammonia decomposition reaction. During the first 17 hours of the test, there was a small increase in the ammonia decomposition activity of the fresh catalyst from 82.2% to 83.6%. This was followed by a plateau when the ammonia decomposition activity stabilized at 81%.

Supplementary Table S2 Performance comparison of SOFCs (with difference

materials or configurations) when operated with H2 and NH3.

| Anode | Degradation ratio a | Ref. |
| --- | --- | --- |
| 1Ru/CeO2+Ni/BCZY | ~19% at 600 ℃ | This work |
| 10Ni/CeO2+Ni/BCZY | ~23% at 600 ℃ |  |
| 1Ru-10Ni/CeO2+Ni/BCZY |  |  |
| Ni/YSZ | 25% at 700 ℃ | Hendriksen et al. [1] |
| LSTNC-infiltrated SDC | 25% at 800 ℃ | Song et al. [2] |
| Ni/YSZ | 23% at 750 ℃ | Yang et al. [3] |
| FeNi/BaZr0.1Ce0.7Y0.1Yb0.1O3 | ~17% at 650 ℃ | Zhang et al. [4] |
| Ni−Fe−BZCYYb | ~29% at 700 ℃ | Pan et al. [5] |
| Reduced-Pr0.6Sr0.4Co0.2Fe0.8O3-δ | 46%~ at 650 ℃ | Xiong et al. [6] |
| Reduced-Pr0.6Sr0.4Co0.2Fe0.75Ru0.05O3-δ |  |  |

a The degradation ratio is the electrochemical performance of NH3 compared to H2.

References

1.	Hendriksen P V, Mondi F, Sun X, et al. Ammonia as an SOFC Fuel. ECS Transactions, 2023, 111(6): 2085–2096 doi:10.1149/11106.2085ecst

2.	Song Y, Li H, Xu M, et al. Infiltrated NiCo alloy nanoparticle decorated perovskite oxide: a highly active, stable, and antisintering anode for direct‐ammonia solid oxide fuel cells. Small, 2020, 16(28): 2001859 doi:10.1002/smll.202001859

3.	Yang S, Kim H, Oh S, et al. Development of direct-ammonia solid oxide fuel cells (DA-SOFCs) and the effect of incorporating internal ammonia decomposition catalysts. ECS Transactions, 2023, 111(6): 2111–2118 doi:10.1149/11106.2111ecst

4.	Zhang H, Zhou Y, Pei K, et al. An efficient and durable anode for ammonia protonic ceramic fuel cells. Energy & Environmental Science, 2022, 15(1): 287–295 doi:10.1039/D1EE02158C

5.	Pan Y, Zhang H, Xu K, et al. A high-performance and durable direct NH3 tubular protonic ceramic fuel cell integrated with an internal catalyst layer. Applied Catalysis B: Environmental, 2022, 306: 121071 doi:10.1016/j.apcatb.2022.121071

6.	Xiong X, Yu J, Huang X, et al. Slightly ruthenium doping enables better alloy nanoparticle exsolution of perovskite anode for high-performance direct-ammonia solid oxide fuel cells. Journal of Materials Science and Technology, 2022, 125(30): 51–58 doi:10.1016/j.jmst.2022.02.031