Supporting Information

Boosting Zn2+ Storage Performance of MnO2 Cathode by Engineering Dual-Crystal-Phases Architecture for Reversible Zn-Ion Batteries

Experiment section

Synthesis of MnO2:

In a typical process, 4 mmol KMnO4 and 4 mmol NH4Cl (KMnO4: NH4Cl = 1:1) were added into the 35 mL deionized water with the constant stirring for 1 h until their completely dissolved. Then, the hybrid solution was transferred to a 100 mL Teflon autoclave in an oven at 140 ℃ for reaction for 12 h. After cooling down to room temperature, the MnO2 powders were obtained by centrifugation and washing by DI water and ethanol several times and dried at 80℃ overnight. The addition concentration of NH4Cl (KMnO4:NH4Cl = 1:1, 1:2, 1:4, 1:6, 1:8, 1:10, 1:12) was controlled to optimize the performances. The obtained powders were denoted as the KMO:NH4+@1:1, KMO:NH4+@1:2, KMO:NH4+@1:4, KMO:NH4+@1:6, KMO: NH4+@1:8, KMO: NH4+@1:10 and KMO: NH4+@1:12 respectively.

Material characterization:

The crystalline structures and composition characteristics of MnO2 powder were measured by X-ray diffraction (XRD, Bruker, D8 DISCOVER). Scanning electron microscope (SEM, Hitachi S-4800) and field emission electron microscopy (FETEM, Talos F200X) were used to investigate the microstructure of the samples. X-ray photoelectron spectroscopy (XPS, PHI5700) was carried out to investigate the surface composition and chemical state of the samples. N2 adsorption/desorption measurement (ASAP 2460) was conducted to understand the pore structure of the samples. Raman spectroscopy was conducted to investigate the composition evolution of the cathodes.

Electrochemical characterization:

The cathodes were fabricated by blade coating of the active slurry (mixing the cathode materials, Super P, and polyvinyl difluoride binder with a mass ratio of 7:2:1 in NMP solvent) onto the graphite paper followed by drying at 60 °C for 12 h. The electrochemical performance of cathode materials was examined in CR2032 coin cells. The cells were assembled using MnO2 cathode, zinc metal plate as the anode, glass fiber (GF/D) as the separator, and 2 M ZnSO4 with 0.1 M MnSO4 as the electrolyte. The galvanostatic charge/discharge and galvanostatic intermittent titration technique (GITT) measurements were conducted on a multichannel battery test equipment (LAND CT2001A). The voltage setting range is 0.8-1.8 V. GITT was executed under a pulse current time of 10 mins and a rest time of 60 mins. The ionic diffusion coefficient was calculated according to the Fick’s second law:

D=4πτ(mBVMMBS)2(∆Es∆Eτ)2                                                (1)

τ (s) is the pulse duration, mB (g) is the electrode’s active mass, VM (cm3 mol1) is molar volume, S is the contact surface area of the electrode, MB (g mol1) is the molar mass of carbon, ΔEs refers to the steady-state voltage change, and ΔEt represents the voltage change during current pulse. The cyclic voltammogram (CV) and electrochemical impedance spectroscopy (with 5 mV amplitude in the frequency from 0.01 to 106 Hz) were conducted on a CHI660e electrochemical workstation.

Figure S1. TEM images of the KMO: NH4+@1:1 sample.

Figure S2. TEM images of the KMO: NH4+@1:2 sample.

Figure S3. Element distribution maps of the KMO: NH4+@1:4 sample.

Figure S4. TEM images and the corresponding EDS of the KMO: NH4+@1:8 sample.

Figure S5. XRD patterns of all the samples.

Figure S6. (a) The Mn3+/Mn4+ ratio from XPS data of the samples. (b) The H-O-H, Mn-OH (Oads), and Mn-O-Mn (Olatt) ratio from XPS data of the samples. (c) Oads/Olatt value of the samples.

Figure S7. CV curves of the (a) KMO: NH4+@1:1, (b) KMO: NH4+@1:2, (c) KMO: NH4+@1:4, (d) KMO: NH4+@1:8 cathodes.

Figure S8. CV curve of the initial five cycles. of the KMO: NH4+@1:4 cathode.

Figure S9. The GCD curves and the plateau capacities of the (a, b) the KMO: NH4+@1:1, (c, d) the KMO: NH4+@1:2, (e, f) the KMO: NH4+@1:8.

Figure S10. The self-discharge behavior curve of the (a) KMO: NH4+@1:1, (b) KMO: NH4+@1:2, (c) KMO: NH4+@1:4, (d) KMO: NH4+@1:8 cathodes.

Figure S11. XRD patterns of the KMO: NH4+@1:4 cathodes during cycling at 1C.

Figure S12. SEM images of the KMO: NH4+@1:4 cathodes during cycling at 1C.

Figure S13. TEM images of the KMO: NH4+@1:4 cathodes after cycling.

Figure S14. Electrochemical kinetic analyses of the (a-c) the KMO: NH4+@1:1, (d-f) the KMO:NH4+@1:2, (g-i) the KMO: NH4+@1:8 cathodes.

Table S1. Textural properties of the MnO2 samples derived from N2 adsorption-desorption measurements.

| Sample | Surface area | Pore volume |
| --- | --- | --- |
| KMO: NH4+@1:1 | 90.3 m2 g−1 | 0.32 cm3 g−1 |
| KMO: NH4+@1:2 | 137.9 m2 g−1 | 0.39 cm3 g−1 |
| KMO: NH4+@1:4 | 156.4 m2 g−1 | 0.41 cm3 g−1 |
| KMO: NH4+@1:8 | 108.5 m2 g−1 | 0.37 cm3 g−1 |

Table S2. Comparison of the electrochemical performance in this work with ever-reported cathodes for Zn-ion batteries.

| Cathode | Rate performance | Cycling performance | Electrolyte | Voltage range | Ref. |  |
| --- | --- | --- | --- | --- | --- | --- |
| (CNF)@MnO2 | 280 mAh g−1 at 0.2 A g−1 210 mAh g−1 at 1.0 A g−1 | 64.3% Capacity retention (700cycle at 0.2 A g−1) | 2 M ZnSO4 +0.1 M MnSO4 | 0.8-1.8V |  | [1] |
| δ-MnO2 NDs | 327 mAh g−1 at 0.1 A g−1 206 mAh g−1 at 1.0 A g−1 125 mAh g−1 at 2.0 A g−1 | 73.8% Capacity retention (50cycle at 0.1 A g−1) | 2 M ZnSO4 +0.1 M MnSO4 | 1-1.9V | [2] |  |
| N-coordinated MnO2 | 325 mAh g−1 at 0.2 A g−1 256 mAh g−1 at 0.5 A g−1 210 mAh g−1 at 1.0 A g−1 | 94% Capacity retention (200cycle at 0.2 A g−1) | 2 M ZnSO4 +0.1 M MnSO4 | 1-1.8V | [3] |  |
| PANI-MnO2 | 280 mAh g−1 at 0.2 A g−1 125 mAh g−1 at 2.0 A g−1 | 90% capacity retention (200 cycle at 0.2 A g−1) | 2 M ZnSO4 +0.1 M MnSO4 | 1-1.8V | [4] |  |
| δ-MnO2/rGO | 221 mAh g−1 at 0.2 A g−1 122 mAh g−1 at 2.0 A g−1 | 84.3% capacity retention (300 cycle at 0.2 A g−1) | 2 M ZnSO4 | 1-1.8V | [5] |  |
| α-MnO2 nanowires | 240 mAh g−1 at 0.1A g−1 | 58% capacity retention (300 cycle at 0.1 A g−1) | 2 M ZnSO4 + 0.2 M MnSO4 | 0.9-1.8V | [6] |  |
| NH4-V2O5 | 274 mAh g−1 at 0.2A g−1 241mAh g−1 at 0.5A g−1 | 62.2% capacity retention (1000 cycle at 0.5 A g−1) | 3 M Zn(CF3SO3)2 | 0.2-1.6V | [7] |  |
| K2V8O21 | 247 mAh g−1 at 0.3A g−1 226 mAh g−1 at 0.5A g−1 139 mAh g−1 at 2A g−1 | 90% capacity retention (50 cycle at 0.5 A g−1) | 2 M ZnSO4 | 0.4-1.4V | [8] |  |
| VS2 | 190 mAh g−1 at 0.05A g−1 112 mAh g−1 at 0.5A g−1 116 mAh g−1 at 2 A g−1 | 98% capacity retention (200 cycle at 0.5 A g−1) | 1 M ZnSO4 | 0.4-1.0V | [9] |  |
| NTNQ | 251 mAh g−1 at 0.1A g−1 203 mAh g−1 at 1A g−1 | 83.2% capacity retention (100 cycle at 0.1 A g−1) | 1 M Zn(CF3SO3)2 | 0.1-1.5V | [10] |  |
| This work | 297 mAh g−1 at 1 C 223 mAh g−1 at 3 C 182 mAh g−1 at 5 C 136 mAh g−1 at 10 C | 93.7% Capacity retention (600 cycle at 1C) | 2 M ZnSO4 +0.1 M MnSO4 | 0.8-1.8V | — |  |

References

[1]	Chen X, Li W, Zeng Z, et al. Engineering stable Zn-MnO2 batteries by synergistic stabilization between the carbon nanofiber core and birnessite-MnO2 nanosheets shell [J]. Chemical Engineering Journal, 2021, 405.

[2]	Tang H, Chen W, Li N, et al. Layered MnO2 nanodots as high-rate and stable cathode materials for aqueous zinc-ion storage [J]. Energy Storage Materials, 2022, 48: 335-43.

[3]	Wang S, Yao S, Dai N, et al. Spin symmetry breaking‐induced hubbard gap near‐closure in N‐coordinated MnO2 for enhanced aqueous zinc‐ion battery performance [J]. Angewandte Chemie International Edition, 2024, 63(35).

[4]	Huang J, Wang Z, Hou M, et al. Polyaniline-intercalated manganese dioxide nanolayers as a high-performance cathode material for an aqueous zinc-ion battery [J]. Nature communications, 2018, 9(1).

[5]	Qiu C, Liu J, Liu H, et al. Suppressed layered‐to‐spinel phase transition in δ‐MnO2 via van der Waals interaction for highly stable Zn/MnO2 batteries [J]. Small Methods, 2022, 6(12).

[6]	Gao X, Wu H, Li W, et al. H+‐insertion boosted α‐MnO2 for an aqueous Zn‐ion battery [J]. Small, 2020, 16(5).

[7]	Lu Y, Wang T, Naresh N, et al. Pre-doped cations in V2O5 for high-performance Zn-ion batteries [J]. Nano Research Energy, 2024, 3(4).

[8]	Tang B, Fang G, Zhou J, et al. Potassium vanadates with stable structure and fast ion diffusion channel as cathode for rechargeable aqueous zinc-ion batteries [J]. Nano Energy, 2018, 51: 579-87.

[9]	He P, Yan M, Zhang G, et al. Layered VS2 nanosheet‐based aqueous Zn ion battery cathode [J]. Advanced Energy Materials, 2017, 7(11).

[10]	Wang J, Gao X, Wang Y, et al. Robust ring insoluble naphthoquinone derivative cathode with high loading and long cycle life for aqueous zinc organic batteries [J]. Nano Research Energy, 2024, 3(4).