Supporting Information

Synergistic d−Band Center Modulation and Interfacial Charge Distribution on ZrO2/CdS Catalyst for Solar−Driven CO2 Conversion

1. Photoelectrochemical measurements

The transient photocurrent, electrochemical impedance spectroscopy (EIS), linear sweep voltammograms (LSV) and open circuit potential (OCP) were carried out by Chenhua CHI 660E in the installation of a standard three-electrode system, comprising silver-silver chloride electrode (Ag/AgCl) as reference electrode, Pt foil as counter electrode, the prepared catalyst on ITO as working electrode. Besides, the measurements were carried out in an aqueous solution of 0.1 M Na2SO4.

2. The formula for converting VB−XPS to NHE was as follows

The conduction band (CB) and valence band (VB) potentials are calculated as follows: [1]

| EVB−NHE = φ + EVB−XPS − 4.44 | (1) |
| --- | --- |
| Eg = EVB − ECB | (2) |

where φ is the work function of the instrument (4.5 eV).

3. The formula for solar−to−chemical (STC)conversion efficiency was as follows

The solar−to−chemical (STC) conversion efficiency could be expressed by the input vs. output energy, which can be calculated by the following formula: [2, 3]

ηSTC= qmIAt ×1000‰ (J∙mol−1∙molW∙cm2∙cm−2∙s= JW∙s=1)

where q is the combustion heat value of CO (qCO = 283.5 kJ·mol−1), m denotes the mole of products (mol), I denotes the light intensity (W·cm−2), A is the irradiation area (cm2), and t denotes the reaction time (s).

Table S1. BET of ZrO2, CdS and ZOCS−20.

| Thermophysical Properties | ZrO2 | CdS | ZOCS−20 |
| --- | --- | --- | --- |
| BET Surface Area (m2·g−1) | 91.656 | 4.470 | 19.293 |
| Pore Volume (cm3·g−1) | 0.314 | 0.016 | 0.061 |
| Average Pore Size (nm) | 19.032 | 16.383 | 8.869 |

Table S2. CO yield for different samples.

| Catalysts | CO Yield (μmol·g−1·h−1) |
| --- | --- |
| CdS | 39.009 |
| ZOCS−10 | 98.516 |
| ZOCS−15 | 203.632 |
| ZOCS−20 | 330.232 |
| ZOCS−25 | 226.473 |
| ZOCS−30 | 140.061 |
| ZrO2 | Trace |

Table S3. Comparison of CO yield and STC conversion efficiency among ZrO2, CdS, and ZOCS−20.

| Catalysts | CO Yield (μmol·g−1·h−1) | STC (‰) |
| --- | --- | --- |
| ZrO2 | 0 | 0 |
| CdS | 39.01 | 0.070 |
| ZOCS−20 | 330.23 | 0.591 |

Table S4. Performance comparison of reported photocatalytic CO2 reduction

| Catalysts | Reaction medium | CO Yield (μmol·g−1·h−1) | Ref. |
| --- | --- | --- | --- |
| ZOCS−20 | CO2 and H2O | 330.23 | This work |
| CTU/TiO2 | CO2 and H2O | 31.32 | [4] |
| Cs3Bi2I9/CeO2 | CO2 and H2O | 58.67 | [5] |
| BiOBr/CdS | CO2 and H2O | 19.40 | [6] |
| Cu2O/Fe2O3 | CO2 and H2O | 4.92 | [7] |
| (Ni, Fe)−N−C | CO2 and H2O | 86.16 | [8] |
| Pt SA/ZrO2 | CO2 and H2O | 16.61 | [9] |
| g−C3N4@CeO2 | CO2 and H2O | 16.80 | [10] |
| CdS/TiO2 | CO2 and H2O | 3.62 | [11] |
| Co2N/BiOBr−1 | CO2 and H2O | 67.80 | [12] |

Table S5. Comparison of STC conversion efficienciy of common photocatalysts.

| Catalysts | Light source | Reaction medium | Reduction products | Dosage (mg) | Yield (μmol·g−1·h−1) | ηSTC (‰) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ZOCS−20 | 300 W Xe lamp | CO2 and H2O | CO | 25 | 330.23 | 0.591 | This work |
| CuPt/WO3 | 300 W Xe lamp | CO2 and H2O | HCOOH and CH3COOH | 40 | 2.62 and 19.41 | 0.043 | [13] |
| Pt/ZnO | 300 W Xe lamp | CO2 and H2O | CO and CH4 | 50 | 115.32 and 9.61 | 0.264 | [14] |
| Ni−Co/ZrO2−VO | 300 W Xe lamp | CO2 and H2O | CO and CH4 | 30 | 663.84 and 3.17 | 0.372 | [15] |
| Au@Cr2O3 | 300 W Xe lamp | CO2 and H2O | CO and H2 | 30 | 0.074 and 0.013 | 0.267 | [16] |
| CoRu HCNp | 300 W Xe lamp | CO2 and H2O | CO and CH4 | 50 | 31.87 and 0.7 | 0.182 | [17] |
| Cu:CsPbBr3 | 300 W Xe lamp | CO2 and H2O | CO and CH4 | 150 | 0.53 and 14.72 | 0.165 | [18] |
| CeO2/WO3 | 300 W Xe lamp | CO2 and H2O | CO and C2H4 | 50 | 64.17 and 124.21 | 0.356 | [19] |
| FS@TC | 300 W Xe lamp | CO2 and H2O | CO and CH4 | 25 | 361.39 and 70.84 | 0.358 | [20] |
| Ni−SA−5/ZrO2 | 300 W Xe lamp | CO2 and H2O | CO and CH4 | 10 | 11.8 and 0.96 | 0.001 | [21] |

Table S6. TRPL fitting parameters of ZrO2, CdS, and ZOCS−20.

| Catalysts | τ1 (ns) | A1 | τ2 (ns) | A2 | τave (ns) |
| --- | --- | --- | --- | --- | --- |
| ZrO2 | 0.5685 | 0.6882 | 8.6227 | 0.34263 | 7.6809 |
| CdS | 0.5530 | 0.7014 | 8.6649 | 0.3439 | 7.7306 |
| ZOCS−20 | 0.5882 | 0.6872 | 9.3966 | 0.3261 | 8.3702 |

Table S7. Gibbs free energy of ZrO2, CdS and ZOCS−20 for photocatalytic CO2 reduction.

| Reaction Coordinate | ZrO2 | CdS | ZOCS−20 |
| --- | --- | --- | --- |
| CO2 | 0 | 0 | 0 |
| ΔG1 | −0.19 eV | −0.79 eV | −0.95 eV |
| *CO2 | −0.19 eV | −0.79 eV | −0.95 eV |
| ΔG2 | 0.94 eV | 0.63 eV | 0.56 eV |
| *COOH | 0.75 eV | −0.16 eV | −0.39 eV |
| ΔG3 | −0.16 eV | −0.56 eV | −0.16 eV |
| *CO | 0.59 eV | −0.72 eV | −0.55 eV |
| ΔG4 | −0.44 eV | 0.87 eV | 0.70 eV |
| CO | 0.15 eV | 0.15 eV | 0.15 eV |

Fig. S1. Raman spectra of ZrO2, CdS, and ZOCS−20

Fig. S2. High−resolution X−ray photoelectron spectroscopy (HR−XPS) spectra of O 1s for ZrO2 and ZOCS−20.

Fig. S3. High−resolution X−ray photoelectron spectroscopy (HR−XPS) spectra of S 2p for CdS and ZOCS−20.

Fig. S4. CO temperature−programmed desorption (CO−TPD) spectra of ZrO2, CdS, and ZOCS−20.

Fig. S5. CO2 reduction reaction system.

Fig. S6. CO2 reduction performance of ZOCS−20 at different temperatures under dark conditions.

Fig. S7. H2 production rate of ZrO2, CdS, and ZOCS−20.

Fig. S8. Infrared thermographic images of different samples.

Fig. S9. Temperature of different samples.

Fig. S10. TEM image of ZOCS−20 after reaction.

Fig. S11. DSC of ZrO2, CdS, and ZOCS−20.

Fig. S12. OCP curves of ZrO2, CdS, and ZOCS−20.

Fig. S13. Catalyst model of ZrO2.

Fig. S14. Catalyst model of CdS.

Fig. S15. Catalyst model of ZOCS−20.

Fig. S16. Adsorption model of CO2 at the ZrO2/CdS interface.

Fig. S17. High−resolution O 1s XPS spectra of ZOCS−20 under dark and light conditions.

Fig. S18. High−resolution S 2p XPS spectra of ZOCS−20 under dark and light conditions.

Fig. S19. DOS of ZrO2 and PDOS for Zr and O.

Fig. S20. DOS of CdS and PDOS for Cd and S.

Fig. S21. Catalytic reduction process of CO2 on ZOCS−20.

Fig. S22. Adsorption configurations of reaction intermediates on the ZrO2 catalyst surface.

Fig. S23. Adsorption configurations of reaction intermediates on the CdS catalyst surface.

Fig. S24. Adsorption configurations of reaction intermediates on the ZOCS−20 catalyst surface.

References

[1] Xiao Y, Li M, Li H, et al. Multi-channel charge transfer in self-supporting B-g-C3Nx/Bi2S3/CdS dual S-scheme heterojunction toward enhanced photothermal-photocatalytic performance. Nano Energy, 2024, 120: 109164.

[2] Xiao S, Li Z, Fu Q, et al. Hybrid microbial photoelectrochemical system reduces CO2 to CH4 with 1.28% solar energy conversion efficiency. Chemical Engineering Journal, 2020, 390: 124530.

[3] Xu L, Ren Y, Fu Y, et al. Strong photo-thermal coupling effect boosts CO2 reduction into CH4 in a concentrated solar reactor. Chemical Engineering Journal, 2023, 468: 143831.

[4] Wang L, Jin P, Duan S, et al. In-situ incorporation of Copper(II) porphyrin functionalized zirconium MOF and TiO2 for efficient photocatalytic CO2 reduction. Science Bulletin, 2019, 64 (13): 926–933.

[5] Feng Y-X, Dong G-X, Su K, et al. Self-template-oriented synthesis of lead-free perovskite Cs3Bi2I9 nanosheets for boosting photocatalysis of CO2 reduction over Z-scheme heterojunction Cs3Bi2I9/CeO2. Journal of Energy Chemistry, 2022, 69: 348–355.

[6] Huang Y, Zhang J, Dai K, et al. Efficient solar-driven CO2 reduction on aminated 2D/2D BiOBr/CdS-diethylenetriamine S-scheme heterojunction. Ceramics International, 2022, 48 (6): 8423–8432.

[7] Wang J-C, Zhang L, Fang W-X, et al. Enhanced Photoreduction CO2 Activity over Direct Z-Scheme α-Fe2O3/Cu2O Heterostructures under Visible Light Irradiation. ACS Applied Materials & Interfaces, 2015, 7 (16): 8631–8639.

[8] Mo S, Zhao X, Li S, et al. Non-Interacting Ni and Fe Dual-Atom Pair Sites in N-Doped Carbon Catalysts for Efficient Concentrating Solar-Driven Photothermal CO2 Reduction. Angewandte Chemie International Edition, 2023, 62 (50): e202313868.

[9] Dong S, Liu W, Liu S, et al. Single atomic Pt on amorphous ZrO2 nanowires for advanced photocatalytic CO2 reduction. Materials Today Nano, 2022, 17: 100157.

[10] Liang M, Borjigin T, Zhang Y, et al. Controlled assemble of hollow heterostructured g-C3N4@CeO2 with rich oxygen vacancies for enhanced photocatalytic CO2 reduction. Applied Catalysis B: Environmental, 2019, 243: 566–575.

[11] Pan X, Xu Y-J. Graphene-Templated Bottom-up Fabrication of Ultralarge Binary CdS–TiO2 Nanosheets for Photocatalytic Selective Reduction. The Journal of Physical Chemistry C, 2015, 119 (13): 7184–7194.

[12] Di J, Chen C, Zhu C, et al. Cobalt nitride as a novel cocatalyst to boost photocatalytic CO2 reduction. Nano Energy, 2021, 79: 105429.

[13] Ren Y, Lan S, Zhu Y-H, et al. Concentrated Solar-Driven Catalytic CO2 Reduction: From Fundamental Research to Practical Applications. ChemSusChem, 2025, 18 (10): e202402485.

[14] Wu M, Ren Y, Zhu F, et al. Photothermal Coupling Effect Boosts the Conversion of CO2 to Solar Fuel Over Pt/ZnO Photocatalyst in a Concentrated Solar Reactor. Industrial & Engineering Chemistry Research, 2023, 62 (24): 9463–9473.

[15] Chen J, Ren Y, Fu Y, et al. Integration of Co Single Atoms and Ni Clusters on Defect-Rich ZrO2 for Strong Photothermal Coupling Boosts Photocatalytic CO2 Reduction. ACS Nano, 2024, 18 (20): 13035–13048.

[16] Rashid R T, Chen Y, Liu X, et al. Tunable green syngas generation from CO2 and H2O with sunlight as the only energy input. Proceedings of the National Academy of Sciences, 2022, 119 (26): e2121174119.

[17] Cheng L, Yue X, Wang L, et al. Dual-Single-Atom Tailoring with Bifunctional Integration for High-Performance CO2 Photoreduction. Advanced Materials, 2021, 33 (49): 2105135.

[18] Bian H, Liu T, Li D, et al. Unveiling the effect of interstitial dopants on CO2 activation over CsPbBr3 catalyst for efficient photothermal CO2 reduction. Chemical Engineering Journal, 2022, 435: 135071.

[19] Wang J, Peng R, Zhu Y-H, et al. The photothermal coupling effect boosts the conversion of CO2 to C2H4 over CeO2/WO3 heterojunctions under concentrated solar irradiation. New Journal of Chemistry, 2025, 49 (17): 7060–7072.

[20] Wang K, Ren Y, Wang N, et al. Band-division utilization of core-shell photocatalyst under condenser solar-light and enhancement of synergistic catalytic CO2 reduction. Chemical Engineering Journal, 2024, 479: 147529.

[21] Xiong X, Mao C, Yang Z, et al. Photocatalytic CO2 Reduction to CO over Ni Single Atoms Supported on Defect-Rich Zirconia. Advanced Energy Materials, 2020, 10 (46): 2002928.