Supplementary Information

Regulating reactive oxygen species balance at the WO3/BN interface for selective photooxidation of methane to methanol

Table of contents

Characterization	3

Supporting Figures	4

1. TEM and HRTEM images of WO3	4

2. TEM and HRTEM images of BN	5

3. XRD patterns of BN	6

4. XPS spectra of BN and WO3/BN-1:1 catalysts	7

5. XPS spectra of WO3 and WO3/BN-1:1 catalysts	8

6. Time-dependent product evolution profiles	9

7. Stability test of WO3/BN-1:1	10

8. XRD patterns of fresh and used WO3/BN-1:1	11

9. XPS spectra of fresh and used WO3/BN-1:1	12

10. Photocatalytic CH4 oxidation under different reaction conditions	13

11. Band structure	14

12. PL spectra of WO3 and WO3/BN-1:1	15

13. Valence-band structure and band alignment of BN and WO3	16

14. EPR signal intensities and radical trapping experiments	17

15. In situ DRIFTS spectra of WO3	18

16. In situ DRIFTS spectra of WO3/BN-1:1	19

17. In situ DRIFTS spectra of BN	20

Supporting Tables	21

1. Performance of CH4 photooxidation	21

2. Control experiments	22

3. Comparison of productivity of photocatalytic CH4 conversion to CH3OH	23

4. Radical trapping experiments	24

Supporting References	25

## Characterization

X-ray diffraction (XRD) measurements were performed on an X’Pert PRO MPD diffractometer using Cu Kα radiation (λ = 1.5406 Å) at an operating voltage of 40 kV and a current of 40 mA to characterize the crystal structures of the as-prepared photocatalysts. High-resolution transmission electron microscopy (HRTEM) and high-angle annular dark-field scanning transmission electron microscopy (HAADF-STEM) observations were carried out using a JEM-2100F microscope to examine the morphology and microstructure of the samples. X-ray photoelectron spectroscopy (XPS) measurements were performed on a Thermo Scientific K-Alpha spectrometer equipped with an Al Kα X-ray source to analyze the elemental composition and chemical states of the sample surfaces and interfaces. Ultraviolet-visible diffuse reflectance spectroscopy (UV-vis DRS) measurements were performed using a Shimadzu UV-2600 UV-vis spectrophotometer equipped with an integrating sphere, with BaSO4 used as the reference, to investigate the optical absorption properties of the samples. Steady-state photoluminescence (PL) measurements were performed using a Hitachi F-7000 fluorescence spectrophotometer at an excitation wavelength of 320 nm to investigate the photoluminescence properties of the samples. Transient surface photovoltage (TPV) measurements were performed using a PL-TPV transient surface photovoltage spectrometer (Beijing Perfectlight Technology Co., Ltd., China) to investigate the separation and recombination dynamics of photogenerated charge carriers in the samples. Electron paramagnetic resonance (EPR) measurements were performed using a CIQTEK EPR200M spectrometer, with 5,5-dimethyl-1-pyrroline N-oxide (DMPO) as the spin-trapping agent, to detect radical species generated in the reaction system.

# Supporting Figures

## 1. TEM and HRTEM images of WO3

Figure S1. TEM and HRTEM images of WO3.

## 2. TEM and HRTEM images of BN

Figure S2. (a) TEM and (b) HRTEM images of BN.

## 3. XRD patterns of BN

Figure S3. XRD patterns of BN.

## 4. XPS spectra of BN and WO3/BN-1:1 catalysts

Figure S4. XPS spectra of B 1s on BN and WO3/BN-1:1 catalysts.

## 5. XPS spectra of WO3 and WO3/BN-1:1 catalysts

Figure S5. XPS spectra of W 4f on WO3 and WO3/BN-1:1 catalysts

## 6. Time-dependent product evolution profiles

Figure S6. Time-dependent product evolution profiles of WO3/BN-1:1 and WO3: (a) CH3OH; (b) HCHO; (c) CO; (d) CO2;

## 7. Stability test of WO3/BN-1:1

Figure S7. Five-cycle CH4 photooxidation performance over WO3/BN-1:1.

## 8. XRD patterns of fresh and used WO3/BN-1:1

Figure S8. XRD patterns of fresh and used WO3/BN-1:1 catalyst after cyclic photocatalysis.

## 9. XPS spectra of fresh and used WO3/BN-1:1

Figure S9. XPS spectra of fresh and used WO3/BN-1:1 catalyst after cyclic photocatalysis.

## 10. Photocatalytic CH4 oxidation under different reaction conditions

Figure S10. Photocatalytic CH4 oxidation under different reaction conditions of WO3/BN-1:1 catalyst.

## 11. Band structure

Figure S11. Tauc plots of (a) WO3 and (b)WO3/BN-1:1 derived from UV-vis DRS spectra.

## 12. PL spectra of WO3 and WO3/BN-1:1

Figure S12. PL spectra of WO3 and WO3/BN-1:1

## 13. Valence-band structure and band alignment of BN and WO3

Figure S13. Band-structure analysis of BN and WO3. Valence-band XPS spectra of (a) BN and (b) WO3; (c) Tauc plot of BN; (d) schematic band alignment of BN and WO3.

## 14. EPR signal intensities and radical trapping experiments

Figure S14. (a) Relative DMPO-OOH and DMPO-OH EPR signal intensities over WO3 and WO3/BN-1:1; (b) radical trapping experiments for photocatalytic methane oxidation over WO3/BN-1:1 and WO3

## 15. In situ DRIFTS spectra of WO3

Figure S15. In situ DRIFTS spectra of WO3

## 16. In situ DRIFTS spectra of WO3/BN-1:1

Figure S16. In situ DRIFTS spectra of WO3/BN-1:1

## 17. In situ DRIFTS spectra of BN

Figure S17. In situ DRIFTS spectra of BN

# Supporting Tables

## 1. Performance of CH4 photooxidation

Table S1. Performance of CH4 photooxidation on WO3 and WO3/BN catalysts; Reaction conditions: 20 mL water, 5 mL CH4, atmospheric pressure, 60 °C, 300 W Xe lamp (600 mW cm-2).

| Samples | CH3OH (μmol g-1 h-1) | HCHO (μmol g-1 h-1) | CO (μmol g-1 h-1) | CO2 (μmol g-1 h-1) | CH3OH selectivity in total products (%) | CH3OH proportion in liquid products (%) |
| --- | --- | --- | --- | --- | --- | --- |
| BN | 202.5 | 104.2 | 0.5 | 10.7 | 63.7 | 66.0 |
| WO3/BN-1:2 | 594.0 | 134.3 | 2.3 | 26.2 | 78.5 | 81.6 |
| WO3/BN-1:1 | 741.6 | 177.3 | 1.6 | 40.3 | 77.2 | 80.7 |
| WO3/BN-2:1 | 418.2 | 349.1 | 2.9 | 33.6 | 52.0 | 54.5 |
| WO3 | 376.5 | 222.8 | 1.1 | 15.5 | 61.1 | 62.8 |

CH3OH proportion in liquid products was calculated as CH3OH/ (CH3OH + HCHO) × 100%

## 2. Control experiments

Table S2. Control experiments under different reaction conditions of WO3/BN-1:1 catalyst.

| Reaction condition | CH3OH (mol g-1 h-1) | HCHO (mol g-1 h-1) | CO2 (mol g-1 h-1) | CO (mol g-1 h-1) |
| --- | --- | --- | --- | --- |
| Without catalyst | 0.0 | 0.0 | 0.0 | 0.0 |
| Without CH4 | 0.0 | 0.0 | 0.0 | 0.0 |
| Dark | 0.0 | 0.0 | 0.0 | 0.0 |
| Without O2 | 282.7 | 83.9 | 12.4 | 0.5 |

## 3. Comparison of productivity of photocatalytic CH4 conversion to CH3OH

Table S3. Comparison of productivity of photocatalytic CH4 conversion to CH3OH.

| Catalysts | Extra oxidants | P (bar) | Catalyst (mg) | CH3OH (mol g-1 h-1) | Reference |
| --- | --- | --- | --- | --- | --- |
| WO3 | H2O2 | 20 | 20 | 253.0 | [1] |
| AuPs/WO3 | H2O2 | 20 | 20 | 367.0 | [1] |
| Au1/WO3 | H2O2 | 20 | 20 | 589.0 | [1] |
| 0.15 wt% Pd1/2DT | H2O2 | 20 | 20 | 43.8 | [2] |
| 0.33 metal wt%FeOx/TiO2 | H2O2 | 1 | 10 | 352.0 | [3] |
| Au1/BP | O2 | 33 | 200 | 56.8 | [4] |
| Au0.25/WO3 | O2 | 30 | 10 | 124 | [5] |
| Pt0.25/WO3 | O2 | 30 | 10 | 602 | [5] |
| Pd0.25/WO3 | O2 | 30 | 10 | 716 | [5] |
| 0.1 wt% Pd/ZnO | O2 | 21 | 10 | 3035.0 | [6] |
| 0.1 wt% Au/ZnO | O2 | 21 | 10 | 2060.0 | [6] |
| 0.1 wt% Pt/ZnO | O2 | 21 | 10 | 2225.0 | [6] |
| 0.1 wt% Ag/ZnO | O2 | 21 | 10 | 365.0 | [6] |
| TiO2 | O2 | 21 | 10 | 950.0 | [7] |
| 2.1% Ag/TiO2 | O2 | 21 | 10 | 3280.0 | [7] |
| 3.2% Ag/TiO2 | O2 | 21 | 10 | 4770.0 | [7] |
| ZnO | O2 | 20 | 10 | 89.0 | [8] |
| Au0.3/ZnO | O2 | 20 | 10 | 998.0 | [8] |
| 3.6-Co-SrTiO3 | / | 10 | 50 | 172.0 | [9] |
| BN | O2 | 1 | 20 | 76.9 | [10] |
| ZnO/BN-0.1:1 | O2 | 1 | 20 | 684.5 | [11] |
| 1 wt% Fe/BN | O2 | 1 | 20 | 257.8 | [12] |
| Ga2O3/BN-1:1 | O2 | 1 | 20 | 618.9 | [13] |
| BiOI/BN | O2 | 1 | 20 | 238.0 | [14] |
| WO3/BN-1:1 | O2 | 1 | 20 | 741.6 | This work |

## 4. Radical trapping experiments

Table S4. Radical trapping experiments over WO3 and WO3/BN-1:1.

| Radical scavenger | Samples | CH3OH (μmol g-1 h-1) | HCHO (μmol g-1 h-1) | CO (μmol g-1 h-1) | CO2 (μmol g-1 h-1) | CH3OH selectivity (%) | CH3OH retention (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Salicylic acid (·OH scavenger) | WO3/BN-1:1 | 216.6 | 9.3 | 1.6 | 28.3 | 84.7 | 29.2 |
|  | WO3 | 265.2 | 4.9 | 2.3 | 29.0 | 88.0 | 70.4 |
| p-Benzoquinone (·OOH scavenger) | WO3/BN-1:1 | 160.6 | 0 | 55.2 | 655.4 | 18.4 | 21.7 |
|  | WO3 | 224.4 | 24.5 | 27.0 | 370.5 | 34.7 | 59.6 |
| No scavenger | WO3/BN-1:1 | 741.6 | 177.3 | 1.6 | 40.3 | 77.2 | 100 |
|  | WO3 | 376.5 | 222.8 | 1.1 | 15.5 | 61.1 | 100 |

CH3OH retention (%) = rCH3OH, with scavenger/rCH3OH, without scavenger × 100%

## Supporting References

1.	Zeng Y, Tang Z, Wu X, et al. Photocatalytic oxidation of methane to methanol by tungsten trioxide-supported atomic gold at room temperature. Applied Catalysis B: Environmental, 2022, 306: 120919.

2.	Wu X, Zhang Q, Li W, et al. Atomic-scale Pd on 2D titania sheets for selective oxidation of methane to methanol. ACS Catalysis, 2021, 11(22): 14038-14046.

3.	Xie J, Jin R, Li A, et al. Highly selective oxidation of methane to methanol at ambient conditions by titanium dioxide-supported iron species. Nature Catalysis, 2018, 1(11): 889-896.

4.	Luo L, Luo J, Li H, et al. Water enables mild oxidation of methane to methanol on gold single-atom catalysts. Nature Communications, 2021, 12(1): 1218.

5.	Jiang Y, Fan Y, Liu X, et al. Steering photooxidation of methane to formic acid over a priori screened supported catalysts. Journal of the American Chemical Society, 2024, 146(23): 16039-16051.

6.	Song H, Meng X, Wang S, et al. Direct and selective photocatalytic oxidation of CH4 to oxygenates with O2 on cocatalysts/ZnO at room temperature in water. Journal of the American Chemical Society, 2019, 141(51): 20507-20515.

7.	Feng N, Lin H, Song H, et al. Efficient and selective photocatalytic CH4 conversion to CH3OH with O2 by controlling overoxidation on TiO2. Nature Communications, 2021, 12(1): 4652.

8.	Zhou W, Qiu X, Jiang Y, et al. Highly selective aerobic oxidation of methane to methanol over gold decorated zinc oxide via photocatalysis. Journal of Materials Chemistry A, 2020, 8(26): 13277-13284.

9.	Zhang Z, Zhang J, Zhu Y, et al. Photo-splitting of water toward hydrogen production and active oxygen species for methane activation to methanol on Co-SrTiO3. Chem Catalysis, 2022, 2(6): 1440-1449.

10.	Cao Y H, Yu W, Han C Q, et al. Methane photooxidation with nearly 100% selectivity towards oxygenates: Proton rebound ensures the regeneration of methanol. Angewandte Chemie International Edition, 2023, 62(18): e202302196.

11.	Yu W, Zhang X, Cao Y, et al. Ultrafast interfacial charge-delivery gating enables radical-suppressed photocatalytic methane-to-C1 oxygenates. Applied Catalysis B: Environment and Energy, 2026, 394: 126819.

12.	He Y, Yu W, Cao Y, et al. Fe-enhanced proton capture on boron nitride surfaces for improved photocatalytic methane conversion to C1 chemicals. Small Science, 2026, 6(5): e70302.

13.	Yu W, Yang Y, Cao Y, et al. In situ H-bond-mediated intermediate stabilization on Ga2O3/BN for highly selective photocatalytic methane oxidation to methanol. Applied Catalysis B: Environment and Energy, 2026, 385: 126333.

14.	Cao Y H, Yu W, Li Y, et al. Engineering ultrafast photo-induced charge and carbon intermediates transfer at interface to break the activity-selectivity trade-off in direct conversion of methane to methanol. Advanced Energy Materials, 2025, 15(6): 2404871.