Electronic Supplementary Information

Figure S1. The linear sweep voltammetry polarization curves of (a) M-P (M = Ni, Co; M-P = 1:1, 2:3, 1:2, 2:5 and 1:3) @Ag NWs. (b) NiCoP (Ni:Co = 1:1, 2:1, 3:1 and 4:1) @Ag NWs. (c) NiCoP@Ag NWs with different electrodeposition time (t = 200, 300, 400 and 500 s).

Fig. S2. The naked eye observed the morphology of bare Ag NWs, NiCoP@Ag NWs, Ni2P@Ag NWs, and Co2P@Ag NWs.

Fig. S3. The line profiles of NiCoP@Ag NWs

Fig. S4. The XPS survey spectra of NiCoP@Ag NWs, Ni2P@Ag NWs,

and Co2P@Ag NWs.

Fig. S5. The optimal absorption site of H.

Fig. S6. Comparison of performance between NiCoP@Ag NWs and Pt/C@Ag NWs catalyst. (a) HER polarization curves. (b) Tafel slopes.

Fig. S7. Cyclic voltammograms (CV) curves for ECSA measurements in the non-Faradaic region over (a) NiCoP@Ag NWs, (b) NiCoP@NF, (c) Ni2P@Ag NWs and (d) Co2P@Ag NWs.

Fig. S8. SEM image of the NiCoP@Ag NWs after stability test.

Fig. S9. The stability test of NiCoP@Ag NWs at a constant current density of 100 mA cm-2 for 50 h.

Table S1. Comparison of the HER performance of NiCoP@Ag NWs in 0.5 M H2SO4 with reported non-noble metal-based catalysts.

| Electrocatalysts | η10mA cm-2 (mV) | Tafel (mV dec-1) | References |
| --- | --- | --- | --- |
| NiCoP@Ag NWs | 109 | 62.6 | This work |
| MoO3/MoS2 | 250 | 125 | [1] |
| NiCoP fibers | 146 | 97.8 | [2] |
| FeCoP2@NPPC | 114 | 79 | [3] |
| Co-MoS2 | 151 | 64 | [4] |
| V-doped WS2 | 185 | 61 | [5] |
| Nb0.7V0.3Se2 | 236 | 72 | [6] |
| Frenkel-defected MoS2 | 164 | 36 | [7] |
| m-CoSe2 | 124 | 37 | [8] |
| FePSe3@N-C/GCE (GCE:Glassy carbon electrode) | 118.5 | 53 | [9] |
| Ni2P/NF | 176 | 138 | [10] |
| Ni-P/NF | 189 | 74 | [11] |
| Cu@MoS2 | 131 | 51 | [12] |
| VSe–NiCo2Se4-NWs/NCNFs | 168 | 49.8 | [13] |
| NiCo2Se4-NWs/NCNFs | 200 | 55.9 | [13] |
| WS2/CoS2/CC | 146 | 64 | [14] |
| CoSe2@MoSe2 | 131 | 48 | [15] |
| CoSe2@MoSe2/GCE | 183 | 43.37 | [15] |
| NiCoP/CC | 197 | 86.7 | [16] |
| CoMn-P@NG | 159(20 mA cm-2) | 64.85 | [17] |
| Mo2C/C | 264 | 88 | [18] |
| (Mo/β-Mo2C)@C | 152 | 51.7 | [19] |
| MoSe2-CoP | 298 | 114 | [20] |
| 316 L SS-1600 | 209.8 | 115.6 | [21] |
| CoTe2@NF | 111 | 79 | [22] |
| V-MoS2 | 194 | 59 | [23] |
| CoN/MoC/NMCNFs | 199.2 | 97.2 | [24] |
| SS-MoC | 182 | 48 | [25] |
| B–MoC | 285 | 128 | [26] |
| Ni-MoC@NGC | 202 | 69 | [27] |
| Terraced α-Mo2C | 294 | 63 | [28] |
| MoC-MoP/BCNC NFs | 158 | 58 | [29] |
| Mo2C&MoS2@NSC | 209 | 85.5 | [30] |
| Fe-CoP/PCNF | 151 | 53.9 | [31] |
| FeNiP/NPC800 | 277 | 95 | [32] |
| 4%-SPCNF | 310.86 | 95.93 | [33] |

References

[1] L. Sharma, T. Botari, C.S. Tiwary, A. Halder. Hydrogen evolution at the in situ MoO3/MoS2 heterojunctions created by nonthermal O2 plasma treatment. ACS Applied Energy Materials, 3 (2020) 5333‒5342

[2] C. Bera, M. Streckova, R. Orinakova, A. Guboova, T. Bystron, V. Girman, F. Kromka, M. Podobova, K. Bouzek. NiCoP fibers as novel catalysts for hydrogen evolution in alkali and acidic environment. International Journal of Hydrogen Energy, 60 (2024) 118‒132

[3] Y.-N. Wang, Z.-J. Yang, D.-H. Yang, L. Zhao, X.-R. Shi, G. Yang, B.-H. Han. FeCoP2 nanoparticles embedded in N and P co-doped hierarchically porous carbon for efficient electrocatalytic water splitting. ACS Applied Materials & Interfaces, 13 (2021) 8832‒8843

[4] H. Duan, C. Wang, G. Li, H. Tan, W. Hu, L. Cai, W. Liu, N. Li, Q. Ji, Y. Wang. Single‐atom‐layer catalysis in a MoS2 monolayer activated by long‐range ferromagnetism for the hydrogen evolution reaction: beyond single‐atom catalysis. Angewandte Chemie, 133 (2021) 7327‒7334.

[5] A. Han, X. Zhou, X. Wang, S. Liu, Q. Xiong, Q. Zhang, L. Gu, Z. Zhuang, W. Zhang, F. Li. One-step synthesis of single-site vanadium substitution in 1T-WS2 monolayers for enhanced hydrogen evolution catalysis. Nature Communications, 12 (2021) 709.

[6] I.H. Kwak, I.S. Kwon, G.M. Zewdie, T.T. Debela, S.J. Lee, J.Y. Kim, S.J. Yoo, J.-G. Kim, J. Park, H.S. Kang. Polytypic phase transition of Nb1–xVxSe2 via colloidal synthesis and their catalytic activity toward hydrogen evolution reaction. ACS nano, 16 (2022) 4278‒4288.

[7] J. Xu, G. Shao, X. Tang, F. Lv, H. Xiang, C. Jing, S. Liu, S. Dai, Y. Li, J. Luo. Frenkel-defected monolayer MoS2 catalysts for efficient hydrogen evolution. Nature communications, 13 (2022) 2193.

[8] X.-L. Zhang, S.-J. Hu, Y.-R. Zheng, R. Wu, F.-Y. Gao, P.-P. Yang, Z.-Z. Niu, C. Gu, X. Yu, X.-S. Zheng. Polymorphic cobalt diselenide as extremely stable electrocatalyst in acidic media via a phase-mixing strategy, Nature Communications, 10 (2019) 5338.

[9] J. Yu, W.-J. Li, H. Zhang, F. Zhou, R. Li, C.-Y. Xu, L. Zhou, H. Zhong, J. Wang. Metallic FePSe3 nanoparticles anchored on N-doped carbon framework for All-pH hydrogen evolution reaction. Nano Energy, 57 (2019) 222-229.

[10] H. Yang, P. Guo, R. Wang, Z. Chen, H. Xu, H. Pan, D. Sun, F. Fang, R. Wu. Sequential phase conversion‐induced phosphides heteronanorod arrays for superior hydrogen evolution performance to Pt in wide pH media. Advanced Materials, 34 (2022) 2107548.

[11] J. Zhang, Z. Zhang, Y. Ji, J. Yang, K. Fan, X. Ma, C. Wang, R. Shu, Y. Chen. Surface engineering induced hierarchical porous Ni12P5-Ni2P polymorphs catalyst for efficient wide pH hydrogen production. Applied Catalysis B: Environmental, 282 (2021) 119609.

[12] L. Ji, P. Yan, C. Zhu, C. Ma, W. Wu, C. Wei, Y. Shen, S. Chu, J. Wang, Y. Du. One-pot synthesis of porous 1T-phase MoS2 integrated with single-atom Cu doping for enhancing electrocatalytic hydrogen evolution reaction. Applied Catalysis B: Environmental, 251 (2019) 87‒93.

[13] W. Zong, R. Lian, G. He, H. Guo, Y. Ouyang, J. Wang, F. Lai, Y.-E. Miao, D. Rao, D. Brett. Vacancy engineering of group VI anions in NiCo2A4 (A= O, S, Se) for efficient hydrogen production by weakening the shackles of hydronium ion. Electrochimica Acta, 333 (2020) 135515.

[14] J. Wu, T. Chen, C. Zhu, J. Du, L. Huang, J. Yan, D. Cai, C. Guan, C. Pan. Rational construction of a WS2/CoS2 heterostructure electrocatalyst for efficient hydrogen evolution at all pH values. ACS Sustainable Chemistry & Engineering, 8 (2020) 4474‒4480.

[15] Z. Chen, W. Wang, S. Huang, P. Ning, Y. Wu, C. Gao, T.-T. Le, J. Zai, Y. Jiang, Z. Hu. Well-defined CoSe2@ MoSe2 hollow heterostructured nanocubes with enhanced dissociation kinetics for overall water splitting. Nanoscale, 12 (2020) 326‒335.

[16] K. Jiang, J. Li, Z. Zheng, T. Zhang, G. Wang, C. Shi, X. Hou. Bimetallic phosphide NiCoP electrocatalyst synthesized by one-step electrodeposition for efficient hydrogen evolution in acidic and alkaline solution. ACS Applied Energy Materials, 7 (2024) 7895‒7905.

[17] J. Liu, W. Li, Z. Cui, J. Li, F. Yang, L. Huang, C. Ma, M. Zeng. CoMn phosphide encapsulated in nitrogen-doped graphene for electrocatalytic hydrogen evolution over a broad pH range. Chemical Communications, 57 (2021) 2400‒2403.

[18] G. Wang, J. Li, B. Zhang, T. Zhang, Z. Zheng, K. Jiang. One-step molten-salt synthesis of adjustable composition molybdenum carbide-based electrocatalysts for hydrogen evolution in both acidic and alkaline media. Sustainable Energy & Fuels, 7 (2023) 5352‒5360.

[19] W. Zhu, Z. Jiang, X. Peng, Z. Li, A.R. Woldu, F. Lu, Y. Fang, P.K. Chu, L. Hu. Janus (Mo/β-Mo2C)@C heterostructure as an efficient electrocatalyst for the hydrogen evolution reaction in acidic and alkaline media. Nanotechnology, 34 (2022) 055704.

[20] A. Kagkoura, C. Stangel, R. Arenal, N. Tagmatarchis. Molybdenum diselenide and tungsten diselenide interfacing cobalt-porphyrin for electrocatalytic hydrogen evolution in alkaline and acidic media. Nanomaterials, 13 (2022) 35.

[21] Y. Liu, K. Zhang, D. Zhang, W. Dong, T. Jiang, H. Zhou, L. Li, B. Mao. Industrial stainless steel meshes for efficient electrocatalytic hydrogen evolution. Journal of Energy Storage, 41 (2021) 102844.

[22] Y. Yin, J. Xu, W. Guo, Z. Wang, X. Du, C. Chen, Z. Zheng, D. Liu, D. Qu, Z. Xie. A single-step fabrication of CoTe2 nanofilm electrode toward efficient overall water splitting. Electrochimica Acta, 307 (2019) 451‒458.

[23] S. Bolar, S. Shit, J.S. Kumar, N.C. Murmu, R.S. Ganesh, H. Inokawa, T. Kuila. Optimization of active surface area of flower like MoS2 using V-doping towards enhanced hydrogen evolution reaction in acidic and basic medium. Applied Catalysis B: Environmental, 254 (2019) 432‒442.

[24] L. Wang, W. He, D. Yin, H. Zhang, D. Liu, Y. Yang, W. Yu, X. Dong. CoN/MoC embedded in nitrogen-doped multi-channel carbon nanofibers as an efficient acidic and alkaline hydrogen evolution reaction electrocatalysts. Renewable and Sustainable Energy Reviews, 181 (2023) 113354.

[25] X. Zhang, T. Liu, T. Guo, Z. Mu, X. Hu, K. He, X. Chen, V.P. Dravid, Z. Wu, D. Wang. High-performance MoC electrocatalyst for hydrogen evolution reaction enabled by surface sulfur substitution. ACS applied materials & interfaces, 13 (2021) 40705‒40712.

[26] Q. Lin, C. Shang, Z. Chen, X. Wang, G. Zhou. Boron-doped molybdenum carbide as a pH-independent electrocatalyst for the hydrogen evolution reaction. International Journal of Hydrogen Energy, 45 (2020) 30659‒30665.

[27] S. Roy, D. Bagchi, L. Dheer, S.C. Sarma, V. Rajaji, C. Narayana, U.V. Waghmare, S.C. Peter. Mechanistic insights into the promotional effect of Ni substitution in non-noble metal carbides for highly enhanced water splitting. Applied Catalysis B: Environmental, 298 (2021) 120560.

[28] J. Bang, I.K. Moon, K. Choi, J. Oh. Phase-engineering terraced structure of edge-rich α-Mo2C for efficient hydrogen evolution reaction. Materials Today Energy, 26 (2022) 100981.

[29] N. Chen, Q. Mo, L. He, X. Huang, L. Yang, J. Zeng, Q. Gao. Heterostructured MoC-MoP/N-doped carbon nanofibers as efficient electrocatalysts for hydrogen evolution reaction. Electrochimica Acta, 299 (2019) 708-716.

[30] Q. Wang, R. Yu, D. Shen, G. Liu, K.H. Luo, C. Wu, S. Gu. One-pot synthesis of Mo2C&MoS2 loaded on N/S co-doped carbon materials as the electrocatalyts for hydrogen evolution reaction. Fuel, 318 (2022) 123615.

[31] X. Chen, B. Yu, Y. Dong, X. Zhu, W. Zhang, S. Ramakrishna, Z. Liu. Electrospun porous carbon nanofibers decorated with iron-doped cobalt phosphide nanoparticles for hydrogen evolution. Journal of Alloys and Compounds, 918 (2022) 165733.

[32] Y. Gong, L.-H. Xu, J. Li, D. Shan. Confinement of transition metal phosphides in N, P-doped electrospun carbon fibers for enhanced electrocatalytic hydrogen evolution. Journal of Alloys and Compounds, 875 (2021) 159934.

[33] H. He, Y. Zhang, W. Zhang, Y. Li, X. Zhu, P. Wang, D. Hu. Porous carbon nanofibers derived from silk fibroin through electrospinning as N-doped metal-free catalysts for hydrogen evolution reaction in acidic and alkaline solutions. ACS Applied Materials & Interfaces, 14 (2021) 834‒849.