Supporting information:

Three-phase anode enabling high water splitting performance of protonic solid oxide electrolysis cell

Fig. S1 Photograph of a representative single cell (button cell) with a diameter of approximately 10 mm.

Fig. S2 Photograph of the actual P-SOEC testing setup

Fig. S3 Schematic diagram of the P-SOEC testing setup, illustrating the measurement configuration.

Fig. S4 XRD patterns of three independently synthesized batches of LBCNA-900 prepared using the same citric acid sol-gel method.

Fig. S5 XPS spectra of Ni 2p for three LBCNA oxides.

Fig. S6 TG results of (a) LBCNA-800 and (b) LBCNA-1000 sample under dry and humid air (pH2O = 0.02 atm) from 50 to 800 °C;

Fig. S7 The EIS of GDC electrolyte-supported symmetrical cells: the comparison of ASR for three electrodes.

Fig. S8 The EIS of BZCYYb4411 electrolyte-supported symmetrical cells with (a) LBCNA-800, (b) LBCNA-900, and (c) LBCNA-1000 electrodes. (d) The comparison of ASR for three electrodes.

Fig. S9 the stability of P-SOEC with LBCNA-900 anode at 600 °C and a constant voltage of 1.2 V.

Fig. S10. (a) I-V curves of P-SOEC with (a) LBCNA-800 and (b) LBCNA-1000 anode at 600-700 °C

Table S1 XRD refinement results of LBCNA oxides.

| LBCNA-800 | a(Å) | b(Å) | c(Å) | Rp (%) | Rwp (%) | Rexp (%) | Chi2 | Space group |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| R-LBCNA | 5.4521 | 5.4521 | 13.1616 | 9.48 | 12.1 | 10.25 | 1.39 | R3c |
| RP-LBCNA | 3.8559 | 3.8559 | 12.8123 |  |  |  |  | I4/mmm |
| Ag | 4.0847 | 4.0847 | 4.0847 |  |  |  |  | Fm3m |

| LBCNA-900 | a(Å) | b(Å) | c(Å) | Rp (%) | Rwp (%) | Rexp (%) | Chi2 | Space group |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| R-LBCNA | 5.4489 | 5.4489 | 13.1493 | 2.18 | 2.81 | 1.95 | 2.07 | R3c |
| RP-LBCNA | 3.8541 | 3.8541 | 12.8189 |  |  |  |  | I4/mmm |
| Ag | 4.0849 | 4.0849 | 4.0849 |  |  |  |  | Fm3m |

| LBCNA-1000 | a(Å) | b(Å) | c(Å) | Rp (%) | Rwp (%) | Rexp (%) | Chi2 | Space group |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| R-LBCNA | 5.4546 | 5.4546 | 13.1769 | 4.52 | 5.67 | 7.72 | 0.54 | R3c |
| RP-LBCNA | 3.8556 | 3.8556 | 12.8138 |  |  |  |  | I4/mmm |
| Ag | 4.0864 | 4.0864 | 4.0864 |  |  |  |  | Fm3m |

Table S2 XPS fitting results of O 1s spectra for LBCNA oxides.

| Samples |  | O1s |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Lattice oxygen | Adsorbed oxygen | hydroxylated oxygen species | Absorbed surface water |
|  |  | Olat | Oad | OOH | OH2O |
| LBCNA-800 | Position (eV) | 528.74 | 529.70 | 531.21 | 532.73 |
|  | Area ratio (%) | 29.9 | 8.58 | 46.04 | 15.48 |
| LBCNA-900 | Position (eV) | 528.87 | 529.87 | 531.20 | 532.70 |
|  | Area ratio (%) | 38.66 | 13.68 | 37.07 | 10.59 |
| LBCNA-1000 | Position (eV) | 528.65 | 529.65 | 531.17 | 532.71 |
|  | Area ratio (%) | 29.06 | 9.10 | 43.41 | 18.43 |

Table S3 XPS fitting results of Ba 3d+Co 2p spectra for LBCNA oxides.

| Samples |  | Ba 3d+Co 2p |  |  |
| --- | --- | --- | --- | --- |
|  |  | Co3+ | Co2+ | Ba2+ |
| LBCNA-800 | Position (eV) | 778.5/793.6 | 781.04/796.55 | 779.91/795.1 |
|  | Area ratio (%) | 18.90 | 26.46 | 47.67 |
| LBCNA-900 | Position (eV) | 778.5/793.7 | 781.00/796.66 | 780.00/795.3 |
|  | Area ratio (%) | 28.98 | 19.64 | 51.39 |
| LBCNA-1000 | Position (eV) | 778.5/793.7 | 781.00/796.64 | 780.18/795.4 |
|  | Area ratio (%) | 28.65 | 21.84 | 42.81 |

Table S4 XPS fitting results of Ag 3d spectra for LBCNA oxides.

| Samples |  | Ag 3d |  |
| --- | --- | --- | --- |
|  |  | Ag+ | Ag0 |
| LBCNA-800 | Position (eV) | 368.50/374.46 | 368.90/374.94 |
|  | Area ratio (%) | 69.18 | 30.82 |
| LBCNA-900 | Position (eV) | 368.22/374.24 | 368.68/374.64 |
|  | Area ratio (%) | 78.49 | 21.51 |
| LBCNA-1000 | Position (eV) | 368.3/374.3 | 368.70/374.70 |
|  | Area ratio (%) | 77.25 | 22.75 |

Table S5 The summary of ASR values for this work and other reported excellent anodes.

| Anodes | Temperature (°C) | ASR(Ω cm2) | Refs |
| --- | --- | --- | --- |
| BaCo0.4Fe0.4Zr0.2O3-δ (BCFZ) | 650 | 0.61 | [1] |
|  | 600 | 1.03 |  |
|  | 550 | 1.92 |  |
| Nd0.5Ba0.5Fe0.9Co0.1O3-δ (NBFC) | 650 | 0.39 | [2] |
|  | 600 | 1 |  |
|  | 550 | - |  |
| Ba2Co1.5Mo0.25Nb0.25O6-δ (BC1.5MN) | 650 | 0.6 | [3] |
|  | 600 | 1.0 |  |
|  | 550 | 1.8 |  |
| Ba0.5Sr0.5Co0.8Fe0.2O3-δ (BSCF) | 650 | 0.79 | [4] |
|  | 600 | 1.31 |  |
|  | 550 | 1.99 |  |
| La0.6Sr0.4Co0.2Fe0.8O3-δ (LSCF) | 650 | 0.18 | [5] |
|  | 600 | 0.51 |  |
|  | 550 | 1.05 |  |
| BaCo0.4Fe0.4Zr0.1Y0.1O3-δ (BCFZY) | 650 | 0.40 | [6] |
|  | 600 | 0.85 |  |
|  | 550 | 1.15 |  |
| Sr2Sc0.1Nb0.1Co1.5Fe0.3O6-δ (SSNCF) | 650 | 0.11 | [7] |
|  | 600 | 0.23 |  |
|  | 550 | 0.47 |  |
| Ba0.5Sr0.5Sc0.175Nb0.025Co0.8O6-δ (BSSNC) | 650 | 0.25 | [8] |
|  | 600 | 0.66 |  |
|  | 550 | 1.86 |  |
| SrCo0.8Fe0.15Zr0.05O3-δ (SCFZ) | 650 | 0.15 | [9] |
|  | 600 | 0.38 |  |
|  | 550 | 1.01 |  |
| PrBa0.8Sr0.2Co2O6-δ (PBSC) | 650 | 0.15 | [10] |
|  | 600 | 0.35 |  |
|  | 550 | 0.95 |  |
| Pr0.2Ba0.2Sr0.2La0.2Ca0.2CoO3-δ (PBSLCC) | 650 | 0.12 | [10] |
|  | 600 | 0.26 |  |
|  | 550 | 0.75 |  |
| Ba(Co0.4Fe0.4Zr0.1Y0.1)0.95Ni0.05F0.1O2.9-δ (BCFZYNF) | 650 | 0.075 | [11] |
|  | 600 | 0.17 |  |
|  | 550 | 0.41 |  |
| La(Co0.2Cu0.2Fe0.2Ni0.2Cr0.2)O3-δ (LCCFN-Cr) | 650 | 0.22 | [12] |
|  | 600 | 0.27 |  |
|  | 550 | 0.46 |  |
| LBCNA-800 | 650 | 0.25 | This work |
|  | 600 | 0.80 |  |
|  | 550 | 1.7 |  |
| LBCNA-900 | 650 | 0.051 |  |
|  | 600 | 0.10 |  |
|  | 550 | 0.31 |  |
| LBCNA-1000 | 650 | 0.052 |  |
|  | 600 | 0.35 |  |
|  | 550 | 0.82 |  |

Table S6 Summary of current density for LBCNA-900 and other recently reported advanced anodes based on fuel-electrode-supported single button cells.

| Time | Materials |  | Inlet gas composition |  | I (A cm–2) |
| --- | --- | --- | --- | --- | --- |
|  | Anode | Electrolyte | Anode | Cathode |  |
| 2018[13] | PBSCF | BZCYYb | Air (12% H2O) | 5% H2/Ar | 0.74 |
| 2018[14] | NBSCF/BZCYYb | BZCYYb | Air (10% H2O) | H2 (10% H2O) | 0.75 |
| 2019[15] | BCFZY | BZCYYb | Air | - | 1 |
| 2019[16] | PBSCF | BZCYYb4411 | Air (3% H2O) | 97% H2(3% H2O) | 1.18 |
| 2020[17] | PNC55 (3D) | BZCYYb4411 | Air (10% H2O) | 10% H2/Ar | 1.17 |
| 2020[18] | PBCC95 | BZCYYb4411 | Air (20% H2O) | 97% H2(3% H2O) | 0.72 |
| 2021[19] | YEBCG | BZCYYb1711 | Air (20% H2O) | 10% H2/N2 | 1.19 |
| 2021[20] | SCFN | BZCYYb1711 | Air | 100% H2 | 0.36 |
| 2022[21] | BCFZYM | BZCYYb1711 | Air (10% H2O) | 97% H2(3% H2O) | 1.24 |
| 2022[22] | BSCFP | BZCYYb1711 | Air (10% H2O) | 100% H2 | 1 |
| 2022[3] | BC1.5MN | BZCYYb1711 | Air (3% H2O) | 97% H2(3% H2O) | 1.34 |
| 2022[23] | PBCFN | BZCYYb1711 | Air (3% H2O) | 97% H2(3% H2O) | 1.04 |
| 2022[24] | LCCN7382 | BZCYYb4411 | Air (3% H2O) | 97% H2(3% H2O) | 0.88 |
| 2023[25] | LCN91 | BZCYYb4411 | Air (3% H2O) | 97% H2(3% H2O) | 0.84 |
| 2023[26] | BCFNbS | BZCYYb1711 | Air (3% H2O) | 97% H2(3% H2O) | 0.91 |
| 2023[27] | BSCFE | BZCYYb1711 | Air (5% H2O) | 97% H2(3% H2O) | 0.98 |
| 2023[28] | BCFZYN | BZCYYb1711 | Air (5% H2O) | 97% H2(3% H2O) | 1.2 |
| 2024[29] | SFN | BZCYYb1711 | Air (3% H2O) | 100% H2 | 0.8 |
| 2024[30] | PSCN | BZCYYb1711 | Air | 97% H2(3% H2O) | 1.25 |
| 2024[11] | BCFZYNF | BZCYYb1711 | Air (3% H2O) | 100% H2 | 1.1 |
| This work | LBCNA-800 | BZCYYb4411 | Air (3% H2O) | 97% H2(3% H2O) | 0.5 |
| This work | LBCNA-1000 | BZCYYb4411 | Air (3% H2O) | 97% H2(3% H2O) | 0.25 |
| This work | LBCNA-900 | BZCYYb4411 | Air (3% H2O) | 97% H2(3% H2O) | 1.8 |

PBSCF= PrBa0.5Sr0.5Co1.5Fe0.5O5+δ [13], PBSCF=PrBa0.5Sr0.5Co1.5Fe0.5O5+δ [16], PNC=PrNi0.5Co0.5O3-δ [17], PBCC95=(PrBa0.8Ca0.2)0.95Co2O6-δ [18], YEBCG=Y0.8Er0.2BaCo3.2Ga0.8O7+δ [19], SCFN= Sr0.9Ce0.1Fe0.8Ni0.2O3-δ [20], BCFZYM=Ba(Co0.4Fe0.4Zr0.1Y0.1)0.95Mg0.05O3-δ [20], BSCFP= Ba0.5Sr0.5(Co0.8Fe0.2)0.95P0.05O3-δ [22], BCMN=Ba2Co1.5Mo0.25Nb0.25O6-δ [31], PBCFN=PrBaCo1.6Fe0.2Nb0.2O5+δ [23], LCCN7382=La0.7Co0.3Co0.8Ni0.2O3-δ [24], LCN91= LaCo0.9Ni0.1O3-δ [25], BCFNS= BaCo0.4Fe0.4Nb0.1Sc0.1O3-δ [26], BSCFE= Ba0.5Sr0.5(Co0.8Fe0.2)0.9Er0.1O3-δ [27], BCFZYN= Ba0.95(Co0.4Fe0.4Zr0.1Y0.1)0.95Ni0.05O3-δ [28], SFN= Sr2.8Fe1.8Nb0.2O7-δ [29], PSCN= PrSrCo1.8Nb0.2O6-δ [30], BCFZYNF= Ba(Co0.4Fe0.4Zr0.1Y0.1)0.95Ni0.05F0.1O2.9-δ [11], BCFZY=Ba(Co0.4Fe0.4Zr0.1Y0.1)O3-δ [15], NBSCF= NdBa0.5Sr0.5Co1.5Fe0.5O5+δ [14], BZCYYb1711= BaZr0.1Ce0.7Y0.1Yb0.1O3-δ.

References

[1] Shang M, J Tong, and R O'Hayre. A promising cathode for intermediate temperature protonic ceramic fuel cells: BaCo0.4Fe0.4Zr0.2O3−δ. RSC Advances, 2013, 3(36): 15769–15775.

[2] Lyagaeva J, N Danilov, A Tarutin, et al. Designing a protonic ceramic fuel cell with novel electrochemically active oxygen electrodes based on doped Nd0.5Ba0.5FeO3−δ. Dalton Transactions, 2018, 47(24): 8149–8157.

[3] He F, S Liu, T Wu, et al. Catalytic self-assembled air electrode for highly active and durable reversible protonic ceramic electrochemical cells. Advanced Functional Materials, 2022, 32(48): 2206756.

[4] Bi L, E Fabbri, and E Traversa. Novel Ba0.5Sr0.5(Co0.8Fe0.2)1−xTixO3−δ (x=0, 0.05, and 0.1) cathode materials for proton-conducting solid oxide fuel cells. Solid State Ionics, 2012, 214(1–5).

[5] Zhou Y, E Liu, Y Chen, et al. An active and robust air electrode for reversible protonic ceramic electrochemical cells. ACS Energy Letters, 2021, 6(4): 1511–1520.

[6] Matsui T, N Kunimoto, K Manriki, et al. Oxygen reduction reaction over (Ba,Sr)6RE2Co4O15–Ba(Ce,Pr,Y)O3 composite cathodes for proton-conducting ceramic fuel cells. Journal of Materials Chemistry A, 2021, 9(27): 15199–15206.

[7] Zhou C, J Sunarso, Y Song, et al. New reduced-temperature ceramic fuel cells with dual-ion conducting electrolyte and triple-conducting double perovskite cathode. Journal of Materials Chemistry A, 2019, 7(21): 13265–13274.

[8] Zhang Y, A Zhu, Y Guo, et al. Electrochemical performance and effect of moisture on Ba0.5Sr0.5Sc0.175Nb0.025Co0.8O3-δ oxide as a promising electrode for proton-conducting solid oxide fuel cells. Applied Energy, 2019, 238(344–350).

[9] Lv X, H Chen, W Zhou, et al. A CO2-tolerant SrCo0.8Fe0.15Zr0.05O3−δ cathode for proton-conducting solid oxide fuel cells. Journal of Materials Chemistry A, 2020, 8(22): 11292–11301.

[10] He F, Y Zhou, T Hu, et al. An efficient high-entropy perovskite-type air electrode for reversible oxygen reduction and water splitting in protonic ceramic cells. Advanced Materials, 2023, 35(16): 2209469.

[11] Chen X, N Yu, Y Song, et al. Synergistic bulk and surface engineering for expeditious and durable reversible protonic ceramic electrochemical cells air electrode. Advanced Materials, 2024, 36(32): 2403998.

[12] Zhang X, C Tang, Y Yang, et al. Novel high-entropy air electrodes enhancing electrochemical performances of reversible protonic ceramic cells. Advanced Functional Materials, 2025, 2421083.

[13] Wu W, H Ding, Y Zhang, et al. 3D self‐architectured steam electrode enabled efficient and durable hydrogen production in a proton‐conducting solid oxide electrolysis cell at temperatures lower than 600 C. Advanced Science, 2018, 5(11): 1800360.

[14] Kim J, A Jun, O Gwon, et al. Hybrid-solid oxide electrolysis cell: A new strategy for efficient hydrogen production. Nano Energy, 2018, 44: 121–126.

[15] Duan C. Selective CO2 electrohydrogenation. Nature Catalysis, 2021, 4(4): 264–265.

[16] Choi S, T C Davenport, and S M Haile. Protonic ceramic electrochemical cells for hydrogen production and electricity generation: exceptional reversibility, stability, and demonstrated faradaic efficiency. Energy & Environmental Science, 2019, 12(1): 206–215.

[17] Ding H, W Wu, C Jiang, et al. Self-sustainable protonic ceramic electrochemical cells using a triple conducting electrode for hydrogen and power production. Nature Communications, 2020, 11(1): 1907.

[18] Tang W, H Ding, W Bian, et al. Understanding of A-site deficiency in layered perovskites: promotion of dual reaction kinetics for water oxidation and oxygen reduction in protonic ceramic electrochemical cells. Journal of Materials Chemistry A, 2020, 8(29): 14600–14608.

[19] Shin J-S, H Park, K Park, et al. Activity of layered swedenborgite structured Y0.8Er0.2BaCo3.2Ga0.8O7+δ for oxygen electrode reactions in at intermediate temperature reversible ceramic cells. Journal of Materials Chemistry A, 2021, 9(1): 607–621.

[20] Song Y, J Liu, Y Wang, et al. Nanocomposites: A new opportunity for developing highly active and durable bifunctional air electrodes for reversible protonic ceramic cells. Advanced Energy Materials, 2021, 11(36): 2101899.

[21] Liang M, Y Song, D Liu, et al. Magnesium tuned triple conductivity and bifunctionality of BaCo0.4Fe0.4Zr0.1Y0.1O3-δ perovskite towards reversible protonic ceramic electrochemical cells. Applied Catalysis B: Environmental, 2022, 318: 121868.

[22] Liu Z, D Cheng, Y Zhu, et al. Robust bifunctional phosphorus-doped perovskite oxygen electrode for reversible proton ceramic electrochemical cells. Chemical Engineering Journal, 2022, 450: 137787.

[23] Xu K, H Zhang, Y Xu, et al. An efficient steam‐induced heterostructured air electrode for protonic ceramic electrochemical cells. Advanced Functional Materials, 2022, 32(23): 2110998.

[24] Wang N, B Yuan, C Tang, et al. Machine‐learning‐accelerated development of efficient mixed protonic–electronic conducting oxides as the air electrodes for protonic ceramic cells. Advanced Materials, 2022, 34(51): 2203446.

[25] Wang N, B Yuan, F Zheng, et al. Machine‐learning assisted screening proton conducting Co/Fe based oxide for the air electrode of protonic solid oxide cell. Advanced Functional Materials, 2023, 34(12): 2309855.

[26] Lu C, R Ren, Z Zhu, et al. Ba Co0.4Fe0.4Nb0.1Sc0.1O3-δ perovskite oxide with super hydration capacity for a high-activity proton ceramic electrolytic cell oxygen electrode. Chemical Engineering Journal, 2023, 472(144878).

[27] Liu Z, Y Lin, H Nie, et al. Highly active nanocomposite air electrode with fast proton diffusion channels via Er doping‐induced phase separation for reversible proton ceramic electrochemical cells. Advanced Functional Materials, 2024, 34(7): 2311140.

[28] Liang M, Y Wang, Y Song, et al. High-temperature water oxidation activity of a perovskite-based nanocomposite towards application as air electrode in reversible protonic ceramic cells. Applied Catalysis B: Environmental, 2023, 331(122682.

[29] Yu N, I T Bello, X Chen, et al. Rational design of Ruddlesden–Popper perovskite ferrites as air electrode for highly active and durable reversible protonic ceramic cells. Nano-Micro Letters, 2024, 16(1): 177.

[30] Kang Zhu L Z, Nai Shi, Bingbing Qiu, Xueyu Hu, Daoming Huan, Changrong Xia, Ranran Peng, Yalin Lu. A superior catalytic air electrode with temperature-induced exsolution toward protonic ceramic cells. ACS Nano, 2024, 18(6): 5141–5151.

[31] He F, S Liu, T Wu, et al. Catalytic self‐assembled air electrode for highly active and durable reversible protonic ceramic electrochemical cells. Advanced Functional Materials, 2022, 32(48): 2206756.