Supporting information for

Scalable Synthesis of IrOx/Ir-Co3O4 Heterostructure for Efficient and Stable Acidic Oxygen Evolution

Fig. S1  (a) Top view of the Co3O4 (220) surface. (b) Top view of the IrO2 (101) surface.

Fig. S2  (a) SEM image of IrOx/Ir-Co3O4. Element mappings of (b) O, (c) Co, and (d) Ir for IrOx/Ir-Co3O4.

Fig. S3  (a) TEM image of Co3O4. (b) Enlarged TEM image of Co3O4 (inset is the magnified view of selected area). (c) TEM image of Ir-Co3O4. (d) Enlarged TEM image of Ir-Co3O4 (inset is the magnified view of selected area).

Fig. S4  XRD patterns of Co3O4, IrOx/Co3O4, Ir-Co3O4, and IrOx/Ir-Co3O4.

Fig. S5  SEM images of (a) Co3O4, (b) IrOx/Co3O4, (c) Ir-Co3O4, and (d) IrOx/Ir-Co3O4.

Fig. S6  CV curves at non-Faradaic potential ranges of the (a) Co3O4, (b) Ir-Co3O4, (c) IrOx/Ir-Co3O4, and (d) IrOx/Co3O4 catalysts with different scan rates (20-100 mV s-1) from 1.116 to 1.216 V vs. RHE.

Fig. S7  (a) SEM images of IrOx/Ir-Co3O4 after 210 h chronopotentiometry test. (b) Co 2p, (c) O 1s, and (d) Ir 4f XPS spectra of IrOx/Ir-Co3O4 after 210 h chronopotentiometry test.

Fig. S8  Long-term stability test of IrxCo3-xO4/Ir-Co3O4||Pt/C MEA in PEMWE at a constant current density of 18 mA cm-2.

Table S1  Ir and Co loading for IrOx/Ir-Co3O4.

| IrOx/Ir-Co3O4 | Content (mg cm-2) | Mass radio of Ir to Co |
| --- | --- | --- |
| Ir | 0.13 | 0.02 |
| Co | 6.36 |  |

Table S2  ECSA, ECSA-normalized activity, Ir loading and mass activity for IrO2 and IrOx/Ir-Co3O4.

| Electrocatalysts | Geometric area activity @1.5 V vs. RHE (mA cm-2) | ECSA (cm2) | ECSA-normalized Activity @1.5 V vs. RHE (mA cm-2) | Ir loading (mg cm-2) | Mass activity @1.5 V vs. RHE (A gIr-1) |
| --- | --- | --- | --- | --- | --- |
| IrO2 | 6.46 | 934 | 0.007 | 1.073 | 6.02 |
| IrOx/Ir-Co3O4 | 29.85 | 1194 | 0.025 | 0.13 | 230 |

Table S3  The performance evaluation indicators summary of Ir-based acidic OER electrocatalysts.

| Electrocatalysts | Overpotential @ 10 mA cm-2 | Stability | Ir loading | Mass activity@1.5 V vs RHE | Ref. |
| --- | --- | --- | --- | --- | --- |
| IrOx/Ir-Co3O4 | 237 mV | 210 h@100 mA cm-2 | 0.13 mg cm-2 | 230 A g Ir-1 | This work |
| IrRux@Ir | 288 mV | 24 h@10 mA cm-2 | 0.07 mg cm-2 | 68.6 A g Ir-1 | [1] |
| 20-Ir-C-1000-300 | 383 mV | 1000 CV cycles | 0.028 mg cm-2 | 16.1 A g Ir-1 | [2] |
| CoIr-CL | 320 mV | 13.5 h@1.6 V | 0.0153 mg cm-2 | 224 A g Ir-1 | [3] |
| Ir@WO3-x | 276 mV | 100 h@10 mA cm-2 | 0.07 mg cm-2 | 48.1 A g Ir-1 | [4] |
| Ir/ATO | 318 mV | Not provided | ~0.12 mg cm-2 | 31.7 A g Ir-1 | [5] |
| IrOx/WO3 | 260 mV | 100 h@10 mA cm-2 | 0.18 mg cm-2 | 180 A g Ir-1 | [6] |
| Ir-CeO2-C-350 NFs | 283 mV | 10 h@10 mA cm-2 | 0.47 mg cm-2 | 13.8 A g Ir-1 | [7] |
| La3Ir1-xMnxO7 | 276 mV | 175 h@10 mA cm-2 | ~0.013 mg cm-2 | 78.8 A g Ir-1 | [8] |
| Ir0.5W0.5/CNT | 283 mV | 10 h@10 mA cm-2 | 0.057 mg cm-2 | 224 A g Ir-1 | [9] |
| Tpyp-Ir(IrOx)-25 | 259 mV | 20 h@10 mA cm-2 | 0.051 mg cm-2 | 588 A g Ir-1 | [10] |
| Ir-Ta2O5 | 218 mV | 200 h@100 mA cm-2 | 0.064 mg cm-2 | 416 A g Ir-1 | [11] |
| GB-rich Ir NTs | 263 mV | 350 h@10 mA cm-2 | 0.04 mg cm-2 | 375 A g Ir-1 | [12] |
| 5Ir-Co3O4-bilayer | 316 mV | 1000 h@10 mA cm-2 | 0.0066 mg cm-2 | 303 A g Ir-1 | [13] |

Table S4  ICP test for IrOx/Ir-Co3O4||Pt/C MEA after 160 h stability.

| IrOx/Ir-Co3O4 | Initial content (mg cm-2) | Dissolved amount | Dissolution rate (μg h-1) |
| --- | --- | --- | --- |
| Ir | 0.13 | 0.0975 | 0.61 |
| Co | 6.36 | 0.46 | 2.87 |

References

- Zheng Y, Zhang F R, Wang G L, et al. CO induced phase-segregation to construct robust and efficient IrRux@Ir core-shell electrocatalyst towards acidic oxygen evolution. Journal of Power Sources, 2022, 528: 231189

- Sadeghi E, Morgen P, Makovec D, et al. Scalable solid-state synthesis of carbon-supported Ir electrocatalysts for acidic oxygen evolution reaction: Exploring the structure-activity relationship. ACS Applied Materials & Interfaces, 2024, 16(40): 53750–53763

- Ying Y F, Godínez Salomón J F, Lartundo-Rojas L, et al. Hydrous cobalt-iridium oxide two-dimensional nanoframes: insights into activity and stability of bimetallic acidic oxygen evolution electrocatalysts. Nanoscale Advances, 2021, 3(7): 1976–1996

- Ma X J, Yang C L, Zhang F R, et al. Oxygen-vacancy-rich tungsten oxide boosted ultrasmall iridium nanoparticles for acidic oxygen evolution. International Journal of Hydrogen Energy, 2023, 48(94): 36776–36783

- Jang H, Lee J H, Lee J R, et al. Metal-support interaction can deactivate IrOx/Sb:SnO2 OER catalysts in polyol process. ACS Applied Energy Materials, 2022, 5(8): 9297–9302

- Guan Z Y, Weng Y X, Li J K, et al. Interfacial engineering to construct an IrOx/WO3 hetero-structured catalyst for efficient acidic OER catalysis. New Journal of Chemistry, 2024, 48(6): 2505–2514

- Chen X J, Liao W Y, Zhong M X, et al. Rational design of robust iridium-ceria oxide-carbon nanofibers to boost oxygen evolution reaction in both alkaline and acidic media. Nano Research, 2023, 16(5): 7724–7732

- Gao H Y, Jang H S, Liu S G, et al. Stabilizing reconstructed Ir-O motifs by Mn doping for enhanced acidic water oxidation. ACS Sustainable Chemistry & Engineering, 2025, 13(9): 3512–3521

- Chang C F, Xie Y H, Luo F, et al. Weakening s-d orbital hybridization of metallic iridium by tungsten atoms for acidic water splitting. Applied Catalysis A: General, 2023, 649: 118941

- Yang X, Liu Y Q, Niu X H, et al. Porphyrin-confined supported ultrasmall Ir clusters as oxygen evolution catalysts for water electrolysis. Inorganic Chemistry, 2024, 63(42): 19798–19808

- Qiao Y J, Luo M, Cai L B, et al. Constructing nanoporous Ir/Ta2O5 interfaces on metallic glass for durable acidic water oxidation. Small, 2024, 20(2): 2305479

- Sun M Z, Huang H L, Niu X F, et al. Grain boundary-derived local amorphization enhances acidic OER. ACS Catalysis, 2024, 14(20): 15764–15776

- Li G N, Priyadarsini A, Xie Z H, et al. Achieving higher activity of acidic oxygen evolution reaction using an atomically thin layer of IrOx over Co3O4. Journal of the American Chemical Society, 2025, 147(8): 7008–7016