Supporting Information

Molecular iron phthalocyanines anchoring onto ZIF-67-Derived cobalt-carbon nanomaterials as bifunctional oxygen catalysts

Table of Contents

1. Material Synthesis and Characterization	3

2. Additional SEM and TEM Images	11

3. Additional XPS Data	15

4. Additional Electrochemical and Theoretical Data	17

5. Additional Tables	22

6. References	26

1 Material synthesis and characterization

1.1 Chemicals

All chemicals were employed as received without undergoing any additional purification steps. Cobalt nitrate hexahydrate (Co(NO3)2·6H2O, AR, Aladdin), 2-methylimidazole (2-MI, AR, 99%, Aladdin), methanol (MeOH, 99.5%, Aladdin), iron(II) phthalocyanine (FePc, AR, > 98.0%, Aladdin), N,N-dimethylformamide (DMF, 99%, Aladdin), N,N-dimethylacetamide (DMA, 99%, Aladdin), potassium hydroxide (KOH, AR, 95.0%, Aladdin) zinc acetate dihydrate (Zn(CH3COO)2), Pt/C(20 wt%, JM), RuO2(Alfa-Aesar), 5 wt% Nafion ionomer(Aladdin), distilled water and ethanol (EtOH, moisture content ≤ 0.3% from Aladdin, 99.9% from J&K).

1.2 Synthesis of Co-ZIF

Typically, Co-ZIF crystals were conveniently synthesized using a simple method. Specifically, 2.09 g of Co(NO3)2·6H2O was dissolved in 200 mL MeOH within a breaker to form the A solution. Moreover, 2.63 g 2-MI was dissolved in 200 m L MeOH to constitute the B solution. Then the mixture of the A and B solution was heated at 70 ℃ for 1 hours with continuous stirring. The resulting purple precipitates were collected by centrifugation, rinsed MeOH three times, and subsequently dried at 85 °C overnight.

1.3 Synthesis of CoNC

The as-obtained Co-ZIF were placed in a CVD tube furnace and heated to 950 °C for 2 hours at a heating rate of 10 °C min⁻¹ under a continuous flow of nitrogen. After the thermal treatment, the furnace was allowed to cool naturally to room temperature, resulting in a black powder identified as Co nano-particle on N-doped carbon (CoNC). The yield of CoNC following carbonization at 950 °C from the composite Co-ZIF was determined to be approximately 31.6%.

1.4 Synthesis of CoNC@FePc

After 1 hour of ultrasonication, the CoNC (20 mg) was dispersed in 10 mL of EtOH (Solution A). Simultaneously, 4 mg of FePc was dispersed in 10 mL of DMF through 1 hour of ultrasonication to form Solution B. Solution B was then gradually added to Solution A with continuous stirring. After 3 hours of stirring, the mixture was collected by centrifugation, washed with ethanol, and subsequently dried at 85 °C overnight, yielding CoNC@FePc.

Material characterization

Morphological analysis of the samples was conducted using a Nova NanoSEM 200 scanning electron microscope (FE-SEM, FEI Inc.) and transmission electron microscope (JEOL JEM-2100F). Powder X-ray diffraction (PXRD) patterns of the products were obtained using a Bruker D8 Advance powder diffractometer. The measurements were conducted at room temperature with the instrument operating at 40 kV and 40 mA. Graphite-monochromated Cu Kɑ radiation (λ = 1.54 Å) was utilized, and the scan rate was set at 10° per minute with a step size of 0.025. The Raman spectrometer (Renishaw in Via, England), which used the 532 nm line for excitation, was calibrated based on the silicon peak at 520.7 cm–1. A cumulative time of 10 seconds was set for the measurements, allowing for the acquisition of the corresponding carbon layer signal. N2 adsorption studies were conducted using the Specific Surface Area & Pore Size Analyzer (BSD-PS1, Beishide Instrument Technology (Beijing) Co., Ltd.) After being activated at 100 ℃, the samples were transferred to a clean ultra-high vacuum system and measurements were taken at a cryogenic temperature of 77 K. Furthermore, X-ray photoelectron spectroscopy (XPS, PHI-5000VPIII) was performed to analyze the elemental valence of the products.

Electrochemical measurements

Electrochemical measurements for the Oxygen Reduction Reaction (ORR) were carried out using a CHI 760E electrochemical workstation (CH Instruments, Inc., Shanghai). This workstation was connected to rotation-control equipment (Pine Instrument Company, USA). The experiments utilized a standard three-electrode system in 0.1 M KOH as the electrolytes. A glassy carbon rotating ring-disk electrode (RRDE) with a diameter of 5.6 mm was used as the working electrode. The catalyst was loaded onto the electrode at a loading of 0.8 mg cm-2. The electrocatalyst ink was prepared as follows: initially, 5 mg of the synthesized catalyst powder was dispersed in a mixed solution consisting of 300 μL of ethanol (EtOH), 150 μL of water (H2O), and 50 μL of a 5 wt% Nafion solution. This mixture was then ultrasonicated for 1 hour to form a homogeneous ink.

Subsequently, the electrocatalytic activities of the catalysts toward the ORR were assessed at room temperature. The measured potentials, referenced to the Ag/AgCl electrode, were converted to a Reversible Hydrogen Electrode (RHE) potential using the Nernst equation:

ERHE=EAg/AgCl+0.0592×pH+EΘAg/AgCl ,EΘAg/AgCl=0.198 V. (1)

Prior to conducting ORR measurements, a series of cyclic voltammograms (CV) were executed at a scan rate of 100 mV/s, typically for a minimum of 40 cycles. This process was employed to clean and stabilize the electrocatalyst surface. Then the formal CV test was conducted at a rate of 5 mV/s.Subsequently, Linear Scan Voltammetry (LSV) measurements were recorded at a scan rate of 5 mV/s under various rotation rates (100, 400, 900, 1600, and 2500 r/min) for obtaining the polarization curves in N2-/O2-saturated 0.1 M KOH solution. The corresponding electron transfer number (n) was determined using Koutechy-Levich (K-L) equation:

1J=1JL+1JK=1Bω12+ 1JK,  	(2)

JL= 0.2 FC0D02/3v-1/6ω1/2= Bω1/2, 	(3)

where J, represents the measured; JL, and Jk are diffusion-limiting, and kinetic current density, respectively; ω is the angular velocity of the electrode; n represents the number of electrons; F is the Faraday constant (F = 96485 C/mol=); C0 is the saturated O2 concentration (1.21×10–6 mol/cm3); D0 is the diffusion coefficient of O2 in 0.1 M KOH (1.9×10–5 cm2/s); ν is the kinetic viscosity (0.01 cm2∙s). The double-layer capacitance (Cdl) of electrocatalyst was derived from CV curves in the non-Faradic potential region with different scan rate from 5 to 120 mV/s. Electrochemical impedance spectroscopy (EIS) measurements were conducted in the frequency range from 106 Hz to 0.01 Hz with a voltage amplitude of 5 mV at 0.7 V vs. RHE. The electrons transferred number (n) and the percentage of peroxide (HO2– %) were calculated via the following equations, based on the disk current (Id) and ring current (Ir).

n=4IdId+Ir/N. 	  (4)

HO2-%= 2Ir/NId+Ir/N ×100 %. 	(5)

Therein, the H2O2 collection coefficient (N) at the ring in RRDE experiments is 0.37.

The resistance to methanol solution (3.0 M) was conducted at 0.367 V vs. RHE by chronoamperometry. And the long-term stability of electrocatalyst was investigated by chronoamperometric responses (CA) at a constant potential of 0.367 V vs. RHE with a rotation rate of 1600 r/min and a constant O2 flow.

For the Oxygen Evolution Reaction, 1.0 M KOH solution was used as the alkaline electrolyte. The LSV measurements were recorded with a scan rate of 5 mV s−1 The overpotential (η) of OER was calculated by η = ERHE – 1.23 V.

Zinc-air battery measurement

The zinc-air battery was tested in a CHI 760E electrochemical workstation (CH Instruments, Shanghai). A polished Zn plate as the anode and a catalyst-coated carbon paper as the cathode were assembled a home-made Zn-air battery, and the electrolyte was set to 6 M KOH and 0.2 M Zn(CH3COO)2. To prepare the electrocatalyst ink, 4 mg of catalyst was dispersed in a mixture of 400 μL EtOH and 40 μL Nafion (the mass loading is calculated to be ~ 1.0 mg/cm2). Both the effective electrode are of Zn anode and carbon paper were 1 cm–2. All the Zn-air batteries were assessed under standard ambient conditions. The discharge power density was calculated using the discharge polarization profiles with the following equation:

P= Ud× Jd, 	(6)

where the P, Ud, Jd are the discharge power density, discharge voltage, and discharge current density, respectively.

DFT Calculation

The density functional theory was used to carry out all the calculations with the Perdew-Burke-Ernzerh exchange-correlation functional of generalized gradient approximation and the projector-augmented wave method, which was implemented through Vienna Ab-initio Simulation Package (VASP). The input model structure file was created by VESTA.[1] The plane wave-basis expansion cutoff energy was fixed at 450 eV, and atomic relaxation was conducted until the force exerted on atoms was less than 0.02 eV Å-1 and energy was concurrently converged to 1×10–5 eV.

The Gibbs free energy change (ΔG) of each lithiation step was defined as:

,	(7)

where ΔE is the electronic energy difference directly obtained from DFT calculations, ΔZPE is the change in zero-point energy, T is the temperature (T= 298.15 K) and ΔS is the change in the entropy, respectively[2]. The zero-point energy and entropy were obtained through vibrational frequencies.

Conventionally, in an alkaline electrolyte, the anode reactions after oxygen adsorption can be written as:

(8)

(9)

(10)

(11)

- Additional SEM and TEM images

Fig. S1 (a–c) SEM images of Co-ZIF; (d) PXRD patterns of Co-ZIF; (e) N2 isotherms; (f) pore size distribution of Co-ZIF. Crystal structure and coordination environment of Co-ZIF: (g) AU; (h) SBU and (i) the discrete nanosized cage in Co-ZIF.

Fig. S2 SEM images of (a-c) CoNC.

Fig. S3 SEM images of (a‒c) CoNC@FePc.

Fig.S4 The EDS pattern of CoNC@FePc.

- Additional XPS data

Fig. S5 (a) XPS full-survey spectra; (b) the high-resolution O 1s spectra of CoNC and CoNC@FePc.

Fig. S6 The deconvoluted Fe 2p spectra of CoNC@FePc.

4 Additional electrochemical and theoretical data

Fig. S7 CV curves for (a) CoNC, and (b) CoNC@FePc in N2-/O2-saturated 0.1 M KOH at 5 mV/s; LSV curves at various rotating speeds from 100 to 2500 r/min: (c) CoNC, and (d) CoNC@FePc.

Fig. S8 K-L plots at various potentials from 0.3–0.7 V for (a) CoNC, and (b) CoNC@FePc; CV curves at different sweep speeds from 5 to 120 mV/s: (c) CoNC, and (d) CoNC@FePc.

Fig. S9 Supplementary electrochemical data of Pt/C. (a) CV curve, (b) LSV curve, (c) K-L plots and (d) CV curve at different sweep speeds from 5 to 120 mV/s.

Fig. S10 The current density retention after long-term durability of OER test.

Fig. S11 Top view and side view of the optimized configurations of oxygen intermediates (OOH*, O*, and OH*) adsorbed on (a) Co@FePc and (b) FePc.

Fig. S12 ORR/OER mechanisms for CoNC@FePc.

Fig. S13 OER free energy diagrams at (a) 0.00 V and (b) 1.23 V.

Fig. S14 After long-term test. (a) XPS full-survey spectrum, the deconvoluted XPS spectra of (b) C 1s, (c) N 1s, (d) O 1s, (e) Co 2p and (f) Fe 2p.

Fig. S15 SEM images of (a-c) CoNC@FePc after the long-term durability test.

Fig. S16 (a) TEM image and (b) EDS mapping images of CoNC@FePc after long-term test.

5Additional tables

Table S1 The BET surface area and total pore volume of the samples

| Sample | BET surface area/(m2∙g–1) | Total pore volume/(cm3∙g–1) |
| --- | --- | --- |
| CoNC | 106.2 | 0.20 |
| CoNC@FePc | 34.2 | 0.11 |

Table S2 N dopant proportions of these carbon materials measured from fitting of the N 1s XPS

| Samples | Relative content of different N species / 100% |  |  |  |
| --- | --- | --- | --- | --- |
|  | Pyridinic-N | Pyrrolic-N | Graphitic-N | Oxidized-N |
| CoNC | 37.7 | 29.9 | 12.2 | 20.2 |
| CoNC@FePc | 44.9 | 36.7 | 8.6 | 9.8 |

Table S3 Comparison of CoNC@FePc with recently reported ORR/OER electrocatalysts

| Catalyst name | Electrochemical performance |  |  |  | Reference |
| --- | --- | --- | --- | --- | --- |
|  | η10/mV | Tafel slope of OER/(mV∙(°)–1) | E1/2 (V vs. RHE) | Tafel slope of ORR/(mV∙(°)–1) |  |
| CoNC@FePc | 314 | 73.4 | 0.87 | 38.8 | This Work |
| CoNC | 377 | 91.2 | 0.79 | 53.3 | This Work |
| CoFe-FeNC | 296 | 44.76 | 0.876 | 80.8 | [3] |
| Co@CNx | 480 | 239 | 0.84 | 62.0 | [4] |
| Fe3C-NCNTs 90 min CC−1 | 281 | 51.5 | 0.85 | / | [5] |
| NDC-800 | 380 | 170.3 | 0.88 | 79.5 | [6] |
| FeSA/NCZ | 320 | 51.0 | 0.87 | 70.0 | [7] |
| CoS2 (400)/N,S-GO | 380 | / | 0.79 | / | [8] |
| Co-ZIF1.5/10CNF2 | 390 | 122 | 0.85 | 65 | [9] |
| Co/N–C-800 | 274 | 43.6 | 0.82 | 103.8 | [10] |
| FeNC/Fe3C-op | 349 | 83.4 | 0.91 | 85.3 | [11] |
| CCSO/NC-2 | 340 | 121.3 | 0.82 | 69.3 | [12] |
| m-Fe/NC@CNT | 338 | 104.9 | 0.85 | 92.5 | [13] |
| P-Co3Fe1/NC-700–10 | 391 | 116 | 0.84 | 80 | [14] |
| N─FeN4 | 360 | 104.7 | 0.91 | 64.9 | [15] |
| Fe3N/FeNP-N-C-6.6% | 294 | 93.8 | 0.867 | 63.9 | [16] |
| NiFe LDH A-FeSACoSA-FeCoAlloy-CNT/NC | 330 | 125.5 | 0.84 | / | [17] |
| Co3O4-S/NSG | 323 | 98.7 | 0.75 | 71.8 | [18] |

Table S4 Comparison of Zn-air battery performance among CoNC@FePc and other previously reported similar electrocatalysts

| Catalyst | Peak power density/(mW∙cm–2) | Specific capacity/(mAh∙g–1) | Reference |
| --- | --- | --- | --- |
| CoNC@FePc | 150.2 | 846.5 | This work |
| CoFe-FeNC | 120.8 | 767.5 | [3] |
| Fe3C-NCNTs 90 min CC−1 | 139.2 | / | [5] |
| FeNC/Fe3C-op | 137.4 | 818.1 | [11] |
| Co@N-CNTs/NSs | 142.3 | 800.8 | [19] |
| Fe-CNCs-800 | 110.2 | 801.21 | [20] |
| CoFe/SNC | 130 | 814 | [21] |
| S-FeCo3P/NPSG | 118 | 731 | [22] |
| CoFe–N–C | 142 | / | [23] |
| Co‐NCNT | 144.6 | / | [24] |
| CNCo-Fe3C | 124.0 | 796.0 | [25] |
| Fe/Co–N/S 1.9 -C | 138.0 | 763.2 | [26] |
| Fe-SA/N-C | 144.3 | 800.9 | [27] |
| Fe3Co-NC@900 | 62.8 | 746.4 | [28] |
| FeCo/LDH-NGCP | 155.9 | 792.7 | [29] |
| FeCo@1D-CNTs/2D-NC | 98.2 | 741.0 | [30] |
| NPC-Fe0.3 | 99.0 | / | [31] |
| FexNC@NiFe(OH)x | 85.1 | 785.2 | [32] |

6 References

1.	Momma, K.; Izumi, F., VESTA 3 for three-dimensional visualization of crystal, volumetric and morphology data. Journal of Applied Crystallography 2011, 44 (6): 1272-1276.

2.	Cao, J.; Zhang, X.; Zhao, S.; Lu, X.; Ma, H., Mechanism of the two-dimensional WSeTe/Zr2CO2 direct Z-scheme van der Waals heterojunction as a photocatalyst for water splitting. PCCP 2022, 24 (35): 21030-21039.

3.	Zhang, S.; Yang, J.; Yang, L.; Yang, T.; Liu, Y.; Zhou, L.; Xu, Z.; Zhou, X.; Tang, J., Boosting ORR/OER bifunctional electrocatalysis by promoting electronic redistribution of Fe-N-C on CoFe-FeNC for ultra-long rechargeable Zn-air batteries. Applied Catalysis B: Environment and Energy 2024, 359: 124485.

4.	Quílez-Bermejo, J.; García-Dalí, S.; Daouli, A.; Zitolo, A.; Canevesi, R. L. S.; Emo, M.; Izquierdo, M. T.; Badawi, M.; Celzard, A.; Fierro, V., Advanced design of metal nanoclusters and single atoms embedded in C1N1-derived carbon materials for ORR, HER, and OER. Advanced Functional Materials 2023, 33 (21): 2300405.

5.	Chen, G.; Liu, Y.; Xue, S.; Zhang, R.; Lv, H.; Zhang, J.; Wu, L.; Che, R., Exceptionally bifunctional ORR/OER performance via synergistic atom–cluster interaction. Small 2024, 20 (19): 2308192.

6.	Li, P.; Wen, J.; Xiang, Y.; Li, M.; Zhao, Y.; Wang, S.; Dou, J.; Li, Y.; Ma, H.; Xu, L., Hierarchical mesoporous N-doped carbon as an efficient ORR/OER bifunctional electrocatalyst for rechargeable zinc–air battery. Inorganic Chemistry Frontiers 2024, 11 (16): 5345-5358.

7.	Jiao, C.; Xu, Z.; Shao, J.; Xia, Y.; Tseng, J.; Ren, G.; Zhang, N.; Liu, P.; Liu, C.; Li, G.; Chen, S.; Chen, S.; Wang, H.-L., High-density atomic Fe-N4/C in tubular, biomass-derived, nitrogen-rich porous carbon as air-electrodes for flexible Zn-air batteries. Advanced Functional Materials 2023, 33 (20): 2213897.

8.	Ganesan, P.; Prabu, M.; Sanetuntikul, J.; Shanmugam, S., Cobalt sulfide nanoparticles grown on nitrogen and sulfur codoped graphene oxide: An efficient electrocatalyst for oxygen reduction and evolution reactions. ACS Catalysis 2015, 5 (6): 3625-3637.

9.	Zhu, S.; Ding, L.; Zhang, X.; Wang, K.; Wang, X.; Yang, F.; Han, G., Biaxially-strained phthalocyanine at polyoxometalate@carbon nanotube heterostructure boosts oxygen reduction catalysis. Angew. Chem. Int. Ed. 2023, 62 (42): e202309545.

10.	Fan, X.-Z.; Du, X.; Pang, Q.-Q.; Zhang, S.; Liu, Z.-Y.; Yue, X.-Z., In situ construction of bifunctional N-doped carbon-anchored Co nanoparticles for OER and ORR. ACS Applied Materials & Interfaces 2022, 14 (6): 8549-8556.

11.	Chang, J.; Zhang, Q.; Yu, J.; Jing, W.; Wang, S.; Yin, G.; Waterhouse, G. I. N.; Lu, S., A Fe single atom seed-mediated strategy toward Fe3C/FeNC Catalysts with outstanding bifunctional ORR/OER activities. Advanced Science 2023, 10 (22): 2301656.

12.	Cai, J.; Zhang, H.; Zhang, L.; Xiong, Y.; Ouyang, T.; Liu, Z.-Q., Hetero-anionic structure activated CoS bonds promote oxygen electrocatalytic activity for high-efficiency zinc-air batteries. Advanced Materials 2023, 35 (36): 2303488.

13.	Gan, R.; Song, Y.; Ma, C.; Shi, J., In situ growth of N-doped carbon nanotubes in Fe-Nx/Fe2O3/Fe3O4-encapsulated carbon sheets for efficient bifunctional oxygen catalysis. Applied Catalysis B: Environmental 2023, 327: 122443.

14.	Xiong, Y.; Jiang, Z.; Gong, L.; Tian, X.; Song, C.; Maiyalagan, T.; Jiang, Z.-J., Construction of Co/FeCo@Fe(Co)3O4 heterojunction rich in oxygen vacancies derived from metal-organic frameworks using O2 plasma as a high-performance bifunctional catalyst for rechargeable zinc-air batteries. Journal of Colloid and Interface Science 2023, 649: 36-48.

15.	Qiao, J.; Lu, C.; Kong, L.; Zhang, J.; Lin, Q.; Huang, H.; Li, C.; He, W.; Zhou, M.; Sun, Z., Spin engineering of Fe-N-C by axial ligand modulation for enhanced bifunctional oxygen catalysis. Advanced Functional Materials 2024, n/a (n/a): 2409794.

16.	Wang, K.; Qiu, C.; Wang, Z.; Chen, Q.; Pan, J.; Li, J.; Wu, M.; Dong, H.; Shi, K.; Liu, Q., Job-synergistic engineering from Fe3N/Fe sites and sharp-edge effect of hollow star-shaped nitrogen-doped carbon structure for high-performance zinc-air batteries. Carbon 2023, 214: 118333.

17.	Hong, W.-X.; Wang, W.-H.; Chang, Y.-H.; Pourzolfaghar, H.; Tseng, I. H.; Li, Y.-Y., A Ni-Fe layered double hydroxide anchored FeCo nanoalloys and Fe-Co dual single-atom electrocatalysts for rechargeable and flexible zinc-air and aluminum-air batteries. Nano Energy 2024, 121: 109236.

18.	Meng, L.; Liu, W.; Lu, Y.; Liang, Z.; He, T.; Li, J.; Nan, H.; Luo, S.; Yu, J., Lamellar-stacked cobalt-based nanopiles integrated with nitrogen/sulfur co-doped graphene as a bifunctional electrocatalyst for ultralong-term zinc-air batteries. Journal of Energy Chemistry 2023, 81: 633-641.

19.	Wu, J.; Zheng, Z.; Chi, H.; Jiang, J.; Zhu, L.; Ye, Z., Ultrasensitive and exclusive chemiresistors with a ZIF-67-derived oxide cage/nanofiber Co3O4/In2O3 heterostructure for acetone detection. ACS Appl. Mater. Interfaces 2024, 16 (7): 9126-9136.

20.	Tian, Y.; Han, Y.; Wang, X.; Ma, Z.; Sun, G.; Li, Y., A lignin–derived N-doped carbon-supported iron-based nanocomposite as high-efficiency oxygen reduction reaction electrocatalyst. International Journal of Biological Macromolecules 2024, 257: 128317.

21.	Li, G.; Tang, Y.; Fu, T.; Xiang, Y.; Xiong, Z.; Si, Y.; Guo, C.; Jiang, Z., S, N co-doped carbon nanotubes coupled with CoFe nanoparticles as an efficient bifunctional ORR/OER electrocatalyst for rechargeable Zn-air batteries. Chemical Engineering Journal 2022, 429: 132174.

22.	Ren, J.-T.; Ying, Y.-D.; Liu, Y.-P.; Li, W.; Yuan, Z.-Y., Charge redistribution caused by sulfur doping of bimetal FeCo phosphides supported on heteroatoms-doped graphene for Zn-air batteries with stable cycling. Journal of Energy Chemistry 2022, 71: 619-630.

23.	Zhou, X.; Gao, J.; Hu, Y.; Jin, Z.; Hu, K.; Reddy, K. M.; Yuan, Q.; Lin, X.; Qiu, H.-J., Theoretically revealed and experimentally demonstrated synergistic electronic interaction of CoFe dual-metal sites on N-doped carbon for boosting both oxygen reduction and evolution reactions. Nano Letters 2022, 22 (8): 3392-3399.

24.	Pei, Z.; Huang, Y.; Tang, Z.; Ma, L.; Liu, Z.; Xue, Q.; Wang, Z.; Li, H.; Chen, Y.; Zhi, C., Enabling highly efficient, flexible and rechargeable quasi-solid-state Zn-air batteries via catalyst engineering and electrolyte functionalization. Energy Storage Materials 2019, 20: 234-242.

25.	Li, S.; Chang, F.; Yuan, Y.; Zhu, K.; Chen, W.; Zhang, Q.; Lu, Z.; Bai, Z.; Yang, L., Co-Fe3C pair sites catalyst with heterometallic dual active sites for efficient oxygen reduction reaction. Journal of Colloid and Interface Science 2023, 651: 734-741.

26.	Cai, J.; Xu, Y.; Sun, Y.; Zhao, H.; Ye, D.; Tang, Y.; Sun, C.; Liu, L.; Zhang, J., Regulating the coordination environment of Fe/Co-N/S-C to enhance ORR and OER bifunctional performance. Inorganic Chemistry Frontiers 2023, 10 (6): 1826-1837.

27.	Li, L.; Li, N.; Xia, J.; Xing, H.; Arif, M.; Zhao, Y.; He, G.; Chen, H., Post-synthetic electrostatic adsorption-assisted fabrication of efficient single-atom Fe-N-C oxygen reduction catalysts for Zn-air batteries. Science China Materials 2023, 66 (3): 992-1001.

28.	Srinivas, K.; Yu, H.; Chen, Z.; Chen, A.; Zhu, M.-q.; Chen, Y.; Yang, C., Densely accessible Fe/Co-Nx dual-atom site coupled core–shell Co3Fe7@C as an efficient bifunctional oxygen electrocatalyst for rechargeable zinc-air batteries. Journal of Materials Chemistry A 2024, 12 (27): 16863-16876.

29.	Zhang, F.; Lei, Y.; Li, G.; Xie, Y.; Guo, X.; Zhang, X.; Wang, X., FeCo bimetallic ZIF derivatives decorated with CoFe-LDH to promote bifunctional oxygen electrocatalysis activation. ChemSusChem 2024, n/a (n/a): e202401556.

30.	Qin, J.-F.; Wang, B.; Zhang, Y.-Z.; Zhang, X.-H.; Hong, M.; Du, C.-C.; Chen, J.-H., Construction of 1D/2D hierarchical carbon structure encapsulating FeCo alloys by one-step annealing leaf-like ZnFeCo-ZIF for highly-efficient bifunctional oxygen electrocatalysis in reversible Zinc-air battery. Journal of Alloys and Compounds 2024, 982: 173710.

31.	Yang, T.; Chen, Y.; Liu, Y.; Liu, X.; Gao, S., Self-sacrificial template synthesis of Fe, N co-doped porous carbon as efficient oxygen reduction electrocatalysts towards Zn-air battery application. Chinese Chemical Letters 2022, 33 (4): 2171-2177.

32.	Luo, H.; Li, Y.; Wang, W.; Zhou, T.; Guo, Z., A highly durable zinc-air battery from a directly integrated FexNC@NiFe(OH)x bifunctional catalyst. Inorganic Chemistry Frontiers 2023, 10 (6): 1758-1768.