Table S1. The comparison of the cycle performance under the different stabilization strategies

| Stabilization strategies | Materials | Current density (mA cm-2) | Lifespan (h) | Journal, Year | Ref |
| --- | --- | --- | --- | --- | --- |
| Artificial SEI layer | DCZ-gel | 1 | 2500 | Nano Micro Lett., 2024 | [1] |
|  | Oriented-Protection | 1 | 2000 | Nat.Commun., 2020 | [2] |
|  | Brightener-Zn | 2 | 3600 | Energy Environ. Sci., 2019 | [3] |
|  | PG-SEI | 1 | 1000 | J. Energy Chem., 2023 | [4] |
|  | Cefe-MOF@Zn | 2 | 4300 | Energy Environ. Sci., 2025 | [5] |
|  | DCL-Cellulose | 1 | 2500 | Nano Micro Lett., 2024 | [1] |
|  | Zn-Nucleation Sites | 2 | 2500 | Adv. Funct. Mater., 2020 | [6] |
|  | PVA@SR-ZnMoO4 | 2 | 4300 | Energy Environ. Sci., 2025 | [5] |
|  | β-PVDF-Zn | 5 | 1000 | Chem. Eng. J., 2021 | [7] |
| Electrolyte modification | Lean-water hydrogel | 1 | 3000 | Nat. Commun., 2023 | [8] |
|  | Dual-Complex-ZnMn | 1 | 2000 | Chem. Eng. J., 2022 | [9] |
|  | CESE-Interface | 1 | 1800 | J. Alloy. Compd., 2024 | [10] |
|  | CESE-PA-Interface | 1 | 4000 | Adv. Funct. Mater., 2024 | [11] |
|  | CES-Zn | 1 | 2000 | J. Alloy. Compd., 2024 | [10] |
|  | Aqueous-Zn | 2 | 2500 | Chem. Electro. Chem., 2023 | [12] |
|  | pH-Buffer-ZnI2 | 1 | 2000 | Angew. Chem. Int. Ed., 2023 | [13] |
|  | Dual-Modulation-Zn | 5 | 1400 | Adv. Funct. Mater., 2024 | [11] |
| Bionic | SA-Electrolyte | 5 | 3000 | Angew. Chem. Int. Ed., 2023 | [14] |
|  | ZnAsp-Additive | 1 | 1800 | Small, 2024 | [15] |
|  | Hydroxyl-Additive | 2 | 1500 | Angew. Chem. Int. Ed., 2024 | [16] |
|  | ZnAsp-Additive | 1 | 1800 | Small, 2024 | [15] |
|  | PolyAnion-Zn | 5 | 2500 | Angew. Chem. Int. Ed., 2024 | [17] |
|  | Silk-Peptide | 1 | 1200 | Adv. Funct. Mater., 2022 | [18] |
|  | Zn-Ce/Yb | 2 | 200times | J. Alloy. Compd., 2024 | [19] |
|  | Zn-Complexity | 1 | 1200 | Adv. Energy Mater., 2022 | [18] |
|  | Cu(I)-MOF/Polymer | 5 | 2500 | Angew. Chem. Int. Ed., 2024 | [17] |
| Structural optimization | 3D-Graphene/Zn | 1 | 2500 | Nat. Commun., 2023 | [20] |
|  | Zn-Structural Design | 1 | 2000 | SmartMat 2024 | [21] |
|  | CAT-Zn-Structural | 5 | 500 | SmartMat, 2024 | [21] |
|  | Zn-Structural Design | 5 | 800 | SmartMat, 2024 | [21] |
|  | Zn-Structural Design | 1 | 2000 | SmartMat, 2024 | [21] |
|  | Zn-Structural | 1 | 3000 | SmartMat, 2024 | [21] |
|  | Zn-Complexity | 2 | 630 | Adv. Energy Mater., 2022 | [22] |
|  | Interface-Bridged-Zn | 1 | 2000 | Angew. Chem. Int. Ed., 2020 | [23] |

Table S2. The performance comparison of the symmetrical cell under the different stabilization strategies

| Materials | Current density (mA cm-2) | Areal capacity (mAh cm-2) | Lifespan (h) | Journal, Year | Ref. |
| --- | --- | --- | --- | --- | --- |
| HB-ZnHCF@Zn | 1 | 0.5 | 5800 | Angew. Chem. Int. Ed., 2023 | [24] |
| ZF@F-TiO2 | 1 | 1 | 450 | Nat. Commun., 2020 | [2] |
| ZnS@Zn | 2 | 2 | 1100 | Adv. Mater., 2020 | [25] |
| BTO@Zn | 1 | 1 | 2000 | Nano Micro Lett., 2021 | [26] |
| DCZ-gel | 0.5 | 0.5 | 2000 | Nano Micro Lett., 2024 | [1] |
| Zeolite-Zn | 2.5 | 2.5 | 450 | Nano Micro Lett., 2022 | [27] |
| GSLE | 1 | 0.2 | 1400 | ACS Appl. Mater. Interfaces, 2025 | [28] |
| CPL-Additive | 1 | 1 | 2100 | J. Alloys Compd., 2024 | [29] |
| StHEI-Zn | 1 | 0.5 | 3000 | Angew. Chem. Int. Ed., 2024 | [30] |
| Zn-PDPTT | 1 | 0.5 | 4300 | Angew. Chem. Int. Ed., 2024 | [31] |
| SCP-Additive | 2 | 1 | 1500 | Iran. J. Polym. Sci. Technol., 2025 | [32] |
| TCOF-S | 2 | 1 | 1200 | Angew. Chem. Int. Ed., 2024 | [33] |
| 3D-C-Zn | 5 | 2 | 880 | ChemNanoMat, 2021 | [34] |
| DCD-Additive | 5 | 1 | 1400 | J. Mater. Chem. A, 2025 | [35] |
| GABA-Additive | 3 | 1 | 3128 | New J. Chem., 2025 | [36] |

Table S3. The performance comparison of full cell in AZIBs with artificial SEI

| Materials | Current density (mA cm-2) | Areal capacity (mAh cm-2) | Lifespan (h) | Journal, Year | Ref. |
| --- | --- | --- | --- | --- | --- |
| HB-ZnHCF@Zn | 1 | 0.5 | 5800 | Angew. Chem. Int. Ed., 2023 | [24] |
| ZF@F-TiO2 | 1 | 1 | 225 | Nat. Commun., 2020 | [2] |
| ZnS@Zn | 2 | 2 | 550 | Adv. Mater., 2020 | [25] |
| BTO@Zn | 1 | 1 | 1000 | Nano Micro Lett., 2021 | [26] |
| DCZ-gel | 0.5 | 0.5 | 2000 | Nano Micro Lett., 2024 | [1] |
| Zeolite-Zn | 2.5 | 2.5 | 225 | Nano Micro Lett., 2022 | [27] |
| GSLE | 1 | 0.2 | 3500 | ACS Appl. Mater. Interfaces, 2025 | [28] |
| CPL-Additive | 1 | 1 | 2100 | J. Alloys Compd., 2024 | [29] |
| StHEI-Zn | 1 | 0.5 | 3000 | Angew. Chem. Int. Ed., 2024 | [30] |
| Zn-PDPTT | 1 | 0.5 | 4300 | Angew. Chem. Int. Ed., 2024 | [31] |
| SCP-Additive | 2 | 1 | 1500 | Iran. J. Polym Sci. Technol., 2025 | [32] |
| TCOF-S | 2 | 1 | 1200 | Angew. Chem. Int. Ed., 2024 | [33] |
| 3D-C-Zn | 5 | 2 | 880 | ChemNanoMat, 2021 | [34] |
| DCD-Additive | 5 | 1 | 3000 | J. Mater. Chem. A, 2025 | [35] |
| GABA-Additive | 3 | 1 | 2000 | New J. Chem., 2025 | [36] |

Reference

[1]	Zhang H, Gan X, Yan Y, et al. A sustainable dual cross-linked cellulose hydrogel electrolyte for high-performance zinc-metal batteries. Nano-Micro Letters, 2024, 16(1): 106.

[2]	Zhang Q, Luan J, Huang X, et al. Revealing the role of crystal orientation of protective layers for stable zinc anode. Nature Communications, 2020, 11(1): 3961.

[3]	Zhao Z, Zhao J, Hu Z, et al. Long-life and deeply rechargeable aqueous Zn anodes enabled by a multifunctional brightener-inspired interphase†. Energy & Environmental Science, 2019, 12(1): 1938-1949.

[4]	Wang H, Luo C, Qian Y, et al. Upcycling of phosphogypsum waste for efficient zinc-ion batteries. Journal of Energy Chemistry, 2023, 81: 157-166.

[5]	Jianbo D, Guolang Z, Wenhao D, et al. Machine learning-assisted benign transformation of three zinc states in zinc ion batteries. Energy & Environmental Science, 2025, 18: 4872-4882.

[6]	Liang P, Yi J, Liu X, et al. Highly reversible Zn anode enabled by controllable formation of nucleation sites for Zn-based batteries. Advanced Functional Materials, 2020, 30(13): 1908528.

[7]	Hieu L T, So S, Kim I T, et al. Zn anode with flexible β-PVDF coating for aqueous Zn-ion batteries with long cycle life. Chemical Engineering Journal, 2021, 411: 128584.

[8]	Wang Y, Li Q, Hong H, et al. Lean-water hydrogel electrolyte for zinc ion batteries. Nature Communications, 2023, 14(1): 3890.

[9]	Huang J, Chi X, Wu J, et al. High-concentration dual-complex electrolyte enabled a neutral aqueous zinc-manganese electrolytic battery with superior stability. Chemical Engineering Journal, 2022, 430: 133058.

[10]	Liang Y, Xie L, Zhang W, et al. Interfacial modulation via cationic electrostatic shielding effect for reversible and durable Zn anodes in hydrogel electrolytes. Journal of Alloys and Compounds, 2024, 976: 173118.

[11]	Tang H, Hu N, Ma L, et al. Interfacial dual-modulation via cationic electrostatic shielding and anionic preferential adsorption toward planar and reversible zinc electrodeposition. Advanced Functional Materials, 2024, 34(38): 2402484.

[12]	Gao X, Dong H, Carmalt C J, et al. Recent advances of aqueous electrolytes for zinc-ion batteries to mitigate side reactions: A review. ChemElectroChem, 2023, 10(19): e202300200.

[13]	Lyu Y, Yuwono J A, Wang P, et al. Organic pH buffer for dendrite-free and shuttle-free Zn-I2 batteries. Angewandte Chemie International Edition, 2023, 62(21): e202303011.

[14]	Dong H, Hu X, Liu R, et al. Bio-inspired polyanionic electrolytes for highly stable zinc-ion batteries. Angewandte Chemie International Edition, 2023, 62(41): e202311268.

[15]	Huang Y, Zhuang Y, Guo L, et al. Stabilizing anode-electrolyte interface for dendrite-free Zn-ion batteries through orientational plating with zinc aspartate additive. Small, 2024, 20(10): 2306211.

[16]	Bu F, Gao Y, Zhao W, et al. Bio-inspired trace hydroxyl-rich electrolyte additives for high-rate and stable Zn-ion batteries at low temperatures. Angewandte Chemie International Edition, 2024, 63(9): e202318496.

[17]	He W, Li X, Dai X, et al. Redox concomitant formation method for fabrication of Cu(I)−MOF/polymer composites with antifouling properties. Angewandte Chemie International Edition, 2024, 63(44): e202411539.

[18]	Wang B, Zheng R, Yang W, et al. Synergistic solvation and interface regulations of eco-friendly silk peptide additive enabling stable aqueous zinc-ion batteries. Advanced Functional Materials, 2022, 32(23): 2112693.

[19]	Yuan X, He C, Wang J, et al. Inhibition of zinc dendrite growth in zinc-air batteries by alloying the anode with Ce and Yb. Journal of Alloys and Compounds, 2024, 970: 172523.

[20]	Mu Y, Li Z, Wu B-K, et al. 3D hierarchical graphene matrices enable stable Zn anodes for aqueous Zn batteries. Nature Communications, 2023, 14(1): 4205.

[21]	Cao Q, Gao Y, Pu J, et al. Materials and structural design for preferable Zn deposition behavior toward stable Zn anodes. SmartMat, 2024, 5(1): e1194.

[22]	Qian G, Zan G, Li J, et al. Structural, dynamic, and chemical complexities in zinc anode of an operating aqueous Zn-ion battery. Advanced Energy Materials, 2022, 12(21): 2200255.

[23]	Cui Y, Zhao Q, Wu X, et al. An interface-bridged organic–inorganic layer that suppresses dendrite formation and side reactions for ultra-long-life aqueous zinc metal anodes. Angewandte Chemie International Edition, 2020, 59(38): 16594-16601.

[24]	Liu M, Yuan W, Ma G, et al. In-Situ Integration of a hydrophobic and fast-Zn2+-conductive inorganic interphase to stabilize Zn metal anodes. Angewandte Chemie International Edition, 2023, 62(27): e202304444.

[25]	Hao J, Li B, Li X, et al. An in-depth study of Zn metal surface chemistry for advanced aqueous Zn-ion batteries. Advanced Materials, 2020, 32(34): 2003021.

[26]	Wu K, Yi J, Liu X, et al. Regulating Zn deposition via an artificial solid–electrolyte interface with aligned dipoles for long life Zn anode. Nano-Micro Letters, 2021, 13(1): 79.

[27]	Shang W, Li Q, Jiang F, et al. Boosting Zn||I2 battery’s performance by coating a zeolite-based cation-exchange protecting layer. Nano-Micro Letters, 2022, 14(1): 82.

[28]	Li Q, Bai M, Wang X, et al. A gradient solid-like electrolyte stabilizing Zn anodes by in situ formation of a ZnSe interphase. ACS Applied Materials & Interfaces, 2025, 17(8).

[29]	Yin J, Li M, Feng X, et al. Comprehensive protection of Zn metal anode via caprolactam towards highly stable aqueous zinc ions batteries. Journal of Alloys and Compounds, 2024, 971: 172785.

[30]	Zhao Y, Chen Z, Gao X, et al. In-situ self-respiratory solid-to-hydrogel electrolyte interface evoked well-distributed deposition on zinc anode for highly reversible zinc-ion Batteries. Angewandte Chemie International Edition, 2025, 64(3): e202415251.

[31]	Chen M, Guo X, Jiang X, et al. Multi-group polymer coating on Zn anode for high overall conversion efficiency photorechargeable zinc-ion batteries. Angewandte Chemie International Edition, 2024, 63(39): e202410011.

[32]	Zhang J, Wei X, Wu Q, et al. Molecule-adsorption-induced interface micro-environment regulating for highly stable aqueous zinc ion batteries. Polymer Science & Technology, 2025.

[33]	Wu Q, Huang J, Zhang J, et al. Multifunctional cellulose nanocrystals electrolyte additive enable ultrahigh-rate and dendrite-free Zn anodes for rechargeable aqueous zinc batteries. Angewandte Chemie International Edition, 2024, 63(14): e202319051.

[34]	Li X, Zeng J, Yao H, et al. Current advances on Zn anodes for aqueous zinc-ion batteries. ChemNanoMat, 2021, 7(11): 1162-1176.

[35]	Liu D, Lv B, Liu Z, et al. Molecular anchoring-induced proton adsorption effect achieves stable zinc metal anodes. Journal of Materials Chemistry A, 2025.

[36]	Liu T, Huang G, Wei Z, et al. Relieving interface corrosion and inducing planar Zn plating achieved by γ-aminobutyric acid towards stable and high-performance Zn ion batteries. New Journal of Chemistry, 2025, 49: 10928-10935.