Supporting Information

Dual Modulation of Fe-N-C Catalysts via Axial and In-Plane Heteroatoms for Oxygen Reduction: A Combined DFT and Machine Learning Study

Note S1: Performance Metrics

In assessing the performance of machine learning models, we employ 2 key performance metrics, including the coefficient of determination (R 2) and root mean squared error (RMSE). These metrics serve as valuable indicators of the model’s predictive accuracy and provide quantitative measures of the variance explained, the average magnitude of errors, and the overall deviation between predicted and actual values.

R 2 represents a numerical characteristic of the relationship between a random variable and multiple random variables, serving as a statistical indicator to reflect the reliability of the dependent variable's variation explained by the regression model. It is calculated using the formula:

R2=1−SSresSStot

Here, SSres represents the residual sum of squares: SSres=i=1n(yi−yi')2, and SStot denotes the total sum of squares: SStot=i=1n(yi−y)2. In these formulas, n represents the total number of data points in the dataset, yi corresponds to the true value, yi'​ represents the predicted value of the sample i of the target variable, and y signifies the mean of the true data. The R2 value, ranging from 0 to 1, serves as a measure of the fitting of a regression model. A value of zero indicates that the model does not explain any of the variance in the data, while a value of one indicates that the model captures all the observed variance.

The RMSE (Root Mean Squared Error) is the square root of the ratio of the square of the deviation between the predicted value and the true value to the number of observations n. It measures the deviation between the predicted value and the true value. It is calculated using the formula:

RMSE=1nin(yi−yi')2

RMSE measures the square root of the average squared difference between the predicted values (yi') and the actual values (yi).

Figure S1. Comparison of oxygen reduction reaction (ORR) pathways on the FeNC-OH single-atom catalyst with and without Hubbard U correction.

Figure S2. Distribution of formation energy Ef values.

Figure S3. a, b) Heatmaps of Pearson correlation coefficients for features of stability model before and after correlation-based filtering. The color scale (red: strong positive, blue: strong negative) is consistent across both subfigures.

Figure S4. Learning curves of the stability RF model for different hyperparameters: (a) max_depth, (b) n_estimators, and (c) max_features.

Figure S5. The formation energy Ef versus (a) electron affinity of the axial atom for structures without in-plane doping and (b) atomic radius of the site1 dopant atom for site1-doped structures without axial ligands.

Figure S6. SHAP analysis for the RF stability model. The color of the dots represents values of the corresponding features. The positive/negative sign of a SHAP value implies a direct correlation between the feature and an increase/decrease in Ef.

Figure S7. Heatmap of average formation energy Ef versus doping site and atomic radius for all structures without axial ligands.

Figure S8. Model accuracy heatmaps across descriptor dimensions (dim1~5) and complexity levels (com1~5) of the accuracy of SISSO analysis of Ef.

Figure S9. Structural diagrams of modified Fe-N-C catalysts with superior ORR performance from training set DFT calculations (The ORR Uonset is marked at the upper left of each structure). Color legend: gray = C, blue = N, purple = Fe, yellow = S, red = O, light blue = F, pink = P, orange = Se, light pink = B, white = H, light green = Cl, brown = Br, dark green = Si.

Figure S10. Distribution of G*OH Adsorption Energy Values.

Figure S11. Heatmaps of Pearson correlation coefficients for features of activity model (a) before and (b) after correlation-based filtering. The color scale (red: strong positive, blue: strong negative) is consistent across both (a) and (b).

Figure S12. Learning curves of different hyperparameters in the RF model for ΔG*OH prediction: (a) max_depth, (b) n_estimators, and (c) max_features.

Figure S13. Scatter plots of ΔG*OH versus (a) number of p electron and (b) electronegativity of the axial atom for Fe-N-C structures modified with axial heteroatoms and no in-plane doping atom. Scatter plots of ΔG*OH versus (c) atomic radius and (d) electronegativity of the shell2 dopant atoms for Fe-N-C structures modified with heteroatoms doped in shell2 and axial atom.

Figure S14. SHAP summary plot for the activity model.

Figure S15. Model accuracy heatmaps across descriptor dimensions and complexity levels of activity model accuracy.

Figure S16. Projected density of state (PDOS) of Fe single atom in a) FeNC-S(3), b) FeNC-S(3)-OH and c) FeNC-S(3)-S.

Figure S17. The charge density difference between the site 3 atom and other parts of the catalyst structure in (a) FeNC-S(3)-OH and (b) FeNC-OH.

Figure S18. Comparison of Fe-3d PDOS a) FeNC-OH and b) FeNC-S(3)-OH. The blue curve corresponds to the dz2 orbital of the central Fe atom, while the gray area represents the sum of other d orbital components.

Figure S19. Gibbs free energy diagrams of ORR on FeNC-O(4)-F, FeNC-N(4)-F, FeNC-P(4)-F, FeNC-P(2)-F and FeNC-S(4)-F at 0V.

Figure S20. Structural diagrams of predicted modified Fe-N-C catalysts with superior ORR performance verified by DFT calculations (The ORR Uonset is marked at the upper left of each structure). Color legend: gray = C, blue = N, purple = Fe, red = O, pink = P, yellow = S, light blue = F.

Figure S21. Training and testing results of (a) RF, (b) KNN, (c) SVM and (d) GBR models for Ef prediction with full feature set without feature filtering (black dots represent the training set, black dots indicate the test set).

Figure S22. Training and testing results of (a) RF, (b) KNN, (c) SVM and (d) GBR models for ΔG*OH prediction with full feature set without feature filtering (black dots represent the training set, black dots indicate the test set).

Table S1. The original 28 features before feature filtering.

| Features |  |
| --- | --- |
| The average atomic radius of the first shell | R1 |
| The average atomic radius of the second shell The average atomic radius of the third shell | R2 R3 |
| The atomic radius of the axial ligand The average electronegativity of the first shell The average electronegativity of the second shell The average electronegativity of the third shell The electronegativity of the axial ligand The average ionization energy of the first shell The average ionization energy of the second shell The average ionization energy of the third shell The ionization energy of the axial ligand The average electron affinity of the first shell The average electron affinity of the second shell The average electron affinity of the third shell The electron affinity of the axial ligand The average p electron of the first shell The average p electron of the second shell The average p electron of the third shell The p electron of the axial ligand The average valence electron of the first shell The average valence electron of the second shell The average valence electron of the third shell The valence electron of the axial ligand The average period of the first shell The average period of the second shell The average period of the third shell The period of the axial ligand | R0 χ1 χ2 χ3 χ0 I1 I2 I3 I0 A1 A2 A3 A0 pe1 pe2 pe3 pe0 ve1 ve2 ve3 ve0 P1 P2 P3 P0 |

Table S2. Intrinsic properties of atoms. The units of R, I, and A are Å, eV, eV, respectively.

| Element | R | χ | I | A | pe | ve | P |
| --- | --- | --- | --- | --- | --- | --- | --- |
| B | 0.85 | 2.04 | 8.298 | 0.280 | 1 | 3 | 2 |
| Br Cl F I O P S Se Si Te C N H | 1.15 1.00 0.50 1.40 0.60 1.00 1.00 1.15 1.10 1.40 0.70 0.65 0.25 | 2.96 3.16 3.98 2.66 3.44 2.19 2.58 2.55 1.90 2.10 2.55 3.04 2.20 | 11.814 12.968 17.423 10.451 13.618 10.487 10.360 9.752 8.152 9.010 11.260 14.534 13.598 | 3.364 3.613 3.401 3.059 1.461 0.747 2.077 2.021 1.390 1.971 1.262 -0.070 0.755 | 17 11 5 23 4 9 10 16 8 22 2 3 0 | 7 7 7 7 6 5 6 6 4 6 4 5 1 | 4 3 2 5 2 3 3 4 3 5 2 2 1 |

Table S3. The hyper-parameters of the ML model for predicting Ef.

| Algorithm | Hyperparameters |
| --- | --- |
| RF KNN SVR GBR | max_depth=7, n_estimators=100, max_features=5 n_neighbors=7, weights=’uniform’ C=100, kernel=’rbf’, gamma=0.1 Learning_rate=0.01, max_depth=4, n_estimators=200 |

Table S4. The hyper-parameters of the ML model for predicting ΔG*OH.

| Algorithm | Hyperparameters |
| --- | --- |
| RF KNN SVR GBR | max_depth=11, n_estimators=220, max_features=7 n_neighbors=5, weights=’uniform’ C=13, kernel=’rbf’, gamma=’scale’ Learning_rate=0.1, max_depth=4, n_estimators=50 |

Table S5. Prediction of Ef and ΔG*OH with different structures of dopant and axial coordinating atoms.

| Structure | Predicted Ef (eV) | Predicted ΔG*OH (eV) |
| --- | --- | --- |
| site_4_doped_with_F_axial_O | -2.3521 | 1.142124 |
| site_4_doped_with_O_axial_F | -3.19142 | 1.155989 |
| site_4_doped_with_F_axial_B | 0.180919 | 1.166919 |
| site_2_doped_with_F_axial_O | -2.25143 | 1.173836 |
| site_4_doped_with_O_axial_B | 0.352783 | 1.177221 |
| site_2_doped_with_F_axial_B | 0.311268 | 1.182146 |
| site_3_doped_with_F_axial_O | -2.25396 | 1.187937 |
| site_3_doped_with_F_axial_B | 0.281192 | 1.19278 |
| site_4_doped_with_F_axial_N | 0.040332 | 1.257964 |
| site_4_doped_with_F_axial_C | -0.12055 | 1.276395 |
| site_2_doped_with_F_axial_N | 0.181893 | 1.285585 |
| site_4_doped_with_O_axial_N | 0.274694 | 1.292524 |
| site_2_doped_with_F_axial_C | -0.00695 | 1.295008 |
| site_4_doped_with_O_axial_C | 0.098521 | 1.297095 |
| site_3_doped_with_F_axial_N | 0.181893 | 1.299686 |
| site_3_doped_with_F_axial_C | -0.00695 | 1.305642 |
| site_4_doped_with_Cl_axial_F | -3.73615 | 1.332505 |
| site_4_doped_with_Br_axial_F | -4.34606 | 1.337083 |
| site_4_doped_with_N_axial_F | -3.17425 | 1.343054 |
| site_4_doped_with_Br_axial_O | -2.51161 | 1.349998 |
| site_4_doped_with_S_axial_F | -3.44361 | 1.354765 |
| site_4_doped_with_Cl_axial_O | -2.47282 | 1.361433 |
| site_2_doped_with_Cl_axial_F | -3.602 | 1.367939 |
| site_3_doped_with_Cl_axial_F | -3.7277 | 1.370517 |
| site_2_doped_with_P_axial_F | -3.27743 | 1.372332 |
| site_4_doped_with_P_axial_F | -3.53344 | 1.377965 |
| site_2_doped_with_Br_axial_F | -3.86431 | 1.379028 |
| site_3_doped_with_P_axial_F | -3.27743 | 1.379628 |
| site_2_doped_with_B_axial_F | -3.53014 | 1.380607 |
| site_2_doped_with_Se_axial_F | -3.38826 | 1.381422 |
| site_3_doped_with_B_axial_F | -3.51751 | 1.381465 |
| site_4_doped_with_Cl_axial_B | 0.063299 | 1.387001 |
| site_4_doped_with_B_axial_F | -3.50701 | 1.394655 |
| site_3_doped_with_Br_axial_F | -3.80268 | 1.397485 |
| site_4_doped_with_I_axial_F | -4.22879 | 1.398488 |
| site_3_doped_with_Se_axial_F | -3.37953 | 1.399538 |
| site_3_doped_with_O_axial_F | -3.33998 | 1.403335 |
| site_3_doped_with_N_axial_F | -3.24851 | 1.406262 |
| site_3_doped_with_I_axial_F | -4.15481 | 1.408002 |
| site_2_doped_with_S_axial_F | -3.37147 | 1.409351 |
| site_3_doped_with_S_axial_F | -3.37752 | 1.411156 |
| site_4_doped_with_Cl_axial_S | -3.32902 | 1.412109 |
| site_2_doped_with_O_axial_F | -3.22527 | 1.412942 |
| site_2_doped_with_N_axial_F | -3.24851 | 1.414545 |
| site_4_doped_with_Br_axial_B | -0.0965 | 1.419402 |
| site_1_doped_with_B_axial_F | -3.01329 | 1.422554 |
| site_4_doped_with_I_axial_O | -2.42619 | 1.425419 |
| site_4_doped_with_Cl_axial_Se | -4.09897 | 1.429839 |
| site_4_doped_with_S_axial_O | -2.47246 | 1.433888 |
| site_2_doped_with_I_axial_F | -4.39438 | 1.436568 |
| site_2_doped_with_Cl_axial_O | -2.31088 | 1.440248 |
| site_3_doped_with_N_axial_F | -3.42259 | 1.441675 |
| site_3_doped_with_Cl_axial_O | -2.3685 | 1.444598 |
| site_2_doped_with_Br_axial_O | -2.42887 | 1.444802 |
| site_4_doped_with_F_axial_P | -0.8073 | 1.44588 |
| site_3_doped_with_B_axial_F | -3.36063 | 1.44599 |
| site_3_doped_with_P_axial_F | -3.41675 | 1.446011 |
| site_3_doped_with_B_axial_F | -3.36063 | 1.448563 |
| site_4_doped_with_F_axial_Si | -0.58601 | 1.44883 |
| site_4_doped_with_Br_axial_N | -0.19558 | 1.451576 |
| site_1_doped_with_C_axial_F | -2.79514 | 1.452605 |
| site_4_doped_with_Cl_axial_Br | -4.31375 | 1.453486 |
| site_3_doped_with_N_axial_F | -3.40267 | 1.453938 |
| site_4_doped_with_Cl_axial_N | -0.09938 | 1.45456 |
| site_3_doped_with_P_axial_F | -3.41675 | 1.455136 |
| site_3_doped_with_Te_axial_F | -3.89972 | 1.455658 |
| site_4_doped_with_Cl_axial_P | -0.86805 | 1.45596 |
| site_4_doped_with_Cl_axial_Si | -0.6053 | 1.458097 |
| site_4_doped_with_F_axial_S | -3.09048 | 1.46531 |
| site_3_doped_with_Si_axial_F | -3.70811 | 1.466894 |
| site_3_doped_with_Br_axial_F | -3.8657 | 1.469112 |
| site_3_doped_with_S_axial_F | -3.39348 | 1.46921 |
| site_2_doped_with_Si_axial_F | -3.67771 | 1.470699 |
| site_4_doped_with_N_axial_O | -2.51725 | 1.471794 |
| site_3_doped_with_Si_axial_F | -3.42745 | 1.473022 |
| site_3_doped_with_Si_axial_F | -3.42745 | 1.473022 |
| site_3_doped_with_I_axial_O | -2.26618 | 1.473647 |
| site_4_doped_with_S_axial_Se | -3.79261 | 1.474091 |
| site_3_doped_with_Br_axial_F | -3.88712 | 1.474246 |
| site_4_doped_with_S_axial_B | 0.333536 | 1.474317 |
| site_2_doped_with_Br_axial_S | -3.27526 | 1.474919 |
| site_4_doped_with_F_axial_Se | -3.62739 | 1.475387 |
| site_3_doped_with_Cl_axial_F | -3.88248 | 1.478542 |
| site_2_doped_with_I_axial_O | -2.1869 | 1.479473 |
| site_3_doped_with_Br_axial_O | -2.39693 | 1.480389 |
| site_3_doped_with_O_axial_B | 0.355886 | 1.480868 |
| site_3_doped_with_I_axial_F | -4.32778 | 1.481425 |
| site_3_doped_with_I_axial_F | -4.32778 | 1.481425 |
| site_2_doped_with_Br_axial_B | 0.249391 | 1.482232 |
| site_4_doped_with_S_axial_P | -0.7127 | 1.482367 |
| site_4_doped_with_S_axial_Si | -0.40075 | 1.48479 |
| site_3_doped_with_Se_axial_F | -3.43168 | 1.485754 |
| site_3_doped_with_Te_axial_F | -4.18851 | 1.486512 |
| site_3_doped_with_Cl_axial_F | -3.87207 | 1.486602 |
| site_3_doped_with_Te_axial_F | -4.18851 | 1.486684 |
| site_3_doped_with_Se_axial_F | -3.39199 | 1.486928 |
| site_4_doped_with_F_axial_Cl | -3.7155 | 1.487129 |
| site_3_doped_with_Cl_axial_B | 0.230852 | 1.487716 |
| site_4_doped_with_Se_axial_F | -4.07254 | 1.488303 |
| site_4_doped_with_F_axial_Br | -3.98137 | 1.489801 |
| site_4_doped_with_I_axial_B | 0.168931 | 1.490154 |
| site_2_doped_with_Cl_axial_B | 0.159921 | 1.491359 |
| site_2_doped_with_Te_axial_F | -4.17675 | 1.491986 |
| site_3_doped_with_S_axial_F | -3.41271 | 1.492818 |
| site_2_doped_with_F_axial_P | -0.71525 | 1.493522 |
| site_4_doped_with_S_axial_Cl | -3.64341 | 1.493681 |
| site_4_doped_with_Cl_axial_C | -0.22159 | 1.493733 |
| site_3_doped_with_F_axial_P | -0.71525 | 1.494347 |
| site_2_doped_with_F_axial_Si | -0.46127 | 1.496186 |
| site_3_doped_with_O_axial_F | -3.39203 | 1.496894 |
| site_3_doped_with_F_axial_Si | -0.49135 | 1.497011 |
| site_2_doped_with_O_axial_B | 0.355886 | 1.499943 |
| site_3_doped_with_O_axial_F | -3.43307 | 1.499982 |
| site_2_doped_with_Br_axial_Se | -4.15987 | 1.505983 |
| site_2_doped_with_Br_axial_P | -0.70986 | 1.510061 |
| site_3_doped_with_I_axial_B | 0.338659 | 1.510825 |
| site_2_doped_with_Br_axial_Si | -0.39506 | 1.512484 |
| site_4_doped_with_Te_axial_F | -4.3085 | 1.517824 |
| site_4_doped_with_Si_axial_F | -4.00377 | 1.518184 |
| site_4_doped_with_Br_axial_C | -0.38538 | 1.520902 |
| site_4_doped_with_O_axial_Si | -0.49163 | 1.521955 |
| site_4_doped_with_O_axial_P | -0.67696 | 1.522604 |
| site_4_doped_with_S_axial_N | 0.112274 | 1.523663 |
| site_2_doped_with_I_axial_B | 0.309399 | 1.52668 |
| site_2_doped_with_Se_axial_O | -2.54454 | 1.526727 |
| site_3_doped_with_Br_axial_B | 0.283864 | 1.529975 |
| site_2_doped_with_F_axial_S | -3.01893 | 1.531653 |
| site_3_doped_with_F_axial_S | -3.04563 | 1.532479 |
| site_4_doped_with_I_axial_N | -0.00346 | 1.533842 |
| site_2_doped_with_Br_axial_Cl | -4.17304 | 1.535462 |
| site_3_doped_with_Br_axial_Se | -4.41009 | 1.537418 |
| site_2_doped_with_Br_axial_N | 0.085266 | 1.53768 |
| site_4_doped_with_N_axial_B | 0.266503 | 1.540262 |
| site_4_doped_with_Br_axial_Cl | -4.58004 | 1.541305 |
| site_2_doped_with_F_axial_Se | -3.66626 | 1.54185 |
| site_3_doped_with_Br_axial_Cl | -3.99926 | 1.541996 |
| site_3_doped_with_F_axial_Se | -3.70209 | 1.542676 |
| site_2_doped_with_F_axial_Cl | -3.78001 | 1.54561 |
| site_3_doped_with_F_axial_Cl | -3.82717 | 1.546435 |
| site_4_doped_with_Br_axial_S | -4.01898 | 1.547246 |
| site_4_doped_with_P_axial_O | -2.75109 | 1.553214 |
| site_2_doped_with_Se_axial_B | 0.333536 | 1.556105 |
| site_4_doped_with_S_axial_C | -0.00852 | 1.5562 |
| site_2_doped_with_Cl_axial_N | 0.012436 | 1.556287 |
| site_4_doped_with_B_axial_O | -2.74824 | 1.556562 |
| site_3_doped_with_Cl_axial_N | 0.092906 | 1.560637 |
| site_4_doped_with_Br_axial_Se | -4.95697 | 1.561541 |
| site_4_doped_with_Te_axial_O | -2.62766 | 1.561792 |
| site_3_doped_with_Br_axial_P | -0.89623 | 1.565735 |
| site_4_doped_with_S_axial_Br | -4.06227 | 1.567686 |
| site_3_doped_with_I_axial_N | 0.173272 | 1.567983 |
| site_2_doped_with_Br_axial_C | -0.03724 | 1.569108 |
| site_3_doped_with_Br_axial_Si | -0.75924 | 1.569715 |
| site_4_doped_with_Cl_axial_Te | -4.83824 | 1.57031 |
| site_4_doped_with_N_axial_Si | -0.54023 | 1.570508 |
| site_4_doped_with_Br_axial_P | -0.96912 | 1.571746 |
| site_4_doped_with_N_axial_P | -0.69998 | 1.572124 |
| site_4_doped_with_F_axial_Te | -4.37013 | 1.572154 |
| site_2_doped_with_F_axial_Br | -4.09054 | 1.572507 |
| site_3_doped_with_F_axial_Br | -4.17484 | 1.573332 |
| site_2_doped_with_Cl_axial_P | -0.76498 | 1.573358 |
| site_2_doped_with_Cl_axial_Si | -0.44806 | 1.573378 |
| site_3_doped_with_Cl_axial_P | -0.74746 | 1.573396 |
| site_3_doped_with_Cl_axial_Si | -0.42312 | 1.573417 |
| site_2_doped_with_P_axial_O | -2.55484 | 1.573872 |
| site_4_doped_with_Br_axial_Si | -0.69555 | 1.574309 |
| site_4_doped_with_Se_axial_O | -2.37095 | 1.577452 |
| site_2_doped_with_S_axial_O | -2.53635 | 1.580807 |
| site_2_doped_with_I_axial_N | 0.148159 | 1.584001 |
| site_4_doped_with_I_axial_C | -0.15289 | 1.586438 |
| site_2_doped_with_Se_axial_Si | -0.36044 | 1.586725 |
| site_2_doped_with_Se_axial_P | -0.68366 | 1.586768 |
| site_3_doped_with_Cl_axial_C | -0.06996 | 1.587538 |
| site_2_doped_with_B_axial_O | -2.80831 | 1.587672 |
| site_2_doped_with_Cl_axial_C | -0.13331 | 1.587974 |
| site_3_doped_with_B_axial_O | -2.83115 | 1.588922 |
| site_3_doped_with_Br_axial_S | -3.5629 | 1.588967 |
| site_3_doped_with_Se_axial_O | -2.54454 | 1.590261 |
| site_3_doped_with_P_axial_O | -2.56072 | 1.592226 |
| site_4_doped_with_P_axial_B | 0.174136 | 1.59343 |
| site_3_doped_with_N_axial_O | -2.64137 | 1.595837 |
| site_3_doped_with_Br_axial_N | 0.119738 | 1.59729 |
| site_3_doped_with_Te_axial_O | -2.43442 | 1.598425 |
| site_2_doped_with_N_axial_O | -2.64137 | 1.598568 |
| site_2_doped_with_Se_axial_S | -2.83789 | 1.598852 |
| site_2_doped_with_Cl_axial_S | -3.1286 | 1.601848 |
| site_4_doped_with_O_axial_Se | -3.24606 | 1.602421 |
| site_1_doped_with_P_axial_F | -2.16442 | 1.602503 |
| site_1_doped_with_Si_axial_F | -1.94741 | 1.602503 |
| site_1_doped_with_Te_axial_F | -0.69196 | 1.602503 |
| site_3_doped_with_Cl_axial_S | -3.18658 | 1.603307 |
| site_4_doped_with_Te_axial_B | 0.129617 | 1.604344 |
| site_4_doped_with_O_axial_S | -2.67525 | 1.604347 |
| site_3_doped_with_P_axial_B | 0.321064 | 1.605137 |
| site_3_doped_with_I_axial_S | -3.64751 | 1.605419 |
| site_3_doped_with_Cl_axial_Br | -4.42923 | 1.605548 |
| site_2_doped_with_S_axial_B | 0.342958 | 1.606635 |
| site_3_doped_with_F_axial_Se | -4.01918 | 1.60669 |
| site_3_doped_with_S_axial_O | -2.53635 | 1.606853 |
| site_3_doped_with_Cl_axial_Se | -4.16911 | 1.607024 |
| site_4_doped_with_O_axial_Cl | -3.43959 | 1.607075 |
| site_2_doped_with_Cl_axial_Se | -3.91528 | 1.607284 |
| site_3_doped_with_I_axial_C | 0.002185 | 1.608116 |
| site_3_doped_with_Cl_axial_Se | -3.95784 | 1.608168 |
| site_2_doped_with_P_axial_B | 0.239278 | 1.60898 |
| site_2_doped_with_Te_axial_O | -2.58745 | 1.610891 |
| site_3_doped_with_Cl_axial_Br | -4.41882 | 1.613169 |
| site_1_doped_with_I_axial_F | -0.33063 | 1.613301 |
| site_1_doped_with_S_axial_F | -1.49286 | 1.613301 |
| site_1_doped_with_Se_axial_F | -0.93017 | 1.613301 |
| site_3_doped_with_Cl_axial_P | -0.93413 | 1.613949 |
| site_3_doped_with_F_axial_Si | -0.76423 | 1.615129 |
| site_3_doped_with_F_axial_P | -0.94386 | 1.61618 |
| site_2_doped_with_Se_axial_N | 0.097919 | 1.616571 |
| site_3_doped_with_Cl_axial_Se | -4.16332 | 1.616948 |
| site_3_doped_with_Cl_axial_Si | -0.81908 | 1.61717 |
| site_2_doped_with_O_axial_Si | -0.48987 | 1.61785 |
| site_3_doped_with_O_axial_Si | -0.48987 | 1.617976 |
| site_3_doped_with_Se_axial_B | 0.333536 | 1.618222 |
| site_3_doped_with_Te_axial_B | 0.180826 | 1.620137 |
| site_2_doped_with_O_axial_P | -0.67475 | 1.620686 |
| site_3_doped_with_O_axial_P | -0.67475 | 1.620813 |
| site_3_doped_with_S_axial_B | 0.342958 | 1.621892 |
| site_3_doped_with_I_axial_P | -0.6532 | 1.622038 |
| site_3_doped_with_I_axial_Cl | -4.46691 | 1.622064 |
| site_3_doped_with_F_axial_Cl | -4.04911 | 1.622191 |
| site_3_doped_with_I_axial_Si | -0.30998 | 1.624234 |
| site_2_doped_with_N_axial_B | 0.264867 | 1.626764 |
| site_3_doped_with_N_axial_O | -2.54719 | 1.627289 |
| site_3_doped_with_N_axial_Si | -0.41239 | 1.628618 |
| site_3_doped_with_B_axial_P | -0.58075 | 1.628931 |
| site_3_doped_with_B_axial_P | -0.58075 | 1.629166 |
| site_4_doped_with_Se_axial_B | 0.251259 | 1.629372 |
| site_3_doped_with_Br_axial_C | -0.00277 | 1.629419 |
| site_3_doped_with_N_axial_Si | -0.41239 | 1.629727 |
| site_2_doped_with_Se_axial_Cl | -3.5701 | 1.630575 |
| site_2_doped_with_Te_axial_B | 0.099019 | 1.632704 |
| site_3_doped_with_B_axial_Si | -0.41857 | 1.633347 |
| site_3_doped_with_N_axial_P | -0.55935 | 1.633774 |
| site_1_doped_with_Br_axial_F | -0.72427 | 1.633781 |
| site_1_doped_with_Cl_axial_F | -1.40719 | 1.633781 |
| site_3_doped_with_I_axial_Se | -4.79558 | 1.63394 |
| site_4_doped_with_Br_axial_Te | -5.80304 | 1.634231 |
| site_3_doped_with_N_axial_P | -0.55935 | 1.634883 |
| site_3_doped_with_B_axial_Si | -0.41857 | 1.635092 |
| site_3_doped_with_O_axial_C | 0.066375 | 1.635212 |
| site_3_doped_with_I_axial_Br | -5.06335 | 1.635371 |
| site_3_doped_with_Cl_axial_P | -0.93413 | 1.635639 |
| site_3_doped_with_P_axial_Si | -0.51873 | 1.635752 |
| site_2_doped_with_I_axial_C | 0.009811 | 1.63606 |
| site_4_doped_with_N_axial_Se | -2.7654 | 1.636305 |
| site_2_doped_with_Se_axial_C | 0.009108 | 1.636804 |
| site_2_doped_with_Si_axial_O | -2.88315 | 1.636832 |
| site_3_doped_with_Cl_axial_Si | -0.81908 | 1.637361 |
| site_3_doped_with_N_axial_B | 0.342076 | 1.638195 |
| site_2_doped_with_F_axial_Te | -4.42291 | 1.638646 |
| site_3_doped_with_F_axial_Te | -4.47138 | 1.639472 |
| site_1_doped_with_C_axial_B | 0.449251 | 1.639591 |
| site_3_doped_with_Cl_axial_S | -3.539 | 1.641115 |
| site_3_doped_with_N_axial_Si | -0.57491 | 1.641488 |
| site_2_doped_with_O_axial_C | 0.093283 | 1.641979 |
| site_3_doped_with_Cl_axial_Br | -4.29896 | 1.642125 |
| site_2_doped_with_N_axial_Si | -0.57491 | 1.642833 |
| site_2_doped_with_Cl_axial_Br | -4.14918 | 1.642879 |
| site_3_doped_with_N_axial_O | -2.56581 | 1.643034 |
| site_3_doped_with_N_axial_B | 0.259268 | 1.643399 |
| site_4_doped_with_N_axial_S | -2.59968 | 1.643619 |
| site_3_doped_with_Br_axial_Si | -0.34909 | 1.643643 |
| site_3_doped_with_Br_axial_P | -0.67539 | 1.644583 |
| site_3_doped_with_F_axial_B | 0.088523 | 1.644769 |
| site_4_doped_with_Si_axial_O | -2.58233 | 1.64564 |
| site_3_doped_with_F_axial_S | -3.45834 | 1.645884 |
| site_3_doped_with_F_axial_B | 0.100516 | 1.647993 |
| site_4_doped_with_N_axial_C | 0.058467 | 1.648823 |
| site_2_doped_with_Si_axial_B | 0.285582 | 1.652062 |
| site_3_doped_with_F_axial_Br | -4.37418 | 1.652543 |
| site_4_doped_with_Si_axial_B | 0.164011 | 1.65333 |
| site_3_doped_with_N_axial_P | -0.72063 | 1.653476 |
| site_3_doped_with_N_axial_B | 0.342076 | 1.653533 |
| site_3_doped_with_P_axial_Si | -0.51873 | 1.65361 |
| site_2_doped_with_N_axial_P | -0.72063 | 1.654821 |
| site_3_doped_with_F_axial_O | -2.77417 | 1.657117 |
| site_2_doped_with_Br_axial_Te | -4.91103 | 1.658957 |
| site_3_doped_with_Br_axial_O | -2.73332 | 1.659405 |
| site_3_doped_with_F_axial_O | -2.81682 | 1.659421 |
| site_4_doped_with_P_axial_N | 0.095638 | 1.659505 |
| site_3_doped_with_O_axial_N | 0.248661 | 1.659552 |
| site_4_doped_with_N_axial_Cl | -3.36192 | 1.661314 |
| site_2_doped_with_O_axial_N | 0.242172 | 1.662756 |
| site_3_doped_with_Br_axial_S | -3.24084 | 1.666976 |
| site_3_doped_with_Cl_axial_S | -3.53321 | 1.667227 |
| site_3_doped_with_Cl_axial_O | -2.69999 | 1.667452 |
| site_3_doped_with_Cl_axial_O | -2.73763 | 1.67088 |
| site_4_doped_with_B_axial_N | 0.1929 | 1.671455 |
| site_4_doped_with_Te_axial_N | -0.07189 | 1.674334 |
| site_3_doped_with_Si_axial_O | -2.94351 | 1.674631 |
| site_3_doped_with_P_axial_B | 0.219349 | 1.675774 |
| site_3_doped_with_P_axial_O | -2.75894 | 1.676305 |
| site_3_doped_with_Br_axial_B | 0.054128 | 1.676351 |
| site_3_doped_with_B_axial_O | -2.67279 | 1.676712 |
| site_3_doped_with_Si_axial_B | 0.31387 | 1.677925 |
| site_1_doped_with_B_axial_O | -2.25435 | 1.678415 |
| site_3_doped_with_P_axial_O | -2.75894 | 1.678668 |
| site_4_doped_with_S_axial_Te | -4.60322 | 1.679153 |
| site_3_doped_with_B_axial_O | -2.67279 | 1.679341 |
| site_3_doped_with_Br_axial_O | -2.75369 | 1.68265 |
| site_4_doped_with_O_axial_Br | -3.71595 | 1.68286 |
| site_3_doped_with_Cl_axial_B | 0.009428 | 1.68311 |
| site_2_doped_with_S_axial_N | 0.119774 | 1.683846 |
| site_4_doped_with_I_axial_Br | -5.08451 | 1.685897 |
| site_3_doped_with_P_axial_B | 0.219349 | 1.686055 |
| site_3_doped_with_Cl_axial_B | 0.009428 | 1.686599 |
| site_3_doped_with_F_axial_Si | -0.74309 | 1.687388 |
| site_4_doped_with_Se_axial_N | 0.055138 | 1.689875 |
| site_2_doped_with_P_axial_N | 0.114961 | 1.690456 |
| site_4_doped_with_I_axial_Cl | -4.47658 | 1.690528 |
| site_3_doped_with_N_axial_Se | -3.25598 | 1.692658 |
| site_3_doped_with_F_axial_P | -0.93187 | 1.693452 |
| site_3_doped_with_N_axial_Se | -3.25598 | 1.693767 |
| site_2_doped_with_O_axial_Se | -2.91135 | 1.69563 |
| site_3_doped_with_Te_axial_N | 0.022053 | 1.695679 |
| site_3_doped_with_O_axial_Se | -2.95532 | 1.695756 |
| site_3_doped_with_Se_axial_N | 0.097919 | 1.696632 |
| site_4_doped_with_P_axial_C | -0.07473 | 1.698089 |
| site_3_doped_with_Cl_axial_Te | -4.77988 | 1.69812 |
| site_2_doped_with_Cl_axial_Te | -4.74855 | 1.698203 |
| site_3_doped_with_Br_axial_B | 0.062351 | 1.698334 |
| site_3_doped_with_O_axial_B | 0.359705 | 1.698918 |
| site_3_doped_with_Br_axial_Cl | -4.11931 | 1.699539 |
| site_3_doped_with_Br_axial_Se | -4.15525 | 1.69984 |
| site_2_doped_with_S_axial_C | 0.007281 | 1.700375 |
| site_2_doped_with_O_axial_S | -2.67308 | 1.702118 |
| site_3_doped_with_O_axial_S | -2.75485 | 1.702244 |
| site_3_doped_with_F_axial_Cl | -4.05435 | 1.702479 |
| site_3_doped_with_I_axial_O | -2.85207 | 1.702857 |
| site_3_doped_with_I_axial_O | -2.85207 | 1.702857 |
| site_4_doped_with_Cl_axial_I | -5.3465 | 1.703057 |
| site_2_doped_with_B_axial_N | 0.15604 | 1.70306 |
| site_3_doped_with_B_axial_N | 0.171621 | 1.704114 |
| site_1_doped_with_C_axial_O | -2.36014 | 1.705362 |
| site_4_doped_with_I_axial_S | -3.84474 | 1.705562 |
| site_3_doped_with_P_axial_N | 0.179036 | 1.705858 |
| site_4_doped_with_P_axial_Se | -3.4489 | 1.706336 |
| site_3_doped_with_S_axial_N | 0.119774 | 1.708785 |
| site_3_doped_with_O_axial_B | 0.359705 | 1.710309 |
| site_3_doped_with_Te_axial_B | 0.075549 | 1.710924 |
| site_3_doped_with_Si_axial_B | 0.235041 | 1.711049 |
| site_3_doped_with_Si_axial_B | 0.235041 | 1.711246 |
| site_3_doped_with_Te_axial_B | 0.075549 | 1.712072 |
| site_2_doped_with_Te_axial_N | -0.07918 | 1.712686 |
| site_3_doped_with_F_axial_Se | -4.01918 | 1.714399 |
| site_4_doped_with_Br_axial_I | -6.34363 | 1.716979 |
| site_3_doped_with_Te_axial_O | -3.03841 | 1.718735 |
| site_3_doped_with_Si_axial_O | -2.74521 | 1.71876 |
| site_3_doped_with_Si_axial_O | -2.74521 | 1.71876 |
| site_3_doped_with_Te_axial_O | -3.03841 | 1.719078 |
| site_3_doped_with_I_axial_B | 0.053864 | 1.719367 |
| site_3_doped_with_I_axial_B | 0.053864 | 1.719367 |
| site_2_doped_with_O_axial_Cl | -3.50098 | 1.720074 |
| site_3_doped_with_O_axial_Cl | -3.58878 | 1.7202 |
| site_3_doped_with_Se_axial_C | 0.004335 | 1.720213 |
| site_3_doped_with_S_axial_C | 0.007281 | 1.72037 |
| site_2_doped_with_S_axial_Si | -0.34787 | 1.720901 |
| site_4_doped_with_P_axial_Si | -0.54041 | 1.720991 |
| site_2_doped_with_P_axial_C | -0.059 | 1.721207 |
| site_3_doped_with_N_axial_S | -2.83412 | 1.721466 |
| site_3_doped_with_Br_axial_Te | -5.25165 | 1.721553 |
| site_3_doped_with_O_axial_Si | -0.48341 | 1.721625 |
| site_3_doped_with_O_axial_Si | -0.48341 | 1.722155 |
| site_3_doped_with_N_axial_S | -2.83412 | 1.722575 |
| site_3_doped_with_I_axial_Te | -5.62902 | 1.722676 |
| site_4_doped_with_B_axial_C | -0.0000979 | 1.723095 |
| site_4_doped_with_P_axial_Cl | -3.63521 | 1.723259 |
| site_3_doped_with_P_axial_C | 0.017678 | 1.723578 |
| site_3_doped_with_S_axial_O | -2.83842 | 1.72414 |
| site_3_doped_with_N_axial_Cl | -3.54624 | 1.724777 |
| site_3_doped_with_Se_axial_B | 0.215354 | 1.724853 |
| site_3_doped_with_Se_axial_O | -2.7548 | 1.725709 |
| site_3_doped_with_N_axial_Cl | -3.52205 | 1.726888 |
| site_1_doped_with_B_axial_C | 0.317214 | 1.72821 |
| site_3_doped_with_Te_axial_C | -0.10905 | 1.729215 |
| site_4_doped_with_Te_axial_C | -0.18907 | 1.729472 |
| site_4_doped_with_P_axial_S | -2.95054 | 1.729605 |
| site_2_doped_with_S_axial_P | -0.68063 | 1.730672 |
| site_3_doped_with_F_axial_N | -0.10035 | 1.731326 |
| site_3_doped_with_Se_axial_B | 0.224048 | 1.731493 |
| site_3_doped_with_O_axial_P | -0.60844 | 1.733457 |
| site_3_doped_with_F_axial_N | -0.08836 | 1.7335 |
| site_3_doped_with_O_axial_P | -0.60844 | 1.733986 |
| site_4_doped_with_O_axial_Te | -3.86482 | 1.73414 |
| site_3_doped_with_Br_axial_Si | -0.75832 | 1.734206 |
| site_4_doped_with_I_axial_P | -0.78319 | 1.734695 |
| site_3_doped_with_Se_axial_O | -2.80206 | 1.735246 |
| site_4_doped_with_N_axial_Br | -3.33527 | 1.735556 |
| site_3_doped_with_N_axial_Se | -2.8466 | 1.73628 |
| site_3_doped_with_Br_axial_Cl | -3.979 | 1.736508 |
| site_4_doped_with_I_axial_Si | -0.47053 | 1.736996 |
| site_3_doped_with_Br_axial_P | -0.88576 | 1.737479 |
| site_2_doped_with_N_axial_Se | -2.8466 | 1.737625 |
| site_3_doped_with_S_axial_B | 0.193804 | 1.739013 |
| site_2_doped_with_N_axial_C | 0.067586 | 1.740052 |
| site_3_doped_with_S_axial_O | -2.79762 | 1.74045 |
| site_4_doped_with_F_axial_I | -5.01534 | 1.741955 |
| site_2_doped_with_P_axial_Si | -0.5369 | 1.742259 |
| site_3_doped_with_P_axial_Si | -0.50182 | 1.742456 |
| site_3_doped_with_N_axial_S | -2.67307 | 1.743159 |
| site_3_doped_with_Br_axial_N | -0.15708 | 1.743329 |
| site_4_doped_with_Se_axial_C | -0.07336 | 1.743348 |
| site_3_doped_with_F_axial_S | -3.46358 | 1.743807 |
| site_2_doped_with_N_axial_S | -2.67307 | 1.744504 |
| site_2_doped_with_Te_axial_C | -0.20104 | 1.745717 |
| site_4_doped_with_Si_axial_N | 0.0167 | 1.747484 |
| site_3_doped_with_N_axial_C | 0.11345 | 1.748817 |
| site_4_doped_with_I_axial_Se | -4.90487 | 1.749056 |
| site_3_doped_with_Te_axial_Si | -0.7442 | 1.749169 |
| site_3_doped_with_Cl_axial_N | -0.17497 | 1.749208 |
| site_3_doped_with_Te_axial_Si | -0.7442 | 1.749958 |
| site_3_doped_with_F_axial_C | -0.29351 | 1.751579 |
| site_3_doped_with_Cl_axial_N | -0.17497 | 1.751806 |
| site_3_doped_with_B_axial_S | -2.73204 | 1.752369 |
| site_3_doped_with_P_axial_Cl | -3.58185 | 1.753134 |
| site_2_doped_with_I_axial_Cl | -4.6682 | 1.753536 |
| site_3_doped_with_S_axial_B | 0.143894 | 1.753782 |
| site_3_doped_with_F_axial_C | -0.25086 | 1.754802 |
| site_2_doped_with_Si_axial_N | 0.059687 | 1.755572 |
| site_3_doped_with_P_axial_S | -2.91715 | 1.755989 |
| site_3_doped_with_B_axial_S | -2.73204 | 1.756388 |
| site_3_doped_with_N_axial_C | 0.064918 | 1.756688 |
| site_3_doped_with_S_axial_Si | -0.35761 | 1.757585 |
| site_3_doped_with_Te_axial_P | -0.87437 | 1.759682 |
| site_3_doped_with_N_axial_Cl | -3.46803 | 1.760295 |
| site_2_doped_with_B_axial_C | 0.006122 | 1.76094 |
| site_3_doped_with_N_axial_C | 0.11345 | 1.761803 |
| site_3_doped_with_B_axial_C | 0.038556 | 1.762093 |
| site_3_doped_with_Si_axial_P | -0.65254 | 1.76215 |
| site_3_doped_with_Si_axial_P | -0.65149 | 1.76215 |
| site_3_doped_with_B_axial_Cl | -3.49077 | 1.762906 |
| site_3_doped_with_Te_axial_P | -0.87437 | 1.763095 |
| site_3_doped_with_B_axial_Si | -0.46428 | 1.763126 |
| site_2_doped_with_B_axial_Si | -0.47688 | 1.76365 |
| site_3_doped_with_F_axial_Br | -4.37943 | 1.764628 |
| site_3_doped_with_Se_axial_Si | -0.34894 | 1.764926 |
| site_3_doped_with_B_axial_Cl | -3.49077 | 1.765199 |
| site_2_doped_with_N_axial_Cl | -3.46803 | 1.766129 |
| site_2_doped_with_S_axial_Se | -3.66167 | 1.766389 |
| site_4_doped_with_Si_axial_C | -0.0778 | 1.767303 |
| site_3_doped_with_Br_axial_Se | -4.35653 | 1.767373 |
| site_3_doped_with_Se_axial_Si | -0.66251 | 1.767436 |
| site_2_doped_with_Se_axial_Br | -4.03602 | 1.767625 |
| site_3_doped_with_P_axial_Se | -3.24666 | 1.768842 |
| site_3_doped_with_P_axial_N | 0.061896 | 1.770443 |
| site_4_doped_with_N_axial_Te | -3.29574 | 1.771994 |
| site_2_doped_with_I_axial_Br | -5.4061 | 1.772315 |
| site_3_doped_with_P_axial_N | 0.061896 | 1.772805 |
| site_2_doped_with_Si_axial_C | 0.010091 | 1.77311 |
| site_1_doped_with_B_axial_Si | -0.21545 | 1.773496 |
| site_3_doped_with_B_axial_Se | -2.99701 | 1.773999 |
| site_3_doped_with_B_axial_Se | -2.99701 | 1.774234 |
| site_3_doped_with_Se_axial_P | -0.75701 | 1.775444 |
| site_3_doped_with_Br_axial_C | -0.26893 | 1.775803 |
| site_4_doped_with_B_axial_Si | -0.37657 | 1.775973 |
| site_3_doped_with_S_axial_P | -0.69036 | 1.776931 |
| site_1_doped_with_C_axial_Si | -0.42996 | 1.777435 |
| site_1_doped_with_B_axial_N | 0.341764 | 1.777922 |
| site_1_doped_with_P_axial_B | 0.728093 | 1.777964 |
| site_1_doped_with_Si_axial_B | 0.765261 | 1.777964 |
| site_1_doped_with_Te_axial_B | 2.621509 | 1.777964 |
| site_3_doped_with_O_axial_Se | -3.21404 | 1.778674 |
| site_3_doped_with_O_axial_Se | -3.23408 | 1.779203 |
| site_3_doped_with_Br_axial_N | -0.1536 | 1.779347 |
| site_2_doped_with_B_axial_P | -0.79164 | 1.779525 |
| site_3_doped_with_I_axial_Si | -0.7396 | 1.779871 |
| site_3_doped_with_I_axial_Si | -0.7396 | 1.779871 |
| site_3_doped_with_B_axial_P | -0.77134 | 1.780299 |
| site_3_doped_with_Cl_axial_C | -0.30527 | 1.782555 |
| site_2_doped_with_Se_axial_Te | -4.57629 | 1.782729 |
| site_3_doped_with_B_axial_N | 0.174393 | 1.78277 |
| site_2_doped_with_I_axial_S | -3.89811 | 1.783308 |
| site_3_doped_with_P_axial_Se | -3.24666 | 1.783805 |
| site_3_doped_with_Se_axial_P | -0.68843 | 1.784946 |
| site_2_doped_with_I_axial_P | -0.65015 | 1.785285 |
| site_3_doped_with_B_axial_N | 0.174393 | 1.785362 |
| site_3_doped_with_Cl_axial_C | -0.30527 | 1.78565 |
| site_3_doped_with_P_axial_Cl | -3.58185 | 1.786966 |
| site_3_doped_with_Br_axial_Te | -4.94837 | 1.787035 |
| site_3_doped_with_I_axial_Cl | -4.4499 | 1.787243 |
| site_3_doped_with_I_axial_Cl | -4.4499 | 1.787243 |
| site_2_doped_with_I_axial_Si | -0.31291 | 1.787907 |
| site_2_doped_with_Br_axial_I | -5.42636 | 1.788999 |
| site_3_doped_with_I_axial_P | -0.97252 | 1.789463 |
| site_3_doped_with_I_axial_P | -0.97252 | 1.789463 |
| site_4_doped_with_B_axial_P | -0.68615 | 1.790379 |
| site_3_doped_with_P_axial_C | 0.004954 | 1.790981 |
| site_3_doped_with_Si_axial_N | 0.090167 | 1.793133 |
| site_3_doped_with_P_axial_S | -2.91715 | 1.794877 |
| site_2_doped_with_O_axial_Br | -3.52134 | 1.795467 |
| site_3_doped_with_O_axial_Br | -3.56339 | 1.795593 |
| site_3_doped_with_P_axial_C | 0.004954 | 1.79583 |
| site_3_doped_with_F_axial_Te | -4.6967 | 1.795971 |
| site_3_doped_with_Se_axial_Si | -0.66699 | 1.797567 |
| site_3_doped_with_Cl_axial_Te | -4.76234 | 1.798129 |
| site_1_doped_with_B_axial_P | -0.34144 | 1.79837 |
| site_3_doped_with_O_axial_Cl | -3.51706 | 1.799533 |
| site_3_doped_with_O_axial_Cl | -3.51473 | 1.800062 |
| site_3_doped_with_S_axial_Si | -0.67447 | 1.801089 |
| site_3_doped_with_B_axial_C | 0.125979 | 1.80221 |
| site_1_doped_with_C_axial_P | -0.64668 | 1.802309 |
| site_3_doped_with_Br_axial_C | -0.25523 | 1.804023 |
| site_1_doped_with_O_axial_F | -2.65435 | 1.804158 |
| site_3_doped_with_I_axial_N | -0.29475 | 1.80497 |
| site_3_doped_with_I_axial_N | -0.29475 | 1.80497 |
| site_3_doped_with_Cl_axial_Te | -4.76234 | 1.80515 |
| site_3_doped_with_B_axial_C | 0.125979 | 1.808255 |
| site_3_doped_with_Br_axial_S | -3.54827 | 1.80843 |
| site_1_doped_with_I_axial_B | 3.36539 | 1.808654 |
| site_1_doped_with_S_axial_B | 0.766114 | 1.808654 |
| site_1_doped_with_Se_axial_B | 1.755969 | 1.808654 |
| site_3_doped_with_Si_axial_C | 0.01381 | 1.808685 |
| site_3_doped_with_Se_axial_P | -0.74781 | 1.809984 |
| site_2_doped_with_F_axial_I | -5.06078 | 1.811454 |
| site_3_doped_with_O_axial_S | -2.79558 | 1.812148 |
| site_3_doped_with_F_axial_I | -5.14618 | 1.812279 |
| site_3_doped_with_O_axial_S | -2.81562 | 1.812677 |
| site_3_doped_with_Te_axial_Cl | -4.33675 | 1.813356 |
| site_3_doped_with_Te_axial_N | -0.07098 | 1.813443 |
| site_3_doped_with_Te_axial_N | -0.07098 | 1.813786 |
| site_3_doped_with_Si_axial_N | 0.098291 | 1.814527 |
| site_3_doped_with_Si_axial_N | 0.098291 | 1.814527 |
| site_1_doped_with_C_axial_N | 0.175124 | 1.817689 |
| site_3_doped_with_S_axial_P | -0.77058 | 1.818039 |
| site_3_doped_with_O_axial_N | 0.258355 | 1.818586 |
| site_3_doped_with_O_axial_N | 0.235987 | 1.81868 |
| site_3_doped_with_Te_axial_Cl | -4.33675 | 1.819727 |
| site_3_doped_with_O_axial_C | 0.08035 | 1.820416 |
| site_3_doped_with_N_axial_Br | -3.81997 | 1.820417 |
| site_3_doped_with_O_axial_C | 0.08035 | 1.820851 |
| site_2_doped_with_P_axial_Se | -2.87651 | 1.822528 |
| site_3_doped_with_N_axial_Br | -3.81997 | 1.822528 |
| site_3_doped_with_Se_axial_N | 0.0699 | 1.823636 |
| site_3_doped_with_O_axial_Te | -3.43132 | 1.824629 |
| site_2_doped_with_S_axial_Cl | -3.56673 | 1.82589 |
| site_3_doped_with_P_axial_Se | -2.83144 | 1.826304 |
| site_3_doped_with_Se_axial_Cl | -3.58415 | 1.826425 |
| site_2_doped_with_O_axial_Te | -3.38735 | 1.826501 |
| site_3_doped_with_Te_axial_Se | -4.68903 | 1.826691 |
| site_3_doped_with_Si_axial_C | 0.023347 | 1.826748 |
| site_3_doped_with_Si_axial_C | 0.023347 | 1.826945 |
| site_3_doped_with_Te_axial_C | -0.20515 | 1.827249 |
| site_3_doped_with_S_axial_N | 0.035156 | 1.827468 |
| site_2_doped_with_I_axial_Se | -5.16298 | 1.82752 |
| site_4_doped_with_I_axial_Te | -5.7029 | 1.82757 |
| site_3_doped_with_Te_axial_C | -0.20515 | 1.82849 |
| site_3_doped_with_I_axial_C | -0.32833 | 1.829362 |
| site_3_doped_with_I_axial_C | -0.32833 | 1.829362 |
| site_3_doped_with_I_axial_Se | -4.92568 | 1.832501 |
| site_3_doped_with_I_axial_Se | -4.92568 | 1.832501 |
| site_3_doped_with_Se_axial_N | 0.07746 | 1.832682 |
| site_3_doped_with_Te_axial_Se | -4.68903 | 1.834269 |
| site_3_doped_with_Se_axial_C | -0.05547 | 1.835494 |
| site_3_doped_with_Si_axial_P | -0.69474 | 1.838601 |
| site_3_doped_with_Te_axial_S | -3.93352 | 1.839254 |
| site_2_doped_with_P_axial_Cl | -3.38265 | 1.84004 |
| site_3_doped_with_I_axial_Br | -5.11167 | 1.841875 |
| site_3_doped_with_I_axial_Br | -5.11167 | 1.841875 |
| site_2_doped_with_Si_axial_P | -0.69764 | 1.841884 |
| site_3_doped_with_S_axial_Se | -3.62499 | 1.843208 |
| site_3_doped_with_Se_axial_C | -0.04626 | 1.843553 |
| site_3_doped_with_Te_axial_S | -3.93352 | 1.844996 |
| site_3_doped_with_S_axial_N | -0.01475 | 1.845905 |
| site_3_doped_with_P_axial_Cl | -3.38265 | 1.846083 |
| site_1_doped_with_Br_axial_B | 2.010659 | 1.846705 |
| site_1_doped_with_Cl_axial_B | 0.929558 | 1.846705 |
| site_1_doped_with_Br_axial_Si | 1.706754 | 1.848316 |
| site_1_doped_with_Cl_axial_Si | 0.466218 | 1.848316 |
| site_1_doped_with_I_axial_Si | 3.010669 | 1.848316 |
| site_1_doped_with_P_axial_Si | 0.075459 | 1.848316 |
| site_1_doped_with_S_axial_Si | 0.237335 | 1.848316 |
| site_1_doped_with_Se_axial_Si | 1.34742 | 1.848316 |
| site_1_doped_with_Te_axial_Si | 2.232637 | 1.848316 |
| site_3_doped_with_S_axial_C | -0.08805 | 1.849153 |
| site_3_doped_with_Si_axial_Cl | -3.59254 | 1.84974 |
| site_3_doped_with_Si_axial_Cl | -3.59254 | 1.84974 |
| site_4_doped_with_B_axial_Se | -3.25733 | 1.852914 |
| site_3_doped_with_Se_axial_S | -3.13028 | 1.853946 |
| site_2_doped_with_B_axial_Se | -3.25654 | 1.855162 |
| site_3_doped_with_Si_axial_Se | -3.32313 | 1.85598 |
| site_3_doped_with_Si_axial_Se | -3.32313 | 1.85598 |
| site_2_doped_with_P_axial_S | -2.52484 | 1.85652 |
| site_3_doped_with_N_axial_Br | -3.43807 | 1.860205 |
| site_4_doped_with_S_axial_I | -5.17254 | 1.86066 |
| site_3_doped_with_N_axial_Te | -3.4094 | 1.86103 |
| site_2_doped_with_B_axial_Cl | -3.65483 | 1.861395 |
| site_3_doped_with_P_axial_S | -2.52484 | 1.861404 |
| site_3_doped_with_Te_axial_Si | -0.44295 | 1.861461 |
| site_4_doped_with_B_axial_Cl | -3.61044 | 1.861985 |
| site_4_doped_with_P_axial_Br | -3.77075 | 1.862864 |
| site_3_doped_with_B_axial_Cl | -3.6422 | 1.864514 |
| site_2_doped_with_N_axial_Te | -3.4094 | 1.865202 |
| site_3_doped_with_B_axial_Se | -3.15061 | 1.865364 |
| site_3_doped_with_S_axial_C | -0.14098 | 1.865374 |
| site_2_doped_with_N_axial_Br | -3.43807 | 1.866038 |
| site_3_doped_with_Te_axial_P | -0.77704 | 1.867456 |
| site_3_doped_with_I_axial_S | -4.0281 | 1.869442 |
| site_3_doped_with_I_axial_S | -4.0281 | 1.869442 |
| site_3_doped_with_Si_axial_S | -2.91168 | 1.869495 |
| site_3_doped_with_Si_axial_S | -2.91168 | 1.869495 |
| site_3_doped_with_S_axial_Cl | -3.54711 | 1.872174 |
| site_1_doped_with_Br_axial_P | 1.405615 | 1.872585 |
| site_1_doped_with_Cl_axial_P | 0.324912 | 1.872585 |
| site_1_doped_with_I_axial_P | 2.587319 | 1.872585 |
| site_1_doped_with_S_axial_P | 0.008431 | 1.872585 |
| site_1_doped_with_Se_axial_P | 1.01019 | 1.872585 |
| site_1_doped_with_Si_axial_P | -0.01925 | 1.872585 |
| site_1_doped_with_Te_axial_P | 1.885896 | 1.872585 |
| site_3_doped_with_Se_axial_Cl | -3.54562 | 1.873187 |
| site_3_doped_with_S_axial_Si | -0.71346 | 1.873611 |
| site_3_doped_with_Te_axial_Se | -4.48812 | 1.877182 |
| site_2_doped_with_B_axial_S | -2.85368 | 1.881668 |
| site_3_doped_with_B_axial_S | -2.835 | 1.882244 |
| site_4_doped_with_Si_axial_P | -0.72327 | 1.883526 |
| site_4_doped_with_B_axial_S | -2.8382 | 1.884283 |
| site_3_doped_with_S_axial_Cl | -3.57278 | 1.885422 |
| site_3_doped_with_N_axial_Te | -3.88476 | 1.886769 |
| site_3_doped_with_N_axial_Te | -3.88476 | 1.887877 |
| site_3_doped_with_Te_axial_Cl | -4.06368 | 1.888324 |
| site_3_doped_with_S_axial_P | -0.8056 | 1.888994 |
| site_3_doped_with_Se_axial_S | -2.8392 | 1.891668 |
| site_3_doped_with_Se_axial_Cl | -3.56137 | 1.891708 |
| site_3_doped_with_F_axial_Te | -4.6967 | 1.894573 |
| site_3_doped_with_Cl_axial_I | -5.34269 | 1.895033 |
| site_2_doped_with_Cl_axial_I | -5.25352 | 1.89559 |
| site_2_doped_with_I_axial_Te | -5.96107 | 1.895972 |
| site_3_doped_with_O_axial_Br | -3.81109 | 1.896251 |
| site_3_doped_with_O_axial_Br | -3.80876 | 1.89678 |
| site_3_doped_with_Se_axial_S | -3.08504 | 1.897784 |
| site_3_doped_with_S_axial_Se | -3.56485 | 1.898893 |
| site_2_doped_with_S_axial_Te | -4.48323 | 1.901421 |
| site_3_doped_with_Br_axial_Te | -5.23951 | 1.902835 |
| site_1_doped_with_F_axial_Si | -0.35572 | 1.902944 |
| site_1_doped_with_O_axial_Si | -0.48621 | 1.902944 |
| site_3_doped_with_Te_axial_S | -3.40035 | 1.903364 |
| site_4_doped_with_Si_axial_Se | -4.20604 | 1.904854 |
| site_2_doped_with_Si_axial_Se | -3.56418 | 1.908333 |
| site_3_doped_with_P_axial_Br | -3.71978 | 1.908799 |
| site_3_doped_with_Si_axial_Se | -3.5566 | 1.908832 |
| site_4_doped_with_Si_axial_Cl | -4.17687 | 1.917211 |
| site_3_doped_with_Se_axial_Br | -3.92759 | 1.919376 |
| site_3_doped_with_Te_axial_Br | -4.88436 | 1.919715 |
| site_1_doped_with_F_axial_P | -0.49603 | 1.920449 |
| site_1_doped_with_O_axial_P | -0.66777 | 1.920449 |
| site_1_doped_with_P_axial_O | -1.28944 | 1.921178 |
| site_1_doped_with_Si_axial_O | -1.22292 | 1.921178 |
| site_1_doped_with_Te_axial_O | 0.573262 | 1.921178 |
| site_1_doped_with_B_axial_Se | -2.65316 | 1.923613 |
| site_3_doped_with_P_axial_Br | -3.71978 | 1.923762 |
| site_1_doped_with_B_axial_Cl | -3.13018 | 1.924495 |
| site_4_doped_with_P_axial_Te | -4.11907 | 1.926907 |
| site_1_doped_with_C_axial_Se | -2.46399 | 1.927551 |
| site_2_doped_with_Si_axial_S | -3.07497 | 1.927623 |
| site_1_doped_with_F_axial_B | 0.4025 | 1.928254 |
| site_1_doped_with_O_axial_B | 0.428012 | 1.928254 |
| site_3_doped_with_Si_axial_Cl | -3.85219 | 1.929148 |
| site_1_doped_with_C_axial_Cl | -2.88921 | 1.929392 |
| site_3_doped_with_Te_axial_Br | -4.88436 | 1.929515 |
| site_4_doped_with_Si_axial_S | -3.51365 | 1.930005 |
| site_1_doped_with_I_axial_O | 1.18657 | 1.930107 |
| site_1_doped_with_S_axial_O | -0.6582 | 1.930107 |
| site_1_doped_with_Se_axial_O | -0.02949 | 1.930107 |
| site_2_doped_with_Si_axial_Cl | -3.83364 | 1.931508 |
| site_1_doped_with_B_axial_S | -2.23205 | 1.933133 |
| site_1_doped_with_C_axial_S | -2.1354 | 1.937071 |
| site_3_doped_with_Si_axial_S | -3.09071 | 1.937715 |
| site_3_doped_with_B_axial_Br | -3.58919 | 1.946303 |
| site_1_doped_with_P_axial_C | 0.48144 | 1.946767 |
| site_1_doped_with_Si_axial_C | 0.491234 | 1.946767 |
| site_1_doped_with_Te_axial_C | 2.200482 | 1.946767 |
| site_3_doped_with_B_axial_Br | -3.58919 | 1.947794 |
| site_3_doped_with_S_axial_Cl | -3.55524 | 1.95008 |
| site_2_doped_with_S_axial_Br | -3.97819 | 1.950118 |
| site_1_doped_with_Br_axial_O | 0.306215 | 1.95094 |
| site_1_doped_with_Cl_axial_O | -0.55138 | 1.95094 |
| site_3_doped_with_Se_axial_Te | -4.36345 | 1.955413 |
| site_3_doped_with_Br_axial_I | -5.50063 | 1.955608 |
| site_3_doped_with_S_axial_Te | -4.45377 | 1.958055 |
| site_3_doped_with_O_axial_Te | -3.85323 | 1.961284 |
| site_3_doped_with_O_axial_Te | -3.85323 | 1.961813 |
| site_3_doped_with_I_axial_Te | -5.68085 | 1.963937 |
| site_3_doped_with_I_axial_Te | -5.68085 | 1.963937 |
| site_3_doped_with_P_axial_Te | -3.27683 | 1.966167 |
| site_1_doped_with_I_axial_C | 2.804876 | 1.967528 |
| site_1_doped_with_S_axial_C | 0.498191 | 1.967528 |
| site_1_doped_with_Se_axial_C | 1.288543 | 1.967528 |
| site_2_doped_with_P_axial_Te | -3.29868 | 1.967887 |
| site_2_doped_with_Te_axial_Cl | -4.36778 | 1.969076 |
| site_3_doped_with_S_axial_Se | -3.59223 | 1.969416 |
| site_3_doped_with_Si_axial_Br | -3.81527 | 1.975147 |
| site_3_doped_with_Si_axial_Br | -3.81527 | 1.975147 |
| site_3_doped_with_P_axial_Te | -3.72815 | 1.975981 |
| site_3_doped_with_Se_axial_Br | -3.87475 | 1.976208 |
| site_4_doped_with_Se_axial_Cl | -4.255 | 1.979532 |
| site_3_doped_with_Se_axial_Te | -4.56869 | 1.98172 |
| site_3_doped_with_B_axial_Te | -3.62423 | 1.982263 |
| site_3_doped_with_B_axial_Te | -3.62423 | 1.982499 |
| site_3_doped_with_P_axial_Te | -3.72815 | 1.986168 |
| site_4_doped_with_O_axial_I | -4.3477 | 1.986635 |
| site_2_doped_with_Te_axial_Si | -0.49262 | 1.987478 |
| site_2_doped_with_Te_axial_P | -0.86977 | 1.989167 |
| site_3_doped_with_Te_axial_Br | -4.60203 | 1.990197 |
| site_1_doped_with_Br_axial_Se | -1.29927 | 1.995946 |
| site_1_doped_with_Cl_axial_Se | -1.78992 | 1.995946 |
| site_1_doped_with_I_axial_Se | -1.25919 | 1.995946 |
| site_1_doped_with_P_axial_Se | -2.14855 | 1.995946 |
| site_1_doped_with_S_axial_Se | -1.78343 | 1.995946 |
| site_1_doped_with_Si_axial_Se | -1.93567 | 1.995946 |
| site_1_doped_with_Te_axial_Se | -1.56912 | 1.995946 |
| site_3_doped_with_Se_axial_Te | -4.30862 | 1.996439 |
| site_2_doped_with_P_axial_Br | -3.35992 | 1.998668 |
| site_1_doped_with_Br_axial_Cl | -0.83638 | 2.000236 |
| site_1_doped_with_I_axial_Cl | -0.5255 | 2.000236 |
| site_1_doped_with_P_axial_Cl | -2.25777 | 2.000236 |
| site_1_doped_with_S_axial_Cl | -1.58547 | 2.000236 |
| site_1_doped_with_Se_axial_Cl | -1.03717 | 2.000236 |
| site_1_doped_with_Si_axial_Cl | -2.00791 | 2.000236 |
| site_1_doped_with_Te_axial_Cl | -0.8549 | 2.000236 |
| site_1_doped_with_Br_axial_S | -0.31832 | 2.002311 |
| site_1_doped_with_Cl_axial_S | -1.15994 | 2.002311 |
| site_1_doped_with_I_axial_S | 0.050637 | 2.002311 |
| site_1_doped_with_P_axial_S | -1.65317 | 2.002311 |
| site_1_doped_with_Se_axial_S | -0.55815 | 2.002311 |
| site_1_doped_with_Si_axial_S | -1.48387 | 2.002311 |
| site_1_doped_with_Te_axial_S | -0.34669 | 2.002311 |
| site_4_doped_with_B_axial_Te | -3.81863 | 2.002725 |
| site_1_doped_with_Br_axial_C | 1.600072 | 2.00322 |
| site_1_doped_with_Cl_axial_C | 0.710255 | 2.00322 |
| site_3_doped_with_S_axial_Br | -3.78748 | 2.003348 |
| site_3_doped_with_P_axial_Br | -3.3548 | 2.003447 |
| site_1_doped_with_P_axial_N | 0.484264 | 2.006041 |
| site_1_doped_with_Si_axial_N | 0.450902 | 2.006041 |
| site_1_doped_with_Te_axial_N | 2.214849 | 2.006041 |
| site_2_doped_with_B_axial_Te | -3.84012 | 2.006508 |
| site_4_doped_with_B_axial_Br | -3.70915 | 2.013937 |
| site_4_doped_with_N_axial_I | -4.086 | 2.015201 |
| site_3_doped_with_Si_axial_Te | -4.00623 | 2.016537 |
| site_3_doped_with_Si_axial_Te | -4.00623 | 2.016537 |
| site_3_doped_with_B_axial_Te | -3.74494 | 2.01696 |
| site_1_doped_with_I_axial_N | 2.767232 | 2.018611 |
| site_1_doped_with_S_axial_N | 0.471673 | 2.018611 |
| site_1_doped_with_Se_axial_N | 1.305104 | 2.018611 |
| site_4_doped_with_Se_axial_P | -0.73018 | 2.020948 |
| site_4_doped_with_Si_axial_Te | -4.86133 | 2.022113 |
| site_4_doped_with_Si_axial_Br | -4.50623 | 2.022368 |
| site_4_doped_with_Se_axial_Si | -0.38695 | 2.02357 |
| site_3_doped_with_S_axial_Br | -3.97912 | 2.024747 |
| site_2_doped_with_Te_axial_S | -3.7417 | 2.025981 |
| site_2_doped_with_Te_axial_Se | -4.87781 | 2.027195 |
| site_1_doped_with_Br_axial_N | 1.546935 | 2.036025 |
| site_1_doped_with_Cl_axial_N | 0.642573 | 2.036025 |
| site_2_doped_with_B_axial_Br | -3.68718 | 2.037854 |
| site_3_doped_with_S_axial_Te | -3.86208 | 2.037916 |
| site_1_doped_with_F_axial_Se | -2.35551 | 2.041671 |
| site_1_doped_with_O_axial_Se | -2.58612 | 2.041671 |
| site_3_doped_with_Br_axial_I | -5.82998 | 2.04313 |
| site_3_doped_with_S_axial_Br | -3.80139 | 2.04389 |
| site_3_doped_with_Si_axial_Te | -4.15482 | 2.044659 |
| site_4_doped_with_Se_axial_S | -3.54845 | 2.045057 |
| site_1_doped_with_F_axial_Cl | -2.24222 | 2.047568 |
| site_1_doped_with_O_axial_Cl | -2.74744 | 2.047568 |
| site_1_doped_with_F_axial_S | -1.964 | 2.049713 |
| site_1_doped_with_O_axial_S | -2.36869 | 2.049713 |
| site_3_doped_with_B_axial_Br | -3.64666 | 2.051894 |
| site_2_doped_with_Si_axial_Te | -4.19274 | 2.053135 |
| site_4_doped_with_Te_axial_Cl | -4.50401 | 2.05665 |
| site_4_doped_with_Se_axial_Br | -4.97348 | 2.060015 |
| site_3_doped_with_Se_axial_Br | -4.01349 | 2.061682 |
| site_2_doped_with_Te_axial_Br | -4.99155 | 2.065383 |
| site_1_doped_with_B_axial_Te | -3.28141 | 2.080988 |
| site_1_doped_with_F_axial_C | 0.219524 | 2.084006 |
| site_1_doped_with_O_axial_C | 0.173906 | 2.084006 |
| site_1_doped_with_C_axial_Te | -3.13969 | 2.084926 |
| site_3_doped_with_Si_axial_Br | -3.93668 | 2.084937 |
| site_3_doped_with_O_axial_I | -4.13986 | 2.087279 |
| site_2_doped_with_O_axial_I | -4.09781 | 2.089151 |
| site_3_doped_with_S_axial_Te | -3.88946 | 2.09071 |
| site_2_doped_with_Si_axial_Br | -3.94427 | 2.092872 |
| site_3_doped_with_Cl_axial_I | -5.38614 | 2.10502 |
| site_3_doped_with_Cl_axial_I | -5.38614 | 2.112765 |
| site_3_doped_with_N_axial_I | -4.1356 | 2.114442 |
| site_4_doped_with_Te_axial_P | -0.8403 | 2.115176 |
| site_4_doped_with_Te_axial_Br | -5.10851 | 2.119065 |
| site_4_doped_with_Te_axial_Si | -0.47443 | 2.120481 |
| site_2_doped_with_N_axial_I | -4.1356 | 2.121395 |
| site_1_doped_with_B_axial_Br | -3.28363 | 2.127709 |
| site_3_doped_with_F_axial_I | -5.36252 | 2.131298 |
| site_4_doped_with_Te_axial_S | -3.83825 | 2.132199 |
| site_1_doped_with_C_axial_Br | -3.02805 | 2.132606 |
| site_1_doped_with_Br_axial_Te | -1.98988 | 2.135271 |
| site_1_doped_with_Cl_axial_Te | -2.47655 | 2.135271 |
| site_1_doped_with_I_axial_Te | -1.95944 | 2.135271 |
| site_1_doped_with_P_axial_Te | -2.90368 | 2.135271 |
| site_1_doped_with_S_axial_Te | -2.51837 | 2.135271 |
| site_1_doped_with_Se_axial_Te | -2.25378 | 2.135271 |
| site_1_doped_with_Si_axial_Te | -2.56349 | 2.135271 |
| site_2_doped_with_Se_axial_I | -5.01798 | 2.145828 |
| site_4_doped_with_Se_axial_Te | -5.57096 | 2.162953 |
| site_1_doped_with_F_axial_O | -1.85907 | 2.166124 |
| site_4_doped_with_Te_axial_Se | -4.96592 | 2.169271 |
| site_1_doped_with_F_axial_Te | -2.9742 | 2.173471 |
| site_1_doped_with_O_axial_Te | -3.23375 | 2.173471 |
| site_1_doped_with_Cl_axial_Br | -2.08624 | 2.182727 |
| site_1_doped_with_I_axial_Br | -1.64411 | 2.182727 |
| site_1_doped_with_P_axial_Br | -2.53229 | 2.182727 |
| site_1_doped_with_S_axial_Br | -1.98235 | 2.182727 |
| site_1_doped_with_Se_axial_Br | -1.70559 | 2.182727 |
| site_1_doped_with_Si_axial_Br | -2.25628 | 2.182727 |
| site_1_doped_with_Te_axial_Br | -1.8059 | 2.182727 |
| site_1_doped_with_F_axial_N | 0.307376 | 2.195704 |
| site_1_doped_with_O_axial_N | 0.225876 | 2.195704 |
| site_1_doped_with_F_axial_Br | -2.74519 | 2.21272 |
| site_1_doped_with_O_axial_Br | -3.10996 | 2.21272 |
| site_4_doped_with_P_axial_I | -4.48393 | 2.221594 |
| site_3_doped_with_F_axial_I | -5.36252 | 2.222556 |
| site_3_doped_with_Br_axial_I | -5.85241 | 2.223123 |
| site_3_doped_with_N_axial_I | -4.79815 | 2.259402 |
| site_3_doped_with_N_axial_I | -4.79815 | 2.261513 |
| site_3_doped_with_Te_axial_I | -5.51863 | 2.282463 |
| site_2_doped_with_S_axial_I | -4.96591 | 2.293524 |
| site_4_doped_with_Se_axial_I | -6.26954 | 2.31057 |
| site_2_doped_with_Te_axial_I | -5.99262 | 2.314232 |
| site_3_doped_with_Te_axial_I | -5.76304 | 2.317919 |
| site_3_doped_with_Te_axial_I | -5.76304 | 2.318601 |
| site_3_doped_with_Se_axial_I | -4.75649 | 2.322901 |
| site_4_doped_with_Si_axial_I | -5.20194 | 2.323356 |
| site_3_doped_with_O_axial_I | -4.7778 | 2.325651 |
| site_3_doped_with_O_axial_I | -4.7778 | 2.32618 |
| site_2_doped_with_P_axial_I | -3.91288 | 2.332519 |
| site_4_doped_with_B_axial_I | -4.27745 | 2.335092 |
| site_3_doped_with_P_axial_I | -3.90775 | 2.337879 |
| site_3_doped_with_S_axial_I | -4.96079 | 2.345412 |
| site_3_doped_with_P_axial_I | -4.35133 | 2.352473 |
| site_3_doped_with_P_axial_I | -4.35133 | 2.36093 |
| site_2_doped_with_B_axial_I | -4.24446 | 2.362469 |
| site_4_doped_with_Te_axial_I | -6.23073 | 2.36266 |
| site_3_doped_with_Se_axial_I | -4.70365 | 2.364026 |
| site_3_doped_with_Se_axial_I | -5.01798 | 2.365303 |
| site_3_doped_with_B_axial_I | -4.30208 | 2.366633 |
| site_3_doped_with_B_axial_I | -4.30208 | 2.366651 |
| site_3_doped_with_B_axial_I | -4.17821 | 2.370089 |
| site_3_doped_with_S_axial_I | -4.38953 | 2.378076 |
| site_3_doped_with_Si_axial_I | -4.63533 | 2.379355 |
| site_3_doped_with_Si_axial_I | -4.63533 | 2.379355 |
| site_2_doped_with_Si_axial_I | -4.52477 | 2.39199 |
| site_3_doped_with_Si_axial_I | -4.50202 | 2.398559 |
| site_3_doped_with_S_axial_I | -4.39984 | 2.414748 |
| site_1_doped_with_B_axial_I | -4.04464 | 2.464237 |
| site_1_doped_with_C_axial_I | -3.73317 | 2.469134 |
| site_1_doped_with_Br_axial_I | -2.32884 | 2.5084 |
| site_1_doped_with_Cl_axial_I | -2.82961 | 2.5084 |
| site_1_doped_with_P_axial_I | -3.32739 | 2.5084 |
| site_1_doped_with_S_axial_I | -2.68727 | 2.5084 |
| site_1_doped_with_Se_axial_I | -2.44372 | 2.5084 |
| site_1_doped_with_Si_axial_I | -2.88666 | 2.5084 |
| site_1_doped_with_Te_axial_I | -2.61213 | 2.5084 |
| site_1_doped_with_F_axial_I | -3.58099 | 2.534836 |
| site_1_doped_with_O_axial_I | -3.92032 | 2.534836 |