Appendices for:

Low-carbon self-compacting glass fiber-reinforced concrete using calcium sulpho-aluminate cement and recycled concrete fine aggregate

Radhika SRIDHARa, Yanfei CHEb, Patraphorn PHORNTHEPKASEMSANTc, Thanongsak IMJAId*, Elhem GHORBELe, Kypros PILAKOUTASf

a School of Engineering and Technology, Walailak University, Nakhon Si Thammarat 80161, Thailand

b Zhejiang Construction Industry Research Institute Co. Ltd., Baoye Group, Shaoxing 312028, China

c Department of Civil Engineering, Faculty of Engineering, Burapha University, Chonburi 20131, Thailand

d Advanced Composite Research Center, Faculty of Engineering, Burapha University, Chonburi 20131, Thailand

e Department of Civil Engineering, CY Cergy Paris University, Neuville sur Oise 95031, France

f Department of Civil and Structural Engineering, The University of Sheffield, Sheffield S13JD, UK

*Corresponding author. E-mail: thanongsak.im@eng.buu.ac.th

Appendix A: Mix designations and details of OPC, CSA cement with RFA and GRC

Table A1 Mix details of OPC, CSA cement with the addition of RFA and glass fibers

| Mix | RFA/cement | Water/cement | Water/dry materials | Fiber (%) | Workability approach |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | 1 (mm) | 2 (mm) | 3 (s) |
| 1a | 0.500 | 0.45 | 0.3 | 4.5 | 135 | 190 | 9.0 |
| 1b |  |  |  | 6.0 | 135 | 180 | 10.0 |
| 2a | 0.625 | 0.45 | 0.28 | 4.9 | 130 | 190 | 11.0 |
| 2b |  |  |  | 6.0 | 125 | 180 | 12.5 |
| 3a | 0.750 | 0.45 | 0.26 | 5.3 | 120 | 185 | 13.0 |
| 3b |  |  |  | 6.0 | 125 | 180 | 14.0 |
| 4a | 0.875 | 0.45 | 0.24 | 5.6 | 115 | 185 | 14.5 |
| 4b |  |  |  | 6.0 | 85 | 175 | 16.0 |
| 5a | 1.000 | 0.45 | 0.22 | 6.0 | 95 | 170 | 15.5 |
| 5b |  |  |  | 6.0 | 95 | 160 | 16.0 |
| 5c |  |  |  | 6.0 | 65 | 150 | 16.0 |

Table A2 Effect of white Portland cement using RFA on workability

| Mix | White cement | SPFA | RFA | Water | SP (%) | Fiber (%) | Workability approach (mm) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | 1 (mm) | 2 (mm) | 3 (s) |
| 1 | 100 | – | 70 | 45 | – | 3 | 70 | 115 | 9.0 |
| 2 | 100 | – | 70 | 30 | 0.3 | 3 | 65 | 80 | 10.0 |
| 3 | 100 | – | 70 | 30 | 0.6 | 3 | 115 | 135 | 11.0 |
| 4 | 100 | – | 70 | 30 | 1.0 | 3 | 140 | 180 | 12.5 |
| 5 | 70 | 30 | 70 | 30 | 0.5 | 3 | 110 | 135 | 14.5 |
| 6 | 70 | 30 | 70 | 30 | 1.0 | 3 | 167 | 187 | 16.5 |
| 7 | 80 | 20 | 60 | 30 | 0.8 | 3 | 125 | 160 | 14.0 |
| 8 | 90 | 10 | 70 | 35 | 0.5 | 4 | 140 | 175 | 15.0 |
| 9 | 100 | 10 | 50 | 40 | 1.2 | 3 | 155 | 180 | 16.0 |
| 10 | 80 | 20 | 50 | 45 | 0.4 | 4 | 120 | 150 | 18.0 |

Table A3 Mix design and flow time of SCC mixes with RFA and GRC

| Fiber type | Initial flow time (s) | Final flow time (s) | GRC flow time (s) | Flow performance |
| --- | --- | --- | --- | --- |
| X-1000 (2%) | 12.7 | 12.5 | 27.5 | good |
| X-1000 (2.5%) | 13.0 | 14.4 | 85.1 | moderate |
| X-1000 (3%) | 12.1 | 14.1 | 22.4 | good |
| X-1000 (3.5%) | 11.7 | 13.0 | 18.2 | good |
| EF-500 (2%) | 13.0 | 14.4 | 85.1 | moderate |
| EF-500 (2.5%) | 14.0 | 15.0 | 90.2 | moderate |
| EF-500 (3%) | 13.5 | 14.2 | 70.0 | moderate |
| EF-500 (3.5%) | 12.0 | 12.8 | 60.5 | moderate |
| MF-2000 (2%) | 21.3 | 22.1 | 40.6 | low |
| MF-2000 (2.5%) | 22.5 | 23.0 | 50.2 | low |
| MF-2000 (3%) | 23.0 | 23.5 | 55.0 | low |
| MF-2000 (3.5%) | 25.0 | 25.0 | 65.4 | low |
| UF-300 (2%) | 53.8 | 53.8 | 75.0 | very low |
| UF-300 (2.5%) | 55.0 | 55.0 | 90.0 | very low |
| UF-300 (3%) | 57.3 | 57.3 | 95.0 | very low |
| UF-300 (3.5%) | 60.0 | 60.0 | 101.6 | very low |
| SF-800 (2%) | 17.2 | 17.2 | 41.9 | moderate |
| SF-800 (2.5%) | 18.0 | 18.0 | 50.2 | moderate |
| SF-800 (3%) | 18.5 | 18.5 | 55.5 | moderate |
| SF-800 (3.5%) | 19.0 | 19.0 | 60.3 | moderate |

Note: X-1000 represents high strength fiber, EF represents eco-friendly fibers, MF represents macro synthetic based poly fiber, UF represents ultra-fine fiber, and SF represents high-performance fiber.

Appendix B: Compression strength performance of OPC, CSA cement with RFA and GRC

Table B1 Compressive strength results of CSA with RFA in GRC

| CSA | SPFA | NFA or RFA | Water | SP | Fiber | Strength (MPa) | STDV (MPa) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 100 | – | 70-NFA | 30 | 0.8 | – | 67.4 | 3.5 |
| 100 | – | 70-NFA | 30 | 0.8 | 17 (1%) | 66.7 | 3.2 |
| 100 | – | 70-NFA | 30 | 0.8 | 34 (2%) | 65.6 | 2.8 |
| 85 | 15 | 70-NFA | 30 | 0.8 | 34 (2%) | 61.1 | 2.9 |
| 70 | 30 | 70-NFA | 30 | 0.8 | 34 (2%) | 60.2 | 3.2 |
| 100 | – | 70-NFA | 30 | 0.8 | 51 (3%) | 64.7 | 3.9 |
| 100 | – | 70-NFA | 30 | 0.8 | 68 (4%) | 64.2 | 2.3 |
| 100 | – | 70-RFA | 30 | 0.9 | 17 (1%) | 63.7 | 3.3 |
| 95 | 05 | 70-RFA | 30 | 0.9 | 34 (2%) | 62.8 | 3.1 |
| 90 | 10 | 70-RFA | 30 | 1.0 | 34 (2%) | 62.1 | 2.7 |
| 85 | 15 | 70-RFA | 30 | 1.0 | 51 (3%) | 58.7 | 2.5 |
| 70 | 30 | 70-RFA | 30 | 1.0 | 68 (4%) | 56.4 | 2.1 |

Appendix C: Flexural strength performance of OPC, CSA cement with RFA and GRC

Box C1 Computer program developed in Compaq Visual FORTRAN 6.6

! Average of test results

implicit none

integer :: NumOfTest

integer :: DataLength

integer :: i,j,k

real,allocatable  :: V(:)

character(len=10) :: Fin, Fout

write (*,*) "Please input the number of tests carried out:"

read (*,*) NumOfTest

write (*,*) "Please input the length of data array:"

read (*,*) Fin

write (*,*) "Please input the output data file name"

read (*,*) Fout

do i=1, DataLength

if (.not. Eof(20)) then

read (20, *) V(1:NumOfTest)

print *, V

k=0

Sum=0

do j=1,NumOfTest

if (V(j)/=0) then

k=k+1

Sum=Sum+V(j)

end if

end do

if (k/=0) then

write (21, '(F8.3)') Sum/k

end if

else

exit

end if

end do

close(20)

close(21)

stop

end

Fig. C1 Model load deflection curves of bending test.

(a)                                         (b)

Fig. C2 Histogram with fitted probability distribution plot for find out modulus of elasticity: (a) 3-parameter weibull; (b) smallest extreme value.

(a)                                         (b)

Fig. C3 Probability plot with 95% confidence level: (a) 3-parameter weibull; (b) smallest extreme value.

Appendix D: Bond strength performance of OPC, CSA cement with RFA and GRC

Table D1 Bond strength results of CSA with RFA in GRC

| Group | Length, l (mm) | Aging temperature (°C) | Aging time (d) | Peak load (N) | Tensile, σ (MPa) | Average bond, τ (MPa) | Standard deviation (MPa) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 4 | 20 | 28 | 15.0 | 153.4 | 0.60 | 0.10 |
| 2 | 4 | 28 | 28 | 14.7 | 150.3 | 0.59 | 0.07 |
| 3 | 6 | 28 | 7 | 19.0 | 194.3 | 0.51 | 0.06 |
| 4 | 6 | 28 | 7 | 18.7 | 191.2 | 0.50 | 0.05 |
| 5 | 6 | 38 | 14 | 17.0 | 173.8 | 0.46 | 0.04 |
| 6 | 8 | 38 | 60 | 26.3 | 268.9 | 0.53 | 0.05 |
| 7 | 10 | 20 | 150 | 38.0 | 388.5 | 0.61 | 0.09 |
| 8 | 6 | 20 | 28 | 23.0 | 235.2 | 0.62 | 0.06 |

Fig. D1 Bond slip behavior results of CSA with RFA in GRC.

Appendix E: Long-term performance of OPC, CSA cement with RFA and GRC

Fig. E1 Time dependent performance of different matrices with the incorporation of OPC, CSA, RFA, GRC.

(a)                                         (b)

Fig. E2 Influence of fiber content, length, and type on LOP and MOR: (a) LOP; (b) MOR.

(a)                                         (b)

Fig. E3 Influence of fiber content, filament diameter, and strand integrity on LOP and MOR: (a) LOP; (b) MOR.

Table E1 Aging test results of GRC wire mesh with RFA

| Age of sample (d) | Measured parameter | Specimen |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| 10 | LOR (MPa) | 7.70 | 7.75 | 8.45 | 7.90 | 8.45 | 7.65 | 8.95 |
|  | MOR (MPa) | 8.45 | 9.00 | 8.50 | 8.70 | 9.00 | 10.00 | 8.30 |
|  | STF (%) | 0.35 | 0.95 | 0.55 | 0.60 | 0.60 | 1.05 | 0.70 |
| 20 | LOR (MPa) | 7.70 | 7.75 | 8.40 | 8.10 | 7.80 | 7.80 | 7.70 |
|  | MOR (MPa) | 18.50 | 16.00 | 18.30 | 14.60 | 7.70 | 9.90 | 8.40 |
|  | STF (%) | 0.30 | 0.28 | 0.55 | 0.60 | 0.47 | 0.45 | 0.75 |
| 30 | LOR (MPa) | 7.10 | 7.15 | 7.60 | 7.90 | 7.75 | 7.65 | 7.60 |
|  | MOR (MPa) | 7.65 | 7.95 | 15.50 | 8.50 | 7.70 | 8.40 | 7.80 |
|  | STF (%) | 0.22 | 0.26 | 0.33 | 0.27 | 0.29 | 0.50 | 0.63 |
| 40 | LOR (MPa) | 6.80 | 6.80 | 7.00 | 6.90 | 6.95 | 7.30 | 7.10 |
|  | MOR (MPa) | 13.50 | 13.80 | 9.20 | 10.20 | 7.30 | 7.80 | 8.40 |
|  | STF (%) | 0.12 | 0.72 | 0.35 | 0.70 | 0.43 | 0.45 | 0.50 |
| 45 | LOR (MPa) | 6.75 | 11.20 | 6.70 | 5.90 | 6.85 | 6.55 | 6.10 |
|  | MOR (MPa) | 11.50 | 12.60 | 9.00 | 8.50 | 8.65 | 9.20 | 6.80 |
|  | STF (%) | 0.08 | 0.47 | 0.42 | 0.52 | 0.31 | 0.49 | 0.35 |
| 60 | LOR (MPa) | 6.60 | 6.15 | 6.55 | 6.80 | 6.60 | 6.90 | 6.80 |
|  | MOR (MPa) | 11.80 | 11.50 | 9.90 | 10.30 | 10.00 | 9.60 | 8.90 |
|  | STF (%) | 0.38 | 0.43 | 0.41 | 0.43 | 0.40 | 0.36 | 0.42 |
| 75 | LOR (MPa) | 7.50 | 8.40 | 8.20 | 8.60 | 8.80 | 9.10 | 8.85 |
|  | MOR (MPa) | 8.90 | 22.80 | 19.70 | 8.90 | 21.80 | 21.00 | 14.60 |
|  | STF (%) | 0.43 | 1.20 | 1.55 | 1.05 | 1.30 | 1.50 | 0.90 |