Appendices for:

Hybrid support vector regression approaches for modeling punching shear strength of reinforced concrete flat plates

Mosbeh R. KALOOPa,b,c, Furquan AHMADd, Pijush SAMUIe, Jong Wan HUa,b*, Basem S. ABDELWAHEDf

a Department of Civil and Environmental Engineering, Incheon National University, Incheon 22012, South Korea

b Incheon Disaster Prevention Research Center, Incheon National University, Incheon 22012, South Korea

c Public Works Engineering Department, Mansoura University, Mansoura 35516, Egypt

d Department of Civil and Environmental engineering, Indian Institute of Technology Patna, Patna 801103, India

e Department of Civil Engineering, National Institute of Technology Patna, Patna 800005, India

f Structural Engineering Department, Mansoura University, Mansoura 35516, Egypt

*Corresponding author. E-mail: jongp24@inu.ac.kr

Appendix. Data used

Table 1 Data used

| DO_1 | ID | column type | h | c | d | ro (%) | fc | fy | Vtest Kn | Group |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | A-1b | S | 152 | 254 | 118 | 1.16 | 25.2 | 332 | 365 | 1 |
| 2 | A-1c | S | 152 | 254 | 118 | 1.16 | 29 | 332 | 356 |  |
| 3 | A1-d | S | 152 | 254 | 118 | 1.16 | 36.8 | 332 | 351 |  |
| 4 | A-1e | S | 152 | 254 | 118 | 1.16 | 20.3 | 332 | 356 |  |
| 5 | A2-b | S | 152 | 254 | 114 | 2.5 | 19.5 | 321 | 400 |  |
| 6 | A-2c | S | 152 | 254 | 114 | 2.5 | 37.4 | 321 | 467 |  |
| 7 | A-7b | S | 152 | 254 | 114 | 2.5 | 27.9 | 321 | 512 |  |
| 8 | A-3b | S | 152 | 254 | 114 | 3.74 | 22.6 | 321 | 445 |  |
| 9 | A-3c | S | 152 | 254 | 114 | 3.74 | 26.5 | 321 | 534 |  |
| 10 | A-3d | S | 152 | 254 | 114 | 3.74 | 34.5 | 321 | 547 |  |
| 11 | A-4 | S | 152 | 356 | 118 | 1.18 | 26.1 | 332 | 400 |  |
| 12 | A-5 | S | 152 | 356 | 114 | 2.5 | 27.8 | 321 | 534 |  |
| 13 | A-6 | S | 152 | 356 | 114 | 3.74 | 25 | 321 | 498 |  |
| 14 | A-13 | S | 152 | 356 | 121 | 0.55 | 26.2 | 294 | 236 |  |
| 15 | B-1 | S | 152 | 254 | 114 | 0.48 | 14.2 | 324 | 178 |  |
| 16 | B-2 | S | 152 | 254 | 114 | 0.48 | 47.6 | 321 | 200 |  |
| 17 | B-4 | S | 152 | 254 | 114 | 1.01 | 47.7 | 303 | 334 |  |
| 18 | B-9 | S | 152 | 254 | 114 | 2 | 43.9 | 341 | 505 |  |
| 19 | B -14 | S | 152 | 254 | 114 | 3.02 | 50.5 | 325 | 578 |  |
| 20 | 5 | C | 150 | 150 | 117 | 0.8 | 26.8 | 441 | 255 | 2 |
| 21 | 6 | C | 150 | 150 | 118 | 0.79 | 26.2 | 454 | 275 |  |
| 22 | 24 | C | 150 | 300 | 128 | 1.01 | 26.4 | 455 | 430 |  |
| 23 | 25 | C | 150 | 300 | 124 | 1.04 | 25.1 | 451 | 408 |  |
| 24 | 32 | C | 150 | 300 | 123 | 0.49 | 26.3 | 448 | 258 |  |
| 25 | 33 | C | 150 | 300 | 125 | 0.48 | 26.6 | 462 | 258 |  |
| 26 | IA15a-5 | C | 150 | 106 | 117 | 0.8 | 23.6 | 441 | 255 |  |
| 27 | IA15a-6 | C | 150 | 106 | 118 | 0.79 | 23 | 454 | 275 |  |
| 28 | IA15c-11 | C | 150 | 106 | 121 | 1.53 | 28.8 | 436 | 333 |  |
| 29 | IA15c-12 | C | 150 | 106 | 122 | 1.54 | 27.7 | 439 | 331 |  |
| 30 | IA30a-24 | C | 150 | 212 | 128 | 1.01 | 23.2 | 455 | 430 |  |
| 31 | IA30a-25 | C | 150 | 212 | 124 | 1.04 | 21.9 | 451 | 408 |  |
| 32 | IA30C-30 | C | 150 | 212 | 120 | 2.16 | 26.8 | 434 | 490 |  |
| 33 | IA30C-31 | C | 150 | 212 | 119 | 2.18 | 26.8 | 448 | 539 |  |
| 34 | IA30d-32 | C | 150 | 212 | 123 | 0.49 | 23.1 | 448 | 258 |  |
| 35 | IA30d-33 | C | 150 | 212 | 125 | 0.48 | 23.4 | 461 | 258 |  |
| 36 | IA30e-34 | C | 150 | 212 | 120 | 1 | 24.2 | 460 | 331 |  |
| 37 | IA30e-35 | C | 150 | 212 | 122 | 0.98 | 21.8 | 458 | 331 |  |
| 38 | R-1 | S | 152 | 305 | 114 | 1.38 | 27.5 | 400 | 394 | 3 |
| 39 | R-2 | S | 152 | 152 | 114 | 1.38 | 26.5 | 400 | 312 |  |
| 40 | S1-60 | S | 152 | 254 | 114 | 1.06 | 23.2 | 400 | 390 |  |
| 41 | S2-60 | S | 152 | 254 | 114 | 1.03 | 22 | 400 | 356 |  |
| 42 | S3-60 | S | 152 | 254 | 114 | 1.13 | 23.8 | 400 | 334 |  |
| 43 | S1-70 | S | 152 | 254 | 114 | 1.06 | 24.4 | 400 | 393 |  |
| 44 | S2-70 | S | 152 | 254 | 114 | 1.02 | 25.3 | 400 | 379 |  |
| 45 | S4-70 | S | 152 | 254 | 114 | 1.13 | 35.1 | 400 | 374 |  |
| 46 | S4A-70 | S | 152 | 254 | 114 | 1.13 | 20.4 | 400 | 312 |  |
| 47 | S5-60 | S | 152 | 203 | 114 | 1.06 | 22.1 | 400 | 343 |  |
| 48 | S5-70 | S | 152 | 203 | 114 | 1.06 | 24.2 | 400 | 379 |  |
| 49 | M1A | S | 152 | 305 | 114 | 1.5 | 23 | 400 | 433 |  |
| 50 | 1 | C | 102 | 221 | 82 | 1.21 | 13.9 | 457 | 182 | 4 |
| 51 | II-4a | C | 102 | 221 | 82 | 0.89 | 23.8 | 559 | 245 |  |
| 52 | II-5 | C | 102 | 221 | 82 | 0.53 | 22.8 | 471 | 152 |  |
| 53 | II-6 | C | 102 | 221 | 82 | 1.33 | 12.3 | 456 | 157 |  |
| 54 | II-8 | C | 102 | 333 | 82 | 0.59 | 24.8 | 456 | 219 |  |
| 55 | IIR20-2 | C | 129 | 201 | 109 | 0.93 | 19.8 | 500 | 307 |  |
| 56 | III-3 | C | 102 | 221 | 82 | 1.21 | 24 | 491 | 201 |  |
| 57 | 7 | C | 102 | 119 | 82 | 0.74 | 13.2 | 456 | 118 |  |
| 58 | M3-1-0 | S | 70 | 152 | 51 | 1.1 | 21.1 | 386 | 79 | 5 |
| 59 | M3-l-0a | S | 70 | 152 | 51 | 2.2 | 18 | 336 | 99 |  |
| 60 | M-4-1-0 | S | 70 | 203 | 51 | 1.1 | 15.5 | 386 | 93 |  |
| 61 | M-4-2-0 | S | 70 | 203 | 50 | 2.2 | 27.2 | 386 | 133 |  |
| 62 | M-5-1-0 | S | 70 | 254 | 51 | 1.1 | 23.3 | 336 | 109 |  |
| 63 | M-5-2-0 | S | 70 | 254 | 51 | 2.2 | 22.9 | 386 | 152 |  |
| 64 | M-6-1-0 | S | 70 | 305 | 51 | 1.1 | 23 | 386 | 114 |  |
| 65 | M-6-2-0 | S | 70 | 305 | 50 | 2.2 | 26.4 | 386 | 159 |  |
| 66 | M-7-1-0 | S | 70 | 356 | 51 | 1.1 | 27.7 | 386 | 139 |  |
| 67 | M-7-2-0 | S | 70 | 356 | 51 | 2.2 | 25 | 386 | 184 |  |
| 68 | M-8-1-0 | S | 70 | 406 | 51 | 1.1 | 24.9 | 386 | 145 |  |
| 69 | M-8-2-0 | S | 70 | 406 | 50 | 2.2 | 24.6 | 386 | 185 |  |
| 70 | M-3-1-2 | S | 70 | 152 | 50 | 1.1 | 27 | 386 | 102 |  |
| 71 | M-2-1-0 | S | 70 | 102 | 50 | 1.1 | 28.5 | 386 | 86 |  |
| 72 | M-2-2-0 | S | 70 | 102 | 50 | 2.2 | 24.9 | 386 | 102 |  |
| 73 | M-3-l-0b | S | 70 | 152 | 50 | 2.2 | 53.8 | 386 | 172 |  |
| 74 | M-3-l-4a | S | 70 | 152 | 50 | 1.1 | 21.1 | 386 | 99 |  |
| 75 | M-3-l-4b | S | 70 | 152 | 50 | 1.1 | 20 | 386 | 112 |  |
| 76 | M-3-2-4 | S | 70 | 152 | 50 | 2.2 | 17 | 386 | 105 |  |
| 77 | 1 | S | 120 | 125 | 100 | 0.8 | 35.7 | 706 | 216 | 6 |
| 78 | 3 | S | 119 | 125 | 99 | 0.81 | 28.6 | 701 | 194 |  |
| 79 | 5 | S | 220 | 250 | 200 | 0.8 | 30.3 | 657 | 603 |  |
| 80 | 6 | S | 219 | 250 | 199 | 0.8 | 28.6 | 670 | 600 |  |
| 81 | 13 | S | 118 | 125 | 98 | 0.35 | 33.3 | 720 | 145 |  |
| 82 | 14 | S | 119 | 125 | 99 | 0.34 | 31.4 | 712 | 148 |  |
| 83 | 17 | S | 220 | 250 | 200 | 0.34 | 31.7 | 668 | 489 |  |
| 84 | 18 | S | 217 | 250 | 197 | 0.35 | 30.2 | 664 | 444 |  |
| 85 | SS2 | S | 100 | 200 | 77 | 1.2 | 23.3 | 500 | 176 | 7 |
| 86 | SS4 | S | 100 | 200 | 77 | 0.92 | 33.4 | 500 | 194 |  |
| 87 | SS6 | S | 100 | 200 | 79 | 0.75 | 21.7 | 480 | 165 |  |
| 88 | SS7 | S | 100 | 200 | 79 | 0.8 | 31.2 | 480 | 186 |  |
| 89 | SS8 | S | 250 | 250 | 200 | 0.98 | 36.3 | 530 | 825 |  |
| 90 | SS9 | S | 160 | 160 | 128 | 0.98 | 34.5 | 485 | 390 |  |
| 91 | SS10 | S | 160 | 160 | 128 | 0.98 | 35.7 | 485 | 365 |  |
| 92 | SS11 | S | 80 | 80 | 64 | 0.98 | 34.5 | 480 | 117 |  |
| 93 | SS12 | S | 80 | 80 | 64 | 0.98 | 35.7 | 480 | 105 |  |
| 94 | SS13 | S | 80 | 80 | 64 | 0.98 | 37.8 | 480 | 105 |  |
| 95 | 1 | S | 52 | 100 | 41 | 0.42 | 31.5 | 530 | 36 | 8 |
| 96 | 2 | S | 52 | 100 | 41 | 0.56 | 31.5 | 530 | 49 |  |
| 97 | 3 | S | 52 | 100 | 41 | 0.69 | 31.5 | 530 | 57 |  |
| 98 | 4 | S | 52 | 100 | 41 | 0.82 | 36.2 | 530 | 56 |  |
| 99 | 5 | S | 52 | 100 | 41 | 0.88 | 36.2 | 530 | 57 |  |
| 100 | 6 | S | 52 | 100 | 41 | 1.03 | 36.2 | 530 | 66 |  |
| 101 | 7 | S | 52 | 100 | 41 | 1.16 | 30.4 | 530 | 71 |  |
| 102 | 8 | S | 52 | 100 | 41 | 1.29 | 30.4 | 530 | 71 |  |
| 103 | 9 | S | 52 | 100 | 41 | 1.45 | 30.4 | 530 | 79 |  |
| 104 | 10 | S | 52 | 100 | 41 | 0.52 | 30.6 | 530 | 44 |  |
| 105 | 11 | S | 52 | 100 | 41 | 0.8 | 30.6 | 530 | 55 |  |
| 106 | 12 | S | 52 | 100 | 41 | 1.11 | 30.6 | 530 | 67 |  |
| 107 | 13 | S | 52 | 100 | 41 | 0.6 | 35.3 | 530 | 49 |  |
| 108 | 14 | S | 52 | 100 | 41 | 0.69 | 35.3 | 530 | 52 |  |
| 109 | 15 | S | 52 | 100 | 41 | 1.99 | 35.3 | 530 | 85 |  |
| 110 | 1A | S | 58 | 100 | 47 | 0.44 | 29.4 | 530 | 45 |  |
| 111 | 2A | S | 58 | 100 | 47 | 0.69 | 29.4 | 530 | 66 |  |
| 112 | 3A | S | 58 | 100 | 47 | 1.29 | 29.4 | 530 | 90 |  |
| 113 | 4A | S | 58 | 100 | 47 | 1.99 | 31.7 | 530 | 97 |  |
| 114 | IB | S | 46 | 100 | 35 | 0.42 | 39.6 | 530 | 29 |  |
| 115 | 2B | S | 46 | 100 | 35 | 0.69 | 39.6 | 530 | 38 |  |
| 116 | 3B | S | 46 | 100 | 35 | 1.29 | 39.6 | 530 | 57 |  |
| 117 | 4B | S | 46 | 100 | 35 | 1.99 | 31.7 | 530 | 73 |  |
| 118 | 1C | S | 65 | 100 | 54 | 0.42 | 28.3 | 530 | 63 |  |
| 119 | 2C | S | 65 | 100 | 54 | 0.69 | 33.5 | 530 | 88 |  |
| 120 | 3C | S | 65 | 100 | 54 | 1.29 | 33.5 | 530 | 124 |  |
| 121 | 4C | S | 65 | 100 | 54 | 1.99 | 28.3 | 530 | 126 |  |
| 122 | S1.1 | C | 120 | 125 | 100 | 0.8 | 28.6 | 706 | 216 | 9 |
| 123 | S1.2 | C | 119 | 125 | 99 | 0.81 | 22.9 | 701 | 194 |  |
| 124 | S2.1 | C | 220 | 250 | 200 | 0.8 | 24.2 | 657 | 603 |  |
| 125 | S2.2 | C | 219 | 250 | 199 | 0.8 | 22.9 | 670 | 600 |  |
| 126 | S1.3 | C | 118 | 125 | 98 | 0.35 | 26.6 | 720 | 145 |  |
| 127 | S1.4 | C | 119 | 125 | 99 | 0.34 | 25.1 | 712 | 148 |  |
| 128 | S2.3 | C | 220 | 250 | 200 | 0.34 | 25.4 | 668 | 489 |  |
| 129 | S2.4 | C | 217 | 250 | 197 | 0.35 | 24.2 | 664 | 444 |  |
| 130 | 8 | S | 101 | 102 | 76 | 2.05 | 24.1 | 430 | 129 | 10 |
| 131 | 9 | S | 101 | 102 | 76 | 2.05 | 22.6 | 430 | 136 |  |
| 132 | 10 | S | 101 | 102 | 76 | 2.05 | 24.6 | 430 | 129 |  |
| 133 | 11 | S | 152 | 152 | 113 | 2.14 | 22.6 | 430 | 311 |  |
| 134 | 12 | S | 152 | 203 | 113 | 2.14 | 24.8 | 430 | 357 |  |
| 135 | 13 | S | 153 | 203 | 122 | 0.66 | 24.8 | 430 | 271 |  |
| 136 | 14 | S | 102 | 152 | 73 | 5.01 | 25 | 430 | 202 |  |
| 137 | 15 | S | 102 | 152 | 81 | 1.47 | 25 | 430 | 160 |  |
| 138 | 16 | S | 102 | 152 | 86 | 0.45 | 23.2 | 430 | 107 |  |
| 139 | 17 | S | 102 | 102 | 81 | 1.47 | 25.5 | 430 | 121 |  |
| 140 | 19 | S | 152 | 203 | 123 | 0.47 | 22.1 | 430 | 271 |  |
| 141 | 20 | S | 152 | 203 | 113 | 2.14 | 15.1 | 430 | 278 |  |
| 142 | 21 | S | 153 | 203 | 122 | 0.66 | 16.1 | 430 | 230 |  |
| 143 | 23 | S | 102 | 152 | 81 | 1.47 | 14.5 | 430 | 108 |  |
| 144 | 25 | S | 153 | 203 | 122 | 0.66 | 52.1 | 430 | 306 |  |
| 145 | 26 | S | 102 | 203 | 73 | 5.01 | 52.1 | 430 | 323 |  |
| 146 | 27 | S | 102 | 152 | 81 | 1.47 | 52.1 | 430 | 243 |  |
| 147 | 28 | S | 102 | 152 | 86 | 0.45 | 52.1 | 430 | 148 |  |
| 148 | NS1 | S | 120 | 150 | 95 | 1.47 | 42 | 490 | 320 | 11 |
| 149 | HS1 | S | 120 | 150 | 95 | 0.49 | 67 | 490 | 178 |  |
| 150 | HS2 | S | 120 | 150 | 95 | 0.84 | 70 | 490 | 249 |  |
| 151 | HS7 | S | 120 | 150 | 95 | 1.19 | 74 | 490 | 356 |  |
| 152 | HS3 | S | 120 | 150 | 95 | 1.47 | 69 | 490 | 356 |  |
| 153 | HS4 | S | 120 | 150 | 90 | 2.37 | 66 | 490 | 418 |  |
| 154 | NS2 | S | 150 | 150 | 120 | 0.94 | 30 | 490 | 396 |  |
| 155 | HS5 | S | 150 | 150 | 125 | 0.64 | 68 | 490 | 365 |  |
| 156 | HS6 | S | 150 | 150 | 120 | 0.94 | 70 | 490 | 489 |  |
| 157 | HS8 | S | 150 | 150 | 120 | 1.11 | 69 | 490 | 436 |  |
| 158 | HS9 | S | 150 | 150 | 120 | 1.61 | 74 | 490 | 543 |  |
| 159 | HS10 | S | 150 | 150 | 120 | 2.33 | 80 | 490 | 645 |  |
| 160 | HS11 | S | 90 | 150 | 70 | 0.95 | 70 | 490 | 196 |  |
| 161 | HS12 | S | 90 | 150 | 70 | 1.52 | 75 | 490 | 258 |  |
| 162 | HS13 | S | 90 | 150 | 70 | 1.87 | 68 | 490 | 267 |  |
| 163 | HS14 | S | 120 | 220 | 95 | 1.47 | 72 | 490 | 498 |  |
| 164 | HS15 | S | 120 | 300 | 95 | 1.47 | 71 | 490 | 560 |  |
| 165 | 65-1-1 | S | 300 | 200 | 275 | 1.49 | 64 | 500 | 2050 | 12 |
| 166 | 95-1-1 | S | 300 | 200 | 275 | 1.49 | 84 | 500 | 2250 |  |
| 167 | 115-1-1 | S | 300 | 200 | 275 | 1.49 | 112 | 500 | 2450 |  |
| 168 | 95-1-3 | S | 300 | 200 | 275 | 2.55 | 90 | 500 | 2400 |  |
| 169 | 65-2-1 | S | 225 | 150 | 200 | 1.75 | 70 | 500 | 1200 |  |
| 170 | 95-2-1D | S | 225 | 150 | 200 | 1.75 | 88 | 500 | 1100 |  |
| 171 | 95-2-1 | S | 225 | 150 | 200 | 1.75 | 87 | 500 | 1300 |  |
| 172 | 115-2-1 | S | 225 | 150 | 200 | 1.75 | 119 | 500 | 1400 |  |
| 173 | 95-2-3 | S | 225 | 150 | 200 | 2.62 | 90 | 500 | 1450 |  |
| 174 | 95-2-3D | S | 225 | 150 | 200 | 2.62 | 80 | 500 | 1250 |  |
| 175 | 95-2-3D+ | S | 225 | 150 | 200 | 2.62 | 98 | 500 | 1450 |  |
| 176 | 115-2-3 | S | 225 | 150 | 200 | 2.62 | 108 | 500 | 1550 |  |
| 177 | 95-3-1 | S | 113 | 100 | 88 | 1.84 | 85 | 500 | 330 |  |
| 178 | HSC0 | S | 225 | 250 | 200 | 0.8 | 90 | 643 | 965 | 13 |
| 179 | HSC1 | S | 225 | 250 | 200 | 0.8 | 91 | 627 | 1021 |  |
| 180 | HSC2 | S | 225 | 250 | 194 | 0.82 | 86 | 620 | 889 |  |
| 181 | HSC4 | S | 225 | 250 | 200 | 1.19 | 92 | 596 | 1041 |  |
| 182 | HSC6 | S | 225 | 250 | 201 | 0.6 | 109 | 633 | 960 |  |
| 183 | HSC9 | S | 225 | 250 | 202 | 0.33 | 84 | 634 | 565 |  |
| 184 | N/HSC8 | S | 225 | 250 | 198 | 0.8 | 95 | 631 | 944 |  |
| 185 | 1 | S | 125 | 150 | 98 | 0.58 | 88.2 | 550 | 224 | 14 |
| 186 | 2 | S | 125 | 150 | 98 | 0.58 | 56.2 | 550 | 212 |  |
| 187 | 3 | S | 125 | 150 | 98 | 0.58 | 26.9 | 550 | 169 |  |
| 188 | 4 | S | 125 | 150 | 98 | 0.58 | 58.7 | 550 | 233 |  |
| 189 | 6 | S | 125 | 150 | 98 | 0.58 | 101.8 | 550 | 233 |  |
| 190 | 12 | S | 125 | 150 | 98 | 1.28 | 60.4 | 550 | 319 |  |
| 191 | 13 | S | 125 | 150 | 98 | 1.28 | 43.4 | 550 | 297 |  |
| 192 | 14 | S | 125 | 150 | 98 | 1.28 | 60.8 | 550 | 341 |  |
| 193 | 16 | S | 125 | 150 | 98 | 1.28 | 98.4 | 550 | 362 |  |
| 194 | 21 | S | 125 | 150 | 98 | 1.28 | 41.9 | 650 | 286 |  |
| 195 | 22 | S | 125 | 150 | 98 | 1.28 | 84.2 | 650 | 405 |  |
| 196 | 23 | S | 125 | 150 | 100 | 0.87 | 56.4 | 650 | 341 |  |
| 197 | 25 | S | 125 | 150 | 100 | 1.27 | 32.9 | 650 | 244 |  |
| 198 | 26 | S | 125 | 150 | 100 | 1.27 | 37.6 | 650 | 294 |  |
| 199 | 27 | S | 125 | 150 | 102 | 1.03 | 33.7 | 650 | 227 |  |
| 200 | P100 | S | 135 | 200 | 100 | 0.97 | 39.4 | 488 | 330 | 15 |
| 201 | P150 | S | 190 | 200 | 150 | 0.9 | 39.4 | 465 | 583 |  |
| 202 | P200 | S | 240 | 200 | 200 | 0.83 | 39.4 | 465 | 904 |  |
| 203 | P300 | S | 345 | 200 | 300 | 0.76 | 39.4 | 468 | 1381 |  |
| 204 | P400 | S | 450 | 300 | 400 | 0.76 | 39.4 | 433 | 2224 |  |
| 205 | P500 | S | 550 | 300 | 500 | 0.76 | 39.4 | 433 | 2681 |  |
| 206 | PG-1 | S | 250 | 260 | 210 | 1.5 | 27.6 | 400 | 1024 | 16 |
| 207 | PG-2 | S | 250 | 260 | 210 | 0.25 | 28.5 | 400 | 445 |  |
| 208 | PG-2b | S | 250 | 260 | 210 | 0.25 | 40.5 | 400 | 439 |  |
| 209 | PG-3 | S | 504 | 520 | 464 | 0.33 | 32.4 | 400 | 2153 |  |
| 210 | PG-4 | S | 250 | 260 | 210 | 0.25 | 32.2 | 400 | 408 |  |
| 211 | PG-5 | S | 250 | 260 | 210 | 0.33 | 29.3 | 400 | 550 |  |
| 212 | PG-6 | S | 136 | 130 | 96 | 1.5 | 34.7 | 400 | 236 |  |
| 213 | PG-7 | S | 140 | 130 | 100 | 0.75 | 34.7 | 400 | 243 |  |
| 214 | PG-8 | S | 142 | 130 | 102 | 0.33 | 34.7 | 400 | 141 |  |
| 215 | PG-9 | S | 142 | 130 | 102 | 0.25 | 34.7 | 400 | 118 |  |
| 216 | PG-10 | S | 250 | 260 | 210 | 0.33 | 28.5 | 400 | 540 |  |
| 217 | C1 | S | 120 | 250 | 100 | 0.8 | 24 | 718 | 270 | 17 |
| 218 | C2 | S | 120 | 250 | 100 | 0.8 | 24.4 | 718 | 250 |  |
| 219 | D1 | S | 145 | 150 | 125 | 0.64 | 27.2 | 718 | 265 |  |
| 220 | 1 | S | 160 | 250 | 124 | 1.54 | 33.1 | 488 | 483 | 18 |
| 221 | 7 | S | 230 | 300 | 190 | 1.3 | 33.5 | 531 | 825 |  |
| 222 | 10 | S | 300 | 350 | 260 | 1.1 | 31 | 524 | 1046 |  |
| 223 | NSC1 | S | 200 | 250 | 158 | 2.17 | 35 | 490 | 678 | 19 |
| 224 | HSC1 | S | 200 | 250 | 138 | 2.48 | 68.5 | 490 | 788 |  |
| 225 | HSC2 | S | 200 | 250 | 128 | 2.68 | 70 | 490 | 801 |  |
| 226 | HSC3 | S | 200 | 250 | 158 | 1.67 | 66.7 | 490 | 802 |  |
| 227 | HSC4 | S | 200 | 250 | 158 | 1.13 | 61.2 | 490 | 811 |  |
| 228 | HSC5 | S | 150 | 250 | 113 | 1.88 | 70 | 490 | 480 |  |
| 229 | NSC2 | S | 200 | 250 | 163 | 0.52 | 33 | 490 | 479 |  |
| 230 | NSC3 | S | 150 | 250 | 105 | 0.4 | 34 | 490 | 228 |  |
| 231 | NS1 | S | 150 | 250 | 105 | 0.45 | 44.7 | 400 | 219 | 20 |
| 232 | NS2 | S | 200 | 250 | 153 | 0.55 | 50.2 | 400 | 491 |  |
| 233 | NS3 | S | 250 | 250 | 183 | 0.35 | 35 | 400 | 438 |  |
| 234 | HS1 | S | 250 | 250 | 183 | 0.35 | 70 | 400 | 574 |  |
| 235 | NS4 | S | 300 | 250 | 218 | 0.73 | 40 | 400 | 882 |  |
| 236 | HS2 | S | 300 | 250 | 218 | 0.73 | 64.7 | 400 | 1023 |  |
| 237 | HS3 | S | 300 | 250 | 220 | 0.43 | 76 | 400 | 886 |  |
| 238 | HS4 | S | 350 | 400 | 268 | 1.13 | 75 | 400 | 1721 |  |
| 239 | HS6 | S | 350 | 400 | 263 | 1.44 | 65.4 | 400 | 2090 |  |
| 240 | NS4 | S | 400 | 400 | 313 | 1.57 | 40 | 400 | 2234 |  |
| 241 | HS7 | S | 400 | 400 | 313 | 1.57 | 60 | 400 | 2513 |  |
| 242 | PG1 | S | 250 | 260 | 210 | 1.5 | 27.6 | 573 | 1023 | 21 |
| 243 | PG11 | S | 250 | 260 | 210 | 0.75 | 31.5 | 570 | 763 |  |
| 244 | PG3 | S | 500 | 520 | 456 | 0.33 | 32.4 | 520 | 2153 |  |
| 245 | PG6 | S | 125 | 130 | 96 | 1.5 | 34.7 | 526 | 238 |  |
| 246 | PG7 | S | 125 | 130 | 100 | 0.75 | 34.7 | 550 | 241 |  |
| 247 | NS1 | S | 120 | 150 | 95 | 1.47 | 42 | 490 | 320 | 22 |
| 248 | HS2 | S | 120 | 150 | 95 | 0.84 | 70 | 490 | 249 |  |
| 249 | HS7 | S | 120 | 150 | 95 | 1.19 | 74 | 490 | 356 |  |
| 250 | HS3 | S | 120 | 150 | 95 | 1.47 | 69 | 490 | 356 |  |
| 251 | HS4 | S | 120 | 150 | 95 | 2.37 | 66 | 490 | 418 |  |
| 252 | NS2 | S | 150 | 150 | 120 | 0.94 | 30 | 490 | 396 |  |
| 253 | HS5 | S | 150 | 150 | 125 | 0.64 | 68 | 490 | 365 |  |
| 254 | HS6 | S | 150 | 150 | 120 | 0.94 | 70 | 490 | 489 |  |
| 255 | HS8 | S | 150 | 150 | 120 | 1.11 | 69 | 490 | 436 |  |
| 256 | HS9 | S | 150 | 150 | 120 | 1.61 | 74 | 490 | 543 |  |
| 257 | HS10 | S | 150 | 150 | 120 | 2.33 | 80 | 490 | 645 |  |
| 258 | HS12 | S | 90 | 150 | 70 | 1.52 | 75 | 490 | 258 |  |
| 259 | HS13 | S | 90 | 150 | 70 | 1.87 | 68 | 490 | 267 |  |
| 260 | HS14 | S | 120 | 220 | 95 | 1.47 | 72 | 490 | 498 |  |
| 261 | HS15 | S | 120 | 300 | 95 | 1.47 | 71 | 490 | 560 |  |
| 262 | HSLW1.5 | S | 150 | 250 | 115 | 1.5 | 75.5 | 435 | 538.5 |  |
| 263 | HSLW2 | S | 150 | 250 | 115 | 2 | 74 | 435 | 613.4 |  |
| 264 | NSLW1 | S | 150 | 250 | 115 | 1 | 36.2 | 435 | 432.1 |  |
| 265 | NSC1 | S | 200 | 250 | 158 | 2.17 | 35 | 400 | 678 |  |
| 266 | HSC1 | S | 200 | 250 | 138 | 2.48 | 69 | 400 | 788 |  |
| 267 | HSC2 | S | 200 | 250 | 128 | 2.68 | 70 | 400 | 801 |  |
| 268 | HSC3 | S | 200 | 250 | 158 | 1.67 | 67 | 400 | 802 |  |
| 269 | HSC4 | S | 200 | 250 | 158 | 1.13 | 61 | 400 | 811 |  |
| 270 | HSC5 | S | 150 | 250 | 113 | 1.88 | 70 | 400 | 480 |  |
| 271 | NS4 | S | 300 | 250 | 218 | 0.73 | 40 | 400 | 882 |  |
| 272 | HS2 | S | 300 | 250 | 218 | 0.73 | 64.7 | 400 | 1023 |  |
| 273 | HS3 | S | 350 | 400 | 263 | 1.44 | 65.4 | 400 | 2090 |  |
| 274 | NS5 | S | 400 | 400 | 313 | 1.58 | 40 | 400 | 2234 |  |
| 275 | ND65-1-1 | S | 320 | 200 | 275 | 1.5 | 64.3 | 500 | 2050 | 12 |
| 276 | ND65-2-1 | S | 240 | 150 | 200 | 1.7 | 70.2 | 500 | 1200 |  |
| 277 | ND95-1-1 | S | 320 | 200 | 275 | 1.5 | 83.7 | 500 | 2250 |  |
| 278 | ND95-1-3 | S | 320 | 200 | 275 | 2.5 | 89.9 | 500 | 2400 |  |
| 279 | ND95-2-1 | S | 240 | 150 | 200 | 1.7 | 88.2 | 500 | 1100 |  |
| 280 | ND95-2-1D | S | 240 | 150 | 200 | 1.7 | 86.7 | 500 | 1300 |  |
| 281 | ND95-2-3 | S | 240 | 150 | 200 | 2.6 | 89.5 | 500 | 1450 |  |

Table 2 References of data

| Group | ID | Ref. |
| --- | --- | --- |
| 1 | A-1b to B -14 | Elstner R, Hognestad E. Shearing strength of reinforced concrete slabs. ACI Journal Proceedings, 1956, 53(7):29–58 |
| 2 | 5 to IA30e-35 | Kinnunen S, Nylander H. Punching of Concrete Slabs Without Shear Reinforcement. Transactions No. 158. 1960 |
| 3 | R-1 to M1A | Moe J. Shearing Strength of Reinforced Concrete Slabs and Footings Under Concentrated Loads. Development Department Bulletin No. D47. 1961 |
| 4 | 1 to 7 | Yitzhaki D. Punching strength of reinforced concrete slabs. ACI Journal Proceedings, 1966, 63(5): 527–542 |
| 5 | M3-1-0 to M3-2-4 | Mowrer R, Vanderbilt M. Shear strength of lightweight aggregate reinforced concrete flat plates. ACI Journal Proceedings, 1967, 64(11):722–729 |
| 6 | 1 to 18 | Kinnunen S, Nylander H, Tolf P. Investigations on punching at the division of building statics and structural engineering. Nordisk Betong, 1978, 3: 25–27 |
| 7 | SS2 to SS13 | Regan P, Walker P, Zakaria K. Tests of Reinforced Concrete Flat Slabs. CIRIA Project RP 220. 1979 |
| 8 | 1 to 4C | Rankin G, Long A. Predicting the punching strength of conventional slab–column specimens. Proceedings of the Institution of Civil Engineers, 1987, 82(2): 327–346 |
| 9 | S1.1 to S2.4 | Tolf P. Plattjocklekens inverkan pøa betongplattors høallfasthet vid genomstansning Försök med cirkulära platter. Stockholm: Royal Institute of Technology, 1988 |
| 10 | 8 to 28 | Gardner N. Relationship of the punching shear capacity of reinforced concrete slabs with concrete strength. ACI Structural Journal, 1990, 87(1): 66–71 |
| 11 | NS1 to HS15 | Marzouk H, Hussein A. Experimental investigation on the behavior of high strength concrete slabs. ACI Structural Journal, 1991, 88(6): 701–713 |
| 12 | 65-1-1 to 95-3-1 | Tomaszewicz A. High Strength Concrete SP2-Plates and Shells, Report 2.3. Punching Shear Capacity of Reinforced Concrete Slabs, Report No. STF70A93082. 1993 |
| 13 | HSC0 to N/HSC8 | Hallgren M. Punching shear capacity of reinforced high strength concrete slabs. Dissertation for the Doctoral Degree. Stockholm: Royal Institute of Technology, 1996 |
| 14 | 1 to 27 | Ramdane K. Punching shear of high performance concrete slabs. In: Proceedings of the 4th International Symposium on Utilization of High Strength High Performance Concrete. Paris: Presses de l'École Nationale des Ponts et Chaussées, 1996, 1015–1026 |
| 15 | P100 to P500 | Kevin K. Influence of size on punching shear strength of concrete slabs. Thesis for the Master’s Degree. Montreal: McGill University, 2000 |
| 16 | PG-1 to PG-10 | Guandalini S, Muttoni A. Symmetrical Punching Tests on Slabs without Transverse Reinforcement. Test Report. 2004 |
| 17 | C1 to D1 | Sundquist H, Kinnunen S. The Effect of Column Head and Drop Panels on the Punching Capacity of Flat Slabs. Bulletin No. 82. 2004 |
| 18 | 1 to 10 | Birkle G, Dilger W. Influence of slab thickness on punching shear strength. ACI Structural Journal, 2008, 105(2): 180–188 |
| 19 | NSC1 to NSC3 | Marzouk H, Hossin M. Crack Analysis of Reinforced Concrete Two-way Slabs. Research Report RCS01. 2007 |
| 20 | NS1 to HS7 | Marzouk, Rizk. Punching Analysis of Reinforced Concrete Two-way Slabs. Research Report RCS01. 2009 |
| 21 | PG1-PG7 | Guandalini S, Burdet O L, Muttoni A. Punching tests of slabs with low reinforcement ratios. ACI Structural Journal, 2009, 160(1): 87–95 |
| 22 | NS1-NS5 | Marzouk H, Hussein A. Experimental investigation on the behavior of high strength concrete slabs. ACI Structural Journal, 1991, 88(6): 701–713 |
| 12 | ND65-1-1 to ND95-2-3 | Tomaszewicz A. High Strength Concrete SP2-Plates and Shells, Report 2.3. Punching Shear Capacity of Reinforced Concrete Slabs, Report No. STF70A93082. 1993 |