Appendices for:

Modeling the mechanical behavior and damage development of concrete materials under neutron irradiation

Yuxiang JINGa,b,c*, Yunping XIc

a Central Research Institute of Building and Construction Co., Ltd. MCC Group, Beijing 100088, China

b Inspection and Certification Co., Ltd. MCC Group, Beijing 100088, China

c Department of Civil, Environmental and Architectural Engineering, University of Colorado Boulder, Boulder, CO 80309, United States of America

*Corresponding author. E-mail: yuxiang.jing@colorado.edu

Appendix A. Generalized self-consistent model

For any phase i (i = 1 is inclusion and i = 2 is matrix) in the composite material shown in Fig. 2(c) that deforms, the elastic equilibrium equation in spherical coordinates is given as

Ui,rr+2rUi, r-2r2Ui-1+υi1-υiεi,r=0, (A1)

where Ui is displacement of phase i in the radial direction (cm); r is the location coordinate in the radial direction when the center of the inclusion is the origin of the system (cm); 𝜐I is Poisson’s ratio for phase i (unitless); 𝜀i is the linear strain for phase i (unitless).

Since a very small-scale deformation is considered, the last term in the above equation can be neglected. Thus, the equation can be simplified to

Ui,rr+2rUi,r-2r2Ui=0. (A2)

The above equation describes the problem shown in Fig. 2(c). Ui1(r) = r is one solution of this second-order linear differential equation. A second solution that is linearly independent of the first solution can be obtained using the reduction of order method. The second solution is in the form

Ui2r=vrUi1r=vrr, (A3)

where v(r) is an arbitrary function.

Substitute Ui2(r) into Eq. (A2) to get

rv,rr+2v,r+2rrv,r+v-2rv=0. (A4)

Rearranging the above equation, then

v,rr+4rv,r=0, (A5)

which is a first-order equation for w=v,r, given by

w,r+4rw=0, (A6)

which can be easily solved by method of separation of variables

w=c1r-4, c1∈R. (A7)

Integrating the equation above, v is obtained

v=c2r-3+c3, c2,c3∈R. (A8)

Then

Ui2r=vrr=c2r-2+c3r, c2,c3∈R. (A9)

When c2 = 0 and c3 = 1, Ui2r=r which is Ui1r. Based on the principle of superposition, Ui2r shown in Eq. (A9) is the general solution of Eq. (A2).

Based on Hooke’s law for an isotropic material, the expressions of displacements and corresponding stresses valid in all phases can be obtained

Ui=Cir+Dir2, (A10)

σri=3KiCi-4GiDir3-3Kiεi, (A11)

where  σri is the stress of phase i in the radial direction (MPa); Ki is bulk modulus of phase i (MPa); Gi is shear modulus of phase i (MPa); Ci are unknown coefficient (unitless), and Di are unknown coefficient (cm3), D1 = 0 to avoid a singularity at r = 0.

Apply continuity conditions at r = R1, which is U1R1=U2R1 and  σr1R1= σr2R1 and assume the radial displacement at boundary r = R2 is δ, then we have

C1R1=C2R1+D2R12, (A12)

3K1C1-3K1ε1=3K2C2-4G2D2R13-3K2ε2, (A13)

U2R2=C2R2+D2R22=δ. (A14)

Then, the three unknown coefficients C1, C2, and D2 can be solved.

C1=δR2-D2R23+D2R13, (A15)

C2=δR2-D2R23, (A16)

D2=3K1ε1-3K2ε2+3δR2K2-K13K11R13-1R23+3K2R23+4G2R13. (A17)

Equations (A10) and (A11) are also valid for the effective medium. For the effective medium and the matrix, the displacement and stress are continuous at boundary r = R2, respectively. Therefore, UeffR2=U2R2 and  σreffR2= σr2R2 which is

CeffR2=δ, (A18)

KeffCeff-3Keffεeff=3K2C2-4G2D2R23-3K2ε2, (A19)

where the subscript eff stands for effective medium. Solve Ceff from Eq. (A-18) and substitute it into Eq. (A19) to get

3KeffδR2-3Keffεeff=3K2C2-4G2D2R23-3K2ε2. (A20)

First, take all strains, ε1, ε2, and εeff to be zero, and all the equations are still valid, then Keff can be solved from Eq. (A20)

Keff=K2+f1(K1-K2)1+1-f1K1-K2K2+43G2. (A21)

Alternative form:

KeffK2=1+d(K1K2-11+1-dK1K2-11+43G2K2

where f1=R13R23, the volume fraction of phase 1 (inclusion). By substituting Keff into Eq. (A20), the strain of the effective medium is obtained

εeff=K1ε1f13K2+4G2+K2ε2(1-f1)(3K1+4G2)K23K1+4G2-4f1G2(K2-K1). (A22)

Apply free boundary condition in the radial direction at boundary r = R2, which is

σr2R2=3K2C2-4G2D2R23-3K2ε2=0. (A23)

Substitute C2 and D2, which are expressed in terms of δ, into the above equation, and the displacement δ can be solved. Then it is inserted into C2, D2, and the following equation to get the radial stress at r = R1

σr2R1=3K2C2-4G2D2R13-3K2ε2, (A24)

which is the internal pressure P at the inclusion-matrix interface of the composite material shown in Figs. 2–3 (c)

P=12K1K2G21-f1K23K1+4G2-4f1G2K2-K1ε1-ε2. (A25)

The effective shear modulus can be obtained through the equations shown below (the detailed derivations can be found in Subsection 2.4 from page 53 to 57 in (Christensen 2005)).

C1GeffG22+2C2GeffG2+C3=0, (A26)

where

C1=8G1G2-14-5υ2η1d103-263G1G2-1η2+2η1η3d73+252G1G2-1η2d53-50G1G2-17-12υ2+8υ22η2d+47-10υ2η2η3

C2=-2G1G2-11-5υ2η1d103+263G1G2-1η2+2η1η3d73-252G1G2-1η2d53+75G1G2-13-υ2η2υ2d+3215υ2-7η2η3

C3=4G1G2-15υ2-7η1d103-263G1G2-1η2+2η1η3d73+252G1G2-1η2d53+25G1G2-1υ22-7η2d-7+5υ2η2η3

η1=49-50υ1υ2G1G2-1+35G1G2υ1-2υ2+352υ1-υ2

η2=5υ1G1G2-8+7G1G2+4

η3=G1G28-10υ2+7-5υ2

Appendix B. Volume fractions of the constituents in hardened cement paste

The volume fractions of each constituent in hardened cement paste can be evaluated using the following equations (Xi and Jennings 1997):

fclinker=b(1-α)ρcp, (B1)

f'CH=b(0.189αC3SWC3S+0.058αC2SWC2S)p, (B2)

fCSH solid=b0.278αC3SWC3S+0.369αC2SWC2Sp, (B3)

fgel pores=0.219fCSH solid, (B44)

fAFm=b0.849αC3AWC3A+0.472αC4AFWC4AFp, (B4)

fcap=1-b-bΩp, (B5)

Ω=0.437αC3SWC3S+0.503αC2SWC2S+0.397αC3AWC3A+0.136αC4AFWC4AF, (B6)

fCSH=fgel pores+fCSH solid, (B7)

fAFt=1-fClinker+fCH+fAFm+fcap+fCSH, (B8)

fLD CSH=0.7fCSH, (B9)

fHD CSH=0.3fCSH-fUHD CSH, (B10)

fUHD CSH=0.2fCSH, fnanoCH=0.83*0.76fUHD CSH (0.2 < w/c ≤0.4), fUHD CSH=0, fnanoCH=0 (w/c > 0.4), fCH=f'CH-fnanoCH, (B11)

b=11+wc, p=ρc1+wc1+wcρcρw, (B12)

where α is the overall hydration degree of Portland cement(unitless); αi is the degree of hydration for reacting compound i in Portland cement (unitless) (i = C3S, C2S, C3A, or C4AF); Wi is weight fraction for reacting compound i in Portland cement (unitless); depending on the type of cement used for the concrete (can be found in ASTM C150); w/c is water-to-cement ratio (unitless); ρc is cement density (g/cm3), and ρw is water density (g/cm3).

The Avrami equations (Taylor 1987) are employed to estimate the ai

αi=1-exp-ait-bici, (B13)

where ai, bi, and ci are coefficients with values shown in Table B1, and t is time (d).

Table B1 Coefficients ai, bi, and ci

| Compound | ai | bi | ci |
| --- | --- | --- | --- |
| C3S | 0.25 | 0.90 | 0.70 |
| C2S | 0.46 | 0.00 | 0.12 |
| C3A | 0.28 | 0.90 | 0.77 |
| C4AF | 0.26 | 0.90 | 0.55 |

The overall hydration degree of the cement-based material is

α=iWiαiiWi, (B14)

It should be noted that the service time of concrete structures concerned in nuclear power plants is very long (more than 60 years); by that time, the effects of the hydration period of cement are not significant because the hydration reactions are almost completed.