Appendices for:

Vulnerability assessment of sustainable seismic retrofit solutions for reinforced concrete structures: A multi-faceted approach

Hafiz Asfandyar AHMED, Yaohan LI*

Department of Construction and Quality Management, Hong Kong Metropolitan University, Hong Kong 00000, China

*Corresponding author. E-mail: engrasfandyar2009@gmail.com

Contents

Contents	1

Appendix A 	2

Appendix B 	3

Appendix A

Fig. A1 Plan of the complete building with highlighted block considered in this study.

Dimensions of considered block: 60’ x 87.5’

Floor area of considered block: 5250 sft

Fig. A2 Equivalent linearization of capacity curve using FEMA 440 along with demand response spectrum and other parameters to determine the performance points e.g., F*max.

Appendix B

B1 - Carbon Emission Factors of Rebar and Structural Steel

Pig iron (BF-BOF) – 100% Virgin (2.09 kgCO2-e/kg),

Direct-reduced iron (EAF) – 100% Virgin (1.54 kgCO2-e/kg),

Direct-reduced iron (EAF) – 100% Recycled (0.39 kgCO2-e/kg)

Finished steel material – Rebar (0.16 kgCO2-e/kg),

Finished steel material – Structural steel (0.21 kgCO2-e/kg).

The emission factors for the EAF process rebar are calculated based on the percentage of recycled scrap used.

For example, the emission factor for the EAF process rebar with 21% recycled content can be calculated as: 1.54 x (1-21%) + 0.39 x 21% +0.16 = 1.459 kg CO2-e/kg.

According to the World Steel Association (WSA, 2011), the emission factor for BF-BOF rebar (13% scrap) is equal to: 2.09–13% × 1.41 + 0.16 = 2.07 kg CO2-e/kg; the emission factor for BF-BOF structural steel (10% scrap) is equal to: 2.09–10% × 1.41 + 0.21 = 2.16 kg CO2-e/kg.

B2 – Data used in Green Concrete LCA tool

Table B1 List of materials

| User Input data | Type of Material |
| --- | --- |
| Ordinary Portland cement (OPC) | ASTM Type-I |
| Admixture | superplasticizer |
| Electricity grid station | location |
| Cement supply | Cherat, Pak |
| Fine aggregate supply | Larunspur, Pak |
| Coarse aggregate supply | Taxila, Pak |
| RCP | Warsak, Pak |

Table B2 Transportation of raw materials

| Transportation detail | Mode | Distance (km) |
| --- | --- | --- |
| Cement raw materials to cement plant | truck class 8b | 15 |
| Gypsum to cement plant | truck class 8b | 275 |
| Cement to concrete plant | truck class 8b | 225 |
| Fine aggregate to concrete plant | truck class 8b | 190 |
| Coarse aggregates to concrete plant | truck class 8b | 150 |
| Admixture to concrete plant | truck class 2 | 270 |

Table B3 Details of processes and technologies selected

| Technology options for | Type of technology selected |
| --- | --- |
| Cement raw materials pre-homogenization | Dry, raw storing, pre-blending |
| Cement raw materials grinding | dry, raw storing, tube mill |
| cement raw meal | Dry, raw meal |
| blending/homogenization | blending, storage |
| Clinker pyro processing | Preheater / precalciner kiln with US average kiln fuel mix |
| Clinker cooling | Reciprocating grate cooler (modern) |
| cement finish | Tube mill |
| milling/grinding/blending |  |
| Cement PM control technology | ESP |
| Conveying within the cement plant | Screw pump |
| Concrete batching plant loading/mixing | Mixer loading (central mix) |
| Concrete batching plant PM control | Fabric filter |

Table B4 Electricity grid mix percentage for Pakistan [100]

| User input data | National grid (%) |
| --- | --- |
| Coal | 12 |
| Natural gas | 29 |
| Fuel oil | 20 |
| Pet coke | – |
| Nuclear | 2.5 |
| Hydropower | 34 |
| Biomass | 0.5 |
| Geothermal | – |
| Solar | 1 |
| Wind | 1 |