
Table S1. Concentration of Mineral Elements in Potash Feldspar Powder Analyzed by Rigaku SmartLab X-Ray Diffractometer
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	Al2O3
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	M-95
	16.95
	66.62
	0.19
	0.09
	0.06
	15.01
	0.56
	0.03
	0.25


[bookmark: _GoBack]
